Supporting Information

Effects of oxide supports and Pt loading on the interfacial structure and catalytic performance of SANIs-inspired catalysts for dry reforming of methane

Chao Hu1*, Hongye Chen1, Ziwen Zhao1, Yue Zhang1, Rui Zhou1, Shenqiao Song1, Nai Rong1, Xiaokang Wan1

1: School of Environment and Energy Engineering, Anhui Jianzhu University, Hefei 230601, China

*Corresponding author: Chao Hu Tel.: +86 551 63828252

E-mail: chaohu@mail.ustc.edu.cn

Submitted to: Korean Journal of Chemical Engineering

Table S1. Detailed preparation parameters of catalysts modified by different metal oxides.

| Catalysts | Metal precursor (mg) | IEP(PH) |
| --- | --- | --- |
| Pt/AlOx-SiO2 | 150.0 | 4.01 |
| Pt/CrOx-SiO2 | 160.0 | 6.93 |
| Pt/ZnOx-SiO2 | 93.2 | 8.15 |
| Pt/NiOx-SiO2 | 127.0 | 7.85 |
| Pt/CoOx-SiO2 | 116.4 | 9.90 |

Table S2. Precursor solution compositions for catalyst preparation.

| Catalysts | H2PtCl6·6H2O amount (μmol) | HCl solution volume (ml) | HCl solution PH |
| --- | --- | --- | --- |
| Pt/AlOx-SiO2 | 60 | 50.00 | 5.4 |
| Pt/CrOx-SiO2 | 60 | 50.00 | 4.3 |
| Pt/ZnOx-SiO2 | 60 | 50.00 | 6.4 |
| Pt/CoOx-SiO2 | 60 | 50.00 | 6.4 |
| 0.37wt% Pt/NiOx-SiO2 | 10 | 8.33 | 5.3 |
| 0.74wt% Pt/NiOx-SiO2 | 20 | 16.67 | 5.3 |
| 2.1wt% Pt/NiOx-SiO2 | 60 | 50.00 | 5.3 |
| 4.2wt% Pt/NiOx-SiO2 | 120 | 100.00 | 5.3 |
| 6.3wt% Pt/NiOx-SiO2 | 180 | 150.00 | 5.3 |

Table S3. Preparation parameters of Pt/NiOx–SiO2 catalysts with different Pt loadings.

| Catalysts | Substrate mass(mg) | IEP (PH) |
| --- | --- | --- |
| Pt/AlOx-SiO2 | 291.6 | 5.4 |
| Pt/CrOx-SiO2 | 381.6 | 4.3 |
| Pt/ZnOx-SiO2 | 290.0 | 6.4 |
| Pt/CoOx-SiO2 | 300.0 | 6.4 |
| Pt/NiOx-SiO2 | 378.0 | 5.3 |

Table S4. Fitted XPS parameters of Ni 2p spectra for Pt/NiOx–SiO2 catalysts.

| Catalysts | Binding Energy |  | Relative Peak Area |  |
| --- | --- | --- | --- | --- |
|  | Ni2+2p3/2 (ev) | Ni2+2p1/2(ev) | Ni2+2p3/2 (a.u.) | Ni2+2p1/2(a.u.) |
| 0.37wt% Pt/NiOx-SiO2 | 873.9 | 856.1 | 240.6 | 499.9 |
| 2.1wt% Pt/NiOx-SiO2 | 872.8 | 855.0 | 250.0 | 500.3 |
| 4.2wt% Pt/NiOx-SiO2 | 872.7 | 855.2 | 210.3 | 410.8 |
| 5.2wt% Pt/NiOx-SiO2 | 872.3 | 855.1 | 192.5 | 375.9 |
| 6.3wt% Pt/NiOx-SiO2 | 871.9 | 854.8 | 179.9 | 369.6 |

Table S5. Fitted XPS parameters of Pt 4f spectra for Pt/NiOx–SiO2 catalysts.

| Catalysts | Binding Energy |  | Relative Peak Area |  |
| --- | --- | --- | --- | --- |
|  | Pt2+4f7/2 (ev) | Pt2+4f5/2 (ev) | Pt2+4f7/2 (a.u.) | Pt2+4f5/2 (a.u.) |
| 0.37wt% Pt/NiOx-SiO2 | 72.31 | 75.73 | 23.65 | 17.95 |
| 2.1wt% Pt/NiOx-SiO2 | 72.46 | 75.78 | 33.09 | 24.37 |
| 4.2wt% Pt/NiOx-SiO2 | 72.58 | 75.93 | 48.50 | 36.54 |
| 5.2wt% Pt/NiOx-SiO2 | 72.62 | 75.87 | 61.33 | 47.78 |
| 6.3wt% Pt/NiOx-SiO2 | 72.74 | 75.93 | 80.61 | 60.16 |

Figure. S1 XPS Analysis and H2-TPR profiles of Pt/NiOx-SiO2. XPS spectra of (a) Ni 2p, H2-TPR profiles of (b) Pt/NiOx-SiO2

Figure. S2 XPS Analysis and H2-TPR profiles of Pt/CoOx-SiO2. XPS spectra of (a) Co 2p, H2-TPR profiles of (b) Pt/CoOx-SiO2

Figure. S3 XPS Analysis and H2-TPR profiles of Pt/ZnOx-SiO2. XPS spectra of (a) Zn 2p, H2-TPR profiles of (b) Pt/ZnOx-SiO2

Figure. S4 XPS Analysis and H2-TPR profiles of Pt/CrOx-SiO2. XPS spectra of (a) Cr 2p, H2-TPR profiles of (b) Pt/CrOx-SiO2

Figure. S5 XPS Analysis and H2-TPR profiles of Pt/AlOx-SiO2. XPS spectra of (a) Al 2p, H2-TPR profiles of (b) Pt/AlOx-SiO2

Figure. S6 TEM, HAADF-STEM images, and corresponding STEM-EDS elemental mappings of 0.37wt% Pt/NiOx-SiO2. (a) TEM image; (b); HRTEM image; (c); Overlay elemental mapping of Ni and Pt (d); Overlay elemental mapping of Ni, Pt, and Si

Figure. S7 TEM, HAADF-STEM images, and corresponding STEM-EDS elemental mappings of 4.2wt% Pt/NiOx-SiO2. (a) TEM image; (b); HRTEM image; (c); Overlay elemental mapping of Ni and Pt (d); Overlay elemental mapping of Ni, Pt, and Si

Figure. S8 TEM, HAADF-STEM images, and corresponding STEM-EDS elemental mappings of 6.3wt% Pt/NiOx-SiO2. (a) TEM image; (b); HRTEM image; (c); Overlay elemental mapping of Ni and Pt (d); Overlay elemental mapping of Ni, Pt, and Si