Support Information

Evaluation of Toxicity and Antibacterial Activity of Sr²⁺-Substituted β-Tricalcium Phosphate Prepared by the Polymeric Precursor Route

S.L.C. Matiasa, J.R.S. Fariasb, R.P. Feitosab, J.N. Silvac, P.M.P. Ferreirad, G.A. Nevesf, J.A. Osajimab, E.C. da Silva Filhob, L.S. Cavalcantee*, A.N.S. Bragaf

aPRPG-PPGCM, Federal University of Piauí–UFPI, Teresina 64000-040, Brazil

bInterdisciplinary Laboratory of Advanced Materials, Federal University of Piauí, Teresina 64064-260, Brazil

cInterdisciplinary Laboratory of Advanced Materials, Federal University of Piauí, Teresina 64064-260, Brazil

dLaboratory of Experimental Cancerology (LabCancer), Department of Biophysics and Physiology, Federal University of Piauí, Teresina, Brazil

ePPGQ-CETEM-CCN-DQ, State University of Piauí-UESPI, N. 2231, João Cabral, Teresina, PI 64002-150, Brazil

fAcademic Unit of Materials Engineering, Federal University of Campina Grande, Campina Grande 58429-900, Brazil

* Tel: +55 86 3213-7942, Mob: +55 86 99412-1001. *Email address: laeciosantos@ccn.uespi.br (L.S. Cavalcante)

Preprint submitted to Journal of Inorganic and Organometallic Polymers and Materials                                                                        August 18, 2026

Figs. SI1(a–d): DSC curves for β-TCP powders prepared by the polymeric precursor method doped with Sr²⁺ ions at different concentrations: (a) 0%, (b) 5%, (c) 10%, and (d) 15%, respectively.

Figs. SI2(a–d): Rietveld refinement plot of β-TCP ceramics doped with Sr²⁺ ions at different concentrations: (a) 0%, (b) 5%, (c) 10%, and (d) 15%, respectively.

Reference for Support Information

[RSI1] Marques, C.F., Matos, A.C., Ribeiro, I.A.C. et al. Insights on the properties of levofloxacin-adsorbed Sr- and Mg-doped calcium phosphate powders. J Mater Sci: Mater Med 27, 123 (2016). https://doi.org/10.1007/s10856-016-5733-2

Figs. SI3(a–d): SEM images in high magnification for β-TCP crystals doped with Sr²⁺ ions at different concentrations: (a) 0%, (b) 5%, (c) 10%, and (d) 15%, respectively.

Figs. SI4(a–d): Histograms of the average pore size distribution for β-TCP ceramics doped with Sr²⁺ ions at different concentrations: (a) 0%, (b) 5%, (c) 10%, and (d) 15%. Inset show the red curves represent the LogNormal fitting for each dataset and statistical data xc (SD), R2, and ².

- (b)

Figs. SI5(a,b): Percentage of mortality (%) at different concentrations tested of β-TCP ceramics doped with Sr²⁺ ions at different concentrations, with responses at (a) 24 h and (b) 48 h points evaluated.