Supporting Information

Magnetically Recoverable Fe2O3/ZSM-5 Composite for Fenton-Like Oxidation of Organic Dyes in Water

Yang Song1, Zhaochen Dong1, Shuying Li1,*, Wenmei Zhao1, Yanzhen Wang1, Xianglong Zhao1, Yang Zhao2, Xiuqin Sun2,*, Mulan Zhu3, Wei Fan4, Feiyong Chen1

1 Resources and Environment Innovation Institute, Shandong Jianzhu University, Jinan 250101, Shandong Province, China.

2 Shandong Coal Field Geological Survey and Research Institute, Jinan 250100, Shandong Province, China.

3 School of Environmental Science and Engineering, Xiamen University of Technology, Xiamen 361024, China

4 School of Environment, Northeast Normal University, 2555 Jingyue Street, Changchun 130117, China

*Corresponding Authors: Email: shuyingli@mail.sdu.edu.cn (Shuying Li); 18653177227@126.com (Xiuqin Sun)

† These authors contributed equally to this work.

Figure S1 Lattice spacing of Fe2O3 (2 2 1) crystal plane.

Figure S2. The SAED pattern of the ZMS-5.

Table S1 The element content of Fe, O, Si, and Al in the Fe2O3/ZSM-5.

| Elemental | Line | Concentration (wt%) |  |
| --- | --- | --- | --- |
| Al | Ka | 2.83 |  |
| Si | Ka | 2.17 |  |
| Fe | Ka | 64.96 |  |
| O | Ka | 30.05 |  |
|  |  | 100.000 | Total |

Figure S3 The X-ray photoelectron spectroscopy of Fe element in the Fe2O3/ZSM-5.

Figure S4 Standard curve of RhB concentration corresponded the absorbance.

Figure S5 Comparison of the RhB removal rate between the degradation of only Fe2O3/ZSM-5 catalyt without H2O2 and the only oxidation with H2O2.