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Figure S1 Lattice spacing of Fe2O3 (2 2 1) crystal plane.
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Figure S2. The SAED pattern of the ZMS-5.





Table S1 The element content of Fe, O, Si, and Al in the Fe2O3/ZSM-5.
	 Elemental 
	Line
	Concentration (wt%)
	

	Al
	Ka
	2.83
	 

	Si
	Ka
	2.17
	 

	Fe
	Ka
	64.96
	 

	O
	Ka
	30.05
	

	
	
	100.000
	Total
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Figure S3 The X-ray photoelectron spectroscopy of Fe element in the Fe2O3/ZSM-5.
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Figure S4 Standard curve of RhB concentration corresponded the absorbance.
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Figure S5 Comparison of the RhB removal rate between the degradation of only Fe2O3/ZSM-5 catalyt without H2O2 and the only oxidation with H2O2.
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