Supplementary Figure 1. Reproducibility of magnetic contrast. (a-c) Ferromagnetic MCD signal appears in a common region at adjacent 5 Fe-Co-Cr ternary islands.

Supplementary Figure 2. Setting of the region of interest (ROI). (a) Composition distribution of contour line. (b) ROI near the magnetic phase boundary

Igor Pro 4.0 is used for the preparation of Figure S2.

Supplementary Figure 3. Verification experiments on Fe-Cr binary alloys system. (a) Chemical composition map and MCD map obtained at the composition-gradient Fe–Cr binary thin film. Experiment was performed by identical technique of this study. (b) MCD histograms of Fe-Cr binary alloy versus the variation of Fe-Cr composition ratio. The peak splitting and increasing width of the MCD histogram were confirmed accompanying with ferromagnetic transition. (c) Width of MCD histograms of Fe-Cr binary alloy versus the variation of Fe-Cr composition ratio. The Width increases around 30.5 at%-Fe, corresponding to the ferromagnetic/paramagnetic transition of the Fe-Cr system. The threshold was currently set as 20% to the maximum, but the same trend was confirmed in the range of 10-25%. Extracted critical exponent was β = 0.318±0.013.

Igor Pro 4.0 is used for the preparation of Figure S3.

Supplemental Figure 4. Reproducibility of ternary magnetic phase diagram. (a, b) Distribution of MCD histograms obtained at adjacent Fe-Co-Cr ternary island. Ferromagnetic and paramagnetic map was generally reproduced.

Igor Pro 4.0 is used for the preparation of Figure S4.