Supporting Information

Dual-Mode Colorimetric Detection of Creatinine Using DTPA-Modified Silver Nanoparticles: Experimental Validation and Computational Analysis

Martina Asti Rahayu1, Sonita Afrita Purba Siboro2, Lala Adetia Marlina3, Muh Rizal B4, Nabilah Firyal Suhendra2*

1Chemical Analysis Study Program, Department of Mathematics and Natural Sciences, Faculty of Science and Technology, Universitas Jambi, Muaro Jambi 36361, Indonesia

2Research Center for Polymer Technology, National Research and Innovation Agency (BRIN), South Tangerang 15314, Indonesia

3Research Center for Computing, National Research and Innovation Agency (BRIN), Bandung 40135, Indonesia

4Department of Chemistry, Faculty of Science and Technology, Universitas Jambi, Jambi 36361, Indonesia.

*Corresponding author: nabilah.firyal.suhendra@brin.go.id

Fig S1. DLS measurement of AgNP-DTPA before and after creatinine addition (90 µM), demonstrating nanoparticle aggregation.

Fig S2. High-resolution XPS spectrum of (a) Ag 3d, (b) C 1s, (c) O 1s, and (d) N 1s in AgNP. The scattered and solid line showing experimental and fitted data, respectively.

Fig S3. DLS measurement of AgNP-DTPA before and after creatinine addition (90 µM), demonstrating nanoparticle aggregation.

Fig S4. UV-Vis absorbance spectrum of the DTPA-AgNP with diluted urine and creatinine-spiked urine (10, 30, 50 µM) (inset: Photograph of unspiked and creatinine-spiked DTPA-AgNP solution)

Table S1. Topological descriptors obtained from QTAIM analysis of the DTPA-AgNP and DTPA-AgNP/creatinine complexes at the DFT/M06-2X/6-311G(d,p)/LanL2DZ level of theory. Listed parameters include the electron density (ρbcp), kinetic energy density (Gbcp) potential energy density (Vbcp)total energy density (Hbcp), Laplacian of electron density (∇2bcp) and the -Gbcp/Vbcp ratio evaluated at the bond critical points. All values are expressed in atomic units or a.u.

| Complexes | BCP | ρbcp | Gbcp | Vbcp | Hbcp | ∇2bcp | -Gbcp/Vbcp |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DTPA-AgNP | Ag⋯O | 0.0426 | 0.0558 | -0.0561 | -0.0003 | 0.2223 | 0.9947 |
|  | Ag⋯O | 0.0352 | 0.0419 | -0.0414 | 0.0005 | 0.1698 | 1.0121 |
|  | Ag⋯O | 0.0480 | 0.0635 | -0.0650 | -0.0015 | 0.2481 | 0.9769 |
|  | Ag⋯O | 0.0384 | 0.0468 | -0.0468 | -0.0001 | 0.1869 | 1.0000 |
|  | Ag⋯O | 0.0299 | 0.0281 | -0.0288 | -0.0007 | -0.0007 | 0.9757 |
|  | Ag⋯O | 0.0162 | 0.0162 | -0.0132 | 0.0008 | 0.0590 | 1.2273 |
|  | Ag⋯H | 0.0208 | 0.0164 | -0.0156 | 0.0008 | 0.0685 | 1.0513 |
|  | Ag⋯H | 0.0145 | 0.0099 | -0.0093 | 0.0007 | 0.0428 | 1.0645 |
| DTPA-AgNP/Cre | Ag⋯O | 0.0550 | 0.0775 | -0.0803 | -0.0028 | 0.0030 | 0.9651 |
|  | Ag⋯C | 0.0062 | 0.0037 | -0.0033 | 0.0004 | 0.0163 | 1.1212 |
|  | Ag⋯H | 0.0212 | 0.0171 | -0.0164 | 0.0008 | 0.0718 | 1.0427 |
|  | Ag⋯H | 0.0084 | 0.0051 | -0.0048 | 0.0003 | 0.0215 | 1.0625 |
|  | Ag⋯H | 0.0067 | 0.0035 | -0.0034 | -0.0001 | 0.0142 | 1.0294 |
|  | Ag⋯O | 0.0489 | 0.0649 | -0.0665 | -0.0015 | 0.2538 | 0.9759 |
|  | Ag⋯O | 0.0199 | 0.0182 | -0.0175 | -0.0008 | 0.0759 | 1.0400 |
|  | Ag⋯O | 0.0348 | 0.0415 | -0.0409 | 0.0005 | 0.1681 | 1.0147 |
|  | O⋯H | 0.0421 | 0.0390 | -0.0414 | -0.0025 | 0.1458 | 0.9420 |
|  | O⋯H | 0.0130 | 0.0096 | -0.0084 | 0.0012 | 0.0434 | 1.1429 |
|  | O⋯N | 0.0103 | 0.0067 | -0.0058 | 0.0009 | 0.0305 | 1.1552 |
|  | O⋯H | 0.0123 | 0.0096 | -0.0081 | 0.0015 | 0.0444 | 1.1852 |