Table 1

Chemical structure, nomenclature, molecular formulas and formula weights of the examined compounds

| Code | Molecular structures | Name | Mol. Formulas/(F. wt) |
| --- | --- | --- | --- |
| Schiff Base |  | (Z)-N,N-dimethyl-3-((1-methylpyrrolidin-2-ylidene)amino)propan-1-amine | C10H21N3 183.3 |
| Surfactant |  | (E)-N,N-dimethyl-N-(3-((1-methylpyrrolidin-2-ylidene)amino)propyl)dodecan-1-aminium bromide | C22H46N3Br 432.54 |

Table 2

Corrosion criterions from WL of C-steel dissolution in 1.0 M HCl in the presence and     absence of Schiff base and Surfactant inhibitors at the studied temperatures

| Inhibitor name | Inhibitor conc. (M) | 25 oC |  |  | 45 oC |  |  | 65 oC |  |  | 85 oC |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | k (mg cm−2 h−1) | Ө | ηw (%) | k (mg cm−2 h−1) | Ө | ηw (%) | k (mg cm−2 h−1) | Ө | ηw (%) | k (mg cm−2 h−1) | Ө | ηw (%) |
| Blank | 1M HCl | 0.4072 | ˗ | ˗ | 0.9767 | ˗ | ˗ | 2.0992 | ˗ | ˗ | 4.3132 | ˗ | ˗ |
| Schiff Base | 1.0×10-4 | 0.2631 | 0.54 | 53.57 | 0.6947 | 0.50 | 50.09 | 1.6693 | 0.48 | 47.75 | 3.6059 | 0.43 | 43.46 |
|  | 5.0×10-4 | 0.2181 | 0.62 | 61.52 | 0.6000 | 0.57 | 56.90 | 1.4589 | 0.54 | 54.34 | 3.1737 | 0.50 | 50.24 |
|  | 1.0×10-3 | 0.1910 | 0.66 | 66.30 | 0.5204 | 0.63 | 62.61 | 1.3362 | 0.58 | 58.18 | 2.9244 | 0.54 | 54.15 |
|  | 5.0×10-3 | 0.1669 | 0.71 | 70.54 | 0.4652 | 0.67 | 66.58 | 1.1933 | 0.63 | 62.65 | 2.6718 | 0.58 | 58.11 |
| Surfactant | 1.0×10-4 | 0.1385 | 0.76 | 75.55 | 0.3920 | 0.72 | 71.84 | 1.0672 | 0.67 | 66.60 | 2.7090 | 0.61 | 61.06 |
|  | 5.0×10-4 | 0.0936 | 0.83 | 83.48 | 0.2713 | 0.81 | 80.51 | 0.7439 | 0.77 | 76.72 | 1.9750 | 0.72 | 71.61 |
|  | 1.0×10-3 | 0.0654 | 0.88 | 88.46 | 0.2196 | 0.84 | 84.22 | 0.5781 | 0.82 | 81.90 | 1.6496 | 0.76 | 76.29 |
|  | 5.0×10-3 | 0.0516 | 0.91 | 90.90 | 0.1728 | 0.88 | 87.58 | 0.4714 | 0.85 | 85.24 | 1.3523 | 0.81 | 80.56 |

Table 3

Activation energy (Ea, kJ mol-1) values for carbon steel in 1.0 M in the absence and presence of different concentrations of both the synthesized Schiff base and cationic surfactant

| Conc. of inhibitor (M) | Ea |  |
| --- | --- | --- |
|  | Schiff Base | Surfactant |
| 1M HCl | 35.92 | 35.92 |
| 1 × 10-4 | 38.74 | 43.96 |
| 5 × 10-4 | 39.61 | 44.99 |
| 1 × 10-3 | 40.51 | 47.23 |
| 5 × 10-3 | 41.10 | 47.89 |

Table 4

The calculated thermodynamic parameters from the adsorption isotherms of the prepared inhibitors at different temperatures

| Inhibitor | Temperature (oC) | Kads (M-1) | ΔGoads (kJ mol-1) | ΔHoads (kJ mol-1) | ΔSoads (J mol-1 K-1) |
| --- | --- | --- | --- | --- | --- |
| Schiff Base | 25 | 11557 | -33.13 | -4.07 | 97.51 |
|  | 45 | 10129 | -35.00 |  | 97.27 |
|  | 65 | 9471 | -37.02 |  | 97.47 |
|  | 85 | 8716 | -38.96 |  | 97.46 |
| Surfactant | 25 | 26841 | -35.22 | -8.76 | 88.77 |
|  | 45 | 22859 | -37.16 |  | 89.29 |
|  | 65 | 18753 | -38.94 |  | 89.27 |
|  | 85 | 14771 | -40.53 |  | 88.73 |

Table 5

PDP parameters for the dissolution of C-steel in 1.0 M HCl in the absence and presence of different doses of the studied inhibitors at 25 °C

| The inhibitors | Conc. of inhibitor (M) | Ecorr (mV vs SCE) | icorr (mA cm-2) | βa (mV dec-1) | βc (mV dec-1) | IEPDP (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Blank | 0.00 | -497.5 | 0.5880 | 181.4 | -140.1 | - |
| Schiff base | 1x10-4 | -500.0 | 0.2717 | 208.8 | -151.9 | 53.79 |
|  | 5x10-4 | -502.5 | 0.2226 | 210.7 | -169.7 | 62.14 |
|  | 1x10-3 | -505.0 | 0.1996 | 211.0 | -170.4 | 66.05 |
|  | 5x10-3 | -506.0 | 0.1771 | 216.5 | -167.8 | 69.88 |
| Surfactant | 1x10-4 | -500.0 | 0.1452 | 216.1 | -136.3 | 75.31 |
|  | 5x10-4 | -503.0 | 0.0966 | 229.4 | -168.5 | 83.57 |
|  | 1x10-3 | -504.0 | 0.0654 | 233.6 | -172.2 | 88.88 |
|  | 5x10-3 | -505.0 | 0.0543 | 236.1 | -182.4 | 90.77 |

Table 6

EIS parameters for C-steel in 1.0 M HCl without and with various doses of the studied inhibitors at 25 °C

| The inhibitor | Conc. of inhibitor (M) | Rs (Ω cm2) | Qdl (mΩ−1sn cm−2) | n | Rct (Ω cm2) | Chsq x103 | Cdl (μF cm-2) | IEEIS (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Absence | 0.00 | 2.19 | 0.5314 | 0.81 | 59.59 | 8.33 | 195.00 | - |
| Schiff Base | 1x10-4 | 2.00 | 0.2542 | 0.71 | 129.0 | 2.30 | 89.92 | 53.81 |
|  | 5x10-4 | 2.76 | 0.2135 | 0.79 | 149.1 | 4.67 | 78.05 | 60.03 |
|  | 1x10-3 | 1.99 | 0.1917 | 0.78 | 167.7 | 6.42 | 70.11 | 64.47 |
|  | 5x10-3 | 2. 26 | 0.1571 | 0.89 | 203.6 | 1.05 | 54.39 | 70.73 |
| Surfactant | 1x10-4 | 2.07 | 0.1438 | 0.81 | 222.1 | 1.38 | 51.98 | 73.17 |
|  | 5x10-4 | 1.86 | 0.0923 | 0.69 | 348.5 | 1.87 | 34.34 | 82.90 |
|  | 1x10-3 | 2.10 | 0.0677 | 0.75 | 471.1 | 1.15 | 25.12 | 87.35 |
|  | 5x10-3 | 2.01 | 0.0499 | 0.74 | 628.5 | 1.28 | 19.17 | 90.52 |

Table 7

Surface composition (wt.%) of C-steel after 24 hrs. immersion in 1.0 M HCl in absence and presence the optimum concentrations of the studied inhibitors

| Samples | Fe | O | C | N | Cl | Br |
| --- | --- | --- | --- | --- | --- | --- |
| Free | 91.9 | 3.85 | 4.25 | 0 | 0 | 0 |
| 1.0 M HCl | 60.23 | 29.28 | 8.31 | 0 | 2.18 | 0 |
| Schiff Base | 68.71 | 10.99 | 14.75 | 2.84 | 2.71 | 0 |
| Surfactant | 70.54 | 7.50 | 15.38 | 2.63 | 2.80 | 1.15 |

Table 8

Critical micelle concentration (Ccmc), effectiveness (πcmc), maximum surface excess (Γmax), and minimum area (Amin) values of the synthesized mono cationic surfactant at 25 oC

| Surfactant name | Ccmc × 103 (mol dm-3) | cmc (mN m-1) | πcmc (mN m-1) | Γmax × 1011 (mol cm-2) | Amin (nm2) |
| --- | --- | --- | --- | --- | --- |
| Surfactant | 3.72 | 25.0 | 47.0 | 1.09 × 10-10 | 1.52 |

Table 9

Quantum chemical parameters for the studied inhibitors

| Parameter | Schiff Base | Surfactant |
| --- | --- | --- |
| E HOMO (eV) | -5.563 | -5.632 |
| E LUMO (eV) | -1.214 | -1.358 |
| ▲E (eV) | 4.349 | 4.275 |
| I (eV) | 5.563 | 5.632 |
| A (eV) | 1.214 | 1.358 |
| χ (eV) | 3.389 | 3.495 |
| η (eV) | 2.175 | 2.137 |
| σ (eV-1) | 0.460 | 0.468 |
| (ω) | 2.640 | 2.857 |
| ΔN (e) | 0.830 | 0.820 |
| µ (D) | 1.998 | 2.125 |
| T.E (eV) | -20879.08 | -98553.69 |
| M.V (cm3/mol) | 212.768 | 314.768 |
| TNC (e) | -4.091 | -7.411 |

Table 10

Comparative evaluation of the corrosion inhibition performance of the synthesized Schiff base and its corresponding surfactant with literature-reported inhibitors

| Inhibitor Name | IE (%) | Ref. |
| --- | --- | --- |
| N¹,N¹′-(1,4-phenylene)bis[N⁴-(4-methoxybenzylidene)benzene-1,4-diamine | 71.42 | [56] |
| 4(p-tolyldiazenyl)-2-((E)-(p-tolylimino)methyl)phenol | 55 | [57] |
| (E)-N-phenethyl-1-(pyridine-4yl)ethan-1-imine | 82.31 | [58] |
| 1-(4-bromophenyl)-N-pentylmethanimine | 84.12 | [59] |
| N,N-bis(2-hydroxyethyl)-N-octylbenzo[d] thiazol-2- ammonium bromide | 87.26 | [11] |
| N-(3-(butylideneamino)propyl)-N,N-dimethyldodecan-1-ammonium bromide | 86.62 | [60] |
| (E)-N-(3-((4-hydroxy-3-methoxybenzylidene)amino)propyl)-N,N-dimethylhexadecan-1-aminium | 84 | [61] |
| nonionic dithiol surfactant (PDP) | 62 | [62] |
| (Z)-N,N-dimethyl-3-((1-methylpyrrolidin-2-ylidene)amino)propan-1-amine | 70.54 | This Study |
| (E)-N,N-dimethyl-N-(3-((1-methylpyrrolidin-2-ylidene)amino)propyl)dodecan-1-aminium bromide | 90.90 | This Study |