Supplementary Material

MOF-derived S-scheme CuFe2O4/CuO/C heterojunctions with broad-spectrum response for efficient and stable tetracycline degradation

Liping Wang*, Ziyun Zhang, Chunyan Gao, Zhicong Li, Zhijuan Wang*, Yingchun Miao*

Corresponding author. wanglp_csu@163.com

Yunnan Key Laboratory of Crystalline Porous Organic Functional Materials, College of Chemistry and Materials Engineering, Qujing Normal University, Qujing, 655011, Yunnan Province, PR China

Fig. S1 Elemental mapping images of CuFe-PBA

Fig. S2 SEM images of CuFe2O4/CuO/C composites

Fig. S3 Elemental mapping images of CuFe2O4/CuO/C synthesized at 400 oC

Table S1 Relative amounts of different elements in CuFe2O4/CuO/C composites

| Sample | Elements (wt%) |  |  |  |
| --- | --- | --- | --- | --- |
|  | Cu | Fe | O | C |
| T300 | 43.58 | 30.07 | 20.56 | 5.80 |
| T350 | 45.87 | 27.19 | 21.72 | 5.22 |
| T400 | 41.23 | 34.62 | 19.82 | 4.34 |
| T450 | 42.30 | 33.09 | 20.60 | 4.01 |
| T500 | 42.99 | 33.19 | 19.94 | 3.68 |

Fig. S4. Tuac plots of T300, T350, T450, and T500

Table S2 The CB and VB values of CuFe2O4/CuO/C composites

| Sample Semiconductor | CuFe2O4 |  | CuO |  |
| --- | --- | --- | --- | --- |
|  | CB (eV) | VB (eV) | CB (eV) | VB (eV) |
| T300 | -0.47 | 0.99 | 0.70 | 1.93 |
| T350 | -0.47 | 0.99 | 0.69 | 1.93 |
| T450 | -0.48 | 1.00 | 0.68 | 1.94 |
| T500 | -0.48 | 1.00 | 0.68 | 1.95 |

Table S3 Calculation of CB and VB vs.vacuum

| Semiconductor | CB vs. NHE (eV) | VB vs. NHE (eV) | CB vs. vacuum (eV) | VB vs. vacuum (eV) |
| --- | --- | --- | --- | --- |
| p-type CuFe2O4 | -0.47 | 0.99 | Evac=－4.5－ENHE Evac=－4.03 | Evac=－4.5－ENHE Evac=－5.49 |
| p-type CuO | 0.69 | 1.93 | Evac=－4.5－ENHE Evac=－5.19 | Evac=－4.5－ENHE Evac=－6.43 |

Table S4 Calculation of Ef and Φ

| Semiconductor | Ef (eV) | Φ=Evac-Ef (eV) |
| --- | --- | --- |
| p-type CuFe2O4 | －5.29 | Φ=0－(－5.29) Φ=5.29 |
| p-type CuO | －6.23 | Φ=0－(－6.23) Φ=6.23 |

Table S5 Degradation products table of tetracycline

| NO. | R. Time | Formula | Calculated | Observed | Error (ppm) | Structure |
| --- | --- | --- | --- | --- | --- | --- |
| TC | 7.82 | C22H24N2O8 | 445.1605 | 445.1612 | 1.57 |  |
| P1 | 7.47 | C21H22N2O8 | 431.1449 | 431.1457 | 1.86 |  |
| P2 | 7.37 | C21H20N2O7 | 413.1343 | 413.1352 | 2.18 |  |
| P3 | 9.78 | C21H20N2O7 | 413.1343 | 413.1352 | 2.18 |  |
| P4 | 6.32 | C22H24N2O9 | 461.1555 | 461.1567 | 2.60 |  |
| P5 | 6.14 | C21H22N2O10 | 463.1347 | 463.1357 | 2.16 |  |
| P6 | 8.01 | C21H24N2O7 | 417.1656 | 417.1664 | 1.92 |  |
| P7 | 7.76 | C20H22N2O7 | 403.1500 | 403.1512 | 2.98 |  |
| P8 | 7.14 | C22H24N2O9 | 461.1555 | 461.1565 | 2.17 |  |
| P9 | 3.71 | C22H24N2O10 | 477.1504 | 477.1516 | 2.51 |  |
| P10 | 6.31 | C22H26N2O10 | 479.1660 | 479.1670 | 2.09 |  |
| P11 | 5.35 | C21H24N2O8 | 433.1605 | 433.1618 | 3.00 |  |
| P12 | 7.47 | C20H22N2O7 | 403.1500 | 403.1509 | 2.23 |  |
| P13 | 7.44 | C21H24N2O7 | 417.1656 | 417.1665 | 2.16 |  |
| P14 | 7.71 | C21H22N2O6 | 399.1551 | 399.1561 | 2.51 |  |

Fig.S5 Mass spectra of intermediates