# Supporting Information

Reconciling electrothermal de-icing and broadband electromagnetic transparency via a hexagonal honeycomb graphene glass fabric metasurface with impedance modulation and resonant coupling

Yuansong Zeng a* , Jiechen Wang a , Guojia Ma a , Qi Tang a, Xiaoqiang Jiang a , Zhuangzhuang Wu a, Yuping Duan b

a Science and Technology on Power Beam Processes Laboratory, AVIC Manufacturing Technology Institute, Beijing 100024, P.R. China

b Key Laboratory of Solidification Control and Digital Preparation Technology (Liaoning Province), School of Materials Science and Engineering, Dalian University of Technology, Dalian 116085, P. R. China.

Corresponding Author

Yuansong Zeng - Science and Technology on Power Beam Processes Laboratory, AVIC Manufacturing Technology Institute, Beijing 100024, People’s Republic of China; orcid.org/0009-0003-8294-8750; Email: yszeng625@163.com

Supplementary information 1:

Fig. S1 a, SEM. b, Particle size distribution of the CIP particles

Supplementary information 2:

Fig. S1 Electromagnetic parameters of signal-absorbing patches a, ε' and ε". b, μ' and μ". c, process for preparing signal-absorbing patches. d, reflection loss

The electromagnetic parameters of the wave-absorbing patches are shown in Fig. S2a and b. The fabrication process is shown in Fig. S2c. First, CIP and PU are mixed. To ensure uniform dispersion of CIP in the PU matrix, mechanical stirring and ultrasonic stirring are alternated twice, with each step lasting 15 minutes. The mixture was vacuum-treated for 10 minutes to remove air bubbles. The CIP-PU mixture was then applied to the mold using a squeegee. After curing for 24 hours, the patch was demolded, completing the preparation of the signal-absorbing patch. The signal-absorbing performance of the signal-absorbing patch is shown in Fig. S2d. The signal-absorbing bandwidth is 4.5 GHz, and the absorption frequency band is 10.1-14.6 GHz.