Facile synthesis of tomato-based carbon nanodots and its utilization in sensitive detection of tartrazine

Haijian Liu*a, Zhenxiang Lia, Wei Zhanga, Ying Liua, Rongkai Pan*a, Guofu Huanga

a Department of Agriculture and Environment, Weifang University of Science and Technology, Shouguang, 262700 Weifang, China.

*Corresponding author:

Haijian Liu, E-mail: liuhaijian.1987@163.com

Rongkai Pan, E-mail: panrk@wfust.edu.cn

Quantum yield measurement

The quantum yield (Φ) of CDs was determined by comparing the integrated fluorescent intensities (excitation at 350 nm) and absorbance values (at 350 nm) of the CDs samples with those of rhodamine B. The quantum yield was calculated by the following equation, where Φ is the quantum yield, k is slope, η is the refractive index of the solvent, S is the standard and X is the sample.

ΦX= ΦS KXKSηXηS

Fig.S1 Photostability of the CDs measured with a fluorescence spectrophotometer at 20 min intervals (λex = 350 nm)

Fig.S2 The fluorescence intensity of  the CDs in the presence of different concentrations of NaCl.

Fig.S3 Effect of (a) pH of buffer solution, (b) dosage of CDs and (c) reaction time on fluorescence quenching efficiency of the CDs-tartrazine system. Where F0 and F are the fluorescence intensity of CDs in the absence and presence of tartrazine. Conditions: tartrazine (15 µΜ)

(a)

(b)

(c)

Table S1 Comparison of our method with other methods for the determination of tartrazine

| Method | Linear range (μM) | LOD (nM) | Reference |
| --- | --- | --- | --- |
| Electrochemical sensor | 0.02-1.18 | 8 | [1] |
| Thin-layer chromatography | 74.9-356 | - | [2] |
| High-performance liquid chromatography | 0.0934-9.34 | 18.5 | [3] |
| Multi-walled carbon nanotubes film-modified electrode | 0.37-74.8 | 187 | [4] |
| Reversed-phase high-performance liquid chromatography | 0.011-39.3 | 3.5 | [5] |
| Capillary zone electrophoresis | 5.6-178 | 2430 | [6] |
| Fluorescence analysis | 0.25-32.5 | 73 | [7] |
| Our method | 0.1-40 | 39 | This work |

Reference

1.	Gan T, Sun JY, Meng W, Song L and Zhang YX (2013) Electrochemical sensor based on graphene and mesoporous TiO2 for the simultaneous determination of trace colourants in food. Food Chemistry 141:3731-3737. doi: 10.1016/j.foodchem.2013.06.084

2.	Soponar F, Mot AC and Sarbu C (2008) Quantitative determination of some food dyes using digital processing of images obtained by thin-layer chromatography. Journal of Chromatography A 1188:295-300. doi: 10.1016/j.chroma.2008.02.077

3.	Li W-J, Zhou X, Tong S-S and Jia Q (2013) Poly(N-isopropylacrylamide-co-N,N '-methylene bisacrylamide) monolithic column embedded with gamma-alumina nanoparticles microextraction coupled with high-performance liquid chromatography for the determination of synthetic food dyes in soft drink samples. Talanta 105:386-392. doi: 10.1016/j.talanta.2012.10.065

4.	Zhang W, Liu T, Zheng X, Huang W and Wan C (2009) Surface-enhanced oxidation and detection of Sunset Yellow and Tartrazine using multi-walled carbon nanotubes film-modified electrode. Colloids and Surfaces B-Biointerfaces 74:28-31. doi: 10.1016/j.colsurfb.2009.06.016

5.	Minioti KS, Sakellariou CF and Thomaidis NS (2007) Determination of 13 synthetic food colorants in water-soluble foods by reversed-phase high-performance liquid chromatography coupled with diode-array detector. Analytica Chimica Acta 583:103-110. doi: 10.1016/j.aca.2006.10.002

6.	Perez-Urquiza M and Beltran JL (2000) Determination of dyes in foodstuffs by capillary zone electrophoresis. Journal of Chromatography A 898:271-275. doi: 10.1016/s0021-9673(00)00841-4

7.	Xu H, Yang XP, Li G, Zhao C and Liao XJ (2015) Green Synthesis of Fluorescent Carbon Dots for Selective Detection of Tartrazine in Food Samples. Journal of Agricultural and Food Chemistry 63:6707-6714. doi: 10.1021/acs.jafc.5b02319