Supplementary Material

Fluorinated magnetic covalent organic framework-enhanced laser desorption/ionization mass spectrometry and imaging for determination of perfluoroalkyl ether carboxylic acids

Yanfang Zhaoa, Jun Wangb, Rabah Boukherroubc, Ke Jiaa, Sabine Szuneritsc, Lu Liua, Xiangrong Chena, Xiangfeng Chen*,a

aKey Laboratory for Applied Technology of Sophisticated Analytical Instruments of Shandong Province, Shandong Analysis and Test Centre, Qilu University of Technology (Shandong Academy of Sciences), Jinan, Shandong, 250014, PR China.

bKey Laboratory of Supervising Technology for Meat and Meat Products, Shandong Institute for Food and Drug Control, Jinan, Shandong, 250101, China

cUniv. Lille, CNRS, Univ. Polytechnique Hauts-de-France, UMR 8520, IEMN, F-59000 Lille, France

Address correspondence to:

Prof. X. F. Chen, qlgdchenxf@126.com

Contents

Fig. S1. FTIR spectra of Fe3O4, F-COF and Fe3O4@F-COF.

Fig. S2. Ultraviolet-visible spectra of Fe3O4, F-COF and Fe3O4@F-COF.

Table S1. Main peaks and LODs (S/N=3) of PFECAs obtained using Fe3O4@F-COF as an adsorbent and matrix in blank spring water samples.

Table S2. Main peaks and LODs (S/N=3) of PFECAs obtained using Fe3O4@F-COF as an adsorbent and matrix in blank human serum samples.

Table S3. Results of the recoveries of PFECAs in real samples.

Fig. S1. FTIR spectra of Fe3O4, F-COF and Fe3O4@F-COF.

Fig. S2. Ultraviolet-visible spectra of Fe3O4, F-COF and Fe3O4@F-COF.

Table S1. Main peaks and LODs (S/N=3) of PFECAs obtained using Fe3O4@F-COF as an adsorbent and matrix in blank spring water samples.

| Analyte | m/z | LOD (ng/L) | LOQ (ng/L) | Linear range (ng/L) | Shot-to-shot RSD (%) | Sample-to-sample RSD (%) |
| --- | --- | --- | --- | --- | --- | --- |
| GenX | 329.08 | 0.10 | 0.35 | 0.50–500 | 4.22 | 5.46 |
| EEA | 345.05 | 0.075 | 0.25 | 0.30–500 | 7.26 | 10.2 |
| ADONA | 377.07 | 0.15 | 0.45 | 0.50–500 | 9.48 | 6.65 |

Table S2. Main peaks and LODs (S/N = 3) of PFECAs obtained using Fe3O4@F-COF as an adsorbent and matrix in blank human serum samples.

| Analyte | m/z | LOD (ng/L) | LOQ (ng/L) | Linear range (ng/L) | Shot-to-shot RSD (%) | Sample-to-sample RSD (%) |
| --- | --- | --- | --- | --- | --- | --- |
| GenX | 329.08 | 0.15 | 0.50 | 0.75–500 | 8.65 | 10.2 |
| EEA | 345.05 | 0.10 | 0.25 | 0.50–500 | 6.44 | 8.54 |
| ADONA | 377.07 | 0.20 | 0.75 | 1.00–500 | 6.18 | 7.23 |

Table S3. Results of the recoveries of PFECAs in real samples.

| Analyte Samples | GenX | EEA | ADONA |
| --- | --- | --- | --- |
| Spring water Detection (μg/L) Recoverya (%) Recoveryb (%) Recoveryc (%) Human serum Detection (μg/L) Recoverya (%) Recoveryb (%) Recoveryc (%) | N.D. 90.12±4.37 96.32±5.73 83.28±1.45 N.D. 107.3±4.32 84.76±1.34 96.31±4.43 | N.D. 101.3±3.86 87.34±3.09 90.29±5.44 N.D. 83.65±1.66 114.4±4.32 105.4±4.38 | N.D. 109.4±4.54 101.7±4.87 92.36±3.76 N.D. 83.43±2.33 89.76±3.16 107.6±4.86 |

Spiked levels: (a) 5 ng/L; (b) 50 ng/L; (c) 250 ng/L; N.D.: not detected.