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Fig. S1. FTIR spectra of Fe3O4, F-COF and Fe3O4@F-COF.
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Fig. S2. Ultraviolet-visible spectra of Fe3O4, F-COF and Fe3O4@F-COF.



[bookmark: _Hlk516581974]Table S1. Main peaks and LODs (S/N=3) of PFECAs obtained using Fe3O4@F-COF as an adsorbent and matrix in blank spring water samples.
	Analyte
	m/z
	LOD 
(ng/L)
	LOQ
(ng/L)
	Linear range 
(ng/L)
	Shot-to-shot RSD (%)
	Sample-to-sample RSD (%)

	GenX
	329.08
	0.10
	0.35
	0.50–500
	4.22
	5.46

	EEA
	345.05
	0.075
	0.25
	0.30–500
	7.26
	10.2

	ADONA
	377.07
	0.15
	0.45
	0.50–500
	9.48
	6.65





Table S2. Main peaks and LODs (S/N = 3) of PFECAs obtained using Fe3O4@F-COF as an adsorbent and matrix in blank human serum samples.
	Analyte
	m/z
	LOD 
(ng/L)
	LOQ
(ng/L)
	Linear range 
(ng/L)
	Shot-to-shot RSD (%)
	Sample-to-sample RSD (%)

	GenX
	329.08
	0.15
	0.50
	0.75–500
	8.65
	10.2

	EEA
	345.05
	0.10
	0.25
	0.50–500
	6.44
	8.54

	ADONA
	377.07
	0.20
	0.75
	1.00–500
	6.18
	7.23







Table S3. Results of the recoveries of PFECAs in real samples.
	Analyte
Samples
	GenX
	EEA
	ADONA

	Spring water
Detection (μg/L)
Recoverya (%)
Recoveryb (%)
Recoveryc (%)
Human serum
Detection (μg/L)
Recoverya (%)
Recoveryb (%)
Recoveryc (%)
	
N.D.
90.12±4.37
96.32±5.73
83.28±1.45

N.D.
107.3±4.32
84.76±1.34
96.31±4.43
	
N.D.
101.3±3.86
87.34±3.09
90.29±5.44

N.D.
83.65±1.66
114.4±4.32
105.4±4.38
	
N.D.
109.4±4.54
101.7±4.87
92.36±3.76

N.D.
83.43±2.33
89.76±3.16
107.6±4.86


[bookmark: _Hlk125648758][bookmark: OLE_LINK55][bookmark: OLE_LINK52]Spiked levels: (a) 5 ng/L; (b) 50 ng/L; (c) 250 ng/L; N.D.: not detected.
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