Supplementary Material

For

ZnO functionalized sugarcane bagasse biochar via termal conversion of zinc hydroxichloride for photocatalytic degradation of paracetamol in aqueous medium

Erik Souza Pereiraa,  Ralf R. Ramalho Juniora*, Sandro José de Andradea

a Laboratory of Inorganic Synthesis and Enviromental Analytical Chemistry, Institute of Physics and Chemistry, Federal University of Itajubá, 3500-903, Minas Gerais, Brazil

Fig.S1. Photocount spectra of Hg vapor lamp used.

Fig. S2. SEM micrographs of BC at 100x (A) and 1000x magnification (B).

Table S1. EDS-general semi-quantification of ZnO@BC.

| Element | Amount (wt%) |
| --- | --- |
| Zn | 41.31 |
| O | 13.06 |
| C | 43.93 |
| Cl | 0.16 |
| Na | 1.4 |
| Si | 0.14 |
| Total | 100.0 |