Supporting Information

Sustainable Regeneration of High-Purity Quartz Sand from Silica Waste via Purification System and Sol-gel Method.

Zehui Zhanga,b, Dake Zhanga,b, Guoqing Zhanga,b, Kun Wanga,b,*, Deren Yanga,b, Xuegong Yu a,b,*

a State Key Laboratory of Silicon and Advanced Semiconductor Materials & School of Materials Science and Engineering, Zhejiang University, Hangzhou 310027, PR China

b Institute of Information and Functional Materials, ZJU-Hangzhou Global Scientific and Technological Innovation Center, Hangzhou 311215, PR China

*Corresponding authors.

E-mail addresses: msekunwang@zju.edu.cn, yuxuegong@zju.edu.cn

Supplementary Tables

Table S1 The metal-impurities content of the silica-based waste materials (unit: ppm).

| Element | Content |  |  |
| --- | --- | --- | --- |
|  | pyrogenic silica | quartz sand | quartz glass |
| Ni | 0.12 | 0.12 | 0.59 |
| Fe | 5.77 | 5.77 | 3.86 |
| Ge | 0.00 | 0.00 | 0.00 |
| Cr | 0.28 | 0.28 | 0.43 |
| Mg | 0.02 | 0.02 | 1.53 |
| Mn | 0.07 | 0.07 | 0.78 |
| Cu | 0.00 | 0.00 | 0.16 |
| Ti | 0.27 | 0.27 | 4.07 |
| Zr | 0.40 | 0.40 | 0.71 |
| Ca | 0.00 | 0.00 | 11.61 |
| Al | 305.63 | 305.63 | 16.80 |
| Ba | 0.00 | 0.00 | 0.38 |
| Na | 4.56 | 4.56 | 5.17 |
| Li | 0.84 | 0.84 | 0.24 |
| K | 1.26 | 1.26 | 1.58 |
| Total | 319.22 | 319.22 | 47.92 |

Table S2 Composition test results of 8% sodium hydroxide used for dissolving silica fume. (unit: ppm)

| Element | Content |
| --- | --- |
| Ni | 3.25 |
| Fe | 5.51 |
| Ge | 0.00 |
| Cr | 0.87 |
| Mg | 0.06 |
| Mn | 0.00 |
| Cu | 0.00 |
| Ti | 2.46 |
| Zr | 2.23 |
| Ca | 2.35 |
| Al | 4.01 |
| Ba | 0.00 |
| Na | 21795.67 |
| Li | 0.03 |
| K | 130.26 |
| Total | 21947.69 |

Table S3 Composition test results of the gel obtained after the sodium silicate solution directly passing through 732 resin. (unit: ppm)

| Element | Content |
| --- | --- |
| Ni | 0.082 |
| Fe | 5.418 |
| Ge | 0.647 |
| Cr | 0.998 |
| Mg | 4.738 |
| Mn | 0.241 |
| Cu | 0.111 |
| Ti | 4.478 |
| Zr | 5.868 |
| Ca | 4.336 |
| Al | 22.95 |
| Ba | 0.076 |
| Na | 162.253 |
| Li | 0.016 |
| K | 0.699 |
| Total | 212.911 |

Table S4 The metal impurities content of the silica-based waste materials (unit: ppm).

| Element | Content |
| --- | --- |
| C | 1.6 |
| H | 3.2 |
| N | 4.8 |

Supplementary Figures

Figure S1. The micro-morphology of the silica waste materials: (a) silica fume, (b) natural quartz sand, (c) quartz products.

Figure S2 The dissolved reactants of three types of silica waste materials.