Supporting document

# Zhihui Qiu, Liwen Zhang, Yihong Ding*, Tianbiao Zeng*

College of Chemistry and Materials Engineering, Wenzhou University, Wenzhou Zhejiang 325035, China.

*: Corresponding authors. Email: yhdd@wzu.edu.cn

Text S1:

By plotting the natural logarithm of the peak current density against the natural logarithm of the scan rate derived from CV curves recorded at various sweep rates, the rate-determining step of the electrode reaction can be quantitatively identified—specifically, whether the electrochemical process is dominated by surface-capacitive behavior, ion diffusion, or a mixed contribution from both. The core analytical relationship is expressed as i = abv, where i is the current (A), v is the scan rate (V s-1), and a and b are adjustable constants. The key diagnostic parameter is the b-value:

b≈0.5: the current is governed by ion diffusion;

b≈1.0: the current is governed by surface capacitance;

0.5<b<1.0: a mixed regime involving both diffusion- and capacitance-controlled contributions.

Text S2:

When the diffusion of lithium ions within the material approaches a quasi-equilibrium state, the Li⁺ diffusion coefficient can be determined by measuring the transient potential response, as described by the following equation:

where τ is the duration of the current pulse; mB, MB, and VM denote the mass, molar mass, and molar volume of the active material, respectively; SS is the contact area between the electrode and the electrolyte; and ΔEτ and ΔES represent the potential change during the current pulse and the steady-state potential change during the subsequent relaxation period, respectively.

，,

Figure S1  XRD of 1Mn/SnS-G,SnS-G and SnS.

Figure S 2. Cycling stability of 2Mn/SnS-G, 3Mn/SnS-G, and 4Mn/SnS-G at a current density of 2 A g⁻¹

Figure S3. (a) Survey spectrum of SnS; (b) C 1s spectrum of SnS; (c) Sn 3d spectrum of SnS; (d) S2p spectrum of SnS.

Figure S4. (a) CV curves of SnS at different scan rates; (b) b-values determined from the prominent peaks in the CV curves of SnS at different scan rates.