Supplementary Materials

# Effects of modification and co-aging with soils on Cd(II) adsorption behaviors and quantitative mechanisms by biochar

Zhuowen Meng1, Shuang Huang1*, Zhongbing Lin1

1 State Key Laboratory of Water Resources and Hydropower Engineering Sciences, Wuhan University, Wuhan 430072, China (First author: 2018202060124@whu.edu.cn; Corresponding author: hsh5527@whu.edu.cn.)

Number of pages = 5

Number of table =  2

Number of figures = 1

The isotherm data of Cd(II) adsorption on biochars were fitted by the Langmuir (LM, Eq (1)) and Freundlich model (FM, Eq (2)):

(1)

(2)

Where Ce (mg·L−1) is the concentration of Cd(II) in the solution after equilibration, Qe (mg·g−1) is the adsorbed amount of Cd(II) on the biochar after equilibration, Qm (mg·g−1) is the maximum Cd(II) adsorption capacity for the biochar, KL (L·mg−1) and KF (mg·g−1) (mg·L−1)−n are the adsorption coefficients of the LM and FM, respectively, and n (dimensionless) is a constant fitted by the FM relevant to the adsorption heterogeneity of biochar surface.

Table S1 Parameters of Cd(II) adsorption on biochars obtained from Langmuir and Freundlich isotherm models.

| Biochar | Langmuir model |  |  | Freundlich model |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | QmL (mg·g-1) | KL (L·mg-1) | R2 | KF (mg·g-1)·(mg·L-1)-n | n | R2 |
| BC | 54.26 | 1.68 | 0.996 | 26.82 | 0.17 | 0.835 |
| MBC | 117.33 | 2.79 | 0.969 | 59.72 | 0.19 | 0.821 |
| OBC | 60.52 | 4.15 | 0.965 | 35.39 | 0.14 | 0.920 |
| PBC | 48.16 | 0.56 | 0.916 | 21.50 | 0.19 | 0.943 |
| PMBC | 105.27 | 0.10 | 0.927 | 21.14 | 0.35 | 0.992 |
| ABC | 47.28 | 0.01 | 0.978 | 2.01 | 0.55 | 0.941 |
| AMBC | 210.81 | 0.01 | 0.954 | 2.96 | 0.70 | 0.972 |
| BBC | 65.78 | 0.01 | 0.964 | 1.72 | 0.61 | 0.960 |
| BMBC | 503.62 | 0.01 | 0.970 | 1.41 | 0.85 | 0.976 |
| CBC | 88.79 | 0.02 | 0.887 | 7.54 | 0.44 | 0.944 |
| CMBC | 82.38 | 0.09 | 0.893 | 19.10 | 0.31 | 0.988 |

QmL (mg·g−1) is the maximum adsorption capacity of Cd(II) by biochars fitted by Langmuir isotherm model;

KL (L·mg−1) and KF (mg·g−1) (mg·L−1)−n are the adsorption coefficients of the LM and FM;

n (dimensionless) is a constant fitted by the FM relevant to the adsorption heterogeneity of biochar surface.

Table S2 Major cations released from and metals adsorbed on biochars during adsorption

| Element (mg·L-1) | K | Na | Ca | Mg | Sum |
| --- | --- | --- | --- | --- | --- |
| BC | 0.315 | 0 | 4.345 | 1.388 | 6.05 |
| MBC | 0.502 | 0 | 3.104 | 2.864 | 6.48 |
| PBC | 0 | 0 | 5.61 | 3.607 | 9.22 |
| PMBC | 0 | 0 | 2.32 | 2.239 | 4.56 |
| ABC | 0 | 0 | 0.644 | 0 | 0.64 |
| AMBC | 0 | 0 | 3.51 | 0.125 | 3.63 |
| BBC | 0 | 0 | 2.138 | 0.083 | 2.22 |
| BMBC | 0 | 0 | 4.844 | 0.092 | 4.94 |
| CBC | 0 | 0 | 0 | 0 | 0 |
| CMBC | 0 | 0 | 0.819 | 1.005 | 1.82 |

Fig. S1 SEM-EDS images of the biochars (BC, MBC, OBC) after the adsorption of Cd(II)