Supporting Information

Enhancing carbon utilization and adsorption performance of sludge derived activated carbon through molten salt synthesis method

En Shi a, Xinyu Wang a, Miao Zhang b*, Xin Wang a, Jianchun Gao b, Yunbin Zheng a

a School of Municipal and Environmental Engineering, Shenyang Jianzhu University, Shenyang, 110168, China

b School of Material Science and Engineering, Shenyang Jianzhu University, Shenyang, 110168, China

E-mail: zhangmiao@sjzu.edu.cn (Miao Zhang)

Fig. S1 FTIR spectra of sludge and SDAC, (a) sludge, (b) SDAC-0 and (c) SDAC-1

Fig. S2 SEM of SDAC, (a) SDAC-0, (b) SDAC-0.1, (c) SDAC-0.5, (d) SDAC-1, (e) SDAC-2, (f) SDAC-5 and (g) SDAC-10

Table S1 Textural properties of SDAC

| Samples | SBET (m²/g) | VTotal (cm3/g) | SMicro (m²/g) | VMicro (cm3/g) |
| --- | --- | --- | --- | --- |
| SDAC-0.1 | 182.35 | 0.17 | 90.41 | 0.04 |
| SDAC-0.5 | 414.60 | 0.28 | 276.84 | 0.13 |
| SDAC-1 | 549.72 | 0.37 | 273.85 | 0.13 |
| SDAC-2 | 416.46 | 0.27 | 208.35 | 0.10 |
| SDAC-5 | 503.19 | 0.41 | 152.37 | 0.07 |
| SDAC-10 | 549.60 | 0.45 | 153.39 | 0.07 |

Table S2 Adsorbing capacity of CO2 and methylene blue (MB) on SDAC

| Samples | CO2 adsorbing capacity a (mg/mg(SDAC)) | MB adsorbing capacity (mg/mg(SDAC)) |
| --- | --- | --- |
| SDAC-0.1 | 0.0401 | 0.0080 |
| SDAC-0.5 | 0.0565 | 0.0411 |
| SDAC-1 | 0.0575 | 0.0786 |
| SDAC-2 | 0.0458 | 0.0771 |
| SDAC-5 | 0.0451 | 0.0659 |
| SDAC-10 | 0.0512 | 0.0784 |
| a CO2 adsorption isotherms were measured at 298K and 1.0 bar |  |  |

Table S3 The yield and carbon utilization potential of SDAC

| Samples | Carbon mass fraction (mg(carbon)/mg(SDAC)) | Yield (mg(SDAC) /g(sludge)) | Carbon utilization potential (mg(carbon) /g(sludge)) |
| --- | --- | --- | --- |
| SDAC-0.1 | 0.2747 | 494.73 | 135.90 |  |
| SDAC-0.5 | 0.3316 | 482.07 | 159.85 |  |
| SDAC-1 | 0.3448 | 517.87 | 178.56 |  |
| SDAC-2 | 0.3593 | 484.73 | 174.16 |  |
| SDAC-5 | 0.3510 | 455.90 | 160.02 |  |
| SDAC-10 | 0.2816 | 448.00 | 126.16 |  |