Supporting information

Pt/TiO2 Catalyzed Hydrogenation of Benzoic Acid with Unprecedented High Activity

Miao Guo,1 Xiangtao Kong,2 Chunzhi Li,1,3 Qihua Yang1*

1 State Key Laboratory of Catalysis, Dalian Institute of Chemical Physics, Chinese Academy of Sciences, Dalian 116023, China.

2 College of Chemistry and Chemical Engineering, Anyang Normal University, Anyang 455000, China.

3 University of Chinese Academy of Sciences, Beijing 100039, China.

Figure S1. TEM image of Pt/TiO2. Scale bar, 50 nm.

Figure S2. TEM images of (a) Pt/TiO2-200 and (b) Pt/TiO2-450. Scale bar, 50 nm.

Figure S3. HRSEM image of (a) Pt/TiO2-200 and (b) Pt/TiO2-450. Scale bar, 50 nm. The inset in panel a and b show particle size distribution of Pt/TiO2-200 and Pt/TiO2-450, respectively.

Figure S4. Reaction profiles of Pt/TiO2 and Pt/TiO2-450. Reaction conditions: 40 oC, 10 bar H2, 0.12 mmol BA, S/C=250, 3 mL hexane.

Figure S5. XPS spectra of Ti 2p of (i) TiO2, (ii) Pt/TiO2, (iii) Pt/TiO2-200 and (iv) Pt/TiO2-450.

Figure S6. TEM image of Pt/TiO2 after 5th recycle. Scale bar, 50 nm.

Table S1. The summarized results of BA hydrogenation under mild conditions in literatures.

| Catalyst | Conditions | TOF (h-1)a | Ref. |
| --- | --- | --- | --- |
| Pd/CN | 85 oC, 1 bar H2, H2O | 0.883 | 1 |
| Pd/AC | 85 oC, 15 bar H2, H2O | 5.7 | 2 |
| Pd/CNF | 85 oC, 15 bar H2, H2O | 0.35 | 3 |
| Pd/MCN | 85 oC, 25 bar H2, H2O | 26 | 4 |
| Pd/CNT | 100 oC, 35 bar H2, H2O | 87 | 5 |
| Pd/UiO-66-2OH | 85 oC, 1 bar H2, H2O | 0.416 | 6 |
| Pd/800N-AC | 110 oC, 25 bar H2, H2O | 35 | 7 |
| Ru/C-TiO2 | 70 oC, 25 bar H2, H2O | 45 | 8 |
| Ru/NFPC | 55 oC, 10 bar H2, H2O | 69.8 | 9 |
| Ru/C | 60 oC, 5 bar, iPrOH | 0.36 | 10 |
| Rh/N-C-700 | 55 oC, 10 bar H2, H2O | 320 | 11 |
| Rh/C | 50 oC, 20 bar H2, 100 bar CO2 | 45 | 12 |
| Pt NWs | 60 oC, 1 bar H2, H2O | 2.03 | 13 |
| Pt NWs | 70 oC, 10 bar H2, acetic acid | 5.3 | 14 |
| Ir/CN | 55 oC, 10 bar H2, H2O | 57 | 15 |
| RuPd/CN | 85 oC, 1 bar H2, H2O | 2.2 | 16 |
| Pt/TiO2 | 40 oC, 10 bar H2, hexane | 638 (2200)b | This work |
| Pt/TiO2 | 80 oC, 50 bar H2, hexane and acetic acid | 4490 (15480)b | This work |
| Pd/C | 80 oC, 50 bar H2, hexane and acetic acid | ~11 | This work |
| Ru/C | 80 oC, 50 bar H2, hexane and acetic acid | 94 | This work |

aApparent TOF; bData in parentheses was normalized by CO chemisorption.

Table S2. Pt/TiO2 catalyzed BA hydrogenation with different solvents.a

| Solvent | Conv. (%) | Sel. (%)b | pc | δd |
| --- | --- | --- | --- | --- |
| n-hexane | > 99 | > 99 | 0.009 | 4.98 |
| H2O | 84 | > 99 | 1.000 | 0.792 |
| cyclohexane | 78 | > 99 | 0.006 | 3.84 |
| Acetic acid | 68 | 96 | 0.648 | 2.61 |
| isopropyl alcohol | 34 | 98 | 0.546 | 3.48 |
| Ethyl acetate | 30 | 97 | 0.228 | 3.53 |
| EtOH | 19 | 96 | 0.654 | 3.66 |
| Tetrahydrofuran | 10 | 89 | 0.207 | 3.37 |
| Acetone | 4 | 93 | 0.355 | 3.12 |

aReaction conditions: BA = 0.12 mmol, S/C = 250, 3 mL solvent, 40 oC and 10 bar H2, 1 h. b Selectivity to CCA. cRelative polarity. The values are normalized from measurements of solvent shifts of absorption spectra and were extracted from Christian Reichardt, Solvents and Solvent Effects in Organic Chemistry, Wiley-VCH Publishers, 3rd ed., 2003. dSolubility of H2 (10−3 mol L-1, taken from ref. 18, 298.15 K, 1 atm H2).

Table S3. Reaction orders for BA hydrogenation with Pt/TiO2 and Pt/TiO2-450.

Reaction rate: r = k[BA]α[H2]β

| Cat. | BA order (α) | H2 order (β) | Overall (α+β) |
| --- | --- | --- | --- |
| Pt/TiO2 | -0.29 | +0.50 | +0.21 |
| Pt/SiO2-450 | +0.45 | +0.02 | +0.47 |

Table S4. The H2-D2 exchange results of Pt/TiO2 catalysts.

| Cat. | Conv. (%) | Normalized activity |
| --- | --- | --- |
| Pt/TiO2 | 5.96 | 100 |
| Pt/TiO2-200 | 1.37 | 23 |
| Pt/SiO2-450 | 0.67 | 11 |

Reaction conditions see experimental section.

Characterization of the pure products using 1H NMR and 13C NMR:

- 4-Methylcyclohexanecarboxylic acid

1H NMR (400 MHz, CDCl3): δ 11.76 (s, 1H), 2.56 (m, J = 4.8 Hz, 0.7H), 2.24 (tt, J = 12.4, 3.6 Hz, 0.3H), 2.03-1.98 (m, 2H), 1.78-1.19 (m, 7H), 0.9 (t, 6 Hz, 3H) ppm, (cis:trans = 70:30) ;

13C NMR (100 MHz, CDCl3): δ 181.63, 181.01, 41.91, 39.15, 33.14, 30.93, 30.29, 29.55, 27.82, 24.90, 21.42, 20.00 ppm.

- 3-Methylcyclohexanecarboxylic acid

1H NMR (400 MHz, CDCl3): δ 11.71 (s, 1H), 2.712-2.520 (m, J =4.8 Hz, 0.21H), 2.333 (tt, J = 12, 3.6 Hz, 0.79H), 1.98-1.94 (2H, m), 1.82-1.65 (m, 2H), 1.45-0.81 (9H, m) ppm, (cis:trans=79:21) ;

13C NMR (100 MHz, CDCl3): δ 182.49, 43.25, 39.03, 37.18, 35.25, 34.35, 33.64, 32.01, 29.71, 28.43, 28.30, 27.46, 25.42, 22.59, 21.88 ppm.

- 2-Methylcyclohexanecarboxylic acid

1H NMR (400 MHz, CDCl3): δ 11.67 (s, 1H), 2.57-2.15 (2 m, H), 1.75-1.22 (m, 9H), 0.98-0.96 (d, 7.2 Hz, 2.6H), 0.94-0.93 (d, 6.8 Hz, 0.4 H) ppm, cis:trans=86:14;

13C NMR (100 MHz, CDCl3): δ 181.29, 45.76, 34.14, 34.06, 31.75, 31.02, 29.83, 29.71, 25.77, 25.31, 24.38, 23.70, 21.45, 20.63 ppm.

- 4-Ethylcyclohexanecarboxylic acid

1H NMR (400 MHz, CDCl3): δ 11.71 (s, 1H,), 2.60-2.55 (m, J = 4.8 Hz, 0.72H), 2.25 (tt, J = 12.4, 3.6 Hz, 0.28H), 2.03-1.96 (m, 2H), 1.85-1.19 (m, 9H), 0.96-0.84 (m, 3H) ppm, (cia:trans=72:28);

13C NMR (100 MHz, CDCl3): δ 183.20, 182.62, 43.81, 40.94, 39.09, 37.96, 32.27, 30.22, 29.51, 29.28, 28.36, 26.46, 12.10, 11.85 ppm.

- 4-Pentylcyclohexanecarboxylic acid

1H NMR (400 MHz, CDCl3): δ 11.47 (s, 1H), 2.59-2.54 (m, J = 4.8 Hz, 0.72H), 2.25 (tt, J = 12.4, 3.6 Hz, 0.28H), 2.02-1.14 (m, 17H), δ 0.88 (t, J = 6.8 Hz, 3H) ppm, (cis:trans=72:28);

13C NMR (100 MHz, CDCl3): δ 181.73, 181.17, 42.33, 39.50, 36.11, 35.88, 34.59, 34.13, 31.21, 31.10, 28.42, 27.82, 25.74, 25.49, 24.96, 21.65 ppm.

- 4-Isopropylcyclohexane-1-carboxylic acid

1H NMR (400 MHz, CDCl3): δ 10.47 (s, 1H), 2.64-2.60 (m, J = 4.4 Hz, 0.68H), 2.24 (tt, J = 12.4, 3.6 Hz, 0.32H), 2.11-2.02 (m, 2H), 1.58-0.95 (m, 9H), 0.87-0.84 (m, 6H) ppm, (cis:trans=68:32);

13C NMR (100 MHz, CDCl3): δ 181.69, 181.11, 42.34, 42.22, 41.98, 38.93, 31.72, 30.43, 28.00, 27.78, 25.64, 25.46, 19.01, 18.71 ppm.

- 4-Trifluoromethylcyclohexanecarboxylic acid

1H NMR (400 MHz, CDCl3): δ 10.47 (s, 1H), 2.72-2.71 (m, J = 3.2 Hz, 0.64H), 2.32 (tt, J = 12.4, 3.6 Hz, 0.36H), 2.26-1.98 (m, 3H), 1.85-1.25 (m, 6H) ppm, (cis:trans=64:36);

13C NMR (100 MHz, CDCl3): δ 180.38, 179.77, 127.94, 127.81, 41.13, 40.36, 40.31, 40.09, 40.04, 39.83, 39.56, 37.50, 26.15, 24.45, 23.09, 23.07, 20.71, 20.68, 20.65, 20.63 ppm.

- 4-Hydroxycyclohexanecarboxylic acid

1H NMR (400 MHz, CDCl3): δ 8.55 (s, 1H), 4.13-4.07 (q, J = 7.2 Hz, 0.1H), 3.81-3.76 (m, J= 4.8 Hz, 0.34H), 3.63-3.58 (q, J = 7.2 Hz , 0.22H), 3.5 (tt, J = 10.8, 4 Hz, 0.23H), 2.41-2.17 (m, 1H), δ 2.01-1.16 (9H, m) ppm, (cis:trans = 60:40);

13C NMR (100 MHz, CDCl3): δ 178.62, 178.12, 177.84, 69.19, 66.37, 42.92, 42.11, 40.88, 33.95, 31.42, 28.93, 27.10, 25.55, 25.14, 23.64 ppm.

- 3-Cyclohexylpropionic acid

1H NMR (400 MHz, CDCl3): δ 11.63 (s, 1H), 2.36 (t, J = 8 Hz, 2H), 1.72-1.63 (m, 5H), 1.56-1.51 (q, J = 7.2 Hz,2H), 1.28-1.09 (m, 6H), 0.94-0.84 (m, 2H) ppm.

13C NMR (100 MHz, CDCl3): δ 179.6, 36.1, 31.9, 31.0, 30.6, 25.5, 25.2 ppm.

- 5-cyclohexylvaleric acid

1H NMR (400 MHz, CDCl3): δ 10.84 (s, 1H), 2.38-2.34 (t, J = 7.2 Hz, 2H), 1.71-1.63 (m, 5H), 1.53 (q, J = 7.2 Hz, 2H), 1.30-1.08 (m, 5H), 0.94-0.84 (m, 2H) ppm.

13C NMR (100 MHz, CDCl3): δ 179.63, 36.09, 31.91, 31.02, 30.66, 25.49, 25.17 ppm.

- Cyclohexanecarboxylic acid methyl ester

1H NMR (400 MHz, CDCl3): δ 3.66 (s, 3H), 2.30 (tt, J= 11.2, 3.6 Hz, 1H), 1.91-1.25 (m, 10H) ppm.

13C NMR (100 MHz, CDCl3): δ 176.59, 51.44, 43.12, 29.03, 25.75, 25.45 ppm.

- Mono-methyl terephthalate

1H NMR (400 MHz, CDCl3): δ 7.69 (s, 1H), 3.68 (s, 2 H), 3.67 (s, 1H), 3.68-3.67 (m, 3H), 2.54-2.24 (m, 2H), 2.10-1.87 (m, 4H, m), 1.72-1.66 (m, 3H), 1.52-1.44 (m, 1H) ppm, (cis:trans = 66:34);

13C NMR (100 MHz, CDCl3): δ 180.23, 179.89, 174.86, 174.45, 50.64, 50.62, 41.32, 41.18, 39.67, 39.33, 26.90, 26.78, 24.89, 24.77 ppm.

- Trans-cyclohexane-1,2-dicarboxylic acid

1H NMR (400 MHz, DMSO-d6): δ 11.59 (s, 1H), 2.66-2.65 (m, 2H), δ 1.90-1.84 (m, 2H), 1.66-1.63 (m, 2H), 1.36-1.34 (m, 4H) ppm, (cis:trans = 0:~100);

13C NMR (100 MHz, DMSO-d6): δ 175.4, 42.1, 26.4, 23.8 ppm.

- 1-Heptyl 2-octylcyclohexane-1,2-dicarboxylate

1H NMR (400 MHz, DMSO-d6): δ 4.03-3.91 (m, 4H), δ 2.82-2.81 (m, 2H), 2.02-1.79 (m, 2H), 1.65-1.27 (m, 24H), 0.89-0.85 (12H, m) ppm, (cis:trans = 0: ~100)

13C NMR (100 MHz, DMSO-d6): δ 173.93, 66.85, 66.83, 42.83, 38.88, 30.57, 30.55, 29.07, 29.06, 26.55, 24.01, 23.96, 23.93, 23.12, 14.18, 11.12 ppm.

- Cyclohexane-1,3-dicarboxylic acid

1H NMR (400 MHz, MeOD): δ 2.59-2.53 (m, J = 6 Hz, 0.47H), 2.24 (tt, J = 12 ,3.2 Hz, 1.54H), 1.91-1.79 (m, 3H), 1.67-1.62 (m, 1H), 1.50-1.17 (m, 4H) ppm, (cis:trans = 77:23);

13C NMR (100 MHz, MeOD):δ 179.12, 178.98, 43.64, 40.25, 32.49, 30.62, 29.75, 29.01, 25.97, 23.23 ppm.

- Cyclohexane-1,4-dicarboxylic acid

1H NMR (400 MHz, MeOD): δ 2.49-2.20 (m, 2H), 2.04-2.02 (m, 1H), 1.91-1.84 (m, 3H), 1.70-1.63 (m, 3H), 1.46-1.40 (m, 1H) ppm, (cis:trans = 77:23);

13C NMR (100 MHz, MeOD): δ 179.16, 178.37, 44.00, 41.94, 29.40, 27.13 ppm.

- Cis-cyclohexane-1,3,5-tricarboxylic acid

1H NMR (400 MHz, MeOD): δ 2.39 (tt, J = 12.4, 3.2 Hz, 3H), 2.21-2.18 (d, J = 12.4 Hz, 3H), 1.42-1.32 (q, J = 12.8 Hz, 3H) ppm, (cis:trans = ~100:0);

13C NMR (100 MHz, MeOD): δ 178.22, 42.81, 32.09 ppm.

- Cis-cyclohexane-1,3,5-tricarboxylic acid trimethyl ester

1H NMR (400 MHz, CDCl3): δ 3.68 (s, 9H), 2.38 (tt, J = 12.4, 3.2 Hz, 3H), 2.28-2.25 (d, J = 12.4 Hz, 3H), 1.57-1.48 (q, J = 12.8 Hz, 3H) ppm, (cis:trans = ~100:0);

13C NMR (100 MHz, CDCl3): δ 174.58, 52.02, 41.86, 30.56 ppm.

REFERENCES

(1) Xu, X.; Tang, M.; Li, M.; Li, H.; Wang, Y. Hydrogenation of Benzoic Acid and Derivatives over Pd Nanoparticles Supported on N‑Doped Carbon Derived from Glucosamine Hydrochloride. ACS Catal., 2014, 4, 3132-3135.

(2) Anderson, J. A.; Athawale, A. Imrie, F. E.; McKenna, F. M.; McCue, A.; Molyneux, D.; Power, K.; Shand, M.; Wells, R. P. K. Aqueous Phase Hydrogenation of Substituted Phenyls over Carbon Nanofibre and Activated Carbon Supported Pd. J. Catal., 2010, 270, 9–15.

(3) Anderson, J.; McKenna, F. M.; Linares-Solano, A.; Wells, R. K. Use of Water as a Solvent in Directing Hydrogenation Reactions of Aromatic Acids over Pd/carbon Nanofibre Catalysts. Catal. Lett., 2007, 119, 16-20.

(4) Jiang, H.; Yu, X.; Nie, R.; Lu, X.; Zhou, D.; Xia, Q. Selective Hydrogenation of Aromatic Carboxylic Acids over Basic N-Doped Mesoporous Carbon Supported Palladium Catalysts. Appl. Catal. A Gen., 2016, 520 , 73-81.

(5) Hu, Y.; Chen, W.; Xie, X.; Song, W. Carbon Nanotubes-Supported Well-Dispersed Pd Nanoparticles for the Efficiently Selective Hydrogenation of Benzoic Acid to Synthesize Cyclohexane Carboxylic Acid. Nano 2019, 14, 1950008.

(6) Chen, D.; Yang, W.; Jiao, L.; Li, L.; Jiang, H. L. Boosting Catalysis of Pd Nanoparticles in MOFs by Pore Wall Engineering: The Roles of Electron Transfer and Adsorption Energy. Adv. Mater., 2020, 2000041.

(7) Nie, R.; Jiang, H.; Lu, X.; Zhou, D.; Xia, Q. Highly Active Electron-Deficient Pd Clusters on N-Doped Active Carbon for Aromatic Ring Hydrogenation. Catal. Sci. Technol., 2016, 6, 1913-1920.

(8) Zhang, H.; Li, G.; Nie, R.; Lu, X.; Xia, Q. One-Pot Synthesized Mesoporous C-TiO2 Hybrid for Ru Catalyzed Low-Temperature Hydrogenation of Benzoic Acid. J. Mater. Sci., 2019, 54, 7529–7540.

(9) Li, M.; Tang, M.; Deng, J.; Wang, Y. Nitrogen-Doped Flower-Like Porous Carbon Materials Directed by In Situ Hydrolysed MgO: Promising Support for Ru Nanoparticles in Catalytic Hydrogenations. Nano Res., 2016, 9, 3129-3140.

(10) Maegawa, T.; Akashi, A.; Yaguchi, K.; Iwasaki, Y.; Shigetsura, M.; Monguchi, Y.; Sajiki, H. Efficient and Practical Arene Hydrogenation by Heterogeneous Catalysts under Mild Conditions. Chem.-Eur. J., 2009, 15, 6953-6963.

(11) Cao, Y.; Tang, M.; Li, M.; Deng, J.; Xu, F.; Xie, L.; Wang, Y. In Situ Synthesis of Chitin-Derived Rh/N–C Cataylsts: Efficient Hydrogenation of Benzoic Acid and Derivatives. ACS Sustainable Chem. Eng., 2017, 5, 9894–9902.

(12) Wang, H.; Zhao, F. Catalytic Ring Hydrogenation of Benzoic Acid with Supported Transition Metal Catalysts in scCO2. Int. J. Mol. Sci., 2007, 8, 628–634.

(13) Yu, T.; Wang, J.; Li, X.; Cao, X.; Gu, H. An Improved Method for the Complete Hydrogenation of Aromatic Compounds under 1 Bar H2 with Platinum Nanowires, ChemCatChem 2013, 5, 2852-2855.

(14) Guo, Z.; Hu, L.; Yu, H.; Cao, X.; Gu, H. Controlled Hydrogenation of Aromatic Compounds by Platinum Nanowire Catalysts. RSC Adv., 2012, 2, 3477-3480.

(15)Tang, M.; Mao, S.; Li, X.; Chen, C.; Li, M.; Wang, Y. Highly Effective Ir-based Catalysts for the Benzoic Acid Hydrogenation: Experiment and Theory Guided Catalysts Rational Design. Green Chem., 2017, 19, 1766-1774.

(16) Tang, M.; Mao, S.; Li, M.; Wei, Z.; Xu, F.; Li, H.; Wang, Y. RuPd Alloy Nanoparticles Supported on N-doped Carbon as An Efficient and Stable Catalyst for Benzoic Acid Hydrogenation. ACS Catal., 2015, 5, 3100-3107.