Bimetallic cobalt-nickel phosphide composite biomass carbon materials as efficient electrocatalysts for zinc-air batteries

Hanshuang Wanga, Min Taoa, Hengyu Linc, Chuanling Zhua, Chang Zoua, Qingye Liua, Jiangtao Li a, Xueyan Sunb*, Wei Zhaoa*, Yilun Liuc

a School of Chemical Engineering, Northwest University, Xi’an 710127, China

b Luoyang Institute of Science and Technology, Luoyang 471023, China

c School of Aerospace Xi'an Jiaotong University, Xi’an 710049, China

*Corresponding Author, E-mail: zhaowei3313@nwu.edu.cn

sunxueyan@lit.edu.cn

Fig. S1. SEM plot of CoNi@NC

Table S1. Specific surface area and pore volume of CoP@NC, CoMnP@NC, CoFeP@NC and CoNiP@NC

| Sample | Specific surface area (m2 g-1) | Pore volume (cm3 g-1) |
| --- | --- | --- |
| CoP@NC | 19.4875 | 0.0779 |
| CoMnP@NC | 16.9112 | 0.0630 |
| CoFeP@NC | 24.4811 | 0.0399 |
| CoNiP@NC | 17.5437 | 0.0889 |

Table S2. ORR onset potentials, half-wave potentials, limiting current values, and Tafel slopes for CoP@NC, CoMnP@NC, CoFeP@NC, CoNiP@NC, and Pt/C

|  | Eonset (V) | E1/2(V) | J0.2V(mA cm-2) | Tafel Slope (mV dec-1) |
| --- | --- | --- | --- | --- |
| CoP@NC | 0.813 | 0.658 | -4.17 | 102.94 |
| CoMnP@NC | 0.841 | 0.666 | -4.27 | 94.18 |
| CoFeP@NC | 0.821 | 0.661 | -4.03 | 93.44 |
| CoNiP@NC | 0.876 | 0.670 | -4.64 | 87.42 |
| Pt/C | 0.892 | 0.828 | -5.43 | 78.12 |

Table S3. OER starting potentials, overpotentials, and tafel slopes for CoP@NC, CoMnP@NC, CoFeP@NC, CoNiP@NC, and RuO2

|  | Eonset (V) | overpotential (V) | Tafel Slope (mV dec-1) |
| --- | --- | --- | --- |
| CoP@NC | 1.566 | 0.539 | 128.41 |
| CoMnP@NC | 1.541 | 0.527 | 126.54 |
| CoFeP@NC | 1.510 | 0.508 | 117.32 |
| CoNiP@NC | 1.501 | 0.503 | 116.26 |
| RuO2 | 1.533 | 0.597 | 133.32 |

Table S4. ORR and OER potential differences for CoP@NC, CoMnP@NC, CoFeP@NC, CoNiP@NC and Pt/C-RuO2 catalysts

|  | EORR (V) | EOER (V) | ∆E (V) |
| --- | --- | --- | --- |
| CoP@NC | 0.658 | 1.769 | 1.111 |
| CoMnP@NC | 0.666 | 1.757 | 1.091 |
| CoFeP@NC | 0.661 | 1.738 | 1.077 |
| CoNiP@NC | 0.670 | 1.733 | 1.063 |
| Pt/C-RuO2 | 0.828 | 1.827 | 0.999 |

Fig. S2. Nitrogen adsorption-desorption hysteresis curves and corresponding pore size distributions for (a, e) CoP@NC, (b, f) CoMnP@NC, (c, g) CoFeP@NC, and (d, h) CoNiP@NC.

Fig. S3. LSV curves of CoP@NC, CoMnP@NC, CoFeP@NC and CoNiP@NC catalysts (a-d) at different rotational speeds and the corresponding Koutecky-Levich plots (e-h).

Fig. S4. K-L plot of CoMP@NC catalyst at 0.2 V.

Table S5. Bifunctional catalytic activity of other catalysts in the literature

| Catalysts | EORR(V)(E1/2) | EOER(V) @j=10 mA cm-2 | ∆E=EOER-EORR |
| --- | --- | --- | --- |
| Mn-CoFeP-2 | 0.670 vs. RHE | 1.733 vs. RHE | 1.063 This work |
| Pt/C1 | 0.97 vs. RHE | 2.19 vs. RHE | 1.22 |
| IrO21 | 0.38 vs. RHE | 1.70 vs. RHE | 1.32 |
| RuO21 | 0.54 vs. RHE | 1.64 vs. RHE | 1.10 |
| Mn-Co3O42 | 0.69 vs. RHE | 1.80 vs. RHE | 1.11 |
| BSCF/g–C3N4VC3 | -0.324 vs. Ag/AgCl | 0.796 vs. Ag/AgCl | 1.12 |
| Co-AQ4 | 0.86 vs. RHE | 1.95 vs. RHE | 1.09 |
| Mn-Ni/RGO5 | 0.750 vs. RHE | 1.929 vs. RHE | 1.191 |
| GCN/CNT6 | 0.71 vs. RHE | 1.78 vs. RHE | 1.07 |

Table S6. The Comparison of liquid Zn-air batteries performance of this work with other non-noble metal-based catalysts recently reported.

| Catalysts | Cycling current density (mA cm-2 ) | Stability |
| --- | --- | --- |
| Mn-CoFeP-2 | 2 | 240 h This work |
| Co/N-CP7 | 5 | 30 h |
| VSMO8 | 5 | 20 h |
| Co-AQ4 | 2 | 100 h |
| Mn-Co3O49 | 2 | 90 h |
| C@CNT[Ni]10 | 5 | 120 h |
| Mo/NiCo2O411 | 5 | 96 h |

References

(1) Rincon, R. A.; Masa, J.; Mehrpour, S.; Tietz, F.; Schuhmann, W. Activation of oxygen evolving perovskites for oxygen reduction by functionalization with Fe-Nx/C groups. Chemical Communications 2014, 50 (94), 14760-14762.

(2) Shui, Z.; Yu, S.; Lu, W.; Xu, L.; Liu, Q.; Zhao, W.; Liu, Y. Bifunctional Electrocatalysts of Mn-doped Co3O4 for Oxygen Reduction and Oxygen Evolution Reactions in Alkaline Medium. Acta Chim. Sinica 2024, 82 (10), 1039-1049.

(3) Chen, F.; Xue, L.; Shang, Z.; Zhang, Z.; Chen, D. An enhanced non-noble perovskite-based oxygen electrocatalyst for efficient oxygen reduction and evolution reactions. Journal of Solid State Chemistry 2020, 282,

(4) Chai, R.-L.; Han, S.-B.; Wang, L.W.; Li, S.-H.; Pan, H.; Zhang, H.B.; Tu, X.Y.; Wang, Z.Y.; Wang, X.; Li, G.-Y.; et al. Electronic Structure Tunable Metallosupramolecular Polymers as Bifunctional Electrocatalysts for Rechargeable Zn-Air Battery. Small 2025, 21 (12),

(5) Xue, Y.; Wang, Y.; Zheng, Z.; Lu, Q.; Chen, W.; Yan, S.; Sun, S.; Zhang, H.; Shao, G. Nickel-hydroxide decorated trimanganese-tetroxide nanorods supported on graphene as bifunctional electrocatalyst for metal-air batteries. J. Electroanal. Chem. 2024, 963,

(6) Divinagracia-Luzadas, M.; Kaneko, K.; Hori, K.; Paraggua, J. A.; Noda, S.; Ocon, J. Synthesis and Evaluation of Self-Supporting Graphitic Carbon Nitride/ Carbon Nanotube (GCN/CNT) ORR/OER Electrodes in Aqueous and Non-Aqueous Media. Curr. Appl Phys. 2025, 71, 14-26.

(7) Li, H.; Qiu, H.; Aliyeva, A.; Wang, J.; Muller, M.; Hansen, L.; Tjardts, T.; Aktas, C.; Benedikt, J. Cobalt-decorated defective carbon paper as a self-supported catalyst for oxygen electrocatalysis and rechargeable zinc-air battery. Journal of colloid and interface science 2025, 689, 137230-137230.

(8) Riquelme-Garcia, P.; Garcia-Rodriguez, M.; Flores-Lasluisa, J. X.; Cazorla-Amoros, D.; Morallon, E. Enhanced electrocatalytic performance of SrMn1-xCoxO3 perovskite metal oxides for oxygen reactions in Zn-air batteries: Influence of Mn/Co ratio. Appl. Surf. Sci. Adv. 2025, 27,

(9) Shui, Z.; Tian, H.; Mu, H.; Xu, L.; Gao, X.; Chen, X. Mn doping for regulating the electronic structure of Co3O4 to construct dual active sites for oxygen electrocatalysis. Inorganic Chemistry Frontiers 2025, 12 (7), 2783-2791.

(10) Modak, A.; Phutela, A.; Kundu, A.; Das, S.; Bhasin, V.; Bhattacharyya, D.; Bhattacharya, S. Hyper-Cross-Linked Polymer-Derived Carbon-Coated Fe-Ni Alloy/CNT as a Bifunctional Electrocatalyst for Rechargeable Zinc-Air Batteries. Journal of Physical Chemistry Letters 2025, 16 (4), 1051-1065.

(11) Sharma, R.; Singh, A.; Halder, A. Synergistic effect of lattice strain, oxygen vacancy and morphology in Mo doped NiCo2O4 for high-performance zinc air batteries. Journal of Energy Storage 2025, 107, 114918.