Supplementary Table 1.

Experimental Results of Specific Surface Area and Pore Size Analyzer

| Sample ID | Weight (g) | Hole volume (Vp, cm3/g) | Total volume (Vs, cm3/g) | Porosity (%) |
| --- | --- | --- | --- | --- |
| 1 | 0.2117 | 0.1829 | 0.094 | 66.053 |
| 2 | 0.2488 | 0.2502 | 0.1105 | 69.35 |
| 3 | 0.2485 | 0.2159 | 0.1104 | 66.153 |
| 4 | 0.2239 | 0.1905 | 0.0995 | 65.69 |
| 5 | 0.2291 | 0.2157 | 0.1018 | 67.936 |
| Mean | 0.2324 | 0.21104 | 0.10324 | 67.036 |
| Std Dev | 0.01612296 | 0.02642249 | 0.007166101 | 1.5592 |

Supplementary Table 2.

Tensile Test Data from Universal Testing Machine

| Number | Thickness (mm) | Width (mm) | Cross-sectional Area (mm2) | Maximum Load (N) | Tensile Strength (N/mm2) |
| --- | --- | --- | --- | --- | --- |
| 1 | 0.51 | 11.26 | 5.7426 | 352.03 | 61.3018 |
| 2 | 0.72 | 12.93 | 9.3096 | 476.82 | 51.2181 |
| 3 | 0.57 | 15.57 | 8.8749 | 544.67 | 61.3714 |
| 4 | 0.48 | 15.04 | 7.2192 | 424.46 | 58.7953 |
| 5 | 0.77 | 15.96 | 12.2892 | 768.79 | 62.5582 |
| Mean | 0.61 | 14.152 | 8.6871 | 513.35 | 59.04896 |
| Std Dev | 0.1286468 | 1.995312006 | 2.460828629 | 159.29 | 4.5872239 |

Supplementary Table 3.

Qualitative morphological grading of cytotoxicity

| Grade | Reactivity | Conditions of all cultures |
| --- | --- | --- |
| 0 | None | Discrete intracytoplasmic granules, no cell lysis, no reduction of cell growth |
| 1 | Slight | Not more than 20% of the cells are round, loosely attached and without intracytoplasmic granules, or show changes in morphology; occasional lysed cells are present; only slight growth inhibition is observed. |
| 2 | Mild | Not more than 50% of the cells are round, devoid of intracytoplasmic granules; not more than 50% growth inhibition is observed. |
| 3 | Moderate | Not more than 70% of the cell layers contain rounded cells or are lysed; cell layers not completely destroyed, but more than 50% growth inhibition is observed. |
| 4 | Severe | Nearly complete or complete destruction of the cell layers. |

Supplementary Table 4.

Cytotoxicity evaluated using neutral red stain

|  | Neutral red stain (Cell lysis test) |  |  |  | MTT assay (Cell viability) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Test item | Cell | lysis | (%) | Grade | Absorbance (OD 570 nm) | Viability (%) | Mortality (%) |
| Blank (B) | 0 | 0 | 0 | 0 | 0.912 ± 0.036 | 100 | 0 |
| Negative control (NC) | 0 | 0 | 0 | 0 | 0.902 ± 0.03 | 99 | 1 |
| Positive control (PC) | 100 | 100 | 100 | 4 | 0.079 ± 0.001 | 9 | 91 |
| Test article group 1 | 0 | 0 | 0 | 0 | 0.644 ± 0.013 | 71 | 29 |
| Test article group 2 |  |  |  |  | 0.69 ± 0.002 | 76 | 24 |

The extraction ratio of test article surface/culture medium volume shall be 3 cm2 /mL,

Test article group 1: Test article extract, original extract

Test article group 2: 50 % extract of the test article

Positive control (PC):

Culture medium with 10% (v/v) DMSO, and incubated at a rotation speed of 100 rpm under 37±1 oC for 72±2h.

Negative control (NC):

The extraction ratio was 0.2 g/mL, took 1.0g HDPE, immersed it in 5.0 mL culture medium, and incubated at a rotation speed of 100 rpm under 37±1 oC for 72±2h.

Blank (B):

Took 5.0 mL of culture medium and then incubated at a rotation speed of 100 rpm under 37±1 oC for 72±2h.

Supplementary Table 5.

The Effect of Extracts of Nano-fiber Collagen Bone Graft Matrix on Percentage of PCEs to Total Erythrocyte and the Frequency of Micronucleated PCE.

| In vivo Mammalian Erythrocyte |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Group | Dose volume (mL/kg b.w.) |  | Dose level (mg/kg b.w.) |  | Concentration | Animal number |
| Negative control (Water for Injection) | 20 |  | - |  | - | 5 |
| Blank control (polar vehicle-Normal saline) | 20 |  | - |  | - | 5 |
| Polar extract (polar vehicle-Normal saline) | 20 |  | - |  | 1x extract | 5 |
| Blank control (Non-polar vehicle-cottonseed oil) | 20 |  | - |  | - | 5 |
| Non-polar extract (Non-polar vehicle-cottonseed oil) | 20 |  | - |  | 1x extract | 5 |
| Positive control (Cyclophosphamide) | 4 |  | 40 |  | 10 mg/mL | 5 |
| Total Erythrocyte | Individual Animal Data Animal (% PCES) |  |  |  |  |  |
| Group | Animal 1 | Animal 2 | Animal 3 | Animal 4 | Animal 5 | Mean ± SD |
| Negative control (Water for Injection) | 3.8 | 4 | 3.4 | 3.8 | 4 | 3.80 ± 0.24 |
| Blank control (polar vehicle-Normal saline) | 3.8 | 3.7 | 3.4 | 3.4 | 3.8 | 3.62 ± 0.20 |
| Polar extract (polar vehicle-Normal saline) | 4.2 | 3.1 | 4.1 | 3.6 | 3.1 | 3.62 ± 0.53 |
| Blank control (Non-polar vehicle-cottonseed oil) | 4 | 3.2 | 3.8 | 3.8 | 3 | 3.56 ± 0.43 |
| Non-polar extract (Non-polar vehicle-cottonseed oil) | 3.6 | 3.9 | 3.5 | 4 | 4.2 | 3.84 ± 0.29 |
| Positive control (Cyclophosphamide) | 1.4 | 1.6 | 1.5 | 2.7 | 1.6 | 1.76 ± 0.5 |
| Frequency of Micronucleated PCES | Individual Animal Data Animal (% PCES) |  |  |  |  |  |
| Group | Animal 1 | Animal 2 | Animal 3 | Animal 4 | Animal 5 | Mean ± SD |
| Negative control (Water for Injection) | 0.5 | 1 | 1 | 0.8 | 0.5 | 0.76 ± 0.25 |
| Blank control (polar vehicle-Normal saline) | 0.8 | 0.8 | 0.5 | 1 | 1.5 | 0.92 ± 0.37 |
| Polar extract (polar vehicle-Normal saline) | 0.5 | 0.8 | 1.3 | 1 | 0.5 | 0.82 ± 0.34 |
| Blank control (Non-polar vehicle-cottonseed oil) | 0.5 | 1 | 1.3 | 0.5 | 0.5 | 0.76 ± 0.37 |
| Non-polar extract (Non-polar vehicle-cottonseed oil) | 1 | 0.8 | 1.3 | 1 | 0.8 | 0.98 ± 0.20 |
| Positive control (Cyclophosphamide) | 16.5 | 7.3 | 14.3 | 8 | 10.8 | 11.38 ± 3.97 |

Supplementary Table 6.

Hematology Assay

| Groups | Negative control | Treatment | Negative control | Treatment |
| --- | --- | --- | --- | --- |
| Gender | Male | Male | Female | Female |
| Dosage (cm2 /rat) | 1 | 37 | 1 | 37 |
| Animal number | 10 | 10 | 10 | 10 |
| WBC (103 /μl) | 11.7 ± 1.2 | 12.0 ± 1.8 | 8.4 ± 0.9 | 9.0 ± 1.2 |
| RBC (106 /μl) | 9.58 ± 0.57 | 9.19 ± 0.41 | 8.82 ± 0.39 | 8.66 ± 0.32 |
| HGB (g/dl) | 16.6 ± 1.0 | 16.1 ± 0.8 | 15.5 ± 0.6 | 15.4 ± 0.5 |
| HCT (%) | 55.6 ± 2.8 | 54.0 ± 1.6 | 50.3 ± 2.1 | 49.3 ± 2.0 |
| MCV (fl) | 58.8 ± 2.1 | 57.6 ± 1.6 | 57.0 ± 1.8 | 56.9 ± 1.6 |
| MCH (pg) | 17.3 ± 0.3 | 17.2 ± 0.7 | 17.6 ± 0.4 | 17.8 ± 0.4 |
| MCHC (g/dl) | 29.5 ± 0.7 | 29.3 ± 0.7 | 30.8 ± 0.5 | 30.3 ± 0.7 |
| Platelet (103 /μl) | 907 ± 109 | 852 ± 80 | 943 ± 106 | 883 ± 106 |
| NEUT (%) | 7.5 ± 1.1 | 11.4 ± 2.0 | 7.6 ± 4.5 | 8.1 ± 2.4 |
| Lymphocyte (%) | 84.8 ± 1.5 | 79.5 ± 3.8 | 84.9 ± 4.0 | 85.0 ± 2.8 |
| Monocyte (%) | 6.1 ± 1.6 | 7.7 ± 2.1 | 6.2 ± 1.7 | 5.8 ± 0.9 |
| Eosinophil (%) | 1.5 ± 0.3 | 1.2 ± 0.4 | 1.3 ± 0.7 | 1.0 ± 0.2 |
| Basophil (%) | 0.1 ± 0.1 | 0.2 ± 0.1 | 0.1 ± 0.1 | 0.1 ± 0.1 |
| MPV (fl) | 8.55 ± 0.31 | 8.66 ± 0.34 | 8.75 ± 0.52 | 8.65 ± 0.21 |
| RDW (%) | 21.1 ± 0.9 | 20.6 ± 1.1 | 19.3 ± 1.2 | 18.7 ± 1.1 |

Mean ± S.D., n＝10

S.D.: standard deviation

WBC: White blood cell count, RBC: Erythrocyte count, HGB: Hemoglobin concentration, HCT: Hematocrit, MCV: Mean corpuscular volume, MCH: Mean corpuscular hemoglobin, MCHC: Mean corpuscular hemoglobin Concentration, NEUT: Neutrophil segment, MPV: Mean platelet volume, RDW: Red blood cell volume distribution width.

Data collated from Appendix 4-1 and 4-2.

Supplementary Table 7.

Clinical chemistry Assay

| Groups | Negative control | Treatment | Negative control | Treatment |
| --- | --- | --- | --- | --- |
| Gender | Male | Male | Female | Female |
| Dosage (cm2 /rat) | 1 | 37 | 1 | 37 |
| Animal number | 10 | 10 | 10 | 10 |
| Na (Sodium): mmol/L | 145 ± 2 | 146 ± 1 | 147 ± 2 | 146 ± 2 |
| K (Potassium): mmol/L | 9.2 ± 0.9 | 8.8 ± 0.7 | 8.1 ± 0.9 | 8.2 ± 1.1 |
| Cl (Chloride): mmol/L | 104 ± 2 | 104 ± 2 | 105 ± 1 | 106 ± 3 |
| AST: U/L | 109.6 ± 11.1 | 118.3 ± 14.8 | 91.9 ± 8.8 | 97.6 ± 7.2 |
| ALT: U/L | 41.9 ± 6.7 | 42.8 ± 6.5 | 32.4 ± 3.5 | 33.6 ± 2.8 |
| Total protein: g/dL | 6.3 ± 0.3 | 6.4 ± 0.2 | 6.9 ± 0.3 | 7.0 ± 0.2 |
| Albumin: g/dL | 3.3 ± 0.2 | 3.4 ± 0.2 | 3.9 ± 0.3 | 4.1 ± 0.3 |
| Globulin: g/dL | 3.0 ± 0.1 | 3.0 ± 0.2 | 3.0 ± 0.1 | 2.9 ± 0.3 |
| A/G ratio | 1.10 ± 0.08 | 1.16 ± 0.09 | 1.30 ± 0.13 | 1.41 ± 0.23 |
| Total Bilirubin: mg/dL | 0.12 ± 0.06 | 0.10 ± 0.00 | 0.10 ± 0.00 | 0.10 ± 0.00 |
| Amylase: U/L | 1615 ± 152 | 1597 ± 199 | 1537 ± 157 | 1426 ± 181 |
| γ-GT: U/L | 0.0 ± 0.0 | 0.0 ± 0.0 | 0.0 ± 0.0 | 0.0 ± 0.0 |
| Alkaline-P'ase: U/L | 119.0 ± 11.2 | 111.1 ± 11.1 | 68.3 ± 11.5 | 71.1 ± 8.7 |
| Alkaline-P’ase: U/L | 119.0 ± 11.2 | 111.1 ± 11.1 | 68.3 ± 11.5 | 71.1 ± 8.7 |
| BUN: mg/dL | 8.6 ± 1.1 | 8.2 ± 1.3 | 9.1 ± 1.1 | 8.6 ± 1.3 |
| Creatinine: mg/dL | 0.35 ± 0.05 | 0.36 ± 0.05 | 0.36 ± 0.05 | 0.33 ± 0.05 |
| Uric Acid: mg/dL | 5.2 ± 0.6 | 5.5 ± 0.4 | 4.6 ± 0.5 | 4.2 ± 0.5 |
| Cholesterol: mg/dL | 55.9 ± 9.3 | 61.6 ± 6.3 | 55.0 ± 6.5 | 53.1 ± 5.7 |
| Triglyceride: mg/dL | 85.6 ± 9.9 | 84.1 ± 8.6 | 82.0 ± 9.5 | 79.3 ± 9.0 |
| Glucose (AC): mg/dL | 313.8 ± 34.2 | 291.7 ± 33.1 | 245.5 ± 29.6 | 248.6 ± 31.5 |
| Ca (Calcium): mg/dL | 11.3 ± 0.5 | 11.1 ± 0.4 | 11.0 ± 0.4 | 10.8 ± 0.3 |
| P (Phosphorous): mg/dL | 11.1 ± 1.4 | 11.3 ± 1.2 | 9.4 ± 0.9 | 9.1 ± 0.9 |
| LDH: U/L | 313 ± 49 | 321 ± 39 | 386 ± 45 | 373 ± 52 |
| Lipase: U/L | 104 ± 16 | 113 ± 15 | 101 ± 12 | 94 ± 12 |
| Mg (Magnesium): Mg/dL | 4.2 ± 0.2 | 4.1 ± 0.2 | 4.0 ± 0.4 | 3.8 ± 0.4 |
| CPK: U/L | 66 ± 5 | 63 ± 9 | 60 ± 8 | 55 ± 7 |

Mean ± S.D., n＝10

S.D.: standard deviation

AST: Aspartate aminotransferase, ALT: Alanine aminotransferase, γ-GT: Gamma-glutamyltransferase, BUN: Blood Urea Nitrogen, LDH: Lactate Dehydrogenase, CPK: Creatine phosphokinase.

Data collated from Appendix 5-1 and 5-2.

Supplementary Table 8.

In Vitro Mammalian Cell Gene Mutation Test Using Mouse Lymphoma (L5178Y) Cells

Supplementary Table 8A.

Suspension Growth (SG) and Relative Total Growth (RTG) Short-term treatment without metabolic activation (-S9)

| Long-term treatment without metabolic activation (-S9) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Treatment group | Duplicate | Daily cell density (x105/mL) |  |  | SGc | SG (Mean ± S.D.) | RSGd | RTGe | RTG (Mean ± S.D.) |
|  |  | Posttreatment a,b | Day 1b | Day 2 |  |  |  |  |  |
| Negative | 1 | 21.6 | 7.8 | 9.21 | 48.49 | 50.08 ± 2.25 | 1 | 100 | 100.00 ± 0.00 |
|  | 2 | 22.5 | 7.98 | 9.21 | 51.68 |  | 1 | 100 |  |
| Blank polar | 1 | 22.6 | 7.62 | 8.91 | 47.95 | 47.69 ± 0.37 | 0.99 | 118.19 | 111.59 ± 9.34 |
|  | 2 | 21.2 | 7.98 | 8.97 | 47.42 |  | 0.92 | 104.98 |  |
| Blank additional | 1 | 21.1 | 7.68 | 9.03 | 45.73 | 44.83 ± 1.26 | 0.94 | 97.28 | 98.15 ± 1.23 |
|  | 2 | 20.6 | 8.03 | 8.5 | 43.94 |  | 0.85 | 99.02 |  |
| Polar extract | 1 | 20.8 | 6.92 | 7.57 | 34.05 | 34.80 ± 1.06 | 0.71 | 63.25 | 62.87 ± 0.55 |
|  | 2 | 19.2 | 7.27 | 8.15 | 35.55 |  | 0.75 | 62.48 |  |
| Additional extract | 1 | 20.9 | 7.21 | 9.03 | 42.52 | 42.83 ± 0.44 | 0.93 | 97.52 | 85.42 ± 17.11 |
|  | 2 | 21.8 | 7.45 | 8.5 | 43.14 |  | 0.98 | 73.32 |  |
| Positive MMS (10 µg/mL) | 1 | 20.6 | 4.05 | 4.46 | 11.63 | 13.92 ± 3.24 | 0.24 | 13.85 | 14.38 ± 0.75 |
|  | 2 | 23.3 | 4.46 | 4.99 | 16.2 |  | 0.31 | 14.91 |  |

a: 8 x 105 cells/mL were treated.

b: Cell density was adjusted to 2 x 105 cells/mL after counting (or original cell density if not sub-cultured).

c: SG = [Post-treatment / treated cell density] × [cell concentration at day 1 /2* x 105] × [cell concentration at day 2/2* x 105]

d: RSG = SG(test) / SG(control) *: RTG = RSG x Day 2 relative PE (refer to table 2).

Supplementary Table 8.

In Vitro Mammalian Cell Gene Mutation Test Using Mouse Lymphoma (L5178Y) Cells

Supplementary Table 8B.

Plating Efficiency at The Time of Mutant Selection

| Short-term treatment without metabolic activation (-S9) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Treatment group | Duplicate | Number of empty wells (EW) |  |  | PE (Absolute cloning efficiency) (%)a (Mean ± S.D.) | Relative PЕ (%)b |
|  |  | Plate A | Plate B | Total |  |  |
| Negative | 1 | 26 | 22 | 48 | 91.57 ± 6.97 | 100 |
|  | 2 | 19 | 22 | 41 |  | 100 |
| Blank polar | 1 | 22 | 25 | 47 | 92.23 ± 6.04 | 101.52 |
|  | 2 | 11 | 30 | 41 |  | 100 |
| Blank additional | 1 | 23 | 19 | 42 | 92.83 ± 3.05 | 109.63 |
|  | 2 | 19 | 26 | 45 |  | 93.97 |
| Polar extract | 1 | 22 | 25 | 47 | 100.96 ± 18.39 | 100 |
|  | 2 | 13 | 18 | 31 |  | 118.11 |
| Additional extract | 1 | 20 | 17 | 37 | 105.55 ± 3.74 | 108.34 |
|  | 2 | 12 | 22 | 34 |  | 119.32 |
| Positive MMS (10 g/mL) | 1 | 18 | 22 | 40 | 104.05 ± 8.50 | 113.15 |
|  | 2 | 19 | 14 | 33 |  | 114.06 |
| Short-term treatment with metabolic activation (+S9) |  |  |  |  |  |  |
| Treatment group | Duplicate | Number of empty wells (EW) |  |  | PE (Absolute cloning efficiency) (%)a (Mean ± S.D.) | Relative PЕ (%)b |
|  |  | Plate A | Plate B |  |  |  |
| Negative | 1 | 23 | 28 | 51 | 82.25 ± 0.86 | 100 |
|  | 2 | 34 | 18 | 52 |  | 100 |
| Blank polar | 1 | 19 | 26 | 45 | 86.16 ± 6.39 | 109.44 |
|  | 2 | 33 | 19 | 52 |  | 100 |
| Blank additional | 1 | 30 | 26 | 56 | 79.3 ± 3.28 | 92.94 |
|  | 2 | 32 | 20 | 52 |  | 100 |
| Polar extract | 1 | 17 | 27 | 44 | 95.06 ± 4.21 | 101.55 |
|  | 2 | 19 | 21 | 40 |  | 120.09 |
| Additional extract | 1 | 24 | 22 | 46 | 91.41 ± 2.98 | 115.96 |
|  | 2 | 24 | 19 | 43 |  | 114.5 |
| Positive MMS (10 g/mL) | 1 | 42 | 40 | 82 | 51.69 ± 2.10 | 64.18 |
|  | 2 | 42 | 44 | 86 |  | 61.48 |
| Long-term treatment witout metabolic activation (-S9) |  |  |  |  |  |  |
| Treatment group | Duplicate | Number of empty wells (EW) |  |  | PE (Absolute cloning efficiency) (%)a (Mean ± S.D.) | Relative PЕ (%)b |
|  |  | Plate A | Plate B | Total |  |  |
| Negative | 1 | 18 | 26 | 44 | 95.85 ± 5.33 | 100 |
|  | 2 | 19 | 20 | 39 |  | 100 |
| Blank polar | 1 | 21 | 12 | 33 | 112.02 ± 2.76 |  |
|  | 2 | 17 | 14 | 31 |  | 114.4 |
| Blank additional | 1 | 27 | 15 | 42 | 105.50 ± 14.87 |  |
|  | 2 | 16 | 14 | 30 |  | 116.46 |
| Polar extract | 1 | 20 | 20 | 40 | 96.51 ± 2.16 | 89.08 |
|  | 2 | 21 | 21 | 42 |  | 83.35 |
| Additional extract | 1 | 19 | 20 | 39 | 93.13 ± 9.18 | 104.88 |
|  | 2 | 26 | 22 | 48 |  | 74.68 |
| Positive MMS (10 g/mL) | 1 | 42 | 40 | 82 | 50.26 ± 4.11 | 57.75 |
|  | 2 | 44 | 46 | 90 |  | 47.54 |

a: PE (%) = [P / number of cells seeded per well] × 100% = [-ln (EW/TW)/1.6 cells] × 100%;

EW: number of empty well;

TW: number of total wells seeded (two 96-well plates, total 192 wells per duplicate);

b: Relative PE (%) = [Plating efficiency (test) / Plating efficiency (control)] × 100%

Supplementary Table 8.

In Vitro Mammalian Cell Gene Mutation Test Using Mouse Lymphoma (L5178Y) Cells

Supplementary Table 8C. Mutant Frequencies and Sizing for Small and Large Colonies

| Short-term treatment without metabolic activation (-S9) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Treatment | Duplicate | Number of mutant colonies |  |  |  | Total Number of small colonies | Total Number of large colonies | MF for 106 cellsa | MF for 106 cells (Mean ± S.D.) | IMF for 106 cells | Small colonies IMF for 106 cells |
|  |  | Plate A | Plate B | Plate C | Plate D |  |  |  |  |  |  |
| Negative | 1 | 13 | 9 | 9 | 11 | 24 | 18 | 66.84 | 63.43 ± 4.83 | 0 | 0 |
|  | 2 | 10 | 9 | 10 | 13 | 22 | 20 | 60.02 |  |  |  |
| Blank polar | 1 | 14 | 9 | 9 | 17 | 33 | 16 | 77.6 | 71.09 ± 9.20 | 7.66 | 10.69 |
|  | 2 | 12 | 11 | 12 | 10 | 27 | 18 | 64.58 |  |  |  |
| Blank additional | 1 | 9 | 9 | 14 | 16 | 30 | 18 | 70.29 | 67.89 ± 3.40 | 4.45 | 4.66 |
|  | 2 | 6 | 11 | 14 | 12 | 23 | 20 | 65.49 |  |  |  |
| Polar extract | 1 | 7 | 12 | 14 | 13 | 29 | 17 | 72.53 | 63.61 ± 12.62 | 0.00** | 0.00** |
|  | 2 | 11 | 8 | 14 | 12 | 30 | 15 | 54.68 |  |  |  |
| Additional extract | 1 | 13 | 10 | 10 | 12 | 24 | 21 | 60.56 | 73.13 ± 17.78 | 5.24 | 3.7 |
|  | 2 | 14 | 19 | 16 | 16 | 41 | 24 | 85.7 |  |  |  |
| Positive MMS (10 g/mL) | 1 | 53 | 53 | 55 | 50 | 165 | 46 | 406.65 | 396.58 ± 14.25 | 333.14 | 281.42 |
|  | 2 | 53 | 53 | 56 | 58 | 179 | 41 | 386.5 |  |  |  |
| Short-term treatment with metabolic activation (+S9) |  |  |  |  |  |  |  |  |  |  |  |
| Treatment | Duplicate | Number of mutant colonies |  |  |  | Total Number of small colonies | Total Number of large colonies | MF for 106 cellsa | MF for 106 cells (Mean ± S.D.) | IMF for 106 cells | Small colonies IMF for 106 cells |
|  |  | Plate A | Plate B | Plate C | Plate D |  |  |  |  |  |  |
| Negative | 1 | 14 | 5 | 11 | 13 | 37 | 6 | 71.67 | 72.20 ± 0.75 | 0 | 0 |
|  | 2 | 8 | 11 | 14 | 10 | 27 | 16 | 72.73 |  |  |  |
| Blank polar | 1 | 11 | 13 | 4 | 12 | 30 | 10 | 60.66 | 62.24 ± 2.24 | 0.00** | 0.00** |
|  | 2 | 11 | 5 | 13 | 9 | 33 | 5 | 63.82 |  |  |  |
| Blank additional | 1 | 16 | 14 | 11 | 11 | 38 | 14 | 94.47 | 82.71 ± 16.64 | 10.51 | 8.72 |
|  | 2 | 8 | 11 | 12 | 11 | 33 | 9 | 70.94 |  |  |  |
| Polar extract | 1 | 17 | 19 | 13 | 15 | 50 | 14 | 99 | 92.04 ± 9.84 | 29.8 | 19.22 |
|  | 2 | 12 | 18 | 14 | 15 | 43 | 16 | 85.08 |  |  |  |
| Additional extract | 1 | 19 | 22 | 15 | 21 | 56 | 21 | 125.3 | 128.64 ± 4.73 | 45.94 | 31.88 |
|  | 2 | 20 | 19 | 20 | 25 | 62 | 22 | 131.98 |  |  |  |
| Positive MMS (10 g/mL) | 1 | 70 | 64 | 66 | 61 | 212 | 49 | 1070.51 | 1041.35 ± 41.24 | 969.15 | 783.91 |
|  | 2 | 61 | 57 | 63 | 64 | 195 | 50 | 1012.19 |  |  |  |
| Long-term treatment without metabolic activation (-S9) |  |  |  |  |  |  |  |  |  |  |  |
| Treatment | Duplicate | Number of mutant colonies |  |  |  | Total Number of small colonies | Total Number of large colonies | MF for 106 cellsa | MF for 106 cells (Mean ± S.D.) | IMF for 106 cells | Small colonies IMF for 106 cells |
|  |  | Plate A | Plate B | Plate C | Plate D |  |  |  |  |  |  |
| Negative | 1 | 10 | 9 | 14 | 2 | 22 | 13 | 51.89 | 46.36 ± 7.83 | 0 | 0 |
|  | 2 | 8 | 11 | 5 | 6 | 23 | 7 | 40.83 |  |  |  |
| Blank polar | 1 | 11 | 11 | 7 | 11 | 37 | 3 | 49.97 | 50.36 ± 0.6 | 4.03 | 11.12 |
|  | 2 | 14 | 9 | 9 | 10 | 33 | 9 | 50.82 |  |  |  |
| Blank additional | 1 | 3 | 7 | 7 | 7 | 16 | 8 | 33.97 | 35.74 ± 2.49 | 0.00** | 0.00** |
|  | 2 | 13 | 5 | 6 | 8 | 25 | 7 | 37.5 |  |  |  |
| Polar extract | 1 | 8 | 10 | 13 | 7 | 26 | 12 | 53.14 | 66.46 ± 18.83 | 16.06 | 4.65 |
|  | 2 | 20 | 11 | 11 | 12 | 40 | 14 | 79.77 |  |  |  |
| Additional extract | 1 | 11 | 9 | 9 | 8 | 24 | 13 | 50.85 | 63.95 ± 18.53 | 28.22 | 16.21 |
|  | 2 | 13 | 13 | 11 | 11 | 32 | 16 | 77.06 |  |  |  |
| Positive MMS (10 g/mL) | 1 | 79 | 77 | 76 | 69 | 226 | 75 | 1440.38 | 1389.87 ± 71.44 | 1343.5 | 1054.7 |
|  | 2 | 68 | 68 | 71 | 69 | 225 | 51 | 1339.35 |  |  |  |

a: MF = [PE (mutant) /PE (viable)] × 106 = [P (mutant) /2 × 10³]/[P (viable) /1.6]* × 106 = {-ln [EW/TW (mutant)]/-ln [EW/TW (viable)]} × 800;

EW (mutant): number of empty well (TFT plate) = TW(TFT plate) — total number of mutant colonies = 384- [sum of the numbers of plate A + B + C+ D];

TW (mutant): number of total wells seeded (TFT plate) (four 96-well plates, total 384 wells, per duplicate);

* value of "P (viable) /1.6" refer to table 2; b: Induced mutation frequency (IMF) =MF (test) - MF (concurrent blank); MF (concurrent blank) - MF (concurrent negative);

** If the IMF is less than zero; the IMF is shown as zero.;

c: Small colonies IMF =MF of small colonies (test) - MF of small colonies (concurrent blank)

MF of small colonies (test or blank) = MF (test or blank) × [number of small colonies / total number of mutant colonies]

Supplementary Table 9.

Histological evaluation system

A. Histological evaluation system - Cell type/response

|  | Score |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Cell type/ response | 0 | 1 | 2 | 3 | 4 |
| Polymorphonuclear cells | 0 | Rare, 1 to 5 / phf a | 5 to 10 / phf | Heavy infilitrate | Packed |
| Lymphocytes | 0 | Rare, 1 to 5 / phf a | 5 to 10 / phf | Heavy infilitrate | Packed |
| Plasma cells | 0 | Rare, 1 to 5 / phf a | 5 to 10 / phf | Heavy infilitrate | Packed |
| Macrophages | 0 | Rare, 1 to 5 / phf a | 5 to 10 / phf | Heavy infilitrate | Packed |
| Giant cells | 0 | Rare, 1 to 2 / phf a | 3 to 5 / phf | Heavy infilitrate | sheets |
| Necrosis | 0 | minimal | Mild | Moederate | Severe |

a: phf = per high power field (400x) field.

B. histological evaluation system - Tissue response

| Response | Score |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 0 | 1 | 2 | 3 | 4 |
| Neovascularization | 0 | Minimal capillary proliferation, focal, I to 34 buds | Groups of 4 to 7 capillaries with supporting fibroblastic structures | Broad bands of capillaries with supporting fibroblastic structures | Extensive bands of capillaries with supporting fibroblastic structures |
| Fibrosis | 0 | Narrow bands | Moderate thick bands | Thick bands | Extensive bands |
| Fatty infiltrate | 0 | Minimal amount of fat associated with fibrosis | Severe layers of fat and fibrosis | Elongated and broad accumulation of fat cells about the implant site | Extensive fat completely surrounding the implants |

Under the conditions of this study, the test sample was considered to demonstrate the following:

__ minimal or no reaction (0,0 to 2,9);

__ slight reaction (3,0 to 8,9);

__ moderate reaction (9,0 to 15,0);

__ severe reaction (15,1)

to the tissue as compared to the negative control sample

Supplementary Table 10

Implantation and Surgery Information of Animals

|  |  | Weight (g) |  | Implantation ID Femur |  |
| --- | --- | --- | --- | --- | --- |
| No. | Animal ID | Before surgery | Before sampling | Left | Right |
| 1 | R-240606-01 | 220.28 | 313.29 | T1 | C1 |
| 2 | R-240606-02 | 247.26 | 347.75 | T2 | C2 |
| 3 | R-240606-03 | 209.51 | 272.11 | T3 | C3 |
| 4 | R-240606-04 | 201.45 | 277.78 | T4 | C4 |
| 5 | R-240606-05 | 225.07 | 320.68 | T5 | C5 |
| 6 | R-240606-06 | 236.55 | 340.27 | T6 | C6 |
| 7 | R-240606-07 | 199.96 | 257.39 | T7 | C7 |
| 8 | R-240606-08 | 248.67 | 348.86 | T8 | C8 |
| 9 | R-240606-09 | 212.39 | 285.63 | T9 | C9 |
| 10 | R-240606-10 | 196.91 | 249.95 | T10 | C10 |
| 11 | R-240606-11 | 231.55 | 275.66 | T11 | C11 |
| 12 | R-240606-12 | 234.02 | 297.42 | T12 | C12 |

Sex: All Female SD Rats; a: Test article implant site; b: Control article implant site.

Body weight measurement:

Before surgery: 221.97  18.08 g; Before sampling: 298.90  34.74g.

Supplementary Table 11

Individual Score of Microscopic Findings

|  | Test group | Implantation ID |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | T1 | T2 | T3 | T4 | T5 | T6 | T7 | T8 | T9 | T10 | T11 | T12 | Sum |  |
| Cell type/ response | Polymorphonuclear cells | 0 | 1 | 0 | 0 | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 2 | 11 |
|  | Lymphocytes | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 0 | 1 | 1 | 0 | 0 | 9 |  |
|  | Plasma cells | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |  |
|  | Macrophages | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |  |
|  | Giant cells | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |  |
|  | Necrosis | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |  |
| Response | Neovascularisation | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 4 |
|  | Fibrosis | 0 | 0 | 1 | 0 | 0 | 1 | 1 | 0 | 1 | 0 | 0 | 0 | 4 |  |
|  | Fatty infiltrate | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |  |
|  | Control group | Implantation ID |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | C1 | C2 | C3 | C4 | C5 | C6 | C7 | C8 | C9 | C10 | C11 | C12 | Sum |  |
| Cell type/ response | Polymorphonuclear cells | 0 | 0 | 1 | 0 | 1 | 0 | 0 | 0 | 1 | 0 | 0 | 0 | 3 | 16 |
|  | Lymphocytes | 1 | 0 | 1 | 1 | 1 | 1 | 0 | 1 | 1 | 1 | 1 | 1 | 10 |  |
|  | Plasma cells | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |  |
|  | Macrophages | 0 | 0 | 1 | 0 | 1 | 0 | 0 | 0 | 1 | 0 | 0 | 0 | 3 |  |
|  | Giant cells | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |  |
|  | Necrosis | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |  |
| Response | Neovascularisation | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 11 |
|  | Fibrosis | 1 | 1 | 1 | 1 | 1 | 1 | 0 | 1 | 1 | 1 | 1 | 1 | 11 |  |
|  | Fatty infiltrate | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |  |

Total scores=(subtotal score of cell type/response)x2+subtotal score of response 𝐸𝑣𝑎𝑙𝑢𝑎𝑡𝑖𝑜𝑛 𝑠𝑐𝑜𝑟𝑒𝑠=(Total scores of test group/12)−(Total scores of control/12)

= (19 × 2 + 6)/12 − (20 × 2 + 11)/12 = 0

* If the calculation result is less than 0, the scores show 0.0.

Supplementary Table 12

Animal Observations:

Test article (T) and predicate device (P) group

| Implantation period | 4 weeks |  |  |  | 12 weeks |  |  |  | 26 weeks |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Weight (g) |  |  |  | Weight (g) |  |  |  | Weight (g) |  |  |
| N=8 | Animal ID | start | Ending |  | Animal ID | start | Ending |  | Animal ID | start | Ending |
| Test: N=8 Predicate: N=8 | 1001 | 2932 | 3060 |  | 1009 | 2911 | 4169 |  | 1017 | 2821 | 4239 |
|  | 1002 | 2951 | 3121 |  | 1010 | 2949 | 4233 |  | 1018 | 2862 | 4255 |
|  | 1003 | 2922 | 3154 |  | 1011 | 2963 | 4212 |  | 1019 | 2914 | 4288 |
|  | 1004 | 3020 | 3162 |  | 1012 | 2946 | 4295 |  | 1020 | 2977 | 4298 |
|  | 1005 | 3013 | 3225 |  | 1013 | 3001 | 4243 |  | 1021 | 2930 | 4272 |
|  | 1006 | 3012 | 3210 |  | 1014 | 2998 | 4274 |  | 1022 | 2952 | 4290 |
|  | 1007 | 2981 | 3215 |  | 1015 | 2920 | 4275 |  | 1023 | 2930 | 4322 |
|  | 1008 | 3022 | 3300 |  | 1016 | 2936 | 4306 |  | 1024 | 3010 | 4366 |
| Mean |  | 2981.625 | 3180.875 |  | Mean | 2953 | 4250.9 |  | Mean | 2924.5 | 4291.3 |
| Std Dev. |  | 41.34502 | 73.11915 |  | Std Dev. | 33.028 | 45.824 |  | Std Dev. | 60.488 | 39.651 |
| Implantation period | 4 weeks |  |  |  | 12 weeks |  |  |  | 26 weeks |  |  |
|  | Weight (g) |  |  |  | Weight (g) |  |  |  | Weight (g) |  |  |
| N=4 | Animal ID | start | Ending |  | Animal ID | start | Ending |  | Animal ID | Animal ID | start |
| Sham N=4 | 1025 | 2921 | 3055 |  | 1029 | 2942 | 4175 |  | 1033 | 2965 | 4312 |
|  | 1026 | 2971 | 3122 |  | 1030 | 2887 | 4183 |  | 1034 | 2878 | 4288 |
|  | 1027 | 2894 | 3095 |  | 1031 | 2903 | 4239 |  | 1035 | 2932 | 4242 |
|  | 1028 | 3017 | 3191 |  | 1032 | 2954 | 4274 |  | 1036 | 2979 | 4329 |
| Mean |  | 2950.75 | 3115.75 |  | Mean | 2921.5 | 4217.8 |  | Mean | 2938.5 | 4292.8 |
| Std Dev. |  | 54.48165 | 57.22106 |  | Std Dev. | 31.67 | 47.084 |  | Std Dev. | 44.889 | 37.783 |

Test: N=8	"SunGraft” Nano-fiber Collagen Bone Graft Matrix; Predicate: N=8 “Socko” Graftend Collagen Bone Graft; Sham N=8.

Those animals were observed during the test period. No abnormal behaviors and wound infections were found.

Supplementary Table 13

Macroscopic Examination of Femoral Specimens

| 4 weeks |  |  |  |
| --- | --- | --- | --- |
| Groups | Test article | Predicate device | Sham |
| Number of implants | 8 | 8 | 8 |
| Treated article | Nano-fiber Collagen Bone Graft Matrix | “Socko” Graftend Collagen Bone Graft | Without implant |
| Gross finding | 0/8 | 0/8 | 0/8 |
| 12 weeks |  |  |  |
| Groups | Test article | Predicate device | Sham |
| Number of implants | 8 | 8 | 8 |
| Treated article | Nano-fiber Collagen Bone Graft Matrix | “Socko” Graftend Collagen Bone Graft | Without implant |
| Gross finding | 0/8 | 0/8 | 0/8 |
| 26 weeks |  |  |  |
| Groups | Test article | Predicate device | Sham |
| Number of implants | 8 | 8 | 8 |
| Treated article | Nano-fiber Collagen Bone Graft Matrix | “Socko” Graftend Collagen Bone Graft | Without implant |

Supplementary Table 14

Histomorphomtetric Measurements

| 4 weeks Histomorphomtetric Measurements (Mean ± S.D.) |  |  |
| --- | --- | --- |
| Treatment | Percentage of material area (%) | Percentage of new bone area (%) |
| P (N=8) | 13.7 20.6 | 16 10 |
| T (N=8) | 39.2 14.1 | 7.2 3.8 |
| C (N=8) | - | 11.1 8.7 |
| 12 weeks Histomorphomtetric Measurements (Mean ± S.D.) |  |  |
| Treatment | Percentage of material area (%) | Percentage of new bone area (%) |
| P (N=8) | 0 | 11.6 5.9 |
| T (N=8) | 9.6 4.2 | 12 4.4 |
| C (N=8) | - - | 6.3 1.8 |
| 26 weeks Histomorphomtetric Measurements (Mean ± S.D.) |  |  |
| Treatment | Percentage of material area (%) | Percentage of new bone area (%) |
| P (N=8) | - | 7.8 2.2 |
| T (N=8) | 4.1 1.9 | 8.9 5.5 |
| C (N=8) | - | 5.7 1.5 |