Supplementary Information

Denary element synergy breaks stability–selectivity tradeoff in the oxidative dehydrogenation of propane using CO2

Duanxing Li, Fang Zhang, Zhiheng Jia and Shinya Furukawa*

Division of Applied Chemistry, Graduate School of Engineering, The University of Osaka

2-1 Yamadaoka, Suita, Osaka, Japan 565-0871

E-mail: furukawa@chem.eng.osaka-u.ac.jp

Supplementary Figure 1. X-ray diffraction patterns of various multicomponent oxide supports.

Supplementary Table 1. Molar ratio, crystal size and specific surface area of synthesized mixed oxides.

| Oxide supports | molar ratioa |  |  |  | d spaceb | crystal sizec | SSAd |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Ce | Pr | Zr | Sm | nm | nm | m2/g |
| CeO2 | 1 (1) | - | - | - | 0.1633 | 7.7 | 150 |
| Ce1Pr1Ox | 0.45 (0.5) | 0.55 (0.5) | - | - | 0.1629 | 11.2 | 50 |
| Ce1Sm1Ox | 0.52 (0.5) | - | - | 0.48 (0.5) | 0.1651 | 9.6 | 54 |
| Ce7Pr2Zr1Ox | 0.71 (0.7) | 0.21 (0.2) | 0.08 (0.1) | - | 0.1623 | 6.7 | 109 |
| Ce1Pr1Zr1Ox | 0.35 (0.34) | 0.34 (0.33) | 0.31 (0.33) | - | 0.1603 | 5.1 | 57 |
| Ce9Pr9Zr1Sm1Ox | 0.45 (0.45) | 0.45 (0.45) | 0.05 (0.05) | 0.05 (0.05) | 0.1627 | 7.7 | 61 |

a. calculated by Vegard's law using (311) diffraction peak around 2θ 56° from Figure S1, values in parentheses indicate expected molar ratios;

b. calculated by Bragg's law using (311) diffraction peak around 2θ 56° from Figure S1;

c. calculated by Scherrer equation using (111) diffraction peak around 2θ 28° from Figure S1;

d. calculated from N2 adsorption data by applying the Brunauer–Emmett–Teller method.

Supplementary Figure 2. a XRD patterns of the PtCoIn alloy catalysts supported on different multicomponent oxides, b N2 adsorption–desorption isotherms of the CPZS support and the corresponding PtCoIn-loaded catalysts. Note: Owing to the strong X-ray scattering ability of Ce and Sm, the diffraction peaks of the supported alloy are obscured in the XRD patterns of catalysts containing high amounts of these elements.

Supplementary Table 2. Size of PtCoIn alloy nanoparticles measured by XRD and CO-pulse.

| Samples | Size of alloy nanoparticles / nm |  |
| --- | --- | --- |
|  | XRD | CO-Pulse |
| PtCoIn_Ce1Pr1Ox | 5.3 | 4.6 |
| PtCoIn_Ce1Pr1Zr1Ox | 5.4 | 5.2 |
| PtCoIn_Ce7Pr2Zr1Ox | 4.4 | 4.7 |
| PtCoIn_Ca4.0_Ce7Pr2Zr1Ox | 3.7 | 3.8 |
| PtCoIn_C9P9Z1S1Ox | 3.8 | 4.3 |
| PtCoIn_Ca2.5_C9P9Z1S1Ox | 3.6 | 3.5 |

Supplementary Figure 3. a Fourier transforms of Pt LII-, Co K- and In K-edge EXAFS of PtCoIn/Ca–C9P9Z1S1 catalysts and reference compounds. b Curve-fitting for the Pt LII-, Co K-, and In K-edge k3-weighted EXAFS oscillations of PtCoIn/Ca–C9P9Z1S1. The k3-weighted EXAFS oscillation was Fourier-transformed in the k range of 3−14 Å−1 for all edges. Curve-fitting was performed using the back Fourier-transforms of the coordination peaks ranging between 1.3−3.7 Å, 1.0−3.0 Å, and 1.2−4.0 Å for Pt LII-, Co K-, and In K-edge, respectively.

Supplementary Table 3. Results of EXAFS curve-fitting for PtCoIn/Ca–C9P9Z1S1 and the reference foils.

| Sample | Edge | Shell | So2[a] | CN[b] | R[c] (Å) | ∆Eo[d] (eV) | σ2[e] (Å2) | R-factor |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Pt foil | Pt LII | Pt–Pt | 0.80 | 12 (fix) | 2.78 ± 0.01 | 6.4 ± 1.9 | 0.000 | 0.020 |
| Co foil | Co K | Co–Co | 0.79 | 12 (fix) | 2.49 ± 0.00 | 1.1 ± 0.3 | 0.006 | 0.001 |
| In foil | In K | In–In | 0.76 | 4 (fix) | 3.13 ± 0.02 | 1.9 ± 1.5 | 0.014 | 0.024 |
|  |  | In–In |  | 8 (fix) | 3.31 ± 0.03 |  | 0.021 |  |
| PtCoIn/ Ca– C9P9Z1S1 | Pt LII | Pt–In | 0.80 (fix) | 5.5 ± 0.7 | 2.71 ± 0.00 | 3.6 ± 0.9 | 0.008 | 0.009 |
|  |  | Pt–Pt |  | 3.3 ± 0.7 | 2.86 ± 0.02 |  | 0.013 |  |
|  | Co K | Co–Co | 0.79 (fix) | 9.0 ± 0.5 | 2.49 ± 0.00 | 0.49 ± 0.68 | 0.007 | 0.002 |
|  |  | Co–In |  | 1.5 ± 0.2 | 2.77 ± 0.05 |  | 0.020 |  |
|  | In K | In–O | 0.76 (fix) | 3.6 ± 4.4 | 2.21 ± 0.05 | 7.56 ± 1.72 | 0.024 | 0.025 |
|  |  | In–Pt |  | 7.3 ± 1.9 | 2.78 ± 0.01 |  | 0.009 |  |
|  |  | In–Co |  | 3.6 ± 1.9 | 2.91 ± 0.03 |  | 0.020 |  |

[a]Amplitude factor. [b]Coordination number. [c]Distance between absorber and backscattering atoms. [d]Correction term in the absorption edge. [e]Disorder term (EXAFS Debye–Waller factor).

Supplementary Figure 4. FT-IR spectra of CO adsorbed on Pt/SiO2, PtCoIn/SiO2, and PtCoIn/Ca–SiO2. For the FT-IR study, SiO2-supported catalysts were used instead of the CeO2-supported ones to avoid interference from the strong infrared absorption of CeO2. The peak positions were consistent with those observed in literature of Pt/SiO2 (2070 cm−1),1 Pt–In/SiO2 (2042 cm−1),2 and Co in Pt–Co alloy surface (1988 cm−1).3

Supplementary Figure 5. HAADF-STEM images of PtCoIn/Ca–C9P9Z1S1 with several regions. More than 100 particles were counted using these images for size-distribution analysis.

Supplementary Figure 6. Catalytic performance of PtCoIn loaded on Ce-based oxides in CO2-ODP: a C3H8 conversion, b CO2 conversion, c net C3H6 selectivity, and d C3H6 selectivity in HC.

Supplementary Figure 7. a C3H6 selectivity in hydrocarbon and b net C3H6 yield of PtCoIn loaded on various oxide supports, c C3H6 selectivity in hydrocarbon, d net C3H6 yield and e CO2 conversion for Ca decorated PtCoIn loaded on various oxide supports.

Supplementary Figure 8. TPR profiles of various multinary oxides used as catalyst supports.

Supplementary Figure 9. a and d total carbon balance, b and e carbon balance in COx, c and f carbon balance in hydrocarbons of abc PtCoIn loaded on various oxides and def PtCoIn loaded on various oxides with Ca decoration.

Supplementary Figure 10. Equilibrium conversions of a C3H8 and b CO2 for DDP, ODP and ODP with DRP.

Supplementary Figure 11. a Dependence of coke accumulation rate and dispersion retention on H2 consumption. b Dependence of overall deactivation constant (kd), coking deactivation constant (kc) and sintering deactivation constant (ks) on H2 consumption.

Supplementary Table 4. Dispersion, composition and surface area of prepared catalysts.

| Alloy | Supporta | BET | Dispersion (%) |  | Dispersion retention |  | Composition ratio (%)b |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | m2 g−1 | Fresh | Spent |  | (%) | Pt | Co | Ni | Sn | In |  | Ca |
| PtCoIn | CeO2 | - | - | - |  |  | 1.0 | 0.7 | - | - | 2.2 | - |  |
|  | CeSmOx | - | 32 | 19 |  | 58 | - | - | - | - | - | - |  |
|  | CePrOx | - | 23 | 18 |  | 79 | - | - | - | - | - | - |  |
|  | Ce7Pr2Zr1Ox | 76 | 22 | 18 |  | 81 | 1.0 | 0.8 | - | - | 2.0 | - |  |
|  | Ce9Pr9Zr1Ti1Ox | - | 16 | 13 |  | 82 | - | - | - | - | - | - |  |
|  | Ce9Pr9Zr1Sm1Ox | 51 | 26 | 23 |  | 89 | 1.0 | 0.9 | - | - | 2.2 | - |  |
|  | Ca_CeSmOx | - | - | - |  | - | - | - | - | - | - | - |  |
|  | Ca_Ce7Pr2Zr1Ox | - | - | - |  | - | - | - | - | - | - | - |  |
|  | Ca_Ce9Pr9Zr1Sm1Ox | 32 | 33 | 29 |  | 88 | 1.0 | 0.7 | - | - | 2.1 | 2.3 |  |
| HEI | Ce7Pr2Zr1Ox | 85 | 41 | 38 |  | 93 | 1.0 | 1.1 | 0.8 | 1.8 | 1.5 | - |  |
|  | Ce9Pr9Zr1Sm1Ox | 68 | 44 | 41 |  | 94 | - | - | - | - | - | - |  |
|  | Ca_Ce7Pr2Zr1Ox | - | - | - |  | - | - | - | - | - | - | - |  |
|  | Ca_Ce9Pr9Zr1Sm1Ox | 70 | 34 | 34 |  | 99.5 | 1.0 | 1.2 | 0.8 | 1.6 | 1.4 | 1.7 |  |

a: Ca_oxide indicates that there is Ca decoration in this catalyst 
b: tested by XRF.

Supplementary Text 1

The apparent deactivation constant, kd, was assumed to consist of two independent contributions: catalyst deactivation caused by coke accumulation (kc) and the reduction in the number of accessible surface metal sites caused by nanoparticle sintering (ks). In the present treatment, these two deactivation processes were approximated as independent, considering that coke deposition and nanoparticle sintering originate from distinct chemical and physical phenomena, respectively. Because coking is commonly described by first-order deactivation kinetics and the gradual decrease in accessible surface metal sites caused by sintering can also be approximated as a first-order process for simplicity, the catalytic activity can be expressed as;

rt=r0e-kdt(6)

=r0e-kct⋅e-kst(7)

=r0e-kc+kst(8)

thus giving

kd=kc+ks(9)

The sintering constant, ks, was estimated from the change in metal dispersion before and after the reaction. Assuming that the number of accessible surface metal sites is proportional to metal dispersion, the decrease in dispersion due to sintering can likewise be approximated by a first-order decay:

Dt=D0e-kst(10)

lnRD=-kst RD=Dt/D0(11)

ks=-lnRDt(12)

where D0, Dt, and RDrepresent the metal dispersions before and after the reaction, and the dispersion retention, respectively. The coking constant was subsequently obtained from Eq. (9) as

kc=kd-ks.(13)

Although this treatment relies on several simplifying assumptions, including independent first-order deactivation processes and proportionality between accessible surface metal sites and metal dispersion, it provides a useful semi-quantitative framework for evaluating the relative contributions of coking and sintering to the overall catalyst deactivation.

Supplementary Figure 12. Fourier transforms of a Pt LII-, Co K- and Ni K-edge EXAFS, b In K- and Sn K-edge EXAFS of HEI/Ca–C9P9Z1S1 catalysts and reference compounds. The k3-weighted EXAFS oscillation was Fourier-transformed in the k range of 3−12 Å−1 for all edges.

Supplementary Figure 13. Curve-fitting for the Pt LII-, Co K-, Ni K-, In K- and Sn K-edge k3-weighted EXAFS oscillations of HEI/Ca–C9P9Z1S1. Curve-fitting was performed using the back Fourier-transforms of the coordination peaks ranging between 1.3−3.7 Å, 1.0−3.0 Å, 1.0−3.0 Å, 1.2−4.0 Å and 1.2−3.8 Å for Pt LII-, Co K-, Ni K-, In K- and Sn K-edge, respectively.

Supplementary Table 5. Results of EXAFS curve-fitting for HEI/Ca–C9P9Z1S1 and the reference foils.

| Sample | Edge | Shell | So2[a] | CN[b] | R[c] (Å) | ∆Eo[d] (eV) | σ2[e] (Å2) | R-factor |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Pt foil | Pt LII | Pt–Pt | 0.90 | 12 (fix) | 2.77 ± 0.01 | 6.3 ± 1.1 | 0.005 | 0.005 |
| Co foil | Co K | Co–Co | 0.76 | 12 (fix) | 2.49 ± 0.00 | 7.3 ± 0.2 | 0.006 | 0.000 |
| Ni foil | Ni K | Ni–Ni | 0.85 | 12 (fix) | 2.48 ± 0.00 | 2.8 ± 0.3 | 0.006 | 0.001 |
| SnO2 | Sn K | Sn–O | 0.99 | 6 (fix) | 2.06 ± 0.01 | 9.0 ± 1.8 | 0.002 | 0.007 |
| In | In K | In–In | 0.88 | 4 (fix) | 3.14 ± 0.02 | 2.9 ± 1.5 | 0.016 | 0.027 |
|  |  | In–In | 0.90 | 8 (fix) | 3.32 ± 0.03 |  | 0.021 |  |
| HEI/Ca_9911 | Pt LII | Pt–Sn/In | 0.90 (fix) | 4.6 ± 0.7 | 2.70 ± 0.01 | 4.8 ± 1.0 | 0.007 | 0.009 |
|  |  | Pt–Pt |  | 4.1 ± 5.9 | 2.84 ± 0.04 |  | 0.020 |  |
|  | Co K | Co–Co | 0.76 (fix) | 6.7 ± 0.9 | 2.48 ± 0.01 | 9.98± 2.4 | 0.009 | 0.008 |
|  |  | Co–Sn/In |  | 5.1 ± 12.1 | 2.66 ± 0.07 |  | 0.036 |  |
|  | Ni K | Ni–Ni | 0.85 (fix) | 4.6 ± 0.3 | 2.47 ± 0.01 | −4.3 ± 2.5 | 0.005 | 0.010 |
|  |  | Ni–Sn/In |  | 1.4 ± 0.7 | 2.69 ± 0.01 |  | 0.010 |  |
|  | Sn K | Sn–O | 0.99 (fix) | 0.6 ± 0.7 | 2.02 ± 0.02 | −1.9 ± 4.1 | 0.003 | 0.022 |
|  |  | Sn–Co/Ni |  | 2.8 ± 0.8 | 2.62 ± 0.04 |  | 0.016 |  |
|  |  | Sn–Pt |  | 1.4 ± 0.4 | 2.64 ± 0.02 |  | 0.011 |  |
|  | In K | In–O | 0.88 (fix) | 2.1 ± 0.3 | 2.06 ± 0.01 | −6.0 ± 2.29 | 0.004 | 0.015 |
|  |  | In–Co/Ni |  | 4.7 ± 0.8 | 2.62 ± 0.04 |  | 0.032 |  |
|  |  | In–Pt |  | 2.3 ± 0.8 | 2.69 ± 0.01 |  | 0.008 |  |

[a]Amplitude factor. [b]Coordination number. [c]Distance between absorber and backscattering atoms. [d]Correction term in the absorption edge. [e]Disorder term (EXAFS Debye–Waller factor).

Supplementary Figure 14. HAADF-STEM images of HEI/Ca–C9P9Z1S1 catalyst. More than 100 particles were counted using these images for size-distribution analysis.

Supplementary Figure 15. XANES spectra of Pt LII-, Co K-, Ni K-, Sn K- and In K-edge of HEI/(Ca–)C7P2Z1 catalyst.

Supplementary Figure 16. k3-weighted EXAFS oscillation of Pt LII-, Co K-, Ni K-, Sn K- and In K-edge of HEI/C7P2Z1 catalyst (green) and HEI/Ca–C7P2Z1 (purple).

Supplementary Figure 17. Fourier transforms of a Pt LII-, Co K-, Ni K-, b In K- and Sn K-edge EXAFS of HEI/Ca–C7P2Z1 catalysts and reference compounds. The k3-weighted EXAFS oscillation was Fourier-transformed in the k range of 3−12 Å−1 for all edges

Supplementary Figure 18. Curve-fitting for the Pt LII-, Co K-, Ni K-, In K- and Sn K-edge k3-weighted EXAFS oscillations of HEI/Ca–C7P2Z1. The k3-weighted EXAFS oscillation was Fourier-transformed in the k range of 3−12 Å−1 for all edges. Curve-fitting was performed using the back Fourier-transforms of the coordination peaks ranging between 1.3−3.3 Å, 1.0−3.0 Å, 1.0−3.3 Å, 1.2−3.6 Å and 1.0−3.5 Å for Pt LII-, Co K-, Ni K-, In K- and Sn K-edge, respectively.

Supplementary Table 6. Results of EXAFS curve-fitting for HEI/Ca–C7P2Z1 and the reference foils.

| Sample | Edge | Shell | So2[a] | CN[b] | R[c] (Å) | ∆Eo[d] (eV) | σ2[e] (Å2) | R-factor |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Pt foil | Pt LII | Pt–Pt | 0.80 | 12 (fix) | 2.78 ± 0.01 | 6.4 ± 1.9 | 0.000 | 0.020 |
| Co foil | Co K | Co–Co | 0.79 | 12 (fix) | 2.49 ± 0.00 | 1.1 ± 0.3 | 0.006 | 0.001 |
| Ni foil | Ni K | Ni–Ni | 0.80 | 12 (fix) | 2.48 ± 0.00 | 1.0 ± 0.5 | 0.006 | 0.001 |
| Sn foil | Sn K | Sn–Sn | 0.75 | 8 (fix) | 3.01 ± 0.01 | 1.2 ± 1.1 | 0.013 | 0.015 |
| In foil | In K | In–In | 0.76 | 4 (fix) | 3.13 ± 0.02 | 1.9 ± 1.5 | 0.014 | 0.024 |
|  |  | In–In |  | 8 (fix) | 3.31 ± 0.03 |  | 0.021 |  |
| HEI/Ca–C7P2Z1 | Pt LII | Pt–Sn | 0.80 (fix) | 3.3 ± 0.6 | 2.55 ± 0.04 | 4.9 ± 1.1 | 0.007 | 0.008 |
|  |  | Pt–Pt |  | 4.6 ± 4.0 | 2.60 ± 0.04 |  | 0.017 |  |
|  | Co K | Co–Co | 0.79 (fix) | 4.7 ± 0.4 | 2.65 ± 0.04 | −0.5 ± 3.0 | 0.006 | 0.016 |
|  |  | Co–In |  | 2.3 ± 0.4 | 2.43 ± 0.02 |  | 0.019 |  |
|  | Ni K | Ni–Ni | 0.80 (fix) | 1.5 ± 0.4 | 2.80 ± 0.04 | −4.2 ± 1.5 | 0.004 | 0.009 |
|  |  | Ni–In |  | 4.4 ± 1.3 | 2.48 ± 0.02 |  | 0.016 |  |
|  | Sn K | Sn–O | 0.75 (fix) | 1.5 ± 0.7 | 2.60 ± 0.03 | 2.1 ± 3.6 | 0.010 | 0.019 |
|  |  | Sn–Co/Ni |  | 3.6 ± 1.0 | 2.11 ± 0.02 |  | 0.002 |  |
|  |  | Sn–Pt |  | 3.6 ± 1.0 | 2.59 ± 0.02 |  | 0.005 |  |
|  | In K | In–O | 0.76 (fix) | 2.0 ± 1.8 | 2.71 ± 0.02 | −6.0 ± 4.48 | 0.013 | 0.018 |
|  |  | In–Co/Ni |  | 2.9 ± 1.3 | 2.17 ± 0.04 |  | 0.025 |  |
|  |  | In–Pt |  | 2.9 ± 1.3 | 2.69 ± 0.03 |  | 0.009 |  |

[a]Amplitude factor. [b]Coordination number. [c]Distance between absorber and backscattering atoms. [d]Correction term in the absorption edge. [e]Disorder term (EXAFS Debye–Waller factor).

Supplementary Figure 19. Net C3H6 yield and C3H6 selectivity in hydrocarbon of PtCoIn/C9P9Z1S1, PtCoIn/Ca–C9P9Z1S1, and HEI/Ca–C9P9Z1S1 catalysts.

Supplementary Figure 20. CO2-ODP performance of HEI/C9P9Z1S1 catalyst.

Supplementary Figure 21. Total carbon balance, carbon balance in CxHy and COx of various catalysts.

Supplementary Figure 22. CO2-ODP performance of HEI/C7P2Z1 and HEI/Ca–C7P2Z1.

Supplementary Figure 23. Control experiments of CO2-ODP with HEI/Ca–Al2O3, Ca–CPZS, sea sand. Direct propane dehydrogenation over HEI/Ca–CPZS.

Supplementary Figure 24. Detailed number indication for Figure 5i. The numbers correspond to the entry numbers in supplementary Tables 7-9.

Supplementary Table 7. Catalytic conditions and performance of reported catalysts (No. 1-20 in Figure S24).

| No. | Catalysts | Temp. | Gas feed ratio C3H8:CO2:Ar | Time (h) |  | C3H8 conv. (%) |  | C3H6 sel. (%) |  | kd (h−1) | τ (h) | ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | i | f | i | f | i | f |  |  |  |
| 1 | Ga8Al2O15 | 500 | 2.5:5:92.5 | 0.25 | 8 | 49.7 | 33.1 | 91.7 | 98 | 0.089 | 11.2 | 4 |
| 2 | Ru1Cr10Ox/SiO2 | 500 | 1:1:1 | 0.67 | 7 | 9 | 6.5 | (85) | (90) | 0.053 | 18.8 | 5 |
| 3 | Pd/CeZrAlOx | 500 | 26:37:37 | 0.17 | 140 | 16 | 2 | 80 | 98 | 0.016 | 62.6 | 6 |
| 4 | 7%Cr/SBA-1 | 550 | 1:5:9 | 0.17 | 4 | 37.7 | 16 | 85 | 91 | 0.347 | 2.9 | 7 |
| 5 | Cr-O/SiO2 | 550 | 1:5 | 0.17 | 0 | 17.2 | − | 94.4 | − | − | − | 8 |
| 6 | Cr2O3–ZrO2 180 | 550 | 2.5:5:92.5 | 0.17 | 6 | 53.3 | 27.8 | (79) | (90.8) | 0.186 | 5.4 | 9 |
| 7 | Ga2O3–M | 550 | 1:5:9 | 0.17 | 4 | 19 | 11 | 91.6 | 95 | 0.167 | 6.0 | 10 |
| 8 | FeCeO2 | 550 | 1:1:2 | 0.10 | 20 | 17.5 | 14 | (48) | (53) | 0.013 | 75.2 | 11 |
| 9 | Fe3Ni/CeO2 | 550 | 1:1:2 | 0.10 | 10 | 4.8 | 3.4 | 30 | 58.2 | 0.036 | 27.5 | 12 |
| 10 | 20%ZnO-ZrO2 | 550 | 1:4:20 | 0.08 | 2 | 24 | 20 | 65 | 70 | 0.165 | 6.1 | 13 |
| 11 | 15V-15Zr@ZSM-5 | 550 | 2.5:5:92.5 | 1.00 | 6 | 35 | 39 | 87 | 90 | 0.000 | 0.0 | 14 |
| 12 | 0.5%PtSnCe/SiO2 | 550 | 1:1:5 | 0.08 | 6 | 55 | 33 | 89.1 | 93.4 | 0.154 | 6.5 | 15 |
| 13 | 2Ga2O3V2O5/ZSM-5 | 550 | − | 0.50 | 6 | 30 | 35 | 87 | 90 | 0.000 | 0.0 | 16 |
| 14 | FeNi/Ceria-Vo-R | 550 | 2.4:4.8:10 | 0.33 | 3 | 23 | 21 | 42 | 42 | 0.054 | 18.6 | 17 |
| 15 | 12% In/HZSM-5 | 580 | 1:4:5 | 1.00 | 6 | 25.2 | 17.6 | 75 | 70 | 0.101 | 9.9 | 18 |
| 16 | GaN/NaZSM-5(470) | 600 | 1:2:7 | 0.08 | 10 | 46 | 34 | 62 | 78 | 0.053 | 18.7 | 19 |
| 17 | CaO/ZSM-5 | 600 | 5 5 90 | 0.08 | − | 23.1 | − | 39 | − | 0.000 | 0.0 | 20 |
| 18 | 2Cr-Ca/ZrO2 | 600 | 1:3:6 | 0.08 | 10 | 20.2 | 9.5 | 93.5 | 94.6 | 0.089 | 11.3 | 21 |
| 19 | PtCoIn/CeO2 | 600 | 1:1:2 | 0.08 | 50 | 61 | 35 | 96 (82) | 97.5 (87) | 0.022 | 46.3 | 22 |
| 20 | HEI/CeO2 | 600 | 1:1:2 | 0.08 | 50 | 30 | 20 | 94 (92) | 88 (86) | 0.008 | 92.6 | 23 |

Supplementary Table 8. Catalytic conditions and performance of reported catalysts (No. 21-40 in Figure S24).

| No. | Catalysts | Temp. | Gas feed ratio C3H8:CO2:Ar | Time (h) |  | C3H8 conv. (%) |  | C3H6 sel. (%) |  | kd (h−1) | τ (h) | ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | i | f | i | f | i | f |  |  |  |
| 21 | HEI/CeO2 | 600 | 1:1:2 | 0.08 | 50 | 30 | 20 | 94 (92) | 88 (86) | 0.008 | 92.6 | 23 |
| 22 | PtCoIn/CPZS | 600 | 1:1:2 | 8.00 | 68 | 47.1 | 36.5 | 97 (42) | 95.8 (53) | 0.007 | 138.0 | * |
| 23 | HEI/CPZS | 600 | 1:1:2 | 4 | 40 | 28.7 | 24.0 | 95 (75) | 94.4 (75) | 0.007 | 146.5 | * |
| 24 | PtCoIn/Ca–CPZS | 600 | 1:1:2 | 3 | 70 | 45.7 | 35.9 | 98 (73) | 97.2 (74) | 0.006 | 168.0 | * |
| 25 | HEI/Ca–CPZS | 600 | 1:1:2 | 1 | 90 | 31 | 22 | 98 (91) | 96.9 (93) | 0.005 | 193 | * |
| 26 | Ga2O3/HZSM-48 | 600 | 2.5:5:92.5 | 1.00 | 10 | 52.6 | 48.2 | 42.2 | 45.6 | 0.020 | 51.1 | 24 |
| 27 | ZnO/HZSM-5 | 600 | 2.5:5:92.5 | 1.00 | 30 | 68.3 | 41.5 | 46.8 | 62.1 | 0.038 | 26.1 | 25 |
| 28 | Cr-MSU-28 | 600 | 1:1:8 | 0.17 | 2 | 44 | 36.8 | 86 | 90.4 | 0.163 | 6.1 | 26 |
| 29 | 5%Cr/SiO2 | 600 | 15:30:55 | − | 20 | 80 | 53 | 50 | 90.6 | 0.063 | 15.8 | 27 |
| 30 | 2%Cr2O3/SiO2 | 600 | 15:30:55 | 0.30 | 17 | 71 | 50 | 66 | 90 | 0.055 | 18.3 | 28 |
| 31 | 15%Ga/ZrO2 | 600 | 2.5:5:92.5 | 0.17 | 3 | 38.6 | 6 | 45.4 | 77 | 0.807 | 1.2 | 29 |
| 32 | Ga2O3/TiO2 | 600 | 2.5:5:92.5 | 0.17 | 3 | 32 | 2.5 | (73) | − | 1.027 | 1.0 | 30 |
| 33 | Ga2O3/Al2O3 | 600 | 2.5:5:92.5 | 0.17 | 3 | 26 | 17 | (94) | − | 0.190 | 5.2 | 30 |
| 34 | Ga2O3/ZrO2 | 600 | 2.5:5:92.5 | 0.17 | 3 | 30 | 7 | (65) | − | 0.614 | 1.6 | 30 |
| 35 | Ga2O3/SiO2 | 600 | 2.5:5:92.5 | 0.17 | 3 | 6.4 | 6 | (92) | − | 0.024 | 41.2 | 30 |
| 36 | Ga2O3/MgO | 600 | 2.5:5:92.5 | 0.17 | 3 | 4.3 | 2.5 | (29) | − | 0.198 | 5.1 | 30 |
| 37 | 10%In2O3/Al2O3 | 600 | 2.5:10:87.5 | 0.17 | 8 | 24 | 20 | 29 | 84 | 0.030 | 33.5 | 31 |
| 38 | In-Al-20 | 600 | 2.5:10:87.5 | 0.17 | 12 | 35 | 29 | (20) | (78) | 0.023 | 42.8 | 32 |
| 39 | 5.2V-MSNS | 600 | 1:4:4 | 0.17 | 24 | 58 | 19 | (84) | (89) | 0.074 | 13.4 | 33 |
| 40 | Cr/MSS-2 | 600 | 1:4:4 | 0.17 | 4 | 69 | 33 | (79) | (90) | 0.394 | 2.5 | 34 |

*: data from this work

Supplementary Table 9. Catalytic conditions and performance of reported catalysts. No. 41-58 in Figure S24.

| No. | Catalysts | Temp. | Gas feed ratio C3H8:CO2:Ar | Time (h) |  | C3H8 conv. (%) |  | C3H6 sel. (%) |  | kd (h−1) | τ (h) | ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | i | f | i | f | i | f |  |  |  |
| 41 | 0.5 Ni-Cr/Si | 600 | 1:1:8 | 0.17 | 12 | 90 | 19 | 0 | 90 | 0.308 | 3.2 | 35 |
| 42 | 7 Ga/SiO2-A | 650 | 1:2 | 0.08 | 20 | 33 | 21 | (78) | (77) | 0.031 | 32.3 | 36 |
| 43 | 0.8GaN–Ga2O3/ZSM-5 | 600 | 1:2:7 | 1.00 | 55 | 55.1 | 31 | (65.3) | (80) | 0.019 | 53.7 | 37 |
| 44 | PtSn/Ce-DMSN-0.5 | 550 | 8:8:8:1 | 0 | 33 | 40.9 | 24 | 96.9 (93.2) | 96.8 (92) | 0.024 | 42.1 | 38 |
| 45 | Pt1Sn7/CeOx–Al2O3 | 550 | 5:3:27 | 0.25 | 12 | 44.2 | 40 | 98.8 | 98 | 0.015 | 68.1 | 39 |
| 46 | PtIn/Al2O3 | 550 | 8:8:34 | 0 | 1.5 | 32.5 | 11 | (90) | (80) | 0.907 | 1.1 | 40 |
| 47 | KPt/Silicalite-1 | 500 | 1:1:4 | 0 | 10 | 50 | 42 | (70) | (90) | 0.032 | 31.0 | 41 |
| 48 | 5GaN/[Ga]MFI-100 | 600 | 1:2:7 | 0 | 6 | 65 | 50 | (72) | (76) | 0.103 | 9.7 | 42 |
| 49 | Ni2.1%Cr3.6%Ox@S1-1.0 | 600 | 1:1:23 | 0 | 36 | 51.7 | 41 | 91.4 | − | 0.012 | 83.3 | 43 |
| 50 | PtMn/SiO2 | 500 | 10:10:5 | 0 | 2 | 31.8 | 27.2 | (97.5) | (97.8) | 0.111 | 9.0 | 44 |
| 51 | 4 wt% Co@Z5–1000 | 600 | 1:2:7 | 3 | 38 | 45.1 | 20 | 95 | 95 | 0.034 | 29.4 | 45 |
| 52 | MoCx/Si-1 | 550 | 1:1:2 | 0 | 24 | 13 | 5 | 93.6 | 95 | 0.043 | 23.0 | 46 |
| 53 | 5Cr-Co/ZSM-5 (w) | 600 | 1:2:97 | 0 | 3 | 53.9 | 46 | 71.65 | 80 | 0.106 | 9.5 | 47 |
| 54 | 10V-0.5Fe/S-1 | 600 | 1:1:3 | 0 | 8 | 52.5 | 40 | 90.6 | 90 | 0.063 | 15.8 | 48 |
| 55 | Co/MgS-1 | 600 | 1:1 | 0 | 8 | 32.3 | 20 | 94.8 | 90 | 0.081 | 12.4 | 49 |
| 56 | Si(5)PtSn/Al2O3 | 550 | 1:1:2 | 0.25 | 8 | 48 | 37 | (87.1) | (87.8) | 0.058 | 17.1 | 50 |
| 57 | PtZn/Co@S-1 | 550 | 1:1:4 | 0 | 60 | 59.68 | 40 | (80) | (94.9) | 0.013 | 75.2 | 51 |
| 58 | 5Fe-5V-Al2O3 | 600 | 15:15:70 | 0.25 | 1 | 41.3 | 35 | 84.4 | − | 0.357 | 2.8 | 52 |

Supplementary Figure 25. Optimized structures of the slab models for (a) bare CeO2(111) and (b) Pt–In/CeO2(111), (c) Pt–In/CaO–CeO2(111), (d) C2H4-adsorbed Pt–In/CaO–CeO2(111). Dotted circle and triangle indicate the location of In–O linkage and the Ca cation on the surface, respectively. (e) Periodic view of the C2H4-adsorbed structure.

Supplementary Table 10. Structural and electronic state information on the π-adsorbed C2H4 on Pt.

| structure | Pt–C1 / Å a | Pt–C2 / Å a | C1–C2 / Å a | HCCH dihedral angle / degree | Hirshfeld charge at Pt b |
| --- | --- | --- | --- | --- | --- |
| C2H4–Pt4In6/ CeO2(111) | 2.184 | 2.204 | 1.413 | 161.38 | −0.01 (−0.13) |
| C2H4–Pt4In6/ CaO–CeO2(111) | 2.202 | 2.236 | 1.406 | 164.40 | +0.05 (+0.02) |
| a C2 atom is closer to the slab surface. b Values in parentheses indicate the charges before adsorption. |  |  |  |  |  |

Supplementary Figure 26. a DOSs projected on the valence 2p states of single oxygen anions. Numbers indicate the oxygen anions designated in b. b The location of the selected oxygen anions on the slab model.

Supplementary References

- Hui Y., et al. Atomically precise design of PtSn catalyst for the understanding of the role of Sn in propane dehydrogenation. Precis. Chem. 2, 245−255 (2024).

- Zhou, T., et al. Reaction-induced dynamic evolution of PtIn/SiO2 catalyst for propane dehydrogenation. Nat. Commun. 16, 5153 (2025).

- Yim, W.-L. & Klüner, T. Understanding of adsorption and catalytic properties of bimetallic Pt–Co alloy surfaces from first principles: insight from disordered alloy surfaces. J. Phys. Chem. C. 114, 7141−7152 (2010).

- Chen, M. et al. Dehydrogenation of propane over spinel-type gallia–alumina solid solution catalysts. J. Catal. 256, 293−300 (2008).

- Jin, R., Easa, J., Tran, D. T. & O’Brien, C. P. Ru-promoted CO2 activation for oxidative dehydrogenation of propane over chromium oxide catalyst. Catal. Sci. Technol. 10, 1769−1777 (2020).

- Nowicka, E. et al. Elucidating the role of CO2 in the soft oxidative dehydrogenation of propane over ceria-based catalysts. ACS Catal. 8, 3454−3468 (2018).

- Michorczyk, P., Pietrzyk, P. & Ogonowski, J. Preparation and characterization of SBA-1-supported chromium oxide catalysts for CO2 assisted dehydrogenation of propane. Microporous Mesoporous Mater. 161, 56−66 (2012).

- Michorczyk, P., Zeńczak, K., Niekurzak, R. & Ogonowski, J. Dehydrogenation of propane with CO2–a new green process for propene and synthesis gas production. Polish J. Chem. Technol. 14, 77−82 (2012).

- Wu, R. et al. Hydrothermally prepared Cr2O3–ZrO2 as a novel efficient catalyst for dehydrogenation of propane with CO2. Catal. Commun. 39, 20−23 (2013).

- Michorczyk, P., Kuśtrowski, P., Kolak, A. & Zimowska, M. Ordered mesoporous Ga2O3 and Ga2O3–Al2O3 prepared by nanocasting as effective catalysts for propane dehydrogenation in the presence of CO2. Catal. Commun. 35, 95−100 (2013).

- Wang, H. & Tsilomelekis, G. Catalytic performance and stability of Fe-doped CeO2 in propane oxidative dehydrogenation using carbon dioxide as an oxidant. Catal. Sci. Technol. 10, 4362−4372 (2020).

- Gomez, E. et al. Combining CO2 reduction with propane oxidative dehydrogenation over bimetallic catalysts. Nat. Commun. 9, 1398 (2018).

- Yang, G. Q. et al. Oxidative dehydrogenation of propane with carbon dioxide catalyzed by ZnxZr1−xO2−x solid solutions. Ind. Eng. Chem. Res. 60, 17850−17861 (2021).

- Farsad, A., Lawson, S., Rezaei, F. & Rownaghi, A. A. Oxidative dehydrogenation of propane over 3D printed mixed metal oxides/H-ZSM-5 monolithic catalysts using CO2 as an oxidant. Catal. Today 374, 173−184 (2021).

- Wang, L., Yang, G. Q., Ren, X. & Liu, Z. W. CeO2-promoted PtSn/SiO2 as a high-performance catalyst for the oxidative dehydrogenation of propane with carbon dioxide. Nanomaterials 12, 417 (2022).

- Lawson, S. et al. Structured bifunctional catalysts for CO2 activation and oxidative dehydrogenation of propane. ACS Sustain. Chem. Eng. 9, 5716−5727 (2021).

- Wang, Y. et al. Defect-dependent selective C–H/C–C bond cleavage of propane in the presence of CO2 over FeNi/ceria catalysts. ACS Sustain. Chem. Eng. 9, 17301−17309 (2021).

- Tian, H. et al. Catalytic performance of In/HZSM-5 for coupling propane with CO2 to propylene. ChemistrySelect 5, 3626−3637 (2020).

- Wang, Z. Y. et al. Oxidative dehydrogenation of propane to propylene in the presence of CO2 over S30 gallium nitride supported on NaZSM-5. Ind. Eng. Chem. Res. 60, 2807−2817 (2021).

- Lawson, S. et al. Integrated direct air capture and oxidative dehydrogenation of propane with CO2 at isothermal conditions. Appl. Catal. B Environ. 303, 120907 (2022).

- Gao, Y. et al. One-pot synthesis of Ca oxide-promoted Cr catalysts for the dehydrogenation of propane using CO2. Ind. Eng. Chem. Res. 59, 12645−12656 (2020).

- Xing, F., Nakaya, Y., Yasumura, S., Shimizu, K. & Furukawa, S. Ternary platinum–cobalt–indium nanoalloy on ceria as a highly efficient catalyst for the oxidative dehydrogenation of propane using CO2. Nat. Catal. 5, 55−65 (2022).

- Xing, F., Ma, J., Shimizu, K. & Furukawa, S. High-entropy intermetallics on ceria as efficient catalysts for the oxidative dehydrogenation of propane using CO2. Nat. Commun. 13, 5065 (2022).

- Ren, Y., Wang, J., Hua, W., Yue, Y. & Gao, Z. Ga2O3/HZSM-48 for dehydrogenation of propane: effect of acidity and pore geometry of support. J. Ind. Eng. Chem. 18, 731−736 (2012).

- Ren, Y., Zhang, F., Hua, W., Yue, Y. & Gao, Z. ZnO supported on high silica HZSM-5 as new catalysts for dehydrogenation of propane to propene in the presence of CO2. Catal. Today 148, 316−322 (2009).

- Baek, J., Yun, H. J., Yun, D., Choi, Y. & Yi, J. Preparation of highly dispersed chromium oxide catalysts supported on mesoporous silica for the oxidative dehydrogenation of propane using CO2: insight into the nature of catalytically active chromium sites. ACS Catal. 2, 1893−1903 (2012).

- Agafonov, Y. A., Gaidai, N. A., Lapidus, A. L. & Zelinsky, N. D. Influence of the preparation conditions for catalysts CrOx/SiO2 on their efficiency in propane dehydrogenation in the presence СО2. Russ. Chem. Bull. 63, 381−388 (2014).

- Botavina, M. A. et al. Towards efficient catalysts for the oxidative dehydrogenation of propane in the presence of CO2: Cr/SiO2 systems prepared by direct hydrothermal synthesis. Catal. Sci. Technol. 6, 840−850 (2016).

- Li, H. et al. Dehydrogenation of ethylbenzene and propane over Ga2O3-ZrO2 catalysts in the presence of CO2. Catal. Commun. 8, 1317−1322 (2007).

- Xu, B., Zheng, B., Hua, W., Yue, Y. & Gao, Z. Support effect in dehydrogenation of propane in the presence of CO2 over supported gallium oxide catalysts. J. Catal. 239, 470−477 (2006).

- Chen, M. et al. Study in support effect of In2O3/MOx (M = Al, Si, Zr) catalysts for dehydrogenation of propane in the presence of CO2. Appl. Catal. A Gen. 407, 20−28 (2011).

- Chen, M. et al. Dehydrogenation of propane over In2O3–Al2O3 mixed oxide in the presence of carbon dioxide. J. Catal. 272, 101−108 (2010).

- Xue, X. L., Lang, W. Z., Yan, X. & Guo, Y. J. Dispersed vanadium in three-dimensional dendritic mesoporous silica nanospheres: active and stable catalysts for the oxidative dehydrogenation of propane in the presence of CO2. ACS Appl. Mater. Interfaces 9, 15408−15423 (2017).

- Wang, H. M., Chen, Y., Yan, X., Lang, W. Z. & Guo, Y. J. Cr doped mesoporous silica spheres for propane dehydrogenation in the presence of CO2: effect of Cr adding time in sol-gel process. Microporous Mesoporous Mater. 284, 69−77 (2019).

- Yun, D. et al. Promotional effect of Ni on a CrOx catalyst supported on silica in the oxidative dehydrogenation of propane with CO2. ChemCatChem 4, 1952−1959 (2012).

- Tedeeva, M. A. et al. Dehydrogenation of propane in the presence of CO2 on GaOx/SiO2 catalyst: influence of the texture characteristics of the support. Fuel 313, 122698 (2022).

- Wang, S.-W. et al. Metal nitride-terminated metal oxides efficiently catalyzing CO2 oxidative dehydrogenation of propane. ACS Catal. 16, 2375−2385 (2026).

- Peng, C. et al. PtSn supported on CeO2 modified dendritic mesoporous SiO2 as an efficient catalyst for oxidative dehydrogenation of propane with CO2. Appl. Catal. B Environ. 385, 126243 (2026).

- Tian, K. et al. Unraveling the hydrogen spillover in tandem propane dehydrogenation and reverse water gas shift reaction. Nat. Commun. 16, 10186 (2025).

- Lin, J. et al. Mechanistic insights into the rapid deactivation of PtIn/Al2O3 catalysts during CO2-assisted propane dehydrogenation. J. Catal. 453, 116484 (2026).

- Li, W. et al. Engineering the electronic structure of Pt-KOx cluster catalyst via alkali metal for efficient oxidative dehydrogenation of propane using CO2. J. Energy Chem. 110, 301−310 (2025).

- Wang, Z. et al. CO2 oxidative dehydrogenation of propane over a GaN supported on Ga-modified MFI zeolite catalyst. Mol. Catal. 585, 115373 (2025).

- Wu, R. et al. NiCrOx@silicalite-1 with advanced CO2 utilization in oxidative dehydrogenation of propane: insights into bifunctional catalysis and reaction efficiency. ACS Sustain. Chem. Eng. 13, 8644−8659 (2025).

- Zhang, H. et al. Comparative study on transition metal promoted Pt/SiO2 for oxidative dehydrogenation of propane with carbon dioxide. J. CO2 Util. 97, 103116 (2025).

- Sun, Y. et al. Boosting CO2 oxidative propane dehydrogenation via separate activation CO2 and propane by in-framework and extra-framework Co species on ZSM-5 zeolite. Appl. Catal. B Environ. 373, 125324 (2025).

- Xu, B. et al. Molybdenum carbide nanoparticles in silicalite-1 zeolite for CO2‑assisted propane dehydrogenation. ACS Catal. 15, 4089−4100 (2025).

- Otieno, H. N. et al. Attractive performance Cr–Co/ZSM-5 catalysts for the oxidative dehydrogenation of propane with carbon dioxide. J. Environ. Chem. Eng. 13, 115787 (2025).

- Wang, F. et al. CO2-assisted oxidative dehydrogenation of propane catalyzed by Fe modified vanadium oxide/silicalite-1 catalysts. Chem. Eng. J. 505, 159104 (2025).

- Yang, L. et al. Alkaline-earth metals promote propane dehydrogenation with carbon dioxide through geometric effects: altering the reaction pathway. Appl. Catal. B Environ. 366, 124985 (2025).

- Kim, J. & Kim, D. H. Enhanced stability of silica-coated PtSn/Al2O3 catalyst for oxidative dehydrogenation of propane with CO2. Fuel 384, 134003 (2025).

- Zhang, S. et al. Facilitating CO2 dissociation via Fe doping on supported vanadium oxides for intensified oxidative dehydrogenation of propane. Chem. Eng. J. 481, 148231 (2024).

- Li, W. et al. Bifunctional catalysts with separated and tunable sites on zeolites for relay catalysis of the oxidative dehydrogenation of propane using CO2. Adv. Funct. Mater. 35, 2414231 (2025).