A Triphenylamine-Functionalized Silica Nanoparticle for Fluorescent Detection of Fe2+/Fe3+ Red Wine

Eda Erdemir*a,b, Garen Suna*a, Nisa Demirbilekc, , Songül Eğlence-Bakıra, Musa Şahina, Erman Karakuş*c

aDepartment of Chemistry, Faculty of Science, Istanbul University, 34134 Istanbul, Turkey

bInstitute of Graduate Studies in Science, Istanbul University, 34134 Istanbul, Turkey

cOrganic Chemistry Laboratory, Chemistry Group, National Metrology Institute, (TUBITAK UME), 41470 Gebze, Kocaeli, Turkey

Corresponding author: Erman Karakuş, Eda Erdemir, Garen Suna

CONTENTS										        PAGE

1. TGA Analysis of SNP–NH2 and TPA–SNP.….……………………..….……………...…………..3

2. Time-Dependant Fluorescence Change of TPA–SNP with Fe2+/3+………………………………....3

3. Determination of Detection Limit of Fe2+/3+……………….…………………………………...…...5

4. Effect of pH …………………………………………………………..….………………………....5

5. UV-vis and fluorescence spectra illustrating the detection mechanism….………………………....5

6. DLS Analysis of SNP, SNP-NH2 and TPA-SNP…………………………………………………..7

7. Comparison Chart of TPA-SNP with Other Reported Silica Nanoparticles Based Fe2+/3+ Selective

Probes…………………………………………………………………………………………………8

1H and 13C NMR of T-T-AL……….…………………………………………………………..……..8

1H and 13C NMR of Br-T-T-AL……….………………………………………………………….….8

1H and 13C NMR of TPA-AL……….…………………………………………………………….….8

Mass spectrum of TPA-AL …………….….……………….………..……………………………….9

1. TGA Analysis

Figure S1. TGA curves of SNP–NH2 and TPA–SNP at a heating rate of 10 °C min−1.

2. Time-Dependent Fluorescence Change of TPA–SNP with Fe2+/3+

Figure S2. Time-Dependent Fluorescence Change of TPA–SNP with Fe2+/3+

3. Determination of Detection Limit of Fe2+/3+

The detection limit was calculated based on regression analysis. A highly precise calibration curve was established correlating fluorescence intensity with concentration within the range of 2.6 – 13.3 μM for Fe2+ and Fe3+ ions. LOD was determined using the formula LOD = 3.3σbi/m, where σbi denotes the standard deviation of all measurements based on linear regression, and m signifies the slope of the calibration curve. Linear regression analysis determined the LOD for Fe2+ and Fe3+ to be 1.24 and 0.97 μM, respectively.

Figure S3. Fluorescence changes of TPA–SNP (25 ppm) upon addition of (a) Fe2+ (b) Fe3+ (2.6 to 13.3 μM).

4. Effect of pH

Figure S4. Effect of pH on the fluorescence intensity of TPA–SNP (25 ppm) in 1:1 THF/PBS in the absence (black line) and presence (red line) of Fe2+/3+ (100 µM).

5. Fluorescence and UV-Vis spectra illustrating the detection mechanism

Figure S5. (a) UV-Vis spectra and (b) fluorescence emission spectra illustrating the detection mechanism of TPA–SNP in the environment of Fe2+/3+.

6. DLS Analysis of SNP, SNP-NH2 and TPA-SNP

Figure S6. DLS Analysis of of SNP, SNP-NH2 and TPA-SNP

Table S1. Comparison of silica nanoparticle-based fluorescent sensing systems reported for Fe³⁺ and Fe²⁺ detection

| Material | Method | Mechanism | LOD | Reference |
| --- | --- | --- | --- | --- |
| Sulfonamide-based nanocomposite (SAN) | Fluorometric analysis | Fluorescence enhancement (Fe³⁺) | 0.027 µM | 24 |
| Salicylic acid-doped silica nanoparticles (SASP) | Fluorometric analysis | Fluorescence quenching | 0.025 µM | 23 |
| EB-integrated mesoporous organosilica hybrids (EB–MOS) | Colorimetric and fluorometric analysis | Fluorescence quenching (Fe³⁺/Hg²⁺) | 0.448 µM | 22 |
| Propidium iodide-integrated mesoporous silica nanoparticles (PIMSNs) | Colorimetric and fluorometric analysis | Fluorescence quenching (Fe³⁺) | 0.5 µM | 25 |
| Rhodamine B-loaded silica nanoparticles (MRB@SiNPs) | Colorimetric and fluorometric analysis | Fluorescence enhancement (Fe³⁺) | 0.0496 µM | 26 |
| BODIPY-modified silica nanoparticles (BOD–SNP) | Fluorometric analysis | Fluorescence enhancement (Fe³⁺) | 1.3 µM | 27 |
| TPA-modified silica nanoparticles (TPA–SNP) | Fluorometric analysis | Fluorescence quenching (Fe³⁺/Fe²⁺) | 0.97 / 1.24 µM | This work |

1H NMR of T-T-AL

13C NMR of T-T-AL

1H NMR of Br-T-T-AL

13C NMR of Br-T-T-AL

1H NMR of TPA-AL

13C NMR of TPA-AL

HRMS spectrum of TPA-AL