Supplementary Material

Table S1. Objective-function terms and adopted weights.

| Term | Weight / penalty | Role |
| --- | --- | --- |
| Global curve-shape error | wF = 1.00 | Controls the overall load-displacement response |
| Peak-load error | wP = 0.75 | Constrains load capacity |
| Peak-displacement error | wU = 0.55 | Constrains peak position |
| Initial-stiffness error | wK = 0.25 | Constrains the pre-peak response |
| Energy penalty | wE = 5.00 | Suppresses non-quasi-static explicit solutions |
| Failed simulation | Πfail = 1.0 × 10^6 | Excludes invalid FE calculations |

Table S2 lists the complete fitted coefficients used to generate the 1000 h extrapolation results summarized in Table 3 of the main text.

Table S2. Fitted coefficients of the temperature-dependent cohesive-parameter evolution models.

| Parameter and temperature | Model form | Fitted coefficients |
| --- | --- | --- |
| K-150 °C | Two-stage exponential | Kc = 34937.65；tc = 250 h；k1 = 4.9170×10⁻⁴；k2 = −2.1170×10⁻⁴ |
| K-180 °C | Standard exponential: | K24 = 32751.53；β = 2.9591×10⁻⁴ |
| K-200 °C | Standard exponential | K24 = 32319.69；β = 1.3401×10⁻⁴ |
| ts0-150 °C | Two-stage exponential | Pc = 69.7139；tc = 100 h；k1 = 3.0124×10⁻⁴；k2 = −2.1416×10⁻⁵ |
| ts0-180 °C | Stretched exponential | A = 66.7835；β = 0.0135867；n = 0.2 |
| ts0-200 °C | Stretched exponential | A = 65.6585；β = 0.0192972；n = 0.2 |
| GIIc-150 °C | Residual exponential | G∞ = 1.82538；A = 0.22369；β = 0.0055259 |
| GIIc-180 °C | Residual exponential | G∞ = 1.90693；A = 0.22322；β = 0.0044740 |
| GIIc-200 °C | Residual exponential | G∞ = 1.77127；A = 0.47753；β = 0.0170182 |