Theoretical Research on Tetrazine-Based Nitrogen-Chain Energetic Materials: Balancing Detonation Performance and Sensitivity via Structural Regulation

Qian Zhang, Xiao-Nan He, Han-Jie Ni, Jia-Nan Li, Lan-Ying Xu, Yan Huang*, Tao Long*

School of Chemistry and Chemical Engineering Huanggang Normal University, Huanggang 438000, China

content

Fig. S1 Designed molecular structures of molecules 01 to 18	2

Table S1 Density of designed molecules 01 to 18 (at B3PW91/6-311+g(d,p) level)	2

Fig. S2 Designed molecular structures of series I to IV	4

Table S2 Density of designed molecules series I to IV (at B3PW91/6-311+g(d,p) level)	4

Table S3 HOMO and LUMO calculation details of designed molecules series I to IV (at M06-2X/6-311+G(d,p) level)	5

Table S4 Theoretical density values for similar nitrogen-rich molecules at different calculation level	6

Table S5 Calculation details of similar nitrogen-rich molecules M01 to M03	6

Fig. S5 Isodesmic reactions of Series III designed molecules	9

Fig. S6 Isodesmic reactions of Series IV designed molecules	10

Table S6 Calculation details of designed molecules series I to IV (at M06-2X/6‑311+G(d,p) level)	10

Fig. S7 AICD map of designed molecules I-04 to I-06 and III-05 to 06 at M06-2X/6-311+G(d,p)                                                                  level (small arrows indicate direction and magnitude of magnetically induced currents on AICD isosurface of 0.05 a.u.)	11

Table S7 The AV1245 index of designed molecules I-04 to I-06 and III-05 to 06 at M06-2X/6-311+G(d,p) level	12

Fig. S8 Possible decomposition reaction of I06	12

Table S8 The coordinates of TS-01 to TS-04 (at M06-2X/def2tzvp level)	13

# Fig. S1 Designed molecular structures of molecules 01 to 18

# Table S1 Density of designed molecules 01 to 18 (at B3PW91/6-311+g(d,p) level)

| Compd. | volume [Angstrom3] | MVM [g/cm3] | overall surface area [Angstrom2] | vσtot2 [(kal/mol]2] | Density a [g/cm3] |
| --- | --- | --- | --- | --- | --- |
| 01 | 187.9 | 1.468 | 184.8 | 49.12 | 1.420 |
| 02 | 247.2 | 1.721 | 237.0 | 24.35 | 1.621 |
| 03 | 280.4 | 1.694 | 263.7 | 46.31 | 1.641 |
| 04 | 187.6 | 1.471 | 185.7 | 63.70 | 1.453 |
| 05 | 245.5 | 1.732 | 231.4 | 28.15 | 1.641 |
| 06 | 282.0 | 1.685 | 262.1 | 35.22 | 1.608 |
| 07 | 185.7 | 1.486 | 179.6 | 53.20 | 1.446 |
| 08 | 247.4 | 1.720 | 236.1 | 22.70 | 1.617 |
| 19 | 280.4 | 1.695 | 264.3 | 27.35 | 1.601 |
| 10 | 219.0 | 1.472 | 219.5 | 74.83 | 1.478 |
| 11 | 274.7 | 1.718 | 267.2 | 27.53 | 1.625 |
| 12 | 309.5 | 1.686 | 300.4 | 56.34 | 1.653 |
| 13 | 214.7 | 1.502 | 213.4 | 63.79 | 1.484 |
| 14 | 274.5 | 1.719 | 265.4 | 33.75 | 1.639 |
| 15 | 309.4 | 1.686 | 296.2 | 48.64 | 1.637 |
| 16 | 214.0 | 1.507 | 212.8 | 41.49 | 1.442 |
| 17 | 272.2 | 1.734 | 264.3 | 26.25 | 1.638 |
| 18 | 307.6 | 1.696 | 300.4 | 30.68 | 1.610 |
| aρ=1.0046×(MVM)+0.0021(vσtot2)-0.1586, ref: B. M. Rice, E. F. C. Byrd. J. Comput. Chem. 2013, 34, 2146-2151. |  |  |  |  |  |

# Fig. S2 Designed molecular structures of series I to IV

# Table S2 Density of designed molecules series I to IV (at B3PW91/6-311+g(d,p) level)

| Compd. | volume [Angstrom3] | MVM [g/cm3] | overall surface area [Angstrom2] | vσtot2 [(kal/mol]2] | Density a [g/cm3] |
| --- | --- | --- | --- | --- | --- |
| I-03 | 336.6 | 1.856 | 299.7 | 17.19 | 1.742 |
| I-04 | 353.1 | 1.929 | 307.0 | 17.96 | 1.817 |
| I-05 | 398.4 | 1.935 | 328.5 | 16.79 | 1.820 |
| I-06 | 368.6 | 1.965 | 344.8 | 15.24 | 1.847 |
| II-03 | 335.9 | 1.860 | 290.4 | 19.14 | 1.750 |
| II-04 | 354.8 | 1.920 | 300.9 | 19.23 | 1.810 |
| II-05 | 399.0 | 1.932 | 321.1 | 12.18 | 1.808 |
| II-06 | 307.1 | 1.872 | 289.8 | 28.12 | 1.781 |
| III-03 | 365.2 | 1.838 | 337.8 | 23.51 | 1.737 |
| III-04 | 383.6 | 1.897 | 346.2 | 19.65 | 1.788 |
| III-05 | 429.8 | 1.902 | 375.3 | 16.07 | 1.786 |
| III-06 | 395.8 | 1.948 | 373.7 | 16.66 | 1.833 |
| IV-03 | 370.7 | 1.810 | 347.0 | 28.98 | 1.721 |
| IV-04 | 388.7 | 1.872 | 346.0 | 29.47 | 1.784 |
| IV-05 | 434.4 | 1.881 | 377.1 | 20.14 | 1.774 |
| IV-06 | 400.4 | 1.925 | 372.6 | 26.36 | 1.831 |
| aρ=1.0046×(MVM)+0.0021(vσtot2)-0.1586, ref: B. M. Rice, E. F. C. Byrd. J. Comput. Chem. 2013, 34, 2146-2151. |  |  |  |  |  |

# Table S3 HOMO and LUMO calculation details of designed molecules series I to IV (at M06-2X/6-311+G(d,p) level)

| Compd. | HOMO |  | LUMO |  | HOMO-LUMO energy gap [eV] |
| --- | --- | --- | --- | --- | --- |
|  |  | Energy [eV] |  | Energy [eV] |  |
| I-01 | 65 | -8.203 | 66 | -2.323 | 5.880 |
| I-02 | 73 | -8.421 | 74 | -1.956 | 6.465 |
| I-03 | 95 | -8.592 | 96 | -2.367 | 6.225 |
| I-04 | 103 | -8.912 | 104 | -2.447 | 6.465 |
| I-05 | 117 | -8.967 | 118 | -2.883 | 6.084 |
| I-06 | 109 | -10.16 | 110 | -4.647 | 5.511 |
| II-01 | 65 | -9.029 | 66 | -2.388 | 6.640 |
| II-02 | 73 | -8.547 | 74 | -1.951 | 6.597 |
| II-03 | 95 | -8.864 | 96 | -2.377 | 6.487 |
| II-04 | 103 | -9.097 | 104 | -2.614 | 6.483 |
| II-05 | 117 | -9.170 | 118 | -2.885 | 6.285 |
| II-06 | 87 | -10.23 | 88 | -3.675 | 6.553 |
| III-01 | 72 | -8.380 | 73 | -2.652 | 5.728 |
| III-02 | 80 | -8.185 | 81 | -2.106 | 6.079 |
| III-03 | 102 | -8.568 | 103 | -2.277 | 6.291 |
| III-04 | 110 | -8.689 | 111 | -2.548 | 6.142 |
| III-05 | 124 | -8.735 | 125 | -2.723 | 6.013 |
| III-06 | 116 | -10.19 | 117 | -4.764 | 5.424 |
| IV-01 | 72 | -8.624 | 73 | -2.821 | 5.803 |
| IV-02 | 80 | -8.486 | 81 | -2.369 | 6.118 |
| IV-03 | 102 | -8.626 | 103 | -2.491 | 6.134 |
| IV-04 | 110 | -8.720 | 111 | -2.726 | 5.994 |
| IV-05 | 124 | -8.819 | 125 | -3.017 | 5.802 |
| IV-06 | 116 | -9.460 | 117 | -4.852 | 4.608 |

# Table S4 Theoretical density values for similar nitrogen-rich molecules at different calculation level

| Compd. | Chemical structure | Geometric optimization structure | Density [g/cm3] |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Method-01 a | Method-02 a | Method-03 a | Ref. |
| M01 |  |  | 1.445 b | 1.453 b | 1.450 b | 1.64 d |
| M02 |  |  | 1.840 b | 1.845 b | 1.788 b | 1.80 c |
| M03 |  |  | 1.781 b | 1.791 b | 1.788 b | 1.907 e |
| a Method-01: m062x/6-311+g(d,p); Method-02: wb97xd/6-311+g(d,p); Method-03: b3pw91/6-311+g(d,p) b ρ=1.0046×(MVM)+0.0021(vσtot2)-0.1586, ref: B. M. Rice, E. F. C. Byrd. J. Comput. Chem. 2013, 34, 2146-2151. c P. Yin, D. A. Parrish, J. M. Shreeve. Chem. Eur. J. 2014, 20, 1-7. d Y. C. Li, C. Qi, S. P. Pang, et al. J. Am. Chem. Soc. 2010, 132, 12172-12173. e D. E. Chavez, J. C. Bottaro, D. A. Parrish, et al. Angew. Chem. Int. Ed. 2015, 54, 12973-12975. |  |  |  |  |  |  |

# Table S5 Calculation details of similar nitrogen-rich molecules M01 to M03

| Compd. | Calculation method | volume [Angstrom3] | MVM [g/cm3] | overall surface area [Angstrom2] | vσtot2 [(kal/mol]2] |
| --- | --- | --- | --- | --- | --- |
| M01 | M06-2X/6‑311+G(d,p) | 181.0 | 1.506 | 188.2 | 43.18 |
|  | ωB97X‑D/def2tvzp | 180.0 | 1.514 | 187.7 | 43.29 |
|  | B3PW91/6‑311+G(d,p) | 179.9 | 1.515 | 187.8 | 41.57 |
| M02 | M06-2X/6‑311+G(d,p) | 244.0 | 1.736 | 247.1 | 121.00 |
|  | ωB97X‑D/def2tvzp | 242.8 | 1.745 | 246.6 | 119.27 |
|  | B3PW91/6‑311+G(d,p) | 242.7 | 1.745 | 246.9 | 91.88 |
| M03 | M06-2X/6‑311+G(d,p) | 224.1 | 1.868 | 225.0 | 30.17 |
|  | ωB97X‑D/def2tvzp | 223.1 | 1.877 | 224.6 | 30.55 |
|  | B3PW91/6‑311+G(d,p) | 223.1 | 1.877 | 224.8 | 29.13 |

Fig. S3 Isodesmic reactions of Series I designed molecules

Fig. S4 Isodesmic reactions of Series II designed molecules

# Fig. S5 Isodesmic reactions of Series III designed molecules

# Fig. S6 Isodesmic reactions of Series IV designed molecules

# Table S6 Calculation details of designed molecules series I to IV (at M06-2X/6‑311+G(d,p) level)

| Compd. | Formula | M.W. | OB% | ΔHgas [kJ/mol] | ΔHsub [kJ/mol] | ΔHsolid [kJ/mol] |
| --- | --- | --- | --- | --- | --- | --- |
| I-01 | C4H4O4N10 | 256.4 | -37.44 | 1505 | 109.1 | 1396 |
| I-02 | C4H6O4N12 | 286.2 | -39.14 | 1698 | 136.9 | 1561 |
| I-03 | C4H4O8N14 | 376.2 | -8.51 | 1782 | 141.2 | 1641 |
| I-04 | C6H4O8N12F2 | 410.2 | -19.50 | 1096 | 146.8 | 948.8 |
| I-05 | C4H4O12N14 | 464.2 | -6.89 | 1428 | 161.1 | 1267 |
| I-06 | C4O12N14 | 436.1 | 14.67 | 1480 | 172.0 | 1308 |
| II-01 | C4H4O4N10 | 256.4 | -37.44 | 1505 | 108.8 | 1396 |
| II-02 | C4H6O4N12 | 286.2 | -39.14 | 1698 | 130.0 | 1568 |
| II-03 | C4H4O8N14 | 376.2 | -8.51 | 1782 | 136.7 | 1645 |
| II-04 | C6H4O8N12F2 | 410.2 | -21.45 | 1096 | 143.7 | 951.9 |
| II-05 | C4H4O12N14 | 464.2 | -6.89 | 1428 | 151.6 | 1276 |
| II-06 | C4H2O8N12 | 346.1 | -4.62 | 1492 | 142.7 | 1350 |
| III-01 | C4H4O4N12 | 284.2 | -33.78 | 1848 | 128.3 | 1720 |
| III-02 | C4H6O4N14 | 314.2 | -35.65 | 2041 | 164.9 | 1876 |
| III-03 | C4H4O8N16 | 404.2 | -7.92 | 2125 | 173.2 | 1951 |
| III-04 | C6H4O8N14F2 | 438.2 | -18.26 | 1438 | 176.7 | 1262 |
| III-05 | C6H4O12N16 | 492.2 | -6.50 | 1770 | 197.3 | 1573 |
| III-06 | C4O12N16 | 464.1 | 13.79 | 1822 | 196.4 | 1626 |
| IV-01 | C4H4O4N12 | 284.2 | -33.78 | 1848 | 131.1 | 1717 |
| IV-02 | C4H6O4N14 | 314.2 | -35.65 | 2041 | 158.4 | 1882 |
| IV-03 | C4H4O8N16 | 404.2 | -7.92 | 2125 | 183.9 | 1941 |
| IV-04 | C6H4O8N14F2 | 438.2 | -18.26 | 1438 | 183.5 | 1255 |
| IV-05 | C6H4O12N16 | 492.2 | -6.50 | 1770 | 202.1 | 1568 |
| IV-06 | C4O12N16 | 464.1 | 13.79 | 1822 | 202.7 | 1620 |

# Fig. S7 AICD map of designed molecules I-04 to I-06 and III-05 to 06 at M06-2X/6-311+G(d,p)                                                                  level (small arrows indicate direction and magnitude of magnetically induced currents on AICD isosurface of 0.05 a.u.)

# Table S7 The AV1245 index of designed molecules I-04 to I-06 and III-05 to 06 at M06-2X/6-311+G(d,p) level

| Compd. | Atom labels | 1000*AV1245 index | Multicenter bond order |
| --- | --- | --- | --- |
| I-04 | 1,3,14,13,10,9 | 12.54718780 | -5.0270527509E-02 |
|  | 1,3,14,13,10,9,11-12,7,5,16,15 | 41.36652068 | 0.0001770930 |
| I-05 | 1,3,14,13,10,9 | 36.90338122 | 0.0034996034 |
|  | 1,3,14,13,10,9,11-12,7,5,16,15 | 32.18070531 | 0.0001387035 |
| I-06 | 1-2,10,9,6,5 | -5.71472512 | 0.0081746099 |
|  | 1-2,10,9,6,5,7-8,4,3,12,11 | -2.77615443 | -1.6444967477E-04 |
| III-05 | 4,5,15,17,10,9 | 17.86460394 | -4.2621950035E-02 |
|  | 4,5,15,17,10,9,2,1,3,7-8,13,11,6 | 4.32701537 | 0.0001734080 |
| III-06 | 1-2,7-8,16-17 | 9.01640382 | -3.6047363924E-02 |
|  | 1-2,7-8,16-17,3-4,18-20,6,5,12 | 11.74862600 | -1.4773297469E-04 |

# Fig. S8 Possible decomposition reaction of I06

# Table S8 The coordinates of TS-01 to TS-04 (at M06-2X/def2tzvp level)

| Molecule | Molecular structure | Coordinates |
| --- | --- | --- |
| TS-01 |  | C -0.48554900 0.46046400 -0.04661400 C 0.12560200 -0.84596300 0.29708400 N -2.72085200 -1.45647600 -0.03717700 N -0.47072600 -1.68537700 0.97027600 N -2.43204900 -0.43172600 -0.44301300 N -1.75470800 0.68945400 -0.30000200 N 0.26010000 1.69987400 0.27661100 N 1.55514300 -1.00094300 -0.31769800 O 1.01012700 1.60275000 1.24356700 O 0.07234200 2.67124600 -0.43444100 O 1.79302800 -0.16530100 -1.18873400 O 2.26216800 -1.90752600 0.06138400 |
| TS-02 |  | C 0.67933100 0.13576500 -0.08051600 C -0.67932900 0.13577700 0.08050800 N -0.71606300 2.44077600 0.49347700 N -1.17748800 1.32971300 0.51298900 N 0.71611000 2.44076600 -0.49347300 N 1.17751000 1.32969300 -0.51299300 N 1.64628700 -0.91106100 0.23595900 N -1.64630300 -0.91103500 -0.23595900 O 1.22476000 -1.80951800 0.95853700 O 2.77333500 -0.79434000 -0.22901100 O -1.22479600 -1.80949800 -0.95854000 O -2.77334600 -0.79429700 0.22902000 |
| TS-03 |  | C -0.10170300 0.00476600 -0.03512800 C 0.12800500 1.41584500 -0.06074300 N 3.02146600 -0.64193800 0.40670800 N 0.39109200 2.54713100 -0.10770100 N 2.11829700 -0.52239200 -0.32183200 N 0.74968800 -0.93923400 -0.06326400 N -1.55789300 -0.41350000 0.02830900 O -2.34169900 0.50029100 0.25771000 O -1.81034700 -1.59205900 -0.13524900 |
| TS-04 |  | C 0.12840800 0.08744800 0.00021400 C -0.14973700 1.44950700 -0.00026300 N -3.11025800 -0.67740600 0.00033400 N -0.41471600 2.59191700 -0.00063400 N -1.97285600 -0.72742000 0.00020900 N -0.74458100 -0.95864500 0.00001300 N 1.54377900 -0.35700400 0.00005400 O 2.06401900 -0.51915600 1.09605300 O 2.06328100 -0.52107200 -1.09599500 |