Table 1. IC50 values of DyFeO3 samples on various cell lines at laser ‘ON’ and ‘OFF’ conditions.

| Sample | Condition | IC50 (μg mL-1) |  |
| --- | --- | --- | --- |
|  |  | MDA-MB-231 cells (cancerous) | HEK293 cells (non-cancerous) |
| Empty DyFeO3 nanoparticles | Laser OFF | 52.2 ± 3.3 | 308.4 ± 8.6 |
| 5-FU-loaded DyFeO3 nanoparticles | Laser OFF | 12.5 ± 1.4 | 231.6 ± 7.3 |
| Empty DyFeO3 nanoparticles | Laser ON (808 nm, 1 W cm-1) | 7.2 ± 1.2 | -- |
| 5-FU-loaded DyFeO3 nanoparticles | Laser OFF | 3.5 ± 0.8 | -- |

Table 2. A critical comparison of ferrite nanocarriers in anticancer drug delivery based on therapeutic efficacy, surface modifications, and design limitations.

| Ferrite Nanocarrier | Drug | Surface Modification / Coating | Cancer Cell Line | IC50 (μg mL-1) | Novelty | Main Drawback | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- |
| β-CD–Dextran coated NiFe2O4 | Camptothecin | β-CD–Dextran | MDA-MB-231 | Not reported | Functionalized polymer coating enabling sustained CPT release | No active targeting ligand; nickel toxicity concerns | [45] |
| β-CD–PEG-folate coated ErFeO3 | Camptothecin | β-CD–Dextran | MCF-7 | Not reported | High drug loading (~88%) | Limited in vivo validation | [46] |
| Ytterbium Ferrite Nanoparticles | Camptothecin | β-CD/Folate-PLGA coating | MCF-7 | 4.92 | Host–guest drug complexation with folate targeting | Not evaluated on normal-cell selectivity | [47] |
| Ho–Ni Ferrite Nanocarrier | Camptothecin | β-CD–PEG–Folate | MDA-MB-231 | 4.61 | Rare-earth co-doped ferrite with targeting ligand | No healthy-cell comparison reported | [48] |
| Holmium Ferrite Nanocarrier | Camptothecin | β-CD–PEG | MCF-7 | 3.12 | Rare-earth ferrite magnetic carrier | No active targeting moiety | [49] |
| PVA-coated Mg–Co Ferrite Nanocomposite | 5-FU | Poly(vinyl alcohol) | MCF-7 | 126 | pH-responsive 5-FU release | Relatively weak tumor specificity; Weak activity | [50] |
| HA-β-CD-coated DyFeO3 (Present Work) | 5-FU | Hyaluronic acid–β-cyclodextrin | MDA-MB-231 | 12.5 ± 1.4 | First HA-β-CD functionalized DyFeO3 carrier; rare-earth ferrite; controlled 5-FU release | Drug loading (2%) lower than some CPT systems | Present work |

Table 3. In vitro antibacterial activity of GM-loaded DyFeO3 nanoparticles under laser ‘ON’ and ‘OFF’ conditions. Extent of activity is shown by the zones of inhibition of each bacterial stain examined using disc diffusion method.

| Name of the test organism | Zone of Inhibition (mm) Mean ± SD |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | GM-loaded polymer-coated DyFeO3 nanoparticles |  |  |  |  |
|  | 500 µg/mL | 250 µg/mL | 100 µg/mL | 50 µg/mL | Positive Control |
| B. fragilis | 10.25 ± 0.35 | 9.75 ± 0.35 | 0 | 0 | 10.6 ± 0.14 |
| P. acnes | 9.50 ± 0.70 | 9 ± 0.70 | 0 | 0 | 10.5 ± 0.70 |
| P. aeruginosa | 10.35 ± 0.49 | 9.25 ± 0.35 | 0 | 0 | 12 ± 0.70 |
| S. aureus | 9.75 ± 0.35 | 8.5 ± 0.70 | 0 | 0 | 11.75 ± 0.35 |
| S. epidermidis | 8.25 ± 0.35 | 0 | 0 | 0 | 11.25 ± 0.35 |
| S. pyogenes | 8.5 ± 0.70 | 7.25 ± 0.35 | 0 | 0 | 10.25 ± 0.35 |
|  | GM-loaded polymer-coated DyFeO3 nanoparticles with laser irradiation |  |  |  |  |
| B. fragilis | 22.85 ± 0.49 | 19.8 ± 0.14 | 16.4 ± 0.14 | 9.85 ± 0.21 | 25.65 ± 0.49 |
| P. acnes | 20.45 ± 0.77 | 19.35 ± 0.49 | 18.35 ± 0.21 | 17.25 ± 0.35 | 23.85 ± 0.21 |
| P. aeruginosa | 22.5 ± 0.14 | 21.35 ± 0.21 | 19.25 ± 0.35 | 14.5 ± 0.70 | 24.2 ± 0.28 |
| S. aureus | 23.95 ± 0.35 | 17.35 ± 0.49 | 15.5 ± 0.70 | 11.05 ± 0.21 | 22.75 ± 0.35 |
| S. epidermidis | 21.15 ± 0.63 | 18.6 ± 0.70 | 18.35 ± 0.21 | 0 | 26.5 ± 0.28 |
| S. pyogenes | 27.3 ± 0.51 | 23.65 ± 0.07 | 19.15 ± 0.21 | 11.45 ± 0.63 | 28.1 ± 0.56 |

SD – Standard Deviation, *Significance - p< 0.05