Supplementary Materials

Text S1 Chemicals and materials

Petroleum hydrocarbon wastewater was collected from a contaminated site in Chongqing, (29°29'14.55″ N, 106°30'11.36″ E). Ferric nitrate nonahydrate (Fe (NO3)3·9H2O) and Manganese nitrate tetrahydrate (Mn (NO3)2·4H2O) were purchased from Aladdin Chemical Reagents Ltd. (Shanghai, China). Corn cobs and wheat straw are purchased from Henan Lize Environmental Protection Technology Ltd. (Henan, China). Citric acid (C6H8O7) and sodium persulfate (Na2S2O8, AR) were purchased from Xilong Science Ltd. (Sichuan, China). Ammonia water (NH3·H2O), nitric acid (HNO3, AR), and reduced iron powder (Fe) were purchased from China National Pharmaceutical Group Chemical Reagent Ltd. (Shanghai, China). Acetone and dichloromethane were purchased from Shanghai McLean Biological Reagents Ltd. (Shanghai, China).

Text S2 Material characterization

(1) SEM analysis

Using a ZEISS Gemini 360 scanning electron microscope, the surface morphology of MnFe2O4@BC before and after reaction, as well as that of the original biochar (BC), was observed using an In Lens detector under the following conditions: an electron beam voltage (EHT) of 10.00 kV, a working distance (WD) of 7.7 mm, and a magnification range of 500–100,000[1].

(2) Specific surface area (BET) analysis

A specific surface area analyzer was used to determine the specific surface area and pore size of the material at a temperature of 400 °C and a reaction time of 2 h[2].

(3) X-ray diffraction (XRD) analysis

An Ultima IV X-ray diffractometer manufactured by Rigaku (Japan) was used, employing a 40 kV, 40 mA copper-targeted K radiation source, with a 10 mm high-limiting slit, an anti-scatter slit of 8.0 mm, and a detector angle 5 θ ranging from 10°to 80°, to scan the MnFe2O4@BC samples before and after reaction at a speed of 0.02°/s, thereby determining their crystal structure[3].

(4) X-ray photoelectron spectroscopy (XPS) analysis

In this study, an ESCALAB 250XI X-ray photoelectron spectrometer manufactured by Thermon Scientific K-Alpha (USA) was employed to conduct qualitative analyses of the catalysts before and after the reaction. This was done to determine their elemental composition and the valence states of surface-active components, and to investigate the roles of the catalysts surface-active components and functional groups during the reaction process[4].

(5) Fourier-transform infrared (FTIR) spectroscopy

An IS5 infrared spectrometer manufactured by Thermon Fisher Scientific (USA) was used to analyses the types of functional groups present in MnFe2O4/BC before and after the reaction, as well as changes in chemical bonds[5].

Table S1 Characteristics of Different Activated PS

| Activation method | Advantages | Disadvantage | Ref. |
| --- | --- | --- | --- |
| Thermal activation | The reaction is convenient and does not require the addition of activators. | Requires high energy consumption, difficult to apply on a large scale | [5] |
| Alkali activation | Interactions of various free radicals | The product pH is too high; a secondary repair will be carried out | [6] |
| Fe2+ activation | High efficiency, fast free radical generation, mild reaction conditions | The concentrations of Fe2+ and Fe3+ ions in the product are high | [7] |
| Ultrasonic activation | The reaction conditions are mild and there is no secondary pollution | Low energy efficiency, weak environmental adaptability, | [10] |
| Ultraviolet light activation | Clean and efficient, highly controllable, with no secondary pollution | Mass transfer limitations and poor environmental adaptability | [4] |
| biological activation | Strong environmental compatibility, no secondary pollution, extremely low energy consumption | Easily disturbed, slow activation rate | [9] |
| Activation of carbon-based supported materials | Efficient, stable, environmentally friendly, highly adaptable, eco-friendly, low secondary pollution, wide applicability, strong anti-interference capability | Preparation cost is relatively high | [8] |

Table S2 Parameter settings for preparing MnFe2O4@biochar (MFB) by sol-gel method

| Name | Calcination temperature | Fe（NO3)3·9H2O (mol) | Mn（NO3)2·4H2O (mol) | Fe:Mn | Citric acid (mol) | BC addition amount (g) |
| --- | --- | --- | --- | --- | --- | --- |
| MFBX/Y 300 | 300 | 10 | 2.5 | 4:1 | 12.5 | 5 |
| MFBX/Y 400 | 400 | 10 | 2.5 | 4:1 | 12.5 | 5 |
| MFBX/Y 500 | 500 | 10 | 2.5 | 4:1 | 12.5 | 5 |
| MFBX/Y700 | 700 | 10 | 2.5 | 4:1 | 12.5 | 5 |
| MFBX/Y 800 | 800 | 10 | 2.5 | 4:1 | 12.5 | 5 |
| MFBX/Y 900 | 900 | 10 | 2.5 | 4:1 | 12.5 | 5 |
| MFBX/Y 2：1 | 400 | 10 | 5 | 2:1 | 15 | 5 |
| MFBX/Y 3：1 | 400 | 10 | 3.4 | 3:1 | 13.4 | 5 |
| MFBX/Y 4：1 | 400 | 10 | 2.5 | 4:1 | 12.5 | 5 |
| MFBX/Y 1:1 | 400 | 10 | 10 | 1:1 | 20 | 5 |
| MFBX/Y 1:3 | 400 | 3.4 | 10 | 1:3 | 13.4 | 5 |
| MFBX/Y 1:4 | 400 | 2.5 | 10 | 1:4 | 12.5 | 5 |
| MFBX/Y 5:1 | 400 | 10 | 2 | 5:1 | 12 | 5 |
| MFBX/Y@1 | 400 | 10 | 2.5 | 4:1 | 12.5 | 1 |
| MFBX/Y@2.5 | 400 | 10 | 2.5 | 4:1 | 12.5 | 2.5 |
| MFBX/Y@5 | 400 | 10 | 2.5 | 4:1 | 12.5 | 5 |
| MFBX/Y@7 | 400 | 10 | 2.5 | 4:1 | 12.5 | 7 |
| MFBX/Y@10 | 400 | 10 | 2.5 | 4:1 | 12.5 | 10 |

Table S3 Elemental composition of MFBX biochar

| Element | Line Type | Weight (%) | Atomic (%) |
| --- | --- | --- | --- |
| C | K series | 47.41 | 67.33 |
| O | K series | 21.74 | 23.18 |
| Si | K series | 0.11 | 0.07 |
| Mn | K series | 6.30 | 1.96 |
| Fe | K series | 24.44 | 7.47 |
| Total | K series | 100 | 100 |

Table S4 Elemental composition of MFBY biochar

| Element | Line Type | Weight (%) | Atomic (%) |
| --- | --- | --- | --- |
| C | K series | 36.05 | 58.03 |
| O | K series | 23.61 | 28.17 |
| Si | K series | 0.35 | 0.24 |
| Mn | K series | 6.77 | 2.35 |
| Fe | K series | 32.77 | 11.20 |
| Total | K series | 100 | 100 |

Table S5 BET data for wheat straw

| Sample | specific surface area (m2/g) | Kong Rong (g/cm3) | Average pore size（nm) | Hole type |
| --- | --- | --- | --- | --- |
| BCX | 149.010 | 0.156 | 4.201 | mesoporous |
| Fe@BCX | 151.422 | 0.222 | 5.869 | mesoporous |
| MFB | 50.430 | 0.126 | 10.006 | mesoporous |
| MFBX | 155.268 | 0.204 | 5.264 | mesoporous |

Table S6 BET data for maize cobs

| Sample | specific surface area (m2/g) | Kong Rong (g/cm3) | Average pore size（nm) | Hole type |
| --- | --- | --- | --- | --- |
| BCY | 52.262 | 0.074 | 5.651 | mesoporous |
| Fe@BCY | 46.843 | 0.095 | 8.138 | mesoporous |
| MFB | 50.430 | 0.126 | 10.006 | mesoporous |
| MFBY | 152.453 | 0.188 | 4.932 | mesoporous |

Table S7 Adsorption of TPH by BC at different concentrations

|  | Quasi-first-order kinetics [Qt=1-exp(-k1t)] |  |  | Quasi-second-order dynamics [t/Qt = 1/(k2Qe2) + t/Qe] |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C0 mg/L | Qe mg/L | K1 (min-1) | R2 |  | C0 mg/L | Qe mg/L | K2 (g/min·m in-1) | R2 |
| 500 | 190.7 | 0.08317 | 0.9909 |  | 500 | 167.4 | 0.00287 | 0.97823 |
| 1000 | 413.2 | 0.08448 | 0.99283 |  | 1000 | 375.1 | 0.00137 | 0.97394 |
| 5000 | 2343.5 | 0.11586 | 0.95369 |  | 5000 | 2243 | 3.90553 | 0.98033 |
| 10000 | 4874 | 0.14272 | 0.91131 |  | 10000 | 4483 | 1.5825 | 0.98191 |

Table S8 Adsorption of TPH by MFBX at different concentrations

|  | Quasi-first-order kinetics |  |  | Quasi-first-order kinetics |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C0 mg/L | Qe mg/L | K1 (min-1) | R2 | C0 mg/L | Qe mg/L | K2 (g/min·m in-1) | R2 |
| 500 | 207.65 | 0.08514 | 0.98406 | 500 | 219.25 | 0.00292 | 0.9822 |
| 1000 | 379.7 | 0.08289 | 0.9673 | 1000 | 464.8 | 0.00144 | 0.9804 |
| 5000 | 2218 | 0.14549 | 0.9859 | 5000 | 2532.5 | 3.167 | 0.97451 |
| 10000 | 4683 | 0.18262 | 0.9986 | 10000 | 5188 | 1.5143 | 0.97976 |

Pour：BCX：Wheat straw biochar, MFBX: MnFe2O4@BCX

Table S9 Comparison of XPS results for fresh and used MFBX

| Elements and functional groups | fresh (%) | used (%) | change |
| --- | --- | --- | --- |
| Fe (Ⅱ) | 45.5 | 65.48 | 19.98↑ |
| Fe (Ⅲ) | 54.5 | 34.52 | 19.98↓ |
| Mn (Ⅱ) | 43.14 | 48.22 | 5.08↑ |
| Mn (Ⅲ) | 45.38 | 36.14 | 9.24↓ |
| Mn (Ⅳ) | 11.48 | 15.64 | 4.16↑ |

Table S10 Comparison of XPS results for fresh and used MFBY

| Elements and functional groups | Fresh (%) | Used (%) | change |
| --- | --- | --- | --- |
| Fe (Ⅱ) | 57.86 | 53.03 | 4.83↓ |
| Fe (Ⅲ) | 42.14 | 46.97 | 4.83↑ |
| Mn (Ⅱ) | 50.21 | 54.17 | 3.96↑ |
| Mn (Ⅲ) | 35.55 | 36.36 | 0.81↓ |
| Mn (Ⅳ) | 10.27 | 13.43 | 3.16↑ |

Fig. S1 Fitting of the adsorption kinetics of wheat straw biochar（BCX）

Fig. S2 Fitting of the adsorption kinetics for MnFe₂O₄@BCX (MFBX)

Pour：BCX：Wheat straw biochar, MFBX: MnFe2O4@BCX

Reference

- Siyu Xu , Liangtao Wen , Chen Yu  Song Li, Jingchun Tang，Activation of peroxymonosulfate by MnFe2O4@BC composite for bisphenol A Degradation: The coexisting of free-radical and non-radical pathway [J]. Chemical engineering journal.442 (2022),136250. https://doi.org/10.1016/j.cej.2022.136250

- Wang S, Wang J. Activation of peroxymonosulfate by sludge-derived biochar for the degradation of triclosan in water and wastewater [J]. Chemical Engineering Journal, 2019, 356: 350-8 https://doi.org/10.1016/j.cej.2018.09.062

- Y. Zhao, M. Song, Q. Cao, P. Sun, Y. Chen, F. Meng, The superoxide radicals’ production via persulfate activated with CuFe2O4@Biochar composites to promote the redox pairs cycling for efficient degradation of o-nitrochlorobenzene in soil, J Hazard Mater 400 (2020), 122887, https://doi.org/10.1016/j.jhazmat.2020.122887

- X. Zhou, L. Kong, Z. Jing, S. Wang, Y. Lai, M. Xie, L. Ma, Z. Feng, J. Zhan, Facile synthesis of superparamagnetic beta-CD-MnFe2O4 as a peroxymonosulfate activator for efficient removal of 2,4- dichlorophenol: structure, performance, and mechanism, J Hazard Mater 394 (2020), 122528, https://doi.org/10.1016/j.jhazmat.2020.122528

- Du J, Bao J, Liu Y, et al. Facile preparation of porous Mn/Fe3O4 cubes as peroxymonosulfate activating catalyst for effective bisphenol A degradation [J]. Chemical Engineering Journal, 2019,376: https://doi.org/10.1016/j.cej.2018.05.177

- Yang S, Gu H, Xie W, et al. Heterogeneous activation of persulfate by iron/manganese binary oxides for effective bisphenol A degradation [J]. Colloids and Surfaces A: Physicochemical and Engineering Aspects, 2024, 685: 133192. https://doi.org/10.1016/j.colsurfa.2024.133192

- Zhao L, Zhang J, Zong Y, et al. Novel insights into Co synergy and electron-transfer pathways during the oxidation of contaminants by Cu-OOSO3- in CuCo2Ox/peroxymonosulfate system [J].Journal of Environmental Chemical Engineering, 2023, 11(2): https://doi.org/10.1016/j.jece.2023.109594

- Hu F, Liu Y, Shi X, et al. Removal of organic contaminants by starch-derived porous carbon via peroxymonosulfate activation: The role of N doping and Fe/Mn loading [J]. Colloids and Surfaces A: Physicochemical and Engineering Aspects, 2022, 649: 12952 https://doi.org/10.1016/j.colsurfa.2022.129520

- Yang S, Gu H, Xie W, et al. Heterogeneous activation of persulfate by iron/manganese binary oxides for effective bisphenol A degradation [J]. Colloids and Surfaces A: Physicochemical and Engineering Aspects, 2024, 685: 133192. https://doi.org/10.1016/j.colsurfa.2024.133192

- Xin J, Liu Y, Niu L, et al. Three-dimensional porous CuFe2O4 for visible-light-driven peroxymonosulfate activation with superior performance for the degradation of tetracycline hydrochloride [J]. Chemical Engineering Journal, 2022, 445: 13661 https://doi.org/10.1016/j.cej.2022.136616