Self-assembly Strategy for Reducing Non-specific Adsorption on Substrates and Application for Quantitative Immunoassay

Yanbing Lv1,2, Man Zhao1, Jinjin Fan1, Ruili Wu1*, Yanxia Xu1, Jinjie Li1, Ning Li1, Huaibin Shen1, Fang Guo2*, and Lin Song Li1*

1Key Lab for Special Functional Materials of Ministry of Education, and School of Materials, Henan University, Kaifeng, 475004, China

2School of Chemistry, Liaoning University, Shenyang, 110036, China

*Correspondence: wrl0378@henu.edu.cn, fguo@lnu.edu.cn, and lsli@henu.edu.cn.

S1. Material and methods

1.1 Reagents and instruments.

TritonX-100, calf serum, bovine serum albumin (BSA), casein, poly(diallyldimethylammoniumchloride) (PDDA), and poly(styrene sulfonic acid) sodium salt (PSS) were purchased from Sigma-Aldrich. NaOH, HCl, KCl, NaCl, NaHCO3, Na2CO3, Na2HPO4, KH2PO4, H3BO3, Na2B4O7·10H2O, sodium dodecyl sulfate (SDS), and sodium dodecyl sulfate (SLS) were purchased from Shanghai Hushi Ltd. 2-[4-(2-Hydroxyethyl)-1-piperazinyl]ethanesulfonic acid (Hepes), Tris(hydroxymethyl)aminoethane (Tris), and Tween-20 were purchased from Shanghai Sangon Ltd (Shanghai, China). Concentrated sulfuric acid (H2SO4, 98%) and hydrogen peroxide (H2O2, 30%) were obtained from Beijing Chemical Reagent Ltd (Beijing, China). N-Hydroxysulfosuccinimide (sulfo-NHS) and 1-ethyl-3-(3-(dimethylamino) propyl) carbodiimide (EDC) were purchased from Thermo Fisher Scientific (USA). meso-tetra(4-sulfonatophenyl)porphine dihydrochloride (sulfonated porphyrin or TSPP) was purchased from Frontier Scientific. Mouse anti-CRP monoclonal capture antibody (McCRP1), mouse anti-CRP monoclonal detection antibody (McCRP2), and CRP antigen were obtained from HyTest Ltd.

Photoluminescence (PL) spectra were measured by JY HORIBA FluoroLog-3. AFM images were collected by atomic force microscopy (Dimension icon, Bruker). The sizes and zeta potential of QDs and the QD-antibodies probes were recorded using dynamic light scattering (Nano-ZS, Malvern Instruments, UK). The fluorescence microscope images were captured with a positive fluorescence microscope (MSHOT). The zeta potential of the glass substrate surface was tested by a solid-state zeta potential meter (Surpass 3) from Anton Paar Ltd. Purified water (18.2 mΩ) was used by the Mill-Q system in all experiments. The self-built fluorescence detection system based on our requirements and design was customized by Shanghai Ruhai Tech. Ltd.

1.2 Synthesis of hydrophobic CdSe/ZnS QDs.

The synthesis of CdSe/ZnS core/shell QDs (PL = 613 nm) was prepared according to the previous literature from our group [1]. Precursor Preparation: Se (0.188 g, 2.4 mmol), OA (2 g, 7.2 mmol), and 17.5 mL of ODE were loaded in a 50 mL three-neck flask and degassed, the mixture was heated to 100 ºC then maintained for 20 min and subsequently heated to 220 ºC then maintained for 3 h. Zinc precursor was prepared by dissolving Zn(Ac)2 (0.8 g, 4.4 mmol) in OA (10.83 g, 38.98 mmol) and 43.20 mL of ODE, and heating to 120 ºC under a vacuum for 2 h.

Synthesis of CdSe QDs: A mixture (4 g in total) of CdO (0.0154 g, 0.12 mmol), oleic acid (0.36 mmol), and ODE was loaded in a 25 mL three-neck flask and heated to 240 ºC under nitrogen flow to obtain a clear colorless solution. When it was heated to 280 ºC, 2 mL (0.24 mmol) Se stock solution was injected into the flask. Aliquots were taken at different time intervals, UV-vis and PL spectra were recorded for each aliquot. When the targeted size of nanocrystals was obtained, the reaction mixture was allowed to cool down to room temperature.

Synthesis of CdSe/ZnS QDs: 3 mL of ODE and 1.0 g of OA were loaded into a 25 mL reaction vessel. The CdSe QDs in hexanes (2.7×10−7 mol) were added, and the system was maintained at 100 ºC under N2 flow for 30 min to remove hexanes and other undesired materials. The solution was heated to 160 ºC under N2 flow for the growth of ZnS shell. At 180, 200, 220, 240, and 250 ºC, the Zn and S precursors (Zn precursor was prepared by dissolving ZnO in the mixture of OA and ODE at 310 ºC while S precursor by dissolving sulfur in ODE at 150 ºC) with calculated amounts were added, respectively. After the reaction was completed, the temperature was cooled down to room temperature.

1.3 Synthesis of corresponding aqueous QDs.

The PMAH have hydrophobic chains available for anchoring the hydrophobic CdSe/ZnS QDs and free carboxylic acid groups available for further surface modification [2]. The hydrophobic QDs and PMAH bound to each other via the phase-transfer stem to form PMAH-stabilized PL QDs. First, 3.61 g of PMAH (0.2 mmol) was dissolved in 20 mL of chloroform. Subsequently, 2 mL of CdSe/ZnS QDs (0.04 mmol, dispersed in chloroform) was added to the PMAH solution, which was then stirred for 24 h (room temperature) in a closed container. The chloroform was then slowly evaporated by rotary evaporation, and the remaining QD film was dispersed in ammonia water (pH 9.0) with sonication. The solutions were passed through a 0.22 μm Nylon syringe filter, washed, and then centrifuged four times at 20,000 g to remove excess oligomers.

1.4 Preparation QD-antibody probe.

The aqueous QDs were conjugated with monoclonal antibody according to the following protocol [3]: First, 150 μL of PMAH-coated aqueous QDs (5 mg/mL) dissolved in 750 μL sodium borate buffer (5 mM, pH 7.2, BS buffer), then it was mixed with 50 μL of suflo-NHS (49 mg/mL in 5 mM BS buffer, pH 7.2) and 50 μL of EDC (17.36 mg/mL in 5 mM MES buffer, pH 5.5). The mixture was activated to react at 4°C for 5 min under ultrasonic. Therewith, the superstratum clear-solution was abandoned after centrifuge separation at 20,000 rpm and 4°C for 30 min. Second, the CRP detection antibodies were added into the QDs with dissolving in 400 μL BS buffer (5 mM, pH 9.0) and incubated at 37°C for 2 h. Afterwards, the mixture was blocked by 1% BSA solution and incubated at 37°C for 30 min. Finally, the probe was washed by 5 mM BS buffer (pH 8.0) under centrifugation. The QDs-mAb was stored in 50 μL BS solution (5 mM, pH 8.0) for future use.

1.4 Preparation of the PDDA, PDDA-glass, and PSS-glass substrates.

Glass substrates (1.5×1.25 cm) were cleaned with water and then dipped into the piranha solution (H2SO4:H2O2 = 7:3) for 30 min [4]. To prepare the PDDA-glass substrate, the glass substrates were treated with a solution of poly(diallyldimethylammoniumchloride) (PDDA, 20 wt%) for 10 min after blowing dry with nitrogen. Then, the PDDA-glass substrates were rinsed with deionized water to remove the residual solution. To prepare the PDDA and PSS-glass substrates, the glass substrates were first dried with nitrogen and then treated with a solution of PDDA (20 wt%) for 10 min. Before the next immersion process, any remaining solution was removed with deionized water. Then the glass substrates were treated with a solution of PSS (2.0 mg/mL) for 10 min. Afterward, the PDDA- and PSS-glass substrates were rinsed with deionized water to remove any residual solution. To prepare the PSS-glass substrate (one layer), we dried the glass substrate with nitrogen, and then the glass substrate was treated with a solution of PSS (2.0 mg/mL) for 10 min. Afterward, the PSS-glass substrates were rinsed with deionized water to remove any remaining residual solution. After blowing dry with nitrogen, the three kinds glass substrates were dipped into the QD solution (1.0 mg/mL, pH = 8) for 10 min to evaluate adsorption.

1.5 Layer assembly of the PSS-glass substrate.

Glass substrates (1.5×1.25 cm) were cleaned with water and then dipped into the piranha solution (H2SO4:H2O2 = 7:3) for 30 min. In this study, we simulated the LBL assembly scheme using the following methods. After blowing dry with nitrogen, the glass substrates were treated with a solution of PSS (2.0 mg/mL) containing 0.5 mol/L of NaCl for 10 min [5]. Then, we removed any residual solution with deionized water and completed the immersion in order according to the corresponding number of layers (1~6 layers). After 15 min of annealing at 140°C, the PSS-glass substrates were dipped into the QD solution (1.0 mg/mL, pH = 8) for 10 min to evaluate adsorption.

1.6 Layer assembly of the TSPP-glass substrate.

Glass substrates (1.5×1.25 cm) were cleaned with water and then dipped into piranha solution (H2SO4:H2O2 = 7:3) for 30 min. After blowing dry with nitrogen, the glass substrates were treated with a TSPP solution (2.0 mg/mL in PBS buffer) for 10 min. We then rinsed off any residual solution with deionized water and then completed the immersion process in order according to the corresponding number of layers (1~5 layers). After 15 min of annealing at 140°C, the TSPP-glass substrates were dipped into the QD solution (1.0 mg/mL, pH = 8) for 10 min to evaluate the adsorption.

1.7 Layer assembly of the PSS and TSPP-glass substrates.

Glass substrates (1.5×1.25 cm) were cleaned with water and then dipped into the piranha solution (H2SO4:H2O2 = 7:3) for 30 min. After blowing dry with nitrogen, the glass substrates were treated with the TSPP solution for 10 min two times. We again rinsed off any residual solution with deionized water, and after annealing for 15 min at 140°C, the TSPP-glass substrates were dipped into the PSS solution for 10 min to create four layers. Finally, the TSPP and PSS-glass substrates were dipped into the QD solution (1.0 mg/mL, pH = 8) for 10 min to evaluate the adsorption after 15 min of annealing at 140°C.

1.8 Preparation of the glass substrate biochips.

The prepared PSS-glass substrate biochips (TSPP-glass substrate biochips or TSPP and PSS-glass substrate biochips) were subjected to a quantum dot-based fluorescence-linked immunosorbent assay (QD-FLISA), and the process was completed as follows. As shown in Scheme 1, the McCRP1 antibodies (4.8 mg/mL) were diluted with a carbonate-bicarbonate buffer (0.05 M, pH 9.6, CB buffer) in a centrifuge tube, and the PSS-glass substrates were incubated at 37°C overnight. Then, the excess binding sites on the PSS-glass substrates were blocked with bovine serum albumin (BSA, 0.5 wt%) in 0.01 M of PBS (pH 7.4), and incubated overnight at 4°C after removing the excess antibodies by washing the substrate with a washing buffer (10 mM PBS containing 0.05% Tween-20, PBS-T). The PSS-glass substrate biochips were prepared by allowing them to dry after dried in a constant temperature humidity chamber for 24 h, and then stored at 4°C until use. The standard solution was prepared by diluting the CRP stock solution (10 μg/mL) with final concentrations of 1, 5, 10, 50, 100, 500, and 1,000 ng/mL with the sample buffer (10% calf serum (v/v) in 0.01 M PBS) in a centrifuge tube. The PSS-glass substrate biochips were incubated at 37°C for 30 min, and then the biochips were washed with the washing buffer (PBS-T). For subsequent operations, the QD-antibody probes were incubated at 37°C for 30 min on the various PSS-glass substrate biochips, and then the PL intensity of each biochip was measured after washing and drying.

The limit of detection (LOD) is one of the key parameters for each protein detection. Here we tested the negative control samples 20 times at the same time, the LOD was calculated as 3 times the ratio of the standard deviation (SD) of negative control samples to the slope of the low-concentration calibration plot (LOD = 3SD/slope) [6.7].

S2. Results and discussion

2.1 Surface modification of glass substrate.

Fig. S1. Fluorescence intensity of glass substrate biochips for 0 ng/mL of CRP antigen detection (red line) and blank glass substrate (black line), inset: the corresponding fluorescence microscopy images of glass substrate for 0 ng/mL CRP antigen (above) and blank glass substrate (below).

2.2 Characterization of aqueous QDs and QD-antibody probe.

As shown in Fig. S2, the fluorescence spectra of the aqueous QDs and QD-antibodies probe are collected, which expresses that the fluorescence peaks keep symmetrical and have almost no changes on peak position and peak shape, and the fluorescence recovery of both QD-antibodies probe keep 85% in Fig. S2a. After coupling the CRP antibody, the hydrodynamic size of the aqueous QDs increases from 57.9 nm to 97.5 nm in Fig. S2b, which means the CRP antibodies are successfully coupled to the aqueous QDs. In Fig. S2c, the zeta potentials of aqueous QDs show a surface charge of -46.1 mV, which has a certain increase after coupling antibodies, and those of both QDs and QDs-antibody still locate the stable range for stabilized colloids (> +30 mV or < -30 mV). In summary, the QD-antibodies probe was successfully prepared, which was used as fluorescent probes for quantitative detection of CRP antigens.

Fig. S2. Photoluminescent spectra (a), dynamic light scattering (b), zeta potential (c) of the aqueous QDs in water (black) and QD-antibodies probe (red).

2.3 Optimization of glass substrate conditions using PSS treatment.

Fig. S3. Atomic force microscopy (AFM) image of glass substrates with different PSS layers, including 1 layer PSS film (a), 3 layers PSS films (b), 4 layers PSS films (c), and 4 layers PSS containing 0.5 mol/L NaCl solution (d).

Fig. S4. Absorption spectra of glass substrates with 4 layers PSS (a) and 4 layers PSS annealed at 140 ºC (b).

Next, we evaluated the stability of the PSS-treated glass substrate after annealing at high-temperature in Fig. S4. The absorption peak at 283 nm on PSS-treated glass substrate was observed, which assigned to the conjugated double bond in the benzene ring. Among them, the absorption peak at 283 nm of the PSS-treated glass substrate without annealing treatment decreases obviously after dipping in aqueous solution for 24 h. However, the absorption peak of PSS-treated glass substrate after annealing treatment is almost unchanged. The above results show that the PSS can get better fixation effect on glass substrate after annealing high-temperature.

2.4 Optimization of glass substrate conditions using TSPP treatment.

Fig. S5. Fluorescence spectra (a) and corresponding fluorescence intensity (b) of different TSPP layers of treated glass substrates for aqueous quantum dot adsorption.

2.5 Optimization of glass substrate conditions using TSPP and PSS treatment.

Fig. S6. Fluorescence spectra (a) and corresponding fluorescence intensity (b) of PSS-glass substrate, TSPP-glass substrate, and TSPP and PSS-glass substrate for aqueous quantum dot adsorption.

2.6 Optimization of coating conditions on PSS-glass substrate.

The coating effect of the captured antibody and (Sheep-anti-Mouse) secondary antibody under these three methods were evaluated respectively, and the results were shown in Fig. S7 (the PL characteristic peak was 570 nm under 512 nm excitation). As shown in Fig. S7, the blank glass substrate could capture the McCRP1 antibody, and the coating effect of the McCRP1 antibody was not affected after being blocked with BSA. The PSS-treated glass substrate (SO3-rich surface) had a better ability to capture antibodies than the untreated glass substrate. Therefore, the SO3-rich surface has an improved ability to bind the captured antibody.

Fig. S7. The fluorescence spectra of captured McCRP1 antibody by (Sheep-anti-Mouse) secondary antibody on different glass substrates, the concentration of captured McCRP1 antibody is 5 μg/mL.

To determine the capture effect of antibodies, we explored coating McCRP1 antibody with different concentrations in Fig. S8. In this test, the fluorescence intensity ratio of high concentration (1,000 ng/mL) to negative (0 ng/mL) was tested. As shown in Fig. S8, it had a better ratio of 1,000/0 ng/mL when the concentration of coating McCRP1 antibody is 5 μg/mL (20.74). Subsequently, the fluorescence intensity of high concentration (1,000 ng/mL) no longer increased significantly, while that of the negative increased slightly.

Fig. S8. Optimization of coating McCRP1 antibodies concentration of PSS-glass substrate biochip.

2.7 Optimization of coating conditions on TSPP-glass substrate.

Fig. S9. Optimization to capture McCRP1 antibodies for TSPP-glass substrate biochip (a), and corresponding fluorescence intensity (b).

Since the TSPP-glass substrate inhibited the adsorption of aqueous QDs significantly, we optimized the concentration of the coating McCRP1 antibodies on the glass substrate biochips and selected three concentrations of 5 μg/mL, 10 μg/mL, 20 μg/mL, and 30 μg/mL for coating on the glass substrate, respectively. The QDs-FLISA was performed for CRP antigen at 0 ng/mL (negative sample) and 1,000 ng/mL, respectively. As shown in Fig. S10, the fluorescence intensity of high concentration (1,000 ng/mL) CRP antigen could be increased by increasing the concentration of CRP-coated antibody on the TSPP-glass substrate, when the concentration of McCRP1 antibody increases to 20 μg/mL under the same CPR concentration, it had a better ratio of 1,000/0 ng/mL (8.77).

Fig. S10. Optimization of coating McCRP1 antibodies concentration of TSPP-glass substrate biochip.

## References

1	Shen H, Wang H, Tang Z, Niu J, Lou S, Du Z, Li LS. High quality synthesis of monodisperse zinc-blende CdSe and CdSe/ZnS nanocrystals with a phosphine-free method. CrystEngComm 2009;11:1733-8.

2	Liu D, Wu F, Zhou C, Shen H, Yuan H, Du Z, Ma L, Li LS. Multiplexed immunoassay biosensor for the detection of serum biomarkers—β-HCG and AFP of down syndrome based on photoluminescent water-soluble CdSe/ZnS quantum dots. Sens. Actuators B 2013;186:235-43.

3	Lv Y, Wu R, Feng K, Li J, Mao Q, Yuan H, Shen H, Chai X, Li LS. Highly sensitive and accurate detection of C-reactive protein by CdSe/ZnS quantum dot-based fluorescence-linked immunosorbent assay. J. Nanobiotech. 2017;15:35.

4	Song YJ, Zhang YQ, Bernard PE, Reuben JM, Ueno NT, Arilinghaus RB, Zu YL, Qin LD. Multiplexed volumetric bar-chart chip for point-of-care diagnostics. Nat. Commun. 2012;3:1283.

5	Lin YW, Tseng WL, Chang HT. Using a layer-by-layer assembly technique to fabricate multicolored-light-emitting films of CdSe@CdS and CdTe quantum dots. Adv. Mater. 2006;18:1381-6.

6	Armbruster DA, Pry T. Limit of blank, limit of detection and limit of quantitation. Clin. biochem. Rev. 2008;29:S49-52.

7	Xu DD, Deng YL, Li CY, Lin Y, Tang HW. Metal-enhanced fluorescent dye-doped silica nanoparticles and magnetic separation: a sensitive platform for one-step fluorescence detection of prostate specific antigen. Biosens. Bioelectron. 2017;87:881-7.