Journal: Journal of Nanobiotechnology

Manuscript ID: JNAN-D-21-00621

Title: Self-assembly Strategy for Reducing Non-specific Adsorption on Substrates and Application for Quantitative Immunoassay

Author(s): Yanbing Lv; Man Zhao; Jinjin Fan; Ruili Wu; Yanxia Xu; Jinjie Li; Ning Li; Huaibin Shen; Fang Guo; Lin Song Li

Reviewer reports:

Reviewer #1: The manuscript by Lv et al reported a self-assembly based methods to reduce non-specific protein absorptions in biosensors, which is realized by modifying the substrate surface with a dense layer of negatively charged film via electrostatic absorption. The authors claimed that the coated biochips based on glass slides have an LOD as low as 0.69 ng/mL for quantitative CRP detection. However, there're several major drawbacks in the current version of this manuscript that must be solved before any further considerations.

1. Will the SO3-rich surface affect the binding of target proteins?

Response: Thanks so much for your suggestion. At present, the captured antibodies were immobilized on substrates based on intermolecular forces (i.e. electrostatic adsorption, hydrophilic and hydrophobic) [1]. To evaluate the effect of SO3-rich surface on glass substrates, the following experiments were carried out: (1) the McCRP1 antibody was captured on a blank glass substrate after piranha solution (H2SO4:H2O2=7:3) treatment; (2) after coated with McCRP1 antibody, the glass substrate was blocked with BSA (0.5 wt%); (3) the PSS-treated glass substrate (SO3-rich surface) were coated with McCRP1 antibody and then blocked with BSA (0.5 wt%). The coating effect of the captured antibody and (Sheep-anti-Mouse) secondary antibody under these three methods were evaluated respectively, and the results were shown in Fig. R1 (the PL characteristic peak was 570 nm under 512 nm excitation). As shown in Fig. R1, the blank glass substrate could capture the McCRP1 antibody, and the coating effect of the McCRP1 antibody was not affected after being blocked with BSA. The PSS-treated glass substrate (SO3-rich surface) had a better ability to capture antibodies than the untreated glass substrate. Therefore, the SO3-rich surface has an improved ability to bind the captured antibody. The related modifications are presented in the Supporting Information.

Fig. R1. The fluorescence spectra of captured McCRP1 antibody by (Sheep-anti-Mouse) secondary antibody on different glass substrates, the concentration of captured McCRP1 antibody is 5 μg/mL.

2. The descriptions regarding the preparation of the supramolecular coatings are too ambiguous and need to be expanded.

Response: The preparation method of the supramolecular coatings was described in detail and related modifications are presented in the Supporting Information. Thanks so much for your suggestion.

3. The authors claimed that treatment with NaCl solution and subsequent annealing at high-temperature could facilitate the immobilization of PSS on the glass surface but lacked the direct evidence.

Response: Thanks so much for your suggestion. Firstly, the root-mean-square (RMS) roughness gradually decreased with the increase of the number of PSS layers in the AFM image (Fig. S3). To further improve the immobilization efficiency and the densification of PSS film, we modulate the effect of PSS film formation by changing the ionic strength of the PSS solution, such as adding a certain concentration of inorganic salt ions to it [2, 3]. When the PSS solution contained 0.5 mol/L NaCl, the density of PSS film on the surface of glass substrate was increased in Fig. R2, indicating that the addition of NaCl solution improved the film-forming performance of PSS on the glass substrate.

Fig. R2. Atomic force microscopy (AFM) image of glass substrates with 4 layers PSS (a) and 4 layers PSS containing 0.5 mol/L NaCl solution (b).

Next, we evaluated the stability of the PSS-treated glass substrate after annealing at high-temperature in Fig. R3. The absorption peak at 283 nm on PSS-treated glass substrate was observed, which was assigned to the conjugated double bond in the benzene ring. Among them, the absorption peak at 283 nm of the PSS-treated glass substrate without annealing treatment decreases obviously after dipping in an aqueous solution for 24 h. However, the absorption peak of PSS-treated glass substrate after annealing treatment is almost unchanged. The above results show that the PSS can get a better fixation effect on glass substrate after annealing high-temperature.

Fig. R3. Absorption spectra of glass substrates with 4 layers PSS (a) and 4 layers PSS annealed at 140ºC (b).

Finally, the microscopic observations of a water droplet on three kinds of glass substrates were shown in Fig. R4. The results show that the contact angle of the PSS-treated glass substrate was 43.3°, slightly increasing to 45.6° of the PSS-treated glass substrate after dipping in aqueous solution for 24 h, which showed that the PSS was immobilized to the glass substrate and has high stability. In conclusion, treatment with NaCl solution and subsequent annealing at high-temperature could facilitate the immobilization of PSS on the glass surface.

Figure R4. Microscopic observations of a water droplet on three kinds of glass substrate with different wettability: blank glass substrates (a), PSS-treated glass substrates (b), and PSS-treated glass substrates after dipping in water (c).

4. This manuscript is very poorly written with many redundancies and grammatical flaws, which makes this manuscript almost incomprehensible. Also, this manuscript lacks any in-depth discussion on the material preparation process and biosensing mechanism.
Response: Thanks so much for your suggestion. Related material preparation processes are provided and biosensing mechanisms are discussed in depth. We have modified it in the Revised Manuscript. Besides, the manuscript has been revised and retouched by LetPub.

Reference:

- Trilling A K, Beekwildera J, Zuilhof H. Antibody orientation on biosensor surfaces: a minireview. Analyst 2013;138:1619.

- Decher, G. Fuzzy nanoassemblies: toward layered polymeric multicomposites. Science 1997;277:1232-7.

- McAloney RA, Sinyor M, Dudnik V, Goh MC. Atomic force microscopy studies of salt effects on polyelectrolyte multilayer film morphology. Langmuir 2001;17:6655-63.

Reviewer #2: The authors conducted a study about reducing non-specific adsorption by functionalizing the glass chip surface via self-assembly of a layer of dense negatively charged film, so as to improve the detection sensitivity which is based on quantum dot fluorescence immunosorbent assay.
The authors started off by identifying the root cause of non-specific binding of quantum dots (QD) by functionalizing the glass substrate surface with negatively charged and positively charged polymers. Realizing the negatively charged surface is beneficial, following that, they developed and optimized three different ways of modification via PSS, TSPP and PSS together with TSPP. Then using CRP detection as a proof-of-concept, they developed and optimized a sandwich type quantum dot fluorescence immunosorbent assay that is capable of CRP detection LOD of 1.26 ng/mL, 5.17 ng/mL, and 0.69 ng/mL, respectively. Additionally, they demonstrated high specify of this type of biochip capable of differentiating target CRP molecules among other noises, and a recovery study where known concentration of target CRP was spiked in samples.

The group (Li, Lin Song) has published a few papers finding applications of CdSe/Zn QD biosensing area and improving the sensing performance, for example, procalcitonin detection work published in Chemistry Letters in 2021, cardiac troponin I detection work published in Taylor & Francis in 2020, and CRP detection work published in Journal of Nanobiotechnology in 2017. This work is mainly focusing on glass substrate surface modification to prevent nonspecific CdSe/Zn QD or CdSe/Zn QD conjugates.

Overall, the experiments are well designed and the results they obtained are logically sound to support their claim of the development of a surface modification method that can effectively reduce non-specific binding. Nevertheless, some recommended edits or improvements to get this work to publication are listed below.

1. English
There is large big room for improvement in written English. Though the messages that the authors wanted to express are largely delivered in the manuscript, there are numerous grammatical and structural errors, some of which are noted in the review comments. I can appreciate the difficulty of writing a scientific paper in a second language since English is not the authors' native language, but I'd suggest they seek the assistance from commercial scientific editing services so that the goals, results and discussions of this study are clear to the audience.
Response: Thank you so much for your suggestion. We have polished our manuscript extensively and tried our best to correct the grammatical, styling, and mistyped errors in our revised manuscript. We tried to remove some redundant wordings in the abstract and discussion, adjust the flow of the result section, and added the future perspective in the conclusion. The figure legends were modified to eliminate some self-explanation issues, and hopefully, we can provide a better illustration of our research work. In addition, this manuscript was copy edited for English language by LetPub, with regard to grammar, punctuation, spelling, and clarity.

2. The authors are claiming better detection sensitivity by reducing non-specific binding. What's the detection curve like without glass substrate surface modification? In this case, even if the zero-target background signal is high, by subtracting this background signal from the signal generated upon target binding, it's still possible to achieve a high detection sensitivity.
Response: Thank you so much for your suggestion. The blank glass substrates produced obvious non-specific adsorption during the detection, which affects the overall performance of the biosensors, such as decreasing detection specificity, reproducibility, and sensitivity [1, 2]. Therefore, we could not accurately distinguish antibody-antigen specific binding or non-specific adsorption in this assay. As shown in Fig. R1, the McCRP1 antibody was coated on the blank glass substrate chip and found that the obvious fluorescence was generated on this biochip without gradient growth trend. It is necessary to modify the surface of the glass substrate to inhibit non-specific adsorption, so that the standard curve established by us can have scientific significance.

Fig. R1. The photographs of blank glass substrates for different concentration of CRP antigens detection results under 365 nm ultraviolet light.

3. It'd have been better to be described why this method is better than methods of preventing non-specific binding, or by conducting a side-by-side comparison study.
Response: Thank you so much for your suggestion. As shown in Fig. S1, the black glass substrate biochip showed significant non-specific adsorption for 0 ng/mL CRP antigen detection (negative sample). In the early stage of experiment exploration, various influencing factors in the process of glass substrate treatment were explored, and it was found that the blank glass substrate by piranha solution (H2SO4:H2O2=7:3) washing had certain adsorption on aqueous QDs. Therefore, the focus of our research is to make the glass substrate produce no obvious non-specific adsorption on aqueous QDs by processing the substrate, so as to ensure the follow-up detection experiments. The aqueous QDs with a large number of negatively charged (carboxyl functional groups, -COOH) on the surface, we consider whether there is an effect between positive and negative charges. To verify this conjecture, the glass substrate was treated with negative charges by the Charge Gun (Milty Pro Zerostat 3), and then the QD-FLISA was performed. As shown in Fig. R2, it was found that the fluorescence intensity of CRP assay increased with the increase of antigen concentration after the negative charge-glass substrate biochip. Therefore, the treatment of negative charge can indeed make the substrate suitable for in vitro diagnostic, and it is feasible to use PSS to treat the negative charge of the substrate.

Fig. R2. The photoluminescence spectra for determination of CRP antigens by negative charge- glass substrate biochip.

4. Authors claim a new surface functionalization method to reduce non-specific binding by enhancing "negative charge" of the glass substrate surface. It's worth to make it clear that, only applies to negatively charged Ab-QD complex. By theory, it will enhance non-specific binding of positively charged QD conjugated molecules, if any.
Response: We agree with the reviewer's suggestion that the treatment of surface negative charge reduces the interference between the glass substrate and aqueous QDs or QD-antibody probes, which is convenient for us to use aqueous QDs as fluorescent probes to detect the substrate in the later stage. Some detection materials we commonly use, such as colloidal gold and organic fluorescent dyes, all have a large amount of negative charge on the surface, so this scheme has certain applicability for materials with the negative charge on the surface, which is of sufficient significance for in vitro diagnostic. Thank you so much for your suggestion.

5. Generally missing info of the mechanism how these layers of molecules bind to each other. For example, what's the affinity between glass substrate and PSS, between glass substrate and TSPP, between Mouse anti-CRP monoclonal capture antibody, etc. And are the adhesions strong enough to stay stable upon rinsing process?
Response: Thank you so much for your suggestion. At present, the captured antibodies were immobilized on substrates based on intermolecular forces (i.e. electrostatic adsorption, hydrophilic and hydrophobic) [3]. The PSS layer was treated on the glass substrate by self-assembly, and then the CRP antibody was captured. The coating effect of the captured antibody and (Sheep-anti-Mouse) secondary antibody under these three methods were evaluated respectively, and the results were shown in Fig. R3 (the PL characteristic peak was 570 nm under 512 nm excitation). As shown in Fig. R3, the blank glass substrate could capture the McCRP1 antibody, and the coating effect of the McCRP1 antibody was not affected after being blocked with BSA. The PSS-treated glass substrate had better ability to capture antibodies than the untreated glass substrate, and the successfully prepared PSS-treated glass substrate biochip is still active after dipping in aqueous solution for 24 h.

Fig. R3. The fluorescence spectra of captured McCRP1 antibody by (Sheep-anti-Mouse) secondary antibody on different glass substrates, the concentration of captured McCRP1 antibody is 5 μg/mL.

6. In general, there is a lack of explanation of replicates and statistical methods used in the study. For example, in Fig 1, Fig 2, Fig 4, Fig 5, Fig 6, Table 2, Fig S4, Fig S5, Fig S6 and Fig S7, what's the replicates number (namely, n)? Is it biological or technical replicates? What's the statistical analysis results?
Response: Thank you so much for your suggestion. In CRP assay, each concentration of CRP antigen was tested three time by glass substrates biochip, namely three parallel experiments, which was biological replication; each glass substrate was tested at 6 points in different positions (as shown in Scheme 1), which was technical replication. Next, we averaged the fluorescence intensity of 6 points on each glass substrate and then averaged the results of three parallel experiments to calculate the deviation (n=3). The related modifications are presented in the Revised Manuscript.

7. In Fig 1, 2, 4, 5, 6, 7, in which wavelength are the PL intensity counts collected? Are there peak shifts upon binding of a serial of entities onto the chip? What is the excitation wavelength used in this study where applicable?
Response: Thank you so much for your suggestion. The excitation wavelength of aqueous QDs used in this paper is 613 nm and the emission is 405 nm, which has been supplemented in the Revised Manuscript. The fluorescence peaks of aqueous QDs did not shift after binding of a serial of entities onto the chip in Fig. R4.

Fig. R4. The fluorescence spectra of aqueous QDs (blank line) and QDs binding of entities onto the chip (red line).

8. In Fig 7, only one set of data is presented, so the conclusion doesn't sound convincing. Suggest repeating and getting another two set of data. Also, for further real world application, are concentrations of interfering "noises" relevant to the concentration level in the real world scenario? If not, how high background noises are there if experiments are done with concentrations relevant to real world case?
Response: Thank you so much for your suggestion. In cross-reaction and specificity assay, each condition was tested three times by glass substrates biochip, the revised picture (Fig. 7) is in the Revised Manuscript. In this experiment, the interference noise is a fixed value, and the test value of the instrument on the glass substrate is about ~1000. During the test, the background fluorescence signal (signal-to-noise ratio) is deducted.

9. Fig 4 (a), In light of steric hindrance, it doesn't necessarily mean that higher coverage of capturing antibody on the chip surface is better for analyte detection (CRP in this case). Better optimization strategy is to detect a certain concentration of analyte with various coverage of capturing antibody to see which works best.
Response: As shown in Fig. 4a, different coating methods were explored, and the optimization result was that the glass substrates of coating antibodies captured better overnight. To determine the capture effect of antibodies, we explored coating McCRP1 antibody with different concentrations in Fig. R5. In this test, the fluorescence intensity ratio of high concentration (1,000 ng/mL) to negative (0 ng/mL) was tested. As shown in Fig. R5, it had a better ratio of 1,000/0 ng/mL when the concentration of coating McCRP1 antibody is 5 μg/mL (20.74). Subsequently, the fluorescence intensity of high concentration (1,000 ng/mL) no longer increased significantly, while that of the negative increased slightly. The related modifications are presented in the Supporting Information. Thank you so much for your suggestion.

Fig. R5. Optimization of coating McCRP1 antibodies concentration of PSS-glass substrate biochip.

10. Authors conducted optimization study by introducing the factors of heating and NaCl addition when functionalizing glass substrate with PSS, but not TSPP or PSS and TSPP co-functionalization study. Has similar work been done to the latter? How did it work?
Response: Thank you so much for your suggestion. To further improve the immobilization efficiency and the densification of PSS film, we modulate the effect of PSS film formation by changing the ionic strength of the PSS solution, such as adding a certain concentration of inorganic salt ions to it [4, 5]. When the PSS solution contained 0.5 mol/L NaCl, the density of PSS film on the surface of glass substrate was increased in Fig. R6, indicating that the addition of NaCl solution made the film-forming property of PSS better on the glass substrate.

Fig. R6. Atomic force microscopy (AFM) image of glass substrates with 4 layers PSS (a) and 4 layers PSS containing 0.5 mol/L NaCl solution (b).

Subsequently, we evaluated the stability of the PSS-treated glass substrate after annealing at high-temperature in Fig. R7. The absorption peak at 283 nm on PSS-treated glass substrate was observed, which was assigned to the conjugated double bond in the benzene ring. Among them, the absorption peak at 283 nm of the PSS-treated glass substrate without annealing treatment decreases obviously after dipping in aqueous solution for 24 h. However, the absorption peak of PSS-treated glass substrate after annealing treatment is almost unchanged. The above results show that the PSS can get a better fixation effect on glass substrate after annealing high-temperature.

Fig. R7. Absorption spectra of glass substrates with 4 layers PSS (a) and 4 layers PSS annealed at 140 ºC (b).

However, TSPP has a good film-forming property on the glass substrate in Fig. 3, and then the TSPP-treated glass substrate was annealed. Since TSPP solution has a certain influence on the fluorescence intensity of aqueous QDs, the substrate was modified with TSPP and then treated with PSS to modify with the glass substrate. According to the result analysis, the detection performance of the TSPP and PSS-treated glass substrate is greatly improved. The related modifications are presented in the Supporting Information. Thank you so much for your suggestion.

11. In Fig S7, the graph is showing increasing McCRP1 antibody concentration up to 20 ug/mL can generate higher detection signal with the same CPR concentration. It's showing there's room to further improve detection sensitivity by increasing McCRP1 antibody concentrations.
Response: Thank you so much for your suggestion. It can be seen from Fig. R8 that the concentration of McCRP1 antibody increases to 20 μg/mL under the same CPR concentration, it had a better ratio of 1,000/0 ng/mL (8.77). With the increase of concentration of McCRP1 antibody, the increase of fluorescence intensity of high concentration almost leveled off. The related modifications are presented in the Supporting Information.

Fig. R8. Optimization of coating McCRP1 antibodies concentration of TSPP-glass substrate biochip.

12. Table 1, The conclusion is overstated by saying that "the sensitivity reported in this paper has been greatly improved compared to the different types of biosensors or biochips". Some studies where comparable or lower LOD of CRP detection was achieved are not listed in this table. For example, Hwang's study whose work was published in ACS Applied Materials & Interfaces in 2019, and Fakanya's study whose work was published in Biosensors in 2014.
Response: Thanks so much for your suggestion. Table 1 has been modified and relevant reference has been supplemented in the Revised Manuscript. Some common methods of biosensors and biochips have been added.

13. SLS is the abbreviation for sodium lauryl sulfate not sodium dodecyl sulfate. This mistake has occurred in several places in the manuscript.
Response: Thanks so much for your suggestion. We have modified it in the Revised Manuscript.

14. Related quantum dot studies can be referred and compared: Food Chemistry 355 (2021): 129443; Angewandte Chemie, 2021, 202108696; Advanced Materials, 2021, 2102054; Applied Nanoscience, 8(5), 1189-1196; Journal of Alloys and Compounds 783 (2019): 813-819.
Response: Thanks so much for your suggestion. The relevant references have been supplemented in the Revised Manuscript.

Overall, I think your experiments are well designed and the results are logically sound to support your claim of the development of a surface modification method by self-assembly strategy that can effectively reduce non-specific binding. Nevertheless, there are some edits or improvements recommended to get this work to final publication. I would be very glad to re-review the paper in greater depth once it has been edited.

Reference:

[1] Fontes CM, Achar RK, Joh DY, Ozer I, Bhattacharjee S, Hucknall A, Chilkoti A. Engineering the surface properties of a zwitterionic polymer brush to enable the simple fabrication of inkjet-printed point-of-care immunoassays. Langmuir 2019;35:1379-1390.

[2] Jiang C, Wang G, Hein R, Liu N, Luo X, Davis JJ. Antifouling strategies for selective in vitro and in vivo sensing. Chem. Rev. 2020;120:3852-3889.

[3] Trilling A K, Beekwildera J, Zuilhof H. Antibody orientation on biosensor surfaces: a minireview. Analyst 2013;138:1619.

[4] Decher, G. Fuzzy nanoassemblies: toward layered polymeric multicomposites. Science 1997;277:1232-7.

[5] McAloney RA, Sinyor M, Dudnik V, Goh MC. Atomic force microscopy studies of salt effects on polyelectrolyte multilayer film morphology. Langmuir 2001;17:6655-63.

Thank you very much for your valuable suggestion again, so that we have a more accurate expression of the paper.

Reviewer #3: The method by developing a low absorption of substrate in glass plates is lack of innovation.

Response: Thanks so much for your suggestion. I have the following description of the innovation of this manuscript:

First, nonspecific adsorption (fouling) can both block specific signal (reducing sensitivity) and greatly reduce assay specificity, which brings about a series of problems. In recent, the nonspecific binding poses a major challenge for label-free biosensors, where it can produce a false positive sensor response and imposes limitations on performance, especially at low analyte concentration. Surfaces resisting non-specific adsorption has played a very important role for diagnostics, drug delivery, and implantable devices. Second, the selection and treatment of substrates are particularly important to inhibit non-specific adsorption. As first generation microfluidic device material, glass substrate is perfect for capillary electrophoresis and solvent-involved applications. Although many other chip materials have been introduced afterward, glass substrate is commonly used. Due to its good optical properties, strong chemical inertness, high mechanical stress resistance, high surface stability, and good biological compatibility, glass substrate is commonly used although many other biochip materials. Third, semiconductor quantum dots (QDs) have been widely used in biomedicine due to their unique optical properties, including high photoluminescence (PL), high quantum yields (QYs), high resistance to photobleaching, and excellent biocompatibility. Optical sensors based on QDs have the advantages of convenience, high accuracy, and high sensitivity, and further needed to conduct on glass substrate as practical applications. Through previous studies, it was found that the untreated glass substrate surface would produce obvious non-specific adsorption. Therefore, the preparation of glass substrates with low nonspecific adsorption has broad applications.

Here in this manuscript, we tried to modify the substrate with polymers material (negatively charged) to obtain a substrate with high stability, high antibody capture efficiency, and inhibition of non-specific adsorption of detection materials. In the field of biosensor detection technologies, such polymer surface modification is expected to reduce the nonspecific binding of a nontarget species to the biosensor surface. The poly(styrene sulfonic acid) sodium salt (PSS)-treated and meso-tetra (4-sulfonatophenyl) porphine dihydrochloride (TSPP)-treated glass substrates could reduce adsorption of aqueous QDs by about 300-fold or 400-fold. The biochip constructed with PSS and TSPP-treated glass substrate has improved the sensitivity of the detection of inflammatory markers to a certain extent. The biochip constructed with this idea is extended to the detection of other highly sensitive substances, which has a broad application space in the biomedical field. Given the profound scientific importance of this breakthrough discovery, in particular the expected far-reaching technological impact in a broad range of high-sensitivity quantitative determination of biomedical field, we trust this paper is worthy to appear in the prestigious space in JOURNAL OF NANOBIOTECHNOLOGY.