Supplementary Materials

Synthesis of MnO2 Nanostructures for Supercapacitor is an Efficient Electrode Material to Improve Energy Storage: Effect of Annealing Temperature

Suprimkumar D. Dhasa,h*,1, Pragati N. Thongeb, Aqsa Ghazala, Aravind H. Patilc, Teja M. Patild, Tushar T. Bhosalee, D. Karthigaimuthuf, Saifan M. Shaikhg, Falah Awwada,h*

aIndustry 4.0, UAEU Science & Innovation Park, United Arab Emirates University, Al Ain, UAE

bSchool of Life Science, Punyashlok Ahilyadevi Holkar, Solapur University, Solapur, Maharashtra 413-255, India

cCenter of Technology Development, Korea Polar Research Institute, Incheon 21990, Republic of Korea

dDepartment of Physics, Bhogawati Mahavidyalaya, Kurukali, Maharastra 416-211. India

eThin film Nanomaterials Laboratory, Department of Physics, Shivaji University, Kolhapur, Maharashtra 416004, India

fDepartment of Mechanical and Aerospace Engineering, United Arab Emirates University, Al Ain 15551, United Arab Emirates

gJaysingpur College, Jaysingpur, 416101, Maharashtra, India

hElectrical and Communication Engineering Department, United Arab Emirates University, Al Ain, UAE

*Corresponding authors:

Dr. Suprimkumar D. Dhas

E-mail: suprimkumardhas@gmail.com

Prof. (Dr.) Falah Awwad

E-mail: F_awwad@uaeu.ac.ae

Preparation of MO-1, MO-2 and MO-3 working electrodes

Initially, the preparation of nickel foam (NF) with a thickness of 1.6 mm involved ultrasonic cleaning. This cleansing process utilized ethanol, hydrochloric acid at a concentration of 4 M, and double-distilled water, each for a duration of 30 min. The purpose was to effectively eliminate the oxide layer along with any residual impurities, as indicated in reference [1]. In the construction of the working electrodes, a composite was prepared comprising 80% active electrode materials, including MO-1, MO-2, and MO-2 NSs. This was complemented by 10% activated carbon and a 10% PVDF inclusion as a binder, mixed in NMP. Prior to electrochemical assessments, this blend was homogenised into a uniform slurry by sonication for 30 minutes. Following sonication, this slurry was uniformly spread over a 1 cm2 area of the NF, which had been previously cleaned and dried. The drying process entailed heating at 80 °C for 3 h, resulting in a thin coating of approximately 3 mg of the active material on the NF. Electrochemical evaluations were conducted on electrodes fabricated from MO-1, MO-2 and MO-3 NPs. An SCE served as the reference in a three-electrode system to examine the electrochemical performance of the MO-1/NF, MO-2/NF, and MO-3/NF electrodes. The configuration was completed with MO-1/NF, MO-2/NF and MO-3/NF as the working electrodes, platinum as the counter electrode, and a 1 M KOH solution as the electrolyte.

Electrochemical Measurement

The MO-1/NF, MO-2/NF, and MO-3/NF electrodes are tailored and applied as working electrodes (1 cm × 1 cm), with an effective working area of 1 cm × 1 cm. A platinum foil (10 mm × 10 mm) is employed as the counter electrode and SCE (saturated calomel electrode) as reference electrode, which apply to a three-electrode system in 1 M KOH solution. The ZIVE electrochemistry workstation is used for the electrochemical measurements. CV tests are conducted in a potential range of 0−0.5 V (versus SCE) at scan rates of 10-100 mV/s. The cycling behaviour is particularly up to 5000 cycles, and GCD tests are carried out at various current densities with a potential range of 0−0.5 V (versus SCE). EIS is used to test the capacitive property at OCV (open circuit voltage) over a frequency range of 1 to 105 Hz.

The ASSCs are assembled with MO-1/NF as the positive electrode and AC/NF as the negative electrode. To prepare the negative electrode, 80 wt% AC, 10 wt% carbon black, and 10 wt% PVDF in NMP solvent. The homogeneous slurry was coated onto an NF via drop casting and then dried for 4 h. The two electrodes of the ASSCs are separated by a separator (NKK, MPF30AC-100), and 1 M KOH is used as the electrolyte.

Fig. S1: 3-D crystal structure of MnO2 polyhedral shape

.

Fig. S2: Comparative plot of IR drop versus current of MO-1, MO-2 and MO-3 electrodes.

Fig. S3: Separate CV curves of the Mo-1 and AC electrode at a scan rate of 5 mV/s.

Fig. S4: The plot of log (current) Verses log (scan rate) of the ASSCs device.

Table S1: Summarized parameters such as electrode material, morphology, electrolyte used, specific capacitance, and cyclic stability of the MnO2-based materials.

| Electrode Composition | Morphology | Electrolyte Used | Specific Capacitance (F/g) | Capacitance retention (%)/over the cycle number | Reference |
| --- | --- | --- | --- | --- | --- |
| MnO2 | Nanospheres | 1 M Na2SO4 | 206.2 @ 1.25 A/g | 72.3% /1,000 | [1] |
| MnO2/rGO | Microspheres | 1 M Na2SO4 | 462 F/g @1 A/g | - | [2] |
| α-MnO₂ | Nanowires | 1 M Na2SO4 | 180 @1 A/g | 78% /2,000 | [3] |
| α-MnO₂ | Hollow spheres | 1 M Na2SO4 | 167 @2.5 mA | 89% /350 | [4] |
| Defective MnO₂ | Porous structure | 1 M Na2SO4 | 202 @1 A/g | 89.4% / 4,000 cycles | [5] |
| α-MnO₂ | Nanorods | 1 M Na2SO4 | 152 @2.5 mA | 87% / 1000 | [6] |
| MnO₂/C | Composite | 1 M Na2SO4 | 152 @ 1 A/g | 83.9% /10,000 | [3] |
| δ-MnO₂ | Nanosheets | 1 M Na2SO4 | 306 @0.2 A/g | 83% /1,000 | [7] |
| MnOx@rGO | Microspheres | 6 M KOH | 402 | 90%/10,000 | [8] |
| Ni–MnO₂ | Composite | 1 M Na2SO4 | 379 @1 A/g | 85%/10,000 | [9] |
| B-doped MnO₂ | NSs | 0.5 M Na2SO4 | 269 @50 mV/s | - | [9] |
| Au–MnO₂ nanowires | Nanowires | 1 M Na2SO4 | 249@1 mV/s | 97% /1,000 | [9] |
| β-MnO₂ | Nanorods | 1 M Na2SO4 | 125 | - | [10] |
| Mn2O3@MnO2 | Core–shell nanofibers | 1 M Na2SO4 | 225 @ 0.2 A/g | 86.5% /5,000 | [11] |
| Β-MnO₂ | Nanorods array | 1 M Na2SO4 | 237.3 @10 A/g | 79.8% /2,000 cycles | [12] |
| CQD-MnO2 | Marshmallow-like | 1 M Na2SO4 | 189 @ 0.14 A/g | 100 % / 1200 cycle | [13] |
| MnO2/CNS | Nanosheet arrays | 1 M Na2SO4 | 339 @ 0.5 A/g | 96.1% /5000 cycles | [14] |
| MnOx/PPy | nanowires core/sheath structure | 1 M Na2SO4 | 1091.4 @ 1 A/g | 97.4% /10,000 | [15] |
| Cu(OH)2@MnO2/CF | nanorods array | 6 M KOH | 708.6 mF cm−2 @2 mA cm−2 | 85.17%/5000 | [16] |
| MnO2 | polyhedral | 2 M KOH | 280 F/g @10 mA/g | 98.3%/5000 | This Work |

References

[1]	Liu J, Bao J, Zhang X, Gao Y, Zhang Y, Liu L, et al. MnO2-based materials for supercapacitor electrodes: challenges, strategies and prospects. RSC Advances 2022;12:35556–78. https://doi.org/10.1039/d2ra06664e.

[2]	Chang H. W, Huang Y. C, Chen J. L, Chen C. L, Chen J. M, Wei D. H, et al. Soft X-ray absorption spectroscopic investigation of MnO2/graphene nanocomposites used in supercapacitor. Catalysis Today 2022;388–389:63–9. https://doi.org/10.1016/j.cattod.2020.12.030.

[3]	Yin B, Zhang S, Jiao Y, Liu Y, Qu F, Wu X. Facile synthesis of ultralong MnO2 nanowires as high performance supercapacitor electrodes and photocatalysts with enhanced photocatalytic activities. CrystEngComm 2014;16:9999–10005. https://doi.org/10.1039/c4ce01302f.

[4]	Huang M, Li F, Dong F, Zhang YX, Zhang LL. MnO2-based nanostructures for high-performance supercapacitors. Journal of Materials Chemistry A 2015;3:21380–423. https://doi.org/10.1039/c5ta05523g.

[5]	Singu BS, Yoon KR. Porous manganese oxide nanospheres for pseudocapacitor applications. Journal of Alloys and Compounds 2017;695:771–8. https://doi.org/10.1016/j.jallcom.2016.08.239.

[6]	Tang N, Tian X, Yang C, Pi Z. Facile synthesis of α-MnO2 nanostructures for supercapacitors. Materials Research Bulletin 2009;44:2062–7. https://doi.org/10.1016/j.materresbull.2009.07.012.

[7]	Zhu YP, Xia C, Lei Y, Singh N, Schwingenschlögl U, Alshareef HN. Solubility contrast strategy for enhancing intercalation pseudocapacitance in layered MnO2 electrodes. Nano Energy 2019;56:357–64. https://doi.org/10.1016/j.nanoen.2018.11.063.

[8]	Jing F, Ma Z, Wang J, Fan Y, Qin X, Shao G. Oxygen vacancy inducing phase transition during charge storage in MnOx@rGO supercapacitor electrode. Chemical Engineering Journal 2022;435:135103. https://doi.org/10.1016/j.cej.2022.135103.

[9]	Zhang X, Liu X, Zeng Y, Tong Y, Lu X. Oxygen Defects in Promoting the Electrochemical Performance of Metal Oxides for Supercapacitors: Recent Advances and Challenges. Small Methods 2020;4:1–18. https://doi.org/10.1002/smtd.201900823.

[10]	Raihana PA, Wulandari W. 王向荣 1 ， 秦鹏 2 ， 刘福祥 1 （ 1. 2016;45:626–30.

[11]	Lu W, Li Y, Yang M, Jiang X, Zhang Y, Xing Y. Construction of Hierarchical Mn2O3@MnO2Core-Shell Nanofibers for Enhanced Performance Supercapacitor Electrodes. ACS Applied Energy Materials 2020;3:8190–7. https://doi.org/10.1021/acsaem.0c00392.

[12]	Zhu J, Zhang D, Zhu Z, Wu Q, Li J. Review and prospect of MnO2-based composite materials for supercapacitor electrodes. Ionics 2021;27:3699–714. https://doi.org/10.1007/s11581-021-04139-1.

[13]	Xu J, Hou K, Ju Z, Ma C, Wang W, Wang C, et al.  Synthesis and Electrochemical Properties of Carbon Dots/Manganese Dioxide (CQDs/MnO2) Nanoflowers for Supercapacitor Applications . Journal of The Electrochemical Society 2017;164:A430–7. https://doi.org/10.1149/2.1241702jes.

[14]	Zhao K, Xu Z, He Z, Ye G, Gan Q, Zhou Z, et al. Vertically aligned MnO2 nanosheets coupled with carbon nanosheets derived from Mn-MOF nanosheets for supercapacitor electrodes. Journal of Materials Science 2018;53:13111–25. https://doi.org/10.1007/s10853-018-2562-3.

[15]	Fu J, Zhang Y, Zhao H, Jiang R, Zhang R. Core/sheath structured ultralong MnOx/PPy nanowires feature improved conductivity and stability for supercapacitor. Journal of Colloid and Interface Science 2020;559:39–44. https://doi.org/10.1016/j.jcis.2019.10.006.

[16]	Wang H, Yan G, Cao X, Liu Y, Zhong Y, Cui L, et al. Hierarchical Cu(OH)2@MnO2 core-shell nanorods array in situ generated on three-dimensional copper foam for high-performance supercapacitors. Journal of Colloid and Interface Science 2020;563:394–404. https://doi.org/10.1016/j.jcis.2019.12.095.