Supplementary Information

Spin-Matched Hydrogenation via High-Spin Co2+ Sites for Robust pH-Universal Ammonia Electrosynthesis

Jiangnan Lv,1# Wanting Rong,1# Tingting Liang,1# Tong Zhang,2 Yuxin Zhang,1 Qiqi Dai,1 Yizhi Gao,1 Lanfang Wang,1 and Yang Liu2*

1School of Materials Science and Engineering, Key Laboratory of Magnetic Molecules and Magnetic Information Materials, Ministry of Education, Shanxi Normal University, Taiyuan 030031, China.

2College of Smart Materials and Future Energy, Fudan University, Shanghai 200433, China.

#These authors contributed equally to this work.

*E-mail address: liuyang_fd@fudan.edu.cn

Figure S1. The spin configurations of Co3O4, Fe3O4 and CoFe2O4.

Figure S2. The TDOS plots of Co3O4, Fe3O4 and CoFe2O4.

Figure S3. Summary of optimized configurations of NO3−RR intermediates on CoFe2O4 (111) surface based on DFT calculations.

In this work, the spinel (111) surfaces of CoFe2O4, Fe3O4, and Co3O4 were selected as theoretical models for the following reasons:

First, the (111) surface is one of the representative low-index facets of spinel oxides and can reasonably reflect the alternating arrangement of metal cation layers along a specific crystallographic direction. Compared with other simple surface terminations, the (111) surface can present metal coordination environments associated with both Td and Oh sites, making it more suitable for comparing the effects of Td/Oh sites in different spinel oxides on the adsorption and hydrogenation of NO3−RR intermediates.

Second, the use of a unified (111) surface model minimizes structural interference arising from different facet effects, thereby enabling a more reliable comparison of adsorption energies, free-energy changes, and electronic structures among CoFe2O4, Fe3O4, and Co3O4. Meanwhile, the low-coordinated metal sites and surface oxygen atoms exposed on the (111) surface can provide reasonable reaction sites for key surface processes, including NO3− adsorption, N−O bond activation, and *NH hydrogenation.

It should be noted that this model is intended to reveal the intrinsic reaction trends, site-dependent differences, and electronic-structure origins among different spinel oxides, rather than to imply that the actual NO3−RR process occurs exclusively on the (111) surface. In real catalysts, multiple facets, defect sites, and local surface reconstruction may coexist. Therefore, the (111) surface is employed here as a representative low-index model surface for a unified comparative analysis of different catalysts.

Figure S4. Summary of optimized configurations of NO3−RR intermediates on Co3O4 (111) surface based on DFT calculations.

Figure S5. Summary of optimized configurations of NO3−RR intermediates on Fe3O4 (111) surface based on DFT calculations.

Figure S6. The PDOS of of NO3⁻ adsorbed at (a) CoFe2O4-Fe, (b) CoFe2O4-Co, (c) Fe3O4-Fe, and (d) Co3O4.-Co. (e) PDOS and orbital overlap analysis of NO3⁻ adsorption.

Figure S7. Free energy of H2O dissociation on on high-spin Oh-Fe sites in Fe3O4 and high-spin Oh-Fe sites in CoFe2O4.

Figure S8. Summary of optimized configurations of *H adsorption on Co3O4, Fe3O4 and CoFe2O4 (111) surfaces based on DFT calculations.

Figure S9. Characterization of Co3O4. (a) XRD pattern, (b,c) XPS spectra of Co 2p and O 1s, (d) TEM image, (e) HRTEM image, (f) elemental maps of Co and O.

Figure S10. Characterization of Fe3O4. (a) XRD pattern, (b,c) XPS spectra of Fe 2p and O 1s, (d) TEM image, (e) HRTEM image, (f) elemental maps of Fe and O.

Figure S11. Statistical size distribution diagrams of CoFe2O4 nanopheres.

Figure S12. (a) Fe K-edge EXAFS and fit for CoFe2O4, shown in k2 weighted R-space. (b) Fe K-edge EXAFS and fit for CoFe2O4, shown in k2 weighted k-space.

Figure S13. (a) Co K-edge EXAFS and fit for CoFe2O4, shown in k2 weighted R-space. (b) Co K-edge EXAFS and fit for CoFe2O4, shown in k2 weighted k-space.

Figure S14. Calibration curve of NO3− using KNO3 solution as standards. (a) UV-vis spectra of assays with various NO3− concentrations. (b) Linear fitting results of the calibration curve.

Figure S15. Calibration curve of NH3 obtained by indophenol blue method using NH4Cl solution as standards. (a) UV-vis spectra of indophenol assays with various NH4+ concentrations. (b) Linear fitting results of the calibration curve.

Figure S16. Calibration curve of NO2− using KNO2 solution as standards. (a) UV-vis spectra of assays with various NO2− concentrations. (b) Linear fitting results of the calibration curve.

Figure S17. Representative GC results of the gas product after NO3−RR. The inset shows the GC calibration curve for H2 detection.

Figure S18. Nyquist plots of Co3O4, Fe3O4 and CoFe2O4.

Figure S19. Chronoamperometry curves in NO3−RR over (c) CoFe2O4, (b) Fe3O4, (c) Co3O4 at various potentials.

Figure S20. The NH3 yield rate curves in NO3−RR over (a) Co3O4, (b) Fe3O4 at various potentials.

Figure S21. The NO2− FE in NO3−RR over Fe3O4 and CoFe2O4 at various potentials.

Figure S22. 14NH4+ and 15NH4+ detections by 1H NMR spectrometry. 1H NMR spectra of (a) 14NH4+ ions and (c) 15NH4+ ions with different concentrations. Maleic acid with a constant concentration was used as an internal standard with a proton signal at d = 6.25 ppm. Calibration curve for (b) 14NH4+ and (d) 15NH4+ detections using 1H NMR.

Figure S23. Quantification of NH3 via UV−vis and NMR measurements at −0.9 VRHE and 1H NMR spectra of 15NH4Cl and 14NH4Cl standards and the electrolyte after electrocatalytic NO3−RR over CoFe2O4, nanoflowers at −0.9 VRHE using 15NO3−, and 14NO3− as N source.

Figure S24. (a) LSV curves and (b) chronoamperometry curve of CoFe2O4 in the electrolyte of 0.5M Na2SO4 with and without 0.2 M KNO3. (c) Comparison of FE and yield of NH3 for CoFe2O4 using carbon paper.

Figure S25. Comparison of (a) TEM image, (b) HRTEM image and (c) elemental maps of Co, Fe, and O of CoFe2O4 after 40 cycles of electrolysis. (d) XRD patterns. XPS spectra of (e) Co 2p, (f) Fe 2p, (g) O 2p.

Table S1. The calculated Gibbs free energy of the reaction intermediates along the reaction pathways for NO3−RR on Co3O4, Fe3O4 and CoFe2O4 (111) under neutral conditions.

| Catalysts | Co3O4 (eV) | Fe3O4 (eV) | CoFe2O4 (eV) |
| --- | --- | --- | --- |
| *NO3 | -1.63563 | -3.54832 | -4.2142 |
| *NO2 | -2.63827 | -2.77973 | -4.14463 |
| *NO | -4.15061 | -4.20991 | -3.66724 |
| *NOH | -3.73694 | -4.01248 | -4.02402 |
| *N | -4.24534 | -4.3486 | -3.43825 |
| *NH | -5.30247 | -6.12315 | -4.49425 |
| *NH2 | -3.88803 | -5.65661 | -5.17081 |
| *NH3 | -3.6849 | -3.77987 | -3.89178 |
| +NH3 | -3.15199 | -3.15199 | -3.15199 |

Table S2. The calculated Gibbs free energy of the reaction intermediates along the reaction pathways for NO3−RR on CoFe2O4 (111) under acidic and alkaline conditions.

| / | acidic | alkaline |
| --- | --- | --- |
| *NO3 | -4.2142 | -4.2142 |
| *NO2 | -4.73623 | -3.31163 |
| *NO | -4.85044 | -2.00124 |
| *NOH | -5.50302 | -1.94152 |
| *N | -5.21305 | -0.93925 |
| *NH | -6.56485 | -1.57875 |
| *NH2 | -7.53721 | -1.83881 |
| *NH3 | -6.55398 | -0.14328 |
| +NH3 | -5.81419 | 0.59651 |

Table S3. Fitting parameters of Fe K-edge EXAFS for CoFe2O4 catalyst.

| Catalyst | Shell | CNa | R(Å)b | σ2(Å2)c | ΔE0(eV)d | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| Fe foil | Fe-Fe | 8* | 2.477±0.005 | 0.0049 | -5.9±1.1 | 0.0061 |
|  | Fe-Fe | 6* | 2.858±0.008 | 0.0060 |  |  |
| Fe3O4 | Fe-O | 2.0±0.1 | 1.954±0.017 | 0.0096 | -0.2±1.3 | 0.0045 |
|  | Fe-O | 3.7±0.1 | 2.085±0.012 | 0.0067 |  |  |
|  | Fe-Fe | 5.9±0.4 | 2.993±0.015 | 0.0127 | -0.1±1.7 |  |
|  | Fe-Fe | 10.3±0.6 | 3.482±0.012 | 0.0097 | -2.2±1.3 |  |
| Fe2O3 | Fe-O | 1.8±0.5 | 1.972±0.024 | 0.0039 | -3.8±2.2 | 0.0058 |
|  | Fe-O | 4.4±0.5 | 2.148±0.011 | 0.0058 |  |  |
|  | Fe-Fe | 6.7±0.4 | 2.966±0.017 | 0.0073 | 1.8±0.5 |  |
|  | Fe-Fe | 2.7±0.3 | 3.438±0.049 | 0.0017 | 9.9±2.5 |  |
| CoFe2O4 | Fe-O | 4.3±0.1 | 1.967±0.010 | 0.0083 | 0.1±0.4 | 0.0062 |
|  | Fe-Fe | 8.6±0.9 | 3.009±0.025 | 0.0146 | 0.9±2.6 |  |
|  | Fe-Co | 7.6±1.6 | 3.519±0.030 | 0.0141 |  |  |

Note: aCN, coordination number; bR, the distance to the neighboring atom; cσ2, the Mean Square Relative Displacement (MSRD); dΔE0, inner potential correction; R factor indicates the goodness of the fit. S02 was fixed to 0.7, according to the experimental EXAFS fit of Fe foil by fixing CN as the known crystallographic value.

Table S4. Fitting parameters of Co K-edge EXAFS for CoFe2O4 catalyst.

| Catalyst | Shell | CNa | R(Å)b | σ2(Å2)c | ΔE0(eV)d | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| Co foil | Co-Co | 12* | 2.493±0.002 | 0.0062 | 7.4±0.3 | 0.0017 |
| Co3O4 | Co-O | 3.8±0.1 | 1.914±0.006 | 0.0011 | -6.8±1.1 | 0.0053 |
|  | Co-Co | 5.1±0.2 | 2.862±0.006 | 0.0050 | -8.3±0.8 |  |
|  | Co-Co | 6.6±0.4 | 3.367±0.007 | 0.0050 |  |  |
| Co2O3 | Co-O | 5.4±0.2 | 1.907±0.007 | 0.0030 | -7.9±1.1 | 0.0014 |
|  | Co-Co | 4.7±0.3 | 2.847±0.011 | 0.0038 | -8.3±1.3 |  |
|  | Co-Co | 7.5±0.4 | 3.344±0.013 | 0.0047 |  |  |
| CoFe2O4 | Co-O | 3.2±0.1 | 2.002±0.010 | 0.0023 | -0.8±0.8 | 0.0069 |
|  | Co-Co | 4.7±0.7 | 3.003±0.030 | 0.0060 | 8.2±5.3 |  |
|  | Co-Fe/Co | 10.9±1.7 | 3.453±0.025 | 0.0104 | -8.0±3.4 |  |

Note: aCN, coordination number; bR, the distance to the neighboring atom; cσ2, the Mean Square Relative Displacement (MSRD); dΔE0, inner potential correction; R factor indicates the goodness of the fit. S02 was fixed to 0.75, according to the experimental EXAFS fit of Co foil by fixing CN as the known crystallographic value.

Table S5. Performance comparison of CoFe2O4 with recently reported electrocatalysts for NO3−RR in neutral electrolytes.

| Catalysts | Electrolyte | FE (NH3) (%) | Potential (VRHE) | NH3 Yieldmax (mmol·h-1·cm-2) | Ref. |
| --- | --- | --- | --- | --- | --- |
| CoFe2O4 | 0.5 M Na2SO4 0.2 M KNO3 | 95.1 | -0.9 | 2.2 | This work |
| Cu-cis-N2O2 | 0.5 M Na2SO4 1000 ppm KNO3 | 88.46 | -1.6 | 1.69 | 1 |
| Co3O4-x/Ti | 0.1 M K2SO4 1400 ppm KNO3 | 100 | -0.5 | 0.68 | 2 |
| 1D MnFeOx | 0.5 M K2SO4 0.05 M KNO3 | 95.9 | -1.0 | 0.72 | 3 |
| CoTPP/CNT/PBFDO | 0.5 M K2SO4 0.1 M KNO3 | 98.1 | -1.55 | 0.31 | 4 |
| Co4Fe6 | 0.1 M Na2SO4 200 ppm NO3--N | 98.6 | -0.69 | 0.16 | 5 |
| CoPhz/CNT | 0.1 M K2SO4 0.1 M KNO3 | 93 | -1.15 | 0.49 | 6 |
| Cu10Ni90 | 0.5 M K2SO4 0.1 M KNO3 | 98 | -0.6 | 0.675 | 7 |
| Ca-Cu2O-OA | 0.5 M Na2SO4 0.1 M NaNO3 | 97.49 | -0.9 | 0.88 | 8 |
| ZIF-67@HMCS | 0.5 M Na2SO4 0.1 M KNO3 | 97.6 | -0.9 | 1.05 | 9 |
| Cu-SA/UiO-bpy | 0.5 M K2SO4 0.1 M KNO3 | 98.1 | -0.8 | 0.435 | 10 |
| Cu2O-InSA | 0.5 M Na2SO4 0.1 M KNO3 | 99.36 | -0.8 | 0.85 | 11 |
| Cu2O@Py-COF | 0.1 M Na2SO4 0.1 M NaNO3 | 84 | -0.7 | 0.1335 | 12 |
| Ni-P HCs | 0.5 M Na2SO4 0.2 M KNO3 | 93.7 | -0.8 | 0.85 | 13 |
| 2H-RhCu | 0.5 M K2SO4 0.1 M KNO3 | 94.8 | -0.3 | 0.08 | 14 |
| Co SAAC/INC | 0.5 M K2SO4 0.1 M KNO3 | 97.2 | -0.6 | 1.12 | 15 |
| SnCu-DG | 0.1M K2SO4 0.5 M KNO3 | 99.5 | -0.8 | 0.446 | 16 |
| CuAl2O4-δ | 0.1 M PBS+ 0.1 M NaNO3 | 92 | -1.2 | 0.164 | 17 |
| RuFeCoNiMnMo HEAs | 0.5 M K2SO4 0.1 M KNO3 | 99.9 | -0.3 | 0.98 | 18 |
| RuSA-CuFe2O4 | 0.1 M Na2SO4 1000 ppm NO3− | 94.54 | -0.59 | 0.48 | 19 |

Table S6. Performance comparison of CoFe2O4 with recently reported electrocatalysts for NO3−RR in acidic and alkaline electrolytes.

| Catalysts | Electrolyte | FE (NH3)max (%) | NH3 Yieldmax (mmol·h-1·cm-2) | Ref. |
| --- | --- | --- | --- | --- |
| CoFe2O4 | 0.05 M H2SO4 0.2 M KNO3 | 91.6 | 1.05 | This work |
| RhNi@Rh BMLs | 100 mM HClO4 50 mM KNO3 | 98.5 | 0.086 | 20 |
| RhNiAu-TML | 100 mM HClO4 50 mM KNO3 | 97.9 | 0.1397 | 21 |
| Si/I-NiO@CC | 0.05 M H2SO4 0.5 M KNO3 | 96.8 | 0.62 | 22 |
| pCo-Cu | 0.5 M H2SO4 0.1 M KNO3 | 92.5 | 0.48 | 23 |
| CoFe2O4 | 1 M KOH 0.2 M KNO3 | 94.3 | 6.3 | This work |
| CuIr | 1 M KOH 0.1 M KNO3 | 93.1 | 6.01 | 24 |
| AumCu SAAs | 1 M KOH 0.1 M KNO3 | 99.86 | 6.21 | 25 |
| Co(OH)2-Ru | 1 M KOH 0.1 M KNO3 | 97.7 | 5.76 | 26 |
| Ru-Co(OH)2/CC | 1 M KOH 0.1 M NO3− | 97.2 | 4.96 | 27 |
| Cu50Co50 | 1 M KOH 0.1 M NO3− | 100 | 4.8 | 28 |
| Ru-CuNW | 1 M KOH 0.032 M NO3− | 95.6 | 4.5 | 29 |
| NiCu-hcp | 1 M KOH 0.1 M KNO3 | 98.3 | 2.85 | 30 |
| RuPdCoCuZn | 1 M KOH 0.1 M KNO3 | ~100 | 2.095 | 31 |
| FeCu-N-C | 1 M KOH 0.5 M KNO3 | ~100 | 1.11 | 32 |
| NiO/WO3 | 1 M KOH 0.1 M KNO3 | 96.1 | 1.22 | 33 |
| CuCoSP | 0.1 M KOH 0.1 M NO3− | 93.3 | 1.17 | 34 |
| RuCuDAs/NGA | 0.1 M KOH 0.1 M KNO3 | 95.7 | 0.32 | 35 |
| Ru-Ni(OH)2 | 1 M KOH 0.1 M KNO3 | 99.7 | 1.33 | 36 |
| W-CCNs | 1 M KOH 0.1 M KNO3 | 91.26 | 0.51 | 37 |
| Cr-Cu2O | 1 M NaOH 0.1 M NaNO3 | 91.6 | 1.88 | 38 |
| R-RuO2/Co(OH)2 | 1 M KOH 0.1 M KNO3 | 97.7 | 2.11 | 39 |
| NF/Ni3N-Cu | 1 M KOH 0.1 M KNO3 | 98.7 | 2.56 | 40 |
| Cu/Mo-WO3 | 0.1 M KOH 0.1 M KNO3 | 98.6 | 0.308 | 41 |
| 5%Ce-Cu/MoO2@C | 1 M KOH 0.1 M KNO3 | 92 | 0.4776 | 42 |
| Cu3N/GDY | 1 M KOH 0.1 M KNO3 | 98.1 | 2.01 | 43 |
| (Cu0.25Ni0.25Fe0.25Co0.25)6Sn5 | 1 M KOH 0.1 M KNO3 | 97.09 | 0.6617 | 44 |

References

1	Cheng, X.-F. et al. Coordination Symmetry Breaking of Single-Atom Catalysts for Robust and Efficient Nitrate Electroreduction to Ammonia. Adv. Mater. 34, 2205767 (2022).

2	Xu, L. et al. Dynamic Cobalt Phase Transition Enables Self-Adaptive Electrocatalytic Nitrate-to-Ammonia Conversion in Neutral Media. Angew. Chem., Int. Ed. 65, e9755292 (2026).

3	Jia, X. et al. Self-Sustaining Dynamic Alkaline Microenvironment-Mediated Efficient Nitrate Electroreduction to Ammonia on MnFeOx in Neutral Electrolyte. Angew. Chem., Int. Ed. 65, e4598330 (2026).

4	Chen, B. et al. Boosting Cobalt Porphyrin for Selective Nitrate Electroreduction. Angew. Chem., Int. Ed. 65, e23415 (2026).

5	Yang, Y. et al. Self-Triggering a Locally Alkaline Microenvironment of Co4Fe6 for Highly Efficient Neutral Ammonia Electrosynthesis. J. Am. Chem. Soc. 147, 8893−8905 (2025).

6	Jin, X. et al. Localized Active H* Enrichment by Cobalt Molecular Catalysts for Enhanced Electrocatalytic Nitrate Reduction. Angew. Chem., Int. Ed., e24566 (2026).

7	Wang, Y. et al. Interfacial Water Structure Modulation on Unconventional Phase Non-Precious Metal Alloy Nanostructures for Efficient Nitrate Electroreduction to Ammonia in Neutral Media. Angew. Chem., Int. Ed. 64, e202508617 (2025).

8	Wang, Y. et al. Boosting Nitrate-to-Ammonia Conversion over Copper-Based Electrocatalysts by Facilitating Hydrogenation and Product Desorption. Angew. Chem., Int. Ed. 64, e202509090 (2025).

9	Tian, Q. et al. Nanocellular Organelle Engineering for Optimizing Reaction Microenvironments in Nitrate-to-Ammonia Electrocatalysis. Angew. Chem., Int. Ed. 64, e202516919 (2025).

10	Zhu, Y. et al. DFT-Guided Design and Synthesis of Bipyridine-Anchored Copper Single-Atom Catalysts for Efficient Nitrate-to-Ammonia Electroreduction Across a Broad pH Range. Angew. Chem., Int. Ed. 65, e17715 (2026).

11	Quan, Q. et al. Low-Valent Single-Atom Indium Site Regulating Ionic Interference and Adsorbed Hydrogen for Near-Unity Electrosynthesis of Ammonia. Angew. Chem., Int. Ed. 65, e20730 (2026).

12	Tahir, W. et al. Covalent Organic Frameworks on Cu2O Nanocubes as Rapid Proton/Electron Transfer Gates for Efficient NH3 Electrosynthesis from Nitrate in Neutral Media. J. Am. Chem. Soc. 148, 743−755 (2026).

13	Hu, Q. et al. Subnanometric Nickel Phosphide Heteroclusters with Highly Active Niδ+-Pδ- Pairs for Nitrate Reduction toward Ammonia. J. Am. Chem. Soc. 147, 12228−12238 (2025).

14	Zhou, J. et al. Modulating the Nitrate Reduction Pathway on Unconventional Phase Ultrathin Nanoalloys for Selective Ammonia Electrosynthesis. J. Am. Chem. Soc. 147, 23226−23238 (2025).

15	Cui, Z., Wang, H., Li, C., Peng, W. & Liu, J. Iodine Dopants Facilitate Tandem Catalysis via Transformation Adsorption Behavior for Efficient Electrochemical Nitrate Reduction Reaction. ACS Nano 19, 31050−31064 (2025).

16	Wu, Q. et al. Constructing Asymmetric Sn-Cu-C Interface via Defective Carbon Trapped Atomic Clusters for Efficient Neutral Nitrate Reduction. Adv. Mater. 37, e2505743 (2025).

17	Niu, L. et al. Promoting Active Hydrogen Supply and Nitrate Adsorption by Disordering Tetrahedral-Octahedral Structure of CuAl2O4-δ for Efficient Nitrate Reduction. Adv. Mater. 38, e17303 (2026).

18	Meng, X. et al. Heterophase fcc-hcp-fcc High-Entropy Alloy Nanomaterials with Tailored Electron Divergence for Selective Ammonia Electrosynthesis. Adv. Mater. 38, e21096 (2026).

19	Wang, Y. et al. A Self-Recycling Ruthenium Incorporated CuFe2O4 Electrocatalyst for Efficient Neutral Ammonia Electrosynthesis. Adv. Mater. 37, e2507277 (2025).

20	Zhong, W. et al. RhNi Bimetallenes with Lattice-Compressed Rh Skin towards Ultrastable Acidic Nitrate Electroreduction. Adv. Mater. 36, 2314351 (2024).

21	Zhong, W. et al. Dual strain regulated RhNiAu trimetallene for efficient plasmonic-promoted acidic nitrate electroreduction. Energy Environ. Sci. 18, 4971−4981 (2025).

22	Feng, C., Bo, K., Wan, J., Zhang, H. & Wang, Y. Triple Synergy Engineering via Metal-Free Dual-Atom Incorporation for Self-Sustaining Acidic Ammonia Electrosynthesis. Angew. Chem., Int. Ed. 64, e202505211 (2025).

23	Ba, J. et al. Red Carbon Mediated Formation of Cu2O Clusters Dispersed on the Oxocarbon Framework by Fehling's Route and their Use for the Nitrate Electroreduction in Acidic Conditions. Adv. Mater. 36, 2400396 (2024).

24	Guo, X. et al. Controlled Defective Engineering on CuIr Catalyst Promotes Nitrate Selective Reduction to Ammonia. ACS Nano 18, 24252-24261 (2024).

25	Yu, J. et al. Electrochemical Nitrate Reduction to Ammonia on AuCu Single-Atom Alloy Aerogels under Wide Potential Window. Angew. Chem., Int. Ed. 64, e202415975 (2025).

26	Tang, Y., Wan, Y., Yan, W., Zhang, J. & Lv, R. Modulated metal-support interactions for efficient nitrate electroreduction at positive potentials. Nat. Commun. 17, 3006 (2026).

27	Zhang, L. et al. High-efficiency ammonia electrosynthesis from nitrate on ruthenium-induced trivalent cobalt sites. Energy Environ. Sci. 18, 5622−5631 (2025).

28	Fang, J.-Y. et al. Ampere-level current density ammonia electrochemical synthesis using CuCo nanosheets simulating nitrite reductase bifunctional nature. Nat. Commun. 13, 7899 (2022).

29	Chen, F.-Y. et al. Efficient conversion of low-concentration nitrate sources into ammonia on a Ru-dispersed Cu nanowire electrocatalyst. Nat. Nanotechnol. 17, 759−767 (2022).

30	Li, P. et al. Modulating Intermediate Adsorption and Interfacial Water Structure to Unlock the Potential of Nickel for Ammonia Electrosynthesis and Zn-NO3− Battery. Angew. Chem., Int. Ed. 65, e1281046 (2026).

31	Zhao, H. et al. Dynamic Proton Allocation Drives High-Efficiency Nitrate Electroreduction on High-Entropy Alloy Aerogels Across Broad Concentration Ranges. Angew. Chem., Int. Ed. 65, e20035 (2026).

32	Hong, S. et al. Operando Cu Aggregation-Induced Spin State Modulation in Fe–Cu Single Atom Catalyst for Enhanced Tandem Electrochemical Nitrate Reduction Reaction. J. Am. Chem. Soc. 148, 15114−15124 (2026).

33	Duan, L. et al. Oxygen-Bridge-Mediated NiO/WO3 Heterostructure for Highly Efficient Electrocatalytic Nitrate-to-Ammonia Conversion. Adv. Funct. Mater. 36, e75297 (2026).

34	He, W. et al. Splicing the active phases of copper/cobalt-based catalysts achieves high-rate tandem electroreduction of nitrate to ammonia. Nat. Commun. 13, 1129 (2022).

35	Liu, K. et al. Tailoring asymmetric RuCu dual-atom electrocatalyst toward ammonia synthesis from nitrate. Nat. Commun. 16, 2167 (2025).

36	Wan, Y. et al. Interfacial Water Regulation for Nitrate Electroreduction to Ammonia at Ultralow Overpotentials. Adv. Mater. 37, 2417696 (2025).

37	Liu, X. et al. Hierarchical Carbon-Based Electrocatalyst with Functional Separation Properties for Efficient pH Universal Nitrate Reduction. Adv. Mater. 37, 2417623 (2025).

38	Zhang, K. et al. Unveiling the Dual Role of Oxophilic Cr4+ in Cr−Cu2O Nanosheet Arrays for Enhanced Nitrate Electroreduction to Ammonia. Angew. Chem., Int. Ed. 63, e202411796 (2024).

39	Zhu, A. et al. Tuning Active Hydrogen on Reconstructed RuO2/Co(OH)2 Catalysts for Selective Ammonia Synthesis. Adv. Mater. 38, e15346 (2026).

40	Ouyang, X. et al. Intensifying Interfacial Reverse Hydrogen Spillover for Boosted Electrocatalytic Nitrate Reduction to Ammonia. Angew. Chem., Int. Ed. 64, e202422585 (2025).

41	Dai, Y. et al. Tandem Active Sites in Cu/Mo-WO3 Electrocatalysts for Efficient Electrocatalytic Nitrate Reduction to Ammonia. Adv. Funct. Mater. 35, 2420282 (2025).

42	Dong, J.-H. et al. Engineering Ce Promoter to Regulate H* Species to Boost Tandem Electrocatalytic Nitrate Reduction for Ammonia Synthesis. Adv. Funct. Mater. 35, 2422025 (2025).

43	Zhang, Z. et al. Graphdiyne Enabled Nitrogen Vacancy Formation in Copper Nitride for Efficient Ammonia Synthesis. J. Am. Chem. Soc. 146, 14898−14904 (2024).

44	Xiang, Z. et al. Active Hydrogen Enrichment on Cu6Sn5-type High Entropy Intermetallics for Efficient Nitrate Reduction Reaction. Adv. Mater. 37, 2501886 (2025).