Supporting information for

Strikingly Distinctive NH3-SCR Behavior over Cu-SSZ-13 in the Presence of NO2

Yulong Shan1, Guangzhi He1,*, Jinpeng Du2, Yu Sun1,4, Zhongqi Liu1,4, Yu Fu1,4, Fudong Liu3, Xiaoyan Shi1,4, Yunbo Yu1,2,4, Hong He1,2,4,*

* Corresponding author: Email: gzhhe@rcees.ac.cn, honghe@rcees.ac.cn

(15 pages, 10 figures, 2 tables)

Fig. S1 NOx, NO and NO2 conversion of Cu-SSZ-13 with different Cu loadings under FSCR conditions. [NO]=[NO2]=250 ppm, [NH3]=500 ppm, [O2]=5 vol.% [H2O]=3.5 vol.%. GHSV = 800,000 h-1.

Generally, the NOx conversion was significantly inhibited at low temperatures (< 200 ℃, Fig. S1a) due to the formation of NH4NO3, which has been reported by previous studies. 1, 2 The inhibition effect results from the negligible degree of NO reduction at low temperatures (Fig. S1b), while NO2 conversion primarily contributed to the NOx reduction (Fig. S1c). This is because NO primarily reacted at active Cu sites, while the formed NH4NO3 made the Cu species inaccessible to NO. Moreover, large amounts of NH4NO3 are easily formed on the Al-rich zeolite that was used in this work. In addition, it should be noted that the NO2 conversion decreased with increasing Cu loading. As the temperature increased to the decomposition temperature of NH4NO3, the deNOx efficiency was rapidly elevated and the both the NO and NO2 conversion levels increased with the increase in Cu loading.

Fig. S2 NH3-TPD profiles of Cu-SSZ-13 with different Cu loadings

Fig. S2 shows the NH3-TPD profiles of Cu-SSZ-13 with various Cu loadings. There are two primary NH3 desorption peaks at ~ 230 and ~360 ℃, which are ascribed to NH3 adsorbed on Lewis acid sites (LASs, primarily Cu sites) and Brønsted acid sites (BASs, primarily -Si-OH-Al-), respectively.3, 4 The total amount of NH3 desorption from LASs and BASs was calculated and shown in Table S2. The number of BASs increased while LASs decreased with decreasing Cu loading. This demonstrated that active Cu2+ sites occupied the BASs in zeolite, converting BASs into LASs, which is consistent with previous studies.3, 5 Therefore, the LASs and BASs are in inverse proportion. As consequence, the NO2 reaction rates decreased with increasing Cu loadings but increased with the amount of BASs.

Fig. S3 NH3-SCR performance of Cu-SSZ-13 with different Cu loadings under NO2-SCR conditions. [NO2]=350 ppm, [NH3]=500 ppm, [O2]=5 vol.% [H2O]=3.5 vol.%. GHSV = 2,400,000 h-1.

During the NO2-SCR reaction, the NO2 conversion decreased markedly with increasing Cu loading, indicating that NO2 rarely reacted at Cu sites. The activation energies of the NO2-SCR reaction are between 16-22 kJ/mol, indicating facile reaction between NO2 and NH3 over Cu-SSZ-13. The reaction between NO2 and NH3 always resulted in NH4NO3 formation through the following reaction:6, 7

2NO2 + 2NH3 = NH4NO3 + N2 + H2O

Fig. S4 NO2 reaction rates as a function of (a) Cu loading and (b) Brønsted acid sites under NO2-SCR conditions. (c) NO2 turnover frequency (TOF) as a function of Brønsted acid sites under NO2-SCR conditions.

Under NO2-SCR conditions, the NO2 reaction rate decreased with the increase in Cu loading (Fig. S4a) while increasing with the increase in BASs (Fig. S4b), indicating that the BASs rather than the Cu2+ sites participated in the reduction of NO2. Moreover, the TOF of NO2 as a function of BASs is approximately constant (Fig. S4c), suggesting a single-site catalysis process. Actually, NO2 disproportionation could occur on the BASs to form nitrates and nitrites, which then react with NH3 to form NH2NO and NH4NO3. The NH2NO could easily decompose to N2 and H2O. This process was also observed in previous studies.8, 9

|  | 2NO2 + ZH → ZHO + HNO3 | （1） |
| --- | --- | --- |
|  | HNO3 + NH3 → NH4NO3 | （2） |
|  | ZNO + NH3 → ZHNONH2 | （3） |
|  | ZHNONH2 → ZH +N2+H2O | （4） |

Fig. S5 Cu K-edge XANES (a, c) and the first derivative spectra (b, d) of Cu-SSZ-13 treated under different atmospheres. The Cu-SSZ-13 sample was treated by (i) NO adsorption, (ii) NH3 adsorption, (iii) NO+NH3 co-adsorption, (iv) NO+NH3 co-adsorption followed by reaction with O2, (v) NO+NH3 co-adsorption followed by reaction with NO2. (vi) SSCR reactants, (vii) FSCR reactants and (viii) NO2-SCR reactants. The pretreated Cu-SSZ-13 is depicted with the label Pre.

### Reduction and oxidation of copper species by SCR reactants

Furthermore, we conducted in-situ/operando XAFS experiments on Cu-SSZ-13 samples to investigate the state of copper species under different conditions. The Cu-SSZ-13 was characterized by XAFS after different SCR reactant treatments at 200 ℃. As shown in Fig. S5a, results showed a weak pre-edge peak A at ~8977.5 eV, which was assigned to the 1s → 3d transition of d9 Cu2+ ions.10, 11 The B and C features at ~8983 and ~8987 eV are attributed to the 1s → 4p transitions of linearly coordinated Cu+ ions and fourfold coordinated Cu2+ ions, respectively.12, 13 These three features were also clearly observed in the first derivative form of the XANES spectra (Fig. S5b). Compared with the pretreated Cu-SSZ-13, both NO and NH3 induced the partial reduction of Cu2+ to Cu+, indicating that both NO and NH3 can be activated by Cu2+ species through transferring electrons to Cu2+. Moreover, Cu2+ ions were more easily reduced by NH3 due to the facile formation of linear [Cu(NH3)2]+ species.14, 15 This is because, compared with NO, NH3 molecules interact more strongly with Cu2+ sites due to the ligand effect between NH3 and Cu2+, which was observed in many studies.16, 17 Moreover, it is noted that more [Cu(NH3)2]+ species were formed when Cu-SSZ-13 was exposed to the NO+NH3 mixture, indicating that NO can further assist the reduction of Cu2+ species by NH3. The reduction of Cu2+ by a NO+NH3 mixture is generally thought of as the reduction cycle of the SSCR reaction.16, 18

Z2Cu2+ + 3NH3 + NO → ZCu+(NH3)2 + ZH + N2 + H2O                    (5)

(Z represents zeolite framework with negative charge)

To investigate the reactivity of [Cu(NH3)2]+ species in an oxidizing atmosphere, the O2 and NO2 was separately induced to oxidize Cu+ ions after treatment by NO+NH3 mixture. After oxidation by O2, the peak of [Cu(NH3)2]+ sharply decreased, concomitant with the appearance of Cu2+ ions at ~8977 and ~8987 eV, similar to the XANES profiles of pretreated Cu-SSZ-13. Nevertheless, a slight amount of [Cu(NH3)2]+ species still existed as indicated by peak B, which is identified more clearly in the first derivative form of the XANES spectra (Fig. S5b). This observation is consistent with previous studies showing that not all Cu+ can be completely oxidized even in an O2 atmosphere.12, 15 Moreover, this phenomenon is more clearly proved by the observation of the further decrease in peak B in Fig. S5a and S5b after deeper oxidation by NO2, which demonstrated that NO2 can further oxidize the residual [Cu(NH3)2]+ species since NO2 has stronger oxidizing power. The complete disappearance of peak B suggests that all the [Cu(NH3)2]+ species are oxidized by NO2. Compared with Cu+ species, Cu2+ has more ligands and NO2 adsorption to form nitrates on Cu2+ species is facile. In addition, higher valence facilitates the interaction between Cu2+ ions and the framework. As a result, the Cu2+ ions are likely bound to the framework to form fw-Cu2+ (framework fixed Cu2+) species, inhibiting the mobility of the copper species.

### State of copper species during SSCR, FSCR and NO2-SCR reactions

To uncover the state and coordination of Cu species under real SCR conditions, we conducted XAFS measurements and depicted the XANES profiles and their first derivative form for Cu-SSZ-13 under SSCR, FSCR and NO2-SCR conditions, with the results shown in Fig. S5c and S5d. Under SSCR conditions, both features A and B were clearly observed, indicating the coexistence of large amounts of [Cu(NH3)2]+ species and Cu2+ ions, which suggests the occurrence of redox between Cu2+ and Cu+ ions under SSCR conditions.19, 20 This was also observed in the WT-EXAFS results (Fig. 3). Under FSCR conditions, however, the XANES profile was more like that of pretreated Cu-SSZ-13, demonstrating that most of the copper species were Cu+ ions, although there was still a slight amount of Cu+ ions. This result suggests that the oxidation of Cu+ is more rapid than the reduction process under FSCR conditions due to the higher oxidizing ability of NO2. This is disadvantageous to the SSCR reaction or NO reduction under FSCR conditions, since the existence of more Cu2+ ions means tight coordination with the zeolite and the weak mobility of active copper species. Under NO2-SCR conditions, furthermore, almost all of the copper species were in the Cu2+ state while few Cu+ species were observed, as indicated by the presence of peak A and the absence of peak B. This demonstrated that the NO2-SCR is independent of the redox of copper species or that the oxidation rate of Cu+ is much higher than the reduction process, which is consistent with the kinetic results (Fig. 2). The in-situ/operando XAFS results show that more Cu2+ ions exist under NO2-SCR conditions than in the pretreated Cu-SSZ-13, indicating that NO2 can oxidize the copper species even though they reacted with NH3 at Brønsted acid sites. This demonstrated that the dynamic [Cu(NH3)2]+ species dominated under SSCR conditions while the fw-Cu2+ primarily existed under FSCR and NO2-SCR conditions.

Fig. S6 Fourier-transformed (FT) k3-weighted EXAFS spectra (phase uncorrected) of Cu-SSZ-13 treated under different atmosphere.

Table S1 EXAFS fitting parameters for Cu-SSZ-13 exposed to different atmospheres

| Sample | Shell | CN | R(Å) | σ2 | ∆E0 | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| pretreated | Cu-O | 3.7±0.4 | 1.93±0.01 | 0.0061 | 0.5±2.6 | 0.0124 |
| SSCR reaction | Cu-O(N) | 3.5±0.1 | 1.95±0.01 | 0.0073 | 3.7±1.0 | 0.0124 |
| FSCR reaction | Cu-O(N) | 3.7±0.1 | 1.94±0.01 | 0.0068 | 1.9±0.8 | 0.0124 |
| NO2-SCR reaction | Cu-O(N) | 3.7±0.1 | 1.95±0.01 | 0.0068 | 1.6±0.9 | 0.0124 |

Figure S6 shows the Fourier-transformed (FT) EXAFS spectra (without phase correction) of Cu-SSZ-13 under various conditions. The first-shell peak is generally attributed to the scattering of O or N atoms, which derived from the zeolite framework O or adsorbed NH3 in this work.10, 11 The second shell is primarily attributed to the zeolite framework T atoms (Si or Al).10, 21 The appearance of the second shell scattering feature indicated the interaction between copper species and the zeolite framework. On the contrary, the absence of the second shell scattering feature suggests high mobility for the copper species. The parameters resulting from the experimental data and the simulated fittings of EXAFS spectra are listed in Table S1.

Compared with the pretreated sample, the Cu-SSZ-13 exposed to SSCR conditions showed decreased intensity for the first-shell peak, with the coordination number (CN) decreasing from 3.7 to 3.5. The decrease in CN indicated the reduction of Cu2+ species to [Cu(NH3)2]+ species. The absence of the second shell scattering feature for NH3-treated Cu-SSZ-13 also proved the formation of dynamic [Cu(NH3)2]+ species, which are unconnected with the zeolite framework. However, when NO2 was involved in the SCR reaction (FSCR or NO2-SCR), the feature of the second shell appeared, indicating the scattering of framework atoms (Si or Al). The Cu2+ species with high charge dominated in the presence of NO2 with high oxidation ability. This high charge for the copper species intensified the electrostatic force between the copper species and zeolite framework, leading to the active sites becoming fixed on the zeolite.

Fig. S7. Gibbs free energy profile of the fast SCR cycle at the Cu-monomer site as well as optimized geometries of the reactants, transition states, intermediates, and products for all elementary steps. The zeolite framework is omitted for clarity. Orange, red, blue, and white circles denote Cu, O, N, and H atoms, respectively.

Fig. S7 shows the NH2NO reaction pathway over the Cu-monomer site, which includes the reduction and oxidation half-cycles. The Cu2+OH(NH3)2 species are first reduced to Cu+(NH3)2 by NH3 and NO with the energy barrier of 0.32 eV, accompanied by the formation of two H2O and one N2 (See Monomer Cu→C in Fig. S7). This process is clearly seen in the operando XAFS results, in which plenty of Cu2+ were reduced to Cu+ in the presence of NH3 and NO. Then, as an oxidizing agent, NO2 oxidizes Cu+(NH3)2 species to Cu2+NO2(NH3)3 with coordination by another NH3. The adsorbed NO2 reacts with one NH3 ligand, resulting in the formation of NH2NO and Cu2+OH(NH3)2. Subsequently, NH2NO is decomposed into N2 and H2O to complete the whole reaction cycle. The NH2NO is easily decomposed into N2 and H2O with a low energy barrier of 0.60 eV (Figure S9). The rate-determining step of the NH2NO reaction pathway over the Cu-monomer site is the oxidation of Cu+(NH3)2 by NO2 with another NH3 coordination, with an extremely high energy barrier of 1.65 eV, which is comparable with the value reported by Janssens et al..22

Fig. S8. Gibbs free energy profile of the fast SCR cycle at the Cu-dimer site as well as optimized geometries of the reactants, transition states, intermediates, and products for all elementary steps. The zeolite framework is omitted for clarity. All legends are the same as those in Figure S8.

It has been proved that Cu dimers play a key role in the standard SCR reaction.12, 14, 15 Therefore, we then calculated the fast SCR pathway with the participation of the Cu dimer. First, the adsorption of NO2 leads to the formation of an NO2-bridging dimer-Cu (see A in Figure S8). Subsequently, NO2 is activated and reacts with one adsorbed NH3 molecule, leading to the formation of Cu2+OH(NH3)2 and an NH2NO species (see B in Figure S8). The NH2NO is then easily decomposed into N2 and H2O with a low energy barrier of 0.60 eV (Figure S9). Then, one NO and one NH3 are adsorbed on Cu2+OH(NH3)2 and Cu+(NH3)2, respectively. The adsorbed NH3 reacts with the -OH group at the other Cu site to generate an H2O molecule and an -NH2 species. The -NH2 species further reacts with the adsorbed NO to form NH2NO (see F in Fig. S8). Accompanied by the decomposition of NH2NO into N2 and H2O, the Cu-dimer site is regenerated. The highest energy barrier of the FSCR cycle over the Cu-dimer site is 1.58 eV, corresponding to the reaction of adsorbed NO2 with an NH3 ligand.

Fig. S9 Gibbs free energy profile of NH2NO decomposition with the assistance of Brønsted acid sites as well as optimized geometries of the reactants, transition states, intermediates, and products for all elementary steps. Except for the Al-O(H) groups involved in the reaction, all other atoms of the zeolite framework are omitted for clarity. Pink, red, blue, and white circles denote Al, O, N, and H atoms, respectively.

Table S2 Elemental analysis and physicochemical properties of Cu-SSZ-13 with various Cu contents

| Sample | Cu wt.% | Cu/Al | Si/Al | NH3 storage (mmol/g) | L (mmol/g) | B (mmol/g) | BET (m2/g) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Cu0.4-SSZ-13 | 0.4 | 0.03 | 5.1 | 2.135 | 0.328 | 1.806 | 626 |
| Cu1.0-SSZ-13 | 1.0 | 0.08 | 5.0 | 2.260 | 0.662 | 1.666 | 575 |
| Cu1.7-SSZ-13 | 1.7 | 0.14 | 5.2 | 2.287 | 1.145 | 1.141 | 566 |
| Cu2.6-SSZ-13 | 2.6 | 0.22 | 5.5 | 2.359 | 1.361 | 0.998 | 592 |
| Cu3.8-SSZ-13 | 3.8 | 0.31 | 5.1 | 2.376 | 1.523 | 0.853 | 544 |

Fig. S10 The SSZ-13 zeolite model used in the DFT calculations. Yellow, pink, red, and white circles denote Si, Al, O, and H atoms, respectively.

References

1. Xie, L.; Liu, F.; Liu, K.; Shi, X.; He, H., Inhibitory effect of NO2 on the selective catalytic reduction of NOx with NH3 over one-pot-synthesized Cu–SSZ-13 catalyst. Catal. Sci. Technol. 2014, 4 (4), 1104-1110.

2. Shan, Y.; Shi, X.; He, G.; Liu, K.; Yan, Z.; Yu, Y.; He, H., Effects of NO2 Addition on the NH3-SCR over Small-Pore Cu–SSZ-13 Zeolites with Varying Cu Loadings. J. Phys. Chem. C 2018, 122 (45), 25948-25953.

3. Wang, D.; Gao, F.; Peden, C. H. F.; Li, J.; Kamasamudram, K.; Epling, W. S., Selective Catalytic Reduction of NOx with NH3 over a Cu-SSZ-13 Catalyst Prepared by a Solid-State Ion-Exchange Method. Chem. Commun. 2014, 6, 1579-1583.

4. Luo, J.; Gao, F.; Kamasamudram, K.; Currier, N.; Peden, C. H. F.; Yezerets, A., New insights into Cu/SSZ-13 SCR catalyst acidity. Part I: Nature of acidic sites probed by NH3 titration. J. Catal. 2017, 348, 291-299.

5. Villamaina, R.; Liu, S.; Nova, I.; Tronconi, E.; Ruggeri, M. P.; Collier, J.; York, A.; Thompsett, D., Speciation of Cu Cations in Cu-CHA Catalysts for NH3-SCR: Effects of SiO2/Al2O3 Ratio and Cu-Loading Investigated by Transient Response Methods. ACS Catal. 2019, 9, 8916-8927.

6. Grossale, A.; Nova, I.; Tronconi, E., Ammonia blocking of the “Fast SCR” reactivity over a commercial Fe-zeolite catalyst for Diesel exhaust aftertreatment. J. Catal. 2009, 265 (2), 141-147.

7. Grossale, A.; Nova, I.; Tronconi, E.; Chatterjee, D.; Weibel, M., NH3–NO/NO2 SCR for Diesel Exhausts Aftertreatment: Reactivity, Mechanism and Kinetic Modelling of Commercial Fe- and Cu-Promoted Zeolite Catalysts. Top. Catal. 2009, 52 (13-20), 1837-1841.

8. Liu, K.; Yan, Z.; Shan, W.; Shan, Y.; Shi, X.; He, H., Quantitative determination of the Cu species, acid sites and NH3-SCR mechanism on Cu-SSZ-13 and H-SSZ-13 at low temperatures. Catal. Sci. Technol. 2020, 10 (4), 1135-1150.

9. Liu, C.; Malta, G.; Kubota, H.; Kon, K.; Toyao, T.; Maeno, Z.; Shimizu, K.-i., In Situ/Operando IR and Theoretical Studies on the Mechanism of NH3–SCR of NO/NO2 over H–CHA Zeolites. J. Phys. Chem. C 2021, 125 (25), 13889-13899.

10. Martini, A.; Borfecchia, E.; Lomachenko, K. A.; Pankin, I. A.; Negri, C.; Berlier, G.; Beato, P.; Falsig, H.;  Bordiga, S.; Lamberti, C., Composition-driven Cu-speciation and reducibility in Cu-CHA zeolite catalysts: a multivariate XAS/FTIR approach to complexity. Chem. Sci. 2017, 8 (10), 6836-6851.

11. Borfecchia, E.; Lomachenko, K. A.; Giordanino, F.; Falsig, H.; Beato, P.; Soldatov, A. V.; Bordiga, S.; Lamberti, C., Revisiting the nature of Cu sites in the activated Cu-SSZ-13 catalyst for SCR reaction. Chem. Sci. 2015, 6 (1), 548-563.

12. Negri, C.; Selleri, T.; Borfecchia, E.; Martini, A.; Lomachenko, K. A.; Janssens, T. V. W.; Cutini, M.; Bordiga, S.; Berlier, G., Structure and Reactivity of Oxygen-Bridged Diamino Dicopper(II) Complexes in Cu-Ion-Exchanged Chabazite Catalyst for NH3-Mediated Selective Catalytic Reduction. J. Am. Chem. Soc. 2020, 142 (37), 15884-15896.

13. Pappas, D. K.; Borfecchia, E.; Dyballa, M.; Pankin, I. A.; Lomachenko, K. A.; Martini, A.; Signorile, M.;  Teketel, S.; Arstad, B.; Berlier, G.; Lamberti, C.; Bordiga, S.; Olsbye, U.; Lillerud, K. P.; Svelle, S.; Beato, P., Methane to Methanol: Structure-Activity Relationships for Cu-CHA. J. Am. Chem. Soc. 2017, 139 (42), 14961-14975.

14. Gao, F.; Mei, D.; Wang, Y.; Szanyi, J.; Peden, C. H., Selective Catalytic Reduction over Cu/SSZ-13: Linking Homo- and Heterogeneous Catalysis. J. Am. Chem. Soc. 2017, 139 (13), 4935-4942.

15. Paolucci, C.; Khurana, I.; Parekh, A. A.; Li, S.; Shih, A. J.; Li, H.; Iorio, J. R. D.; Albarracin-Caballero, J. D.;  Yezerets, A.; Miller, J. T.; Delgass, W. N.; Ribeiro, F. H.; Schneider, W. F.; Gounder, R., Dynamic multinuclear sites formed by mobilized copper ions in NOx selective catalytic reduction. Science 2017, 357, 898-903.

16. Paolucci, C.; Parekh, A. A.; Khurana, I.; Di Iorio, J. R.; Li, H.; Albarracin Caballero, J. D.;  Shih, A. J.;  Anggara, T.;  Delgass, W. N.;  Miller, J. T.;  Ribeiro, F. H.;  Gounder, R.; Schneider, W. F., Catalysis in a Cage: Condition-Dependent Speciation and Dynamics of Exchanged Cu Cations in SSZ-13 Zeolites. J. Am. Chem. Soc.  2016, 138 (18), 6028-48.

17. Zhang, Y.; Peng, Y.; Li, K.; Liu, S.; Chen, J.; Li, J.; Gao, F.; Peden, C. H. F., Using Transient FTIR Spectroscopy to Probe Active Sites and Reaction Intermediates for Selective Catalytic Reduction of NO on Cu/SSZ-13 Catalysts. ACS Catal. 2019, 6, 6137-6145.

18. Paolucci, C.; Verma, A. A.; Bates, S. A.; Kispersky, V. F.; Miller, J. T.; Gounder, R.; Delgass, W. N.; Ribeiro, F. H.; Schneider, W. F., Isolation of the Copper Redox Steps in the Standard Selective Catalytic Reduction on Cu-SSZ-13. Angew. Chem. Ind. Ed. 2014, 126 (44), 12022-12027.

19. Liu, C.; Kubota, H.; Amada, T.; Kon, K.; Toyao, T.; Maeno, Z.; Ueda, K.; Ohyama, J.; Satsuma, A.; Tanigawa, T.; Tsunoji, N.; Sano, T.; Shimizu, K.-i., In Situ Spectroscopic Studies on the Redox Cycle of NH3–SCR over Cu‐CHA Zeolites. ChemCatChem 2020, 12, 1-11.

20. Bates, S. A.; Verma, A. A.; Paolucci, C.; Parekh, A. A.; Anggara, T.; Yezerets, A.; Schneider, W. F.; Miller, J. T.;  Delgass, W. N.; Ribeiro, F. H., Identification of the active Cu site in standard selective catalytic reduction with ammonia on Cu-SSZ-13. J. Catal. 2014, 312, 87-97.

21. Sushkevich, V. L.; Safonova, O. V.; Palagin, D.; Newton, M. A.; van Bokhoven, J. A., Structure of copper sites in zeolites examined by Fourier and wavelet transform analysis of EXAFS. Chemical Science 2020, 11 (20), 5299-5312.

22. Janssens, T. V. W.; Falsig, H.; Lundegaard, L. F.; Vennestrøm, P. N. R.; Rasmussen, S. B.; Moses, P. G.;  Giordanino, F.; Borfecchia, E.; Lomachenko, K. A.; Lamberti, C.; Bordiga, S.; Godiksen, A.; Mossin, S.; Beato, P., A Consistent Reaction Scheme for the Selective Catalytic Reduction of Nitrogen Oxides with Ammonia. ACS Catal. 2015, 5 (5), 2832-2845.