In-situ generation of Silver Nano-particles on Langmuir-Blodgett Film Template of MoS2 : Fabrication and Its Application in SERS

Chayan Kumar Mitraa, Surojit Pande b, Joydeep Chowdhury* a

a Department of Physics, Jadavpur University, 188, Raja S.C. Mallick Rd, Kolkata 700032, India

b Department of Chemistry, Birla Institute of Technology and Science, Pilani, Rajasthan-333031, India

*Corresponding Author: joydeep72_c@rediffmail.com / joydeep.chowdhury@jadavpuruniversity.in

Fig.S1. EDX spectra of the as synthesised MoS2-Ag substrates (a) S1 substrate , (b) S2 substrate and  (c) S3 substrate  respectively.

The enhancement factors (EFs) of the SERS bands of R6G molecule have been calculated using the following relation as reported elsewhere[1, 2]:

EF=ISERS∕NSERSIbulk∕Nbulk

ISERS and Ibulk denote the SERS and normal Raman intensities of R6G molecule and NSERS and Nbulk denote the number of the R6G probe molecule present in SERS and normal Raman measurements. Now NSERS and Nbulk has been estimated from the following relations :

NBulk=CBulkALaserdNA

NSERS=CSERSALaserVNAADC

| SERS (cm-1) | EFs with R6G concentration ( 10-8M) |  |  |
| --- | --- | --- | --- |
|  | S1 | S2 | S3 |
| 611 | 1.2 ×105 | 6.2 ×105 | 1.9 ×106 |
| 770 | 2.2 ×105 | 6.1 ×105 | 9.3 ×105 |
| 1571 | 9.2 ×104 | 3.4 ×105 | 9.8 ×105 |

where CBulk is the concentration of the probe molecules of R6G in the Normal Raman Scattering. In the contemporary experiment 100× objective lens has been used  having the confocal depth (d)~0.8 μm and  the laser spot area(ALaser) ~4×10-13m2 with the excitation wavelength ~532 nm. CSERS is the concentration of R6G molecule at SERS experiment, NA is the Avogadro number and V is the volume of the probe molecule which is ~25 μl for the contemporary experimental work and ADC is the area of the drop casted probe molecules on the as prepared Ag-MoS2 substrates S1, S2 and S3 tracing a circular deposit of radius ~ 4×10-5 m2. The enhancement factors of the R6G molecules so absorbed on the substrates S1, S2 and S3 were presented in Table S1.

Table S1: Calculation of Enhancement Factors for R6G absorbed on the substrate

| Substrate | EF | Ref. |
| --- | --- | --- |
| Au-Ag NP/rGO | 1.12 × 108 | [3] |
| Ag-Au core-shell nanowire networks | 1.5 × 10⁵ | [4] |
| 3D RGO@MoS2/Ag NPs | 2.2 × 109 | [5] |
| Ag/ZnO Nanowire Arrays | 3.5 × 106 | [6] |
| Au/Ag-TiO2/SnO2 NPs | 2.07 × 108 | [7] |
| Ti3C2Tx/AgNPs | 3.8 × 108 | [8] |
| Ag-MoS2- S3 | 1.46 × 1010 | Current Work |

Table S2: EFs of the existing recent reports in comparison with the as prepared substrate

References:

1. 	Mitra CK, Sharma MD, Ghosh M, et al (2024) Gold Nano-colloids impregnated in Langmuir-Blodgett Film of MoS2 flakes as SERS active platform: Fabrication and its application in Malathion detection. Current Applied Physics 63:18–31. https://doi.org/10.1016/j.cap.2024.04.002

2. 	Saha S, Ghosh M, Dutta B, Chowdhury J (2016) Silver coated gold nanocolloids entrapped in organized Langmuir–Blodgett Film of stearic acid: Potential evidence of a new SERS active substrate. Appl Surf Sci 362:364–373. https://doi.org/https://doi.org/10.1016/j.apsusc.2015.11.137

3. 	Pillai N, Shatar L, Mustafa FH, et al (2026) Enhancement Factors of SERS Substrates Based on Monometallic and Bimetallic Nanoparticles Embedded on Reduced Graphene Oxide. Plasmonics 21:1551–1566. https://doi.org/10.1007/s11468-025-03311-x

4. 	Mikhailova PS, Arsenov P V, Atlanov MA, et al (2026) Morphology-dependent SERS enhancement in Ag-Au core-shell nanowire networks. Nano-Structures & Nano-Objects 46:101649. https://doi.org/https://doi.org/10.1016/j.nanoso.2026.101649

5. 	Qian Q, He H, Fu S, et al (2026) 3D RGO@MoS2/Ag NPs based SERS platform for label-free detection of IL-6. Mater Chem Phys 358:132416. https://doi.org/https://doi.org/10.1016/j.matchemphys.2026.132416

6. 	Jung Y, Gwon G, Lee J-S, et al (2024) Enhancing Surface-Enhanced Raman Scattering Intensity through Light Diffuse Reflection on Ag/ZnO Nanowire Arrays. The Journal of Physical Chemistry C 128:6748–6757. https://doi.org/10.1021/acs.jpcc.4c00350

7. 	Hazra S, Jangra P, Dahiya S, et al (2026) Flexible and Transparent SERS Substrate Using Au–Ag Bimetallic Conducting Thin Films for Detection of Molecular Level R6G Dye and Vitamin B12. ACS Appl Nano Mater. https://doi.org/10.1021/acsanm.6c02673

8. 	Li L, Zhang T, Zhang L, et al (2024) Synergistic enhancement of chemical and electromagnetic effects in a Ti3C2Tx/AgNPs two-dimensional SERS substrate for ultra-sensitive detection. Anal Chim Acta 1331:343330. https://doi.org/https://doi.org/10.1016/j.aca.2024.343330