A selective resonance Rayleigh scattering method for trace vitamin B2 based on molecularly imprinted nanosilver probe

Yue Luo1,2, Dan Li1,2, Chongning Li1,2*, Guiqing Wen1,2, Aihui Liang1,2*，Zhiliang Jiang1,2*

1 Key Laboratory of Ecology of Rare and Endangered Species and Environmental Protection (Guangxi Normal University), Ministry of Education, Guilin 541004, China;

2 Guangxi Key Laboratory of Environmental Pollution Control Theory and Technology, Guilin 541004, China.

Figure S1 Fourier transform infrared spectra of Fe₃O₄ and Fe₃O₄@AgNP

| A | B |
| --- | --- |
| C | D |
| E | F |

Figure S2 RRS and Abs spectra of Fe3O4@AgNP, Fe3O4 and AgNP

A: RRS spectra of Fe3O4@AgNP (5, 10, 15, 20, 25, 30, 35 mg/L); B: Abs spectra of Fe3O4@AgNP (5, 10, 15, 20, 25, 30, 35 mg/L); C: RRS spectra of Fe3O4 (5, 10, 15, 20, 25, 30, 35 mg/L); D: Abs spectra of Fe3O4 (5, 10, 15, 20, 25, 30, 35 mg/L); E: RRS spectra of AgNP (17.3, 21.6, 25.9, 30.2, 34.6, 38.9, 43.2 mg/L); F: Abs spectra of AgNP (4.3, 6.5, 8.6, 13.0, 17.3, 21.6 mg/L).

The arrow represents concentration from low to high.

Figure S3 Stability of 25 mg/L Fe₃O₄ 50nm@AgNP nanosol.

| -5.09mV A | B -10.9mV |
| --- | --- |

Figure S4 Zeta potential and particle size analysis of Fe3O4@AgNP, AgNP and Fe3O4

A: Potentiometric distribution diagram of 0.05 g/L Fe₃O₄; B: Potentiometric distribution diagram of 0.10 g/L Fe₃O₄@AgNP; C: Particle size distribution diagram of 0.10 g/L Fe₃O₄@AgNP

| A | B |
| --- | --- |

Figure S5 Hysteresis curve

A: Fe3O4; B: AgNP@Fe3O4.

Figure S6 Absorption spectra of Fe3O4@AgNP elution

Rinse frequency from the first to the fifth time.

| A | B |
| --- | --- |
| C | D |
| E | F |

Figure S7 Selection of preparation conditions for Fe3O4@AgNP

A: 0.04 mmol VB2, Fe3O4 (10, 25, 35, 45, 55) mmol, 0.02 mmol AgNO3, 0.2 mmol sodium citrate, 0.6 mmol H2O2, 0.06 mmol NaBH4, 10 min, 250 ℃; B: 0.04 mmol VB2, 35 mg Fe3O4, AgNO3 (0.01, 0.02, 0.03, 0.04) mmol, 0.2 mmol sodium citrate, 0.6 mmol H2O2, 0.06 mmol NaBH4, 10 min, 250 ℃; C: 0.04 mmol VB2, 35 mg Fe3O4, 0.02 mmol AgNO3, 0.2 mmol sodium citrate (0.05, 0.1, 0.2, 0.3,0.4)mmol, 0.6 mmol H2O2, 0.06 mmol NaBH4, 15 min, 250 ℃; D: 0.04 mmol VB2, 35 mg Fe3O4, 0.02 mmol AgNO3, 0.3 mmol sodium citrate, H2O2 ( 0.2, 0.4, 0.6, 0.8, 1), 0.06 mmol NaBH4, 15 min, 250 ℃; E: 0.04 mmol VB2, 35 mg Fe3O4, 0.02 mmol AgNO3, 0.3 mmol sodium citrate, 0.6 mmol H2O2, 0.06 mmol NaBH4, 15 min, 250 ℃; F: 0.04 mmol VB2, 35 mg Fe3O4, 0.02 mmol AgNO3, 0.3 mmol sodium citrate, 0.6 mmol H2O2, 0.06 mmol NaBH4, 15 min, temperature (210, 220, 230, 240, 250) ℃;

| A | B |
| --- | --- |

Figure S8 Condition optimization of Fe3O4@AgNP analysis system.

A: Effect of Fe₃O₄@AgNP; B: Effect of pH.

Table S1 The influence of foreign substance on the RRS determination

| Foreign substance | Multiple | Relative error (%) | Foreign substance | Multiple | Relative error (%) |
| --- | --- | --- | --- | --- | --- |
| Mn2+ | 1000 | -6.5% | Cd2+ | 1000 | -3.7% |
| Mg2+ | 1000 | 7.5% | As3+ | 1000 | 5.3% |
| CO32- | 1000 | 4.1% | SO42- | 1000 | -8.1% |
| NO2+ | 1000 | 5.4% | Fe3+ | 900 | -6.3% |
| Ni2+ | 1000 | 4.3% | Vitamin B6 | 1000 | 6.7% |
| I- | 1000 | 0.86% | Nicotinamide | 1000 | 2.1% |