
Table 4. Elemental composition (wt%) of fluorine, calcium, and phosphorus and calcium-to-phosphorus (Ca/P) ratio in enamel specimens after pH cycling.
	Restorations
	Conditions
	Elemental analysis (%wt)
	Calcium/phosphate (Ca/P) ratio

	
	
	Fluorine (F)
	Calcium (Ca)
	Phosphate (P)
	

	Resin composite
	No toothpaste
	0.00
	27.89
	13.25
	2.11

	
	Fluoride toothpaste
	0.55
	27.82
	12.51
	2.22

	
	Fluoride + HA
	0.28
	28.29
	12.87
	2.20

	
	HA toothpaste
	0.00
	27.11
	12.62
	2.15

	GIC
	No toothpaste
	0.58
	29.53
	13.97
	2.11

	
	Fluoride toothpaste
	0.73
	21.91
	10.94
	2.00

	
	Fluoride toothpaste + HA
	0.37
	24.45
	11.70
	2.09

	
	HA toothpaste
	0.70
	29.83
	12.64
	2.36




