Table 4. Elemental composition (wt%) of fluorine, calcium, and phosphorus and calcium-to-phosphorus (Ca/P) ratio in enamel specimens after pH cycling.

| Restorations | Conditions | Elemental analysis (%wt) |  |  | Calcium/phosphate (Ca/P) ratio |
| --- | --- | --- | --- | --- | --- |
|  |  | Fluorine (F) | Calcium (Ca) | Phosphate (P) |  |
| Resin composite | No toothpaste | 0.00 | 27.89 | 13.25 | 2.11 |
|  | Fluoride toothpaste | 0.55 | 27.82 | 12.51 | 2.22 |
|  | Fluoride + HA | 0.28 | 28.29 | 12.87 | 2.20 |
|  | HA toothpaste | 0.00 | 27.11 | 12.62 | 2.15 |
| GIC | No toothpaste | 0.58 | 29.53 | 13.97 | 2.11 |
|  | Fluoride toothpaste | 0.73 | 21.91 | 10.94 | 2.00 |
|  | Fluoride toothpaste + HA | 0.37 | 24.45 | 11.70 | 2.09 |
|  | HA toothpaste | 0.70 | 29.83 | 12.64 | 2.36 |