Table 2. Lesion depth of artificial initial carious lesions before and after pH cycling.

| Restorative material | Toothpaste | n | Baseline LD (gHAp/cm³) | LD after pH cycling (gHAp/cm³) | Change in LD (%) |
| --- | --- | --- | --- | --- | --- |
| Resin composite | Fluoride | 10 | 111.767 ± 8.408 | 134.833 ± 14.096† | 20.459 ± 5.587ᵃᵇ |
|  | Fluoride + HA | 10 | 111.167 ± 7.101 | 132.200 ± 12.859† | 18.800 ± 6.313ᵃᵇ |
|  | HA | 10 | 111.066 ± 6.625 | 128.266 ± 10.057† | 15.581 ± 7.476ᵃ |
|  | No toothpaste | 10 | 110.700 ± 4.517 | 138.300 ± 11.458† | 24.398 ± 8.606ᵇ |
| GIC | Fluoride | 10 | 111.667 ± 7.445 | 108.067 ± 8.225† | −3.234 ± 3.161ᵃ* |
|  | Fluoride + HA | 10 | 112.400 ± 8.362 | 109.333 ± 8.038† | −2.693 ± 2.337ᵃ* |
|  | HA | 10 | 112.266 ± 7.359 | 108.500 ± 5.013† | −3.213 ± 3.112ᵃ* |
|  | No toothpaste | 10 | 111.633 ± 5.734 | 115.533 ± 5.994† | 3.501 ± 1.491ᵇ* |

Data are presented as mean ± standard deviation (SD). HA, hydroxyapatite; GIC, glass ionomer cement.
†Significant difference between baseline and post–pH cycling lesion depth within the same experimental group (p < 0.05; paired t-test).
Within each restorative material, different lowercase superscript letters in the percentage-change column indicate significant differences among toothpaste groups (p < 0.05; Tukey post hoc test following two-way ANOVA). Groups sharing a superscript letter are not significantly different.
*Significant difference between resin composite and GIC for the corresponding toothpaste group (p < 0.05).