Table 3. Mean and standard deviation of surface roughness (Ra) values (nm)
	Restoration
	Tested Groups
	

	
	No toothpaste
	Fluoride toothpaste
	Fluoride + HA
	HA toothpaste
	P - value

	Composite
	2771.98±265.69 Aa
	1826.99±159.63 Ab
	1493.17±289.44 Abc
	1203.18±251.99 Ac
	< 0.01

	GIC
	2494.66±315.96 Aa
	1996.87±326.34 Ab
	1585.17±255.25 Abc
	1345.61± 229.74 Ac
	< 0.01

	P - value
	0.079
	0.276
	0.553
	0.360
	


Different superscript lowercase letters within the same row indicate statistically significant differences between groups (p < 0.05), as determined by two-way ANOVA. Different uppercase letters within the same column indicate a statistically significant difference between restoration types (p < 0.05).

