Table 3. Mean and standard deviation of surface roughness (Ra) values (nm)

| Restoration | Tested Groups |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | No toothpaste | Fluoride toothpaste | Fluoride + HA | HA toothpaste | P - value |
| Composite | 2771.98±265.69 Aa | 1826.99±159.63 Ab | 1493.17±289.44 Abc | 1203.18±251.99 Ac | < 0.01 |
| GIC | 2494.66±315.96 Aa | 1996.87±326.34 Ab | 1585.17±255.25 Abc | 1345.61± 229.74 Ac | < 0.01 |
| P - value | 0.079 | 0.276 | 0.553 | 0.360 |  |

Different superscript lowercase letters within the same row indicate statistically significant differences between groups (p < 0.05), as determined by two-way ANOVA. Different uppercase letters within the same column indicate a statistically significant difference between restoration types (p < 0.05).