Table 1. Mineral density of artificial initial carious lesions before and after pH cycling.

| Restorative material | Toothpaste | n | Baseline MD (gHAp/cm³) | MD after pH cycling (gHAp/cm³) | Change in MD (%) |
| --- | --- | --- | --- | --- | --- |
| Resin composite | Fluoride | 10 | 19.953 ± 2.715 | 19.737 ± 2.694 | −0.911 ± 5.620ᵃ |
|  | Fluoride + HA | 10 | 21.004 ± 3.094 | 19.968 ± 2.928† | −4.785 ± 4.807ᵃᵇ |
|  | HA | 10 | 21.044 ± 3.514 | 18.343 ± 3.325† | −12.866 ± 5.285ᵇ |
|  | No toothpaste | 10 | 21.387 ± 2.738 | 17.695 ± 3.285† | −17.333 ± 10.435 |
| GIC | Fluoride | 10 | 21.752 ± 3.089 | 22.875 ± 3.133† | 5.291 ± 3.090ᵃ* |
|  | Fluoride + HA | 10 | 21.013 ± 3.425 | 21.054 ± 3.276 | 0.371 ± 4.125ᵇ* |
|  | HA | 10 | 21.468 ± 3.242 | 22.950 ± 3.204† | 7.116 ± 3.884ᵃ* |
|  | No toothpaste | 10 | 21.429 ± 2.299 | 22.090 ± 2.754† | 2.915 ± 2.927ᵃᵇ* |

Data are presented as mean ± standard deviation (SD). HA, hydroxyapatite; GIC, glass ionomer cement.
†Significant difference between baseline and post–pH cycling values within the same experimental group (p < 0.05; paired t-test).
Within each restorative material, different lowercase superscript letters in the percentage-change column indicate significant differences among toothpaste groups (p < 0.05; Tukey post hoc test following two-way ANOVA).
*Significant difference between resin composite and GIC for the corresponding toothpaste group (p < 0.05).