Supplementary data

	Table S1 Composition of the tested toothpaste, batch numbers, and expiration dates in detail.

	Products
	Batch number and Expiration date
	Detailed compositions

	Fluoride toothpaste
(Fluoride 1,500 ppm)
	MGF0903243
EXP 090327
	Commercial fluoride toothpaste (SYSTEMA® Ultra care & protect): Water, Sorbitol, Hydrated Silica, PEG-8, Sodium Lauryl Sulfate, Cellulose Gum, Flavor, CI 77891, Sodium Saccharin, Sodium Fluoride, Methylparaben, Dipotassium Glycyrrhizate, o-Cymen-5-ol, Butylparaben

	Fluoride and HAP toothpaste
(Fluoride 1,498 ppm +
5% Micro-hydroxyapatite)
	MGF002220124
EXP 220726
	Commercial micro-hydroxyapatite combined with fluoride toothpaste (CUDENT®): Aqua(Water), Hydrated Silica, Sorbitol, Glycerin, Hydroxyapatite, Cellulose Gum, Sodium Monofluorophosphate, Sodium Lauroyl Sarcosinate, Aroma (Flavor),  Calcium Carbonate, Sodium Benzoate, Rebaudioside A, Xylitol, Limonene, Menthol, Mentha Piperita (Peppermint) Oil , Cl 42090 (Blue 1)

	HAP toothpaste
(Hydroxyapatite)
	MGF30092022
EXP: 30092025
	Commercial hydroxyapatite toothpaste (Biorepair®):  Aqua, Zinc Hydroxyapatite (microRepair), Glycerin, Sorbitol, Silica, PEG-32,Callulose Gum, Aroma, Sodium Myristoyl Sarcosinate, Sodium Methyl Cocoyl Taurate, Sodium Saccharin, Citric Acid, Phenoxyethanol, Benzyl Alcohol, Sodium Benzoate.



Table S2. Two-way ANOVA results for the effects of restoration type and toothpaste on surface roughness (Ra).
	Source
	Sum of Squares
	df
	Mean Square
	F
	Sig.

	Corrected Model
	12942860.6a
	7
	1848980.085
	26.059
	< .001

	Intercept
	162457263
	1
	162457263
	2289.617
	< .001

	Restoration
	12095.506
	1
	12095.506
	0.170
	0.682

	Toothpaste
	12539292.2
	3
	4179764.069
	58.908
	< 0.001

	Restoration * Toothpaste
	391472.879
	3
	130490.960
	1.839
	0.156

	Error
	2838155.586
	40
	70953.890
	
	

	Total
	178238279
	48
	
	
	

	Corrected Total
	15781016.2
	47
	
	
	

	a. R squared = 0.820 (Adjusted R Squared = 0.789)




