Supporting information

Facile fabrication of ternary MoO2/Fe2O3/CNFs nanofibers with efficient electromagnetic wave absorption performance

Fuyao Chen 1,2*, Zhehong Lu 3, Han Chen 1, Dongqi Liu 4*, Jingshuai Liu 1, Xuzhen Zhang1, Junmin Wan 1, Yi Huang 1, Juming Yao 1*

1: School of Materials Science and Engineering, Zhejiang Sci-Tech University, Hangzhou, 311200, China.

2: Tongxiang Research Institute of Zhejiang Sci-Tech University, JiaXing, 314000, China.

3: College of Chemistry and Molecular Sciences, Henan University, Kaifeng, 475004, China.

4: Xi’an Modern Chemistry Research Institute, Xi’an 710065, China.

Corresponding author：Dr Fuyao Chen, Dr Dongqi Liu, Prof. Juming Yao.

Address: School of Materials Science and Engineering, Zhejiang Sci-Tech University, Hangzhou, 311200, China.

Xi'an Modern Chemistry Research Institute, Xi'an, 710000, China.

Tel./fax： Fuyao Chen, +86 17855371372; Dongqi Liu, +86 18691850785; Juming Yao, +86 13967196026

Email: 17855371372@163.com, ldqnjust1997@163.com, yaoj@zstu.edu.cn

Experimental Section

Figure S1. XPS survey spectrum of MoO2/Fe2O3/CNF-2 composites.

Figure S2. SEM images of MoO2/PVA (a), Fe2O3/PVA (b), MoO2/Fe2O3/PVA-1 (c), and MoO2/Fe2O3/PVA-3 (d).

Figure S3. SEM images of MoO2/CNF (a), Fe2O3/CNF (b), MoO2/Fe2O3/CNF-1 (c), and MoO2/Fe2O3/CNF-3 (d).

Figure S4. Fiber diameter distribution of MoO2/PVA (a), Fe2O3/PVA (b), MoO2/Fe2O3/PVA-1 (c), MoO2/Fe2O3/PVA-2 (d) and MoO2/Fe2O3/PVA-3 (e).

Figure S5. Fiber diameter distribution of MoO2/CNF (a), Fe2O3/CNF (b), MoO2/Fe2O3/CNF-1 (c), MoO2/Fe2O3/CNF-2 (d) and MoO2/Fe2O3/CNF-3 (e).

Figure S6. N2 adsorption-desorption isotherms and pore size distribution curves of MoO2/Fe2O3/CNF-1 (a), MoO2/Fe2O3/CNF-3 (b).

Figure S7. Relationship between RL and 1/4λ of MoO2/CNF (a), Fe2O3/CNF (b), MoO2/Fe2O3/CNF-1 (c), MoO2/Fe2O3/CNF-2 (d) and MoO2/Fe2O3/CNF-3 (e).

Figure S8. CST far-field simulation at 10.56 GHz of PEC coated with MoO2/CNF (a), Fe2O3/CNF (b), MoO2/Fe2O3/CNF-1 (c) and MoO2/Fe2O3/CNF-3 (d)

Fig S1. XPS survey spectrum of MoO2/Fe2O3/CNF-2 composites

Fig S2. SEM images of MoO2/PVA (a), Fe2O3/PVA (b), MoO2/Fe2O3/PVA-1 (c), and MoO2/Fe2O3/PVA-3 (d).

Fig S3. SEM images of MoO2/CNF (a), Fe2O3/CNF (b), MoO2/Fe2O3/CNF-1 (c), and MoO2/Fe2O3/CNF-3 (d).

Fig S4. Fiber diameter distribution of MoO2/PVA (a), Fe2O3/PVA(b), MoO2/Fe2O3/PVA-1(c), MoO2/Fe2O3/PVA-2(d) and MoO2/Fe2O3/PVA-3(e).

Fig S5. Fiber diameter distribution of MoO2/CNF (a), Fe2O3/CNF (b), MoO2/Fe2O3/CNF-1(c), MoO2/Fe2O3/CNF-2(d) and MoO2/Fe2O3/CNF-3 (e).

Fig S6. N2 adsorption-desorption isotherms and pore size distribution curves of MoO2/Fe2O3/CNF-1 (a), MoO2/Fe2O3/CNF-3 (b)

Fig S7 Relationship between RL and 1/4λ of MoO2/CNF (a), Fe2O3/CNF (b), MoO2/Fe2O3/CNF-1(c), MoO2/Fe2O3/CNF-2(d) and MoO2/Fe2O3/CNF-3(e).

Fig. S8. CST far-field simulation at 10.56 GHz of PEC coated with MoO2/CNF (a), Fe2O3/CNF (b), MoO2/Fe2O3/CNF-1 (c) and MoO2/Fe2O3/CNF-3 (d)