Electrochemical Detection of Propyl Gallate in Packaged Foods Using a SnS2-Co1Fe2@N-CNTs Composite

Yili Zhanga, Jingyu Denga, Zitong Yanga, Wenkai Qia, Rui Xieb, Yuxia Zhanga*, Zhaohui Houa*

aKey Laboratory of Hunan Province for Advanced Carbon-based Functional Materials, School of Chemistry and Chemical Engineering, Hunan Institute of Science and Technology, Yueyang 414006, China

bSchool of Chemical Engineering and Materials, Yueyang University, Yueyang 414011, China

*Corresponding Author

- mail addresses: zyxia2010@126.com (Y. Zhang), zhaohuihou@126.com (Z. Hou).

Fig. S1 TEM images of the SnS2-Co1Fe2@N-CNTs composite: (a) overall morphology; (b) magnified view showing interfacial contact; (c) HRTEM image

Fig. S2  (a) N2 adsorption-desorption isotherms, and (b) BJH pore size distributions of the N-CNTs, Co1Fe2@N-CNTs and SnS2-Co1Fe2@N-CNTs.

Fig. S3 DPV curves measured in 2.5 mM Fe(CN)63-/4-

Fig. S4 The relationship between the anodic peak potential (Epa) and the natural logarithm of the scan rate (ln ν) was analyzed for the SnS2-Co1Fe2@N-CNTs/GCE in 0.1 M PBS containing 1 mM PG to evaluate the electron transfer kinetics.

Fig. S5 The linear plot between various pH values vs. the corresponding potential.

Fig. S6 Repeatability of current responses for Electrode 1 (Batch A) over 12 consecutive measurements

Fig. S7 Repeatability (n=12) for a single electrode from Batch B

Fig. S8. XRD analysis of the electrode after 50 CV cycles

Table S1. Textural properties of N-CNTs, Co1Fe2@N-CNTs and SnS2-Co1Fe2@N-CNTs samples derived from N2 physisorption.

| Sample | BET surface area (m2 g-1) | Total pore volume (cm3 g-1) | Average pore size Dpore (nm) |
| --- | --- | --- | --- |
| N-CNTs | 75.89 | 0.208 | 8.36 |
| Co1Fe2@N-CNTs | 77.99 | 0.140 | 6.36 |
| SnS2-Co1Fe2@N-CNTs | 59.30 | 0.108 | 6.21 |

Table. S2 Comparison of the electrochemical active surface areas (A) of different materials

| Materials | Ip (μA) | A (cm²) |
| --- | --- | --- |
| GCE | 32.26 | 0.0829 |
| SnS2/GCE | 38.78 | 0.0997 |
| N-CNTs/GCE | 43.25 | 0.111 |
| Co1Fe2@N-CNTs/GCE | 62.61 | 0.161 |
| SnS-Co1Fe2@N-CNTs/GCE | 89.45 | 0.230 |

Table. S3 Quantification of propyl gallate (PG) in food samples using a  SnS2-Co1Fe2@N-CNTs modified electrode.

| Sample | Added (μM) | Found (μM) | Found (μM) | Found (μM) | Found (n=3) (μM) | Recovery (%) | RSD (%, n=3) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Biscuits | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
|  | 50 | 48.95 | 47.55 | 50.02 | 48.84 | 97.68 | 2.53 |
|  | 100 | 99.79 | 98.30 | 98.59 | 98.89 | 98.89 | 0.63 |
|  | 200 | 201.99 | 198.66 | 197.49 | 199.38 | 99.69 | 1.17 |
| Cured meat | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
|  | 50 | 48.92 | 49.95 | 49.09 | 49.32 | 98.63 | 1.12 |
|  | 100 | 99.63 | 98.57 | 98.11 | 98.77 | 98.77 | 0.79 |
|  | 200 | 197.48 | 197.54 | 195.98 | 197.00 | 98.50 | 0.45 |

Table. S4  Spiked recovery test results for HPLC analysis of propyl gallate (PG) in actual samples.

| Sample | Added (μM) | Found (μM) | Recovery (%) | RSD (%, n=3) |
| --- | --- | --- | --- | --- |
| biscuits | 0 | 0 | 0 | 0 |
|  | 50 | 48.58 | 97.16 | 2.49 |
|  | 100 | 98.86 | 98.86 | 0.97 |
|  | 200 | 200.55 | 100.28 | 0.11 |
| Cured meat | 0 | 0 | 0 | 0 |
|  | 50 | 47.76 | 95.52 | 1.03 |
|  | 100 | 96.15 | 96.15 | 1.50 |
|  | 200 | 196.28 | 98.14 | 1.79 |

Table. S5 Comparison of previously reported modified electrodes for the detection of PG.

| Modified electrode | Technique | Linear range (μM) | LOD (μM) | Real sample matrix | Reference |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ag@Ti₃C₂Tₓ/CdTe QDs/GCE | DPV | 0.1-400 | 0.0032 | Chicken meat, ice cream |  | [1] |
| NiFeCo-LDH/G aerogel/SPCE | DPV | 0.001-297.43 | 0.00087 | Edible oils, cookies |  | [2] |
| NiFe-Oxide@LIG | DPV | 0.5-5 | 0.01 | Food samples |  | [3] |
| SrTiO₃@g-C₃N₄/GCE | DPV | 5-1300 | 0.014 | Peanut butter, noodles, cooking oil |  | [4] |
| CdTe QDs/Ti₃C₂Tₓ/GCE | DPV | 0.1-1000 | 0.052 | Chicken meat, noodle |  | [5] |
| MoSe₂@g-C₃N₄/GCE | DPV | 0.1-1285 | 0.0735 | Coffee cream, ice cream, edible oil |  | [6] |
| Mo₂C@fGO/GCE | DPV | 1-750 | 0.457 | Edible oils, snacks |  | [7] |
| SrAl₂O₄/FCNF/GCE | i-t | 0.1-1104.75 | 0.075 | Canola oil |  | [8] |
| SnS2-Co1Fe2@N-CNTs/GCE | DPV | 0.1-1000 | 0.049 | Biscuits, cured meat |  | This work |

References

[1] B. Parasuraman, B. Ganapathi, G. Jacob, V. Raghavan, P. Thangavelu, Ultrasensitive Detection of Propyl Gallate and Vanillin in Food Products Using a Ag Decorated MXene/CdTe Quantum Dots Based Electrochemical Sensor, ACS Applied Engineering Materials. 4 (2026) 287-300, https://doi.org/10.1021/acsaenm.5c00978.

[2] M.M. Stanley, B. Sriram, S.-F. Wang, S. Kogularasu, Y.-Y. Lee, M. George, Rational confinement of ternary layered double hydroxide within three-dimensional graphene aerogel: An electrochemical tool for propyl gallate sensing, Chemical Engineering Journal. 485 (2024) 149682, https://doi.org/10.1016/j.cej.2024.149682.

[3] S. Chinnapaiyan, N.R. Barveen, S.-C. Weng, G.-L. Kuo, Y.-W. Cheng, R.A. Wahyuono, C.-H. Huang, Smartphone-based electrochemical sensing of propyl gallate in food samples by employing NiFe-Oxide decorated flexible laser-induced graphene electrode, Sensors and Actuators B: Chemical. 423 (2025) 136763, https://doi.org/10.1016/j.snb.2024.136763.

[4] G.M. Gopakumar, A. Bindu, B. Saraswathyamma, A. Ayari-Akkari, A. Akremi, P.-Y. Chen, M. Govindasamy, Redefining the monitoring of antioxidants: Interfacial charge redistribution in SrTiO3@ GCN nanocomposite for improved electrochemical detection of propyl gallate in food matrices, Innovative Food Science & Emerging Technologies. https://doi.org/10.1016/j.ifset.2025.104195.

[5] B. Parasuraman, G. Bharathi, P. Thangavelu, Non‐Enzymatic Electrochemical Sensor for Nanomolar Detection of Propyl Gallate in Food Samples Using (2D/0D) MXene/CdTe QDs Nanocomposites, ChemistrySelect. 10 (2025) e03004, https://doi.org/10.1002/slct.202503004.

[6] N.K. Sakthivel, R.P. Veerasamy, A. Akremi, T. Alshahrani, M. Govindasamy, Enhanced electrochemical detection of propyl gallate in foods using molybdenum diselenide decorated on graphitic carbon nitride modified electrode, Food Chemistry. 493 (2025) 145836-145836, https://doi.org/10.1016/j.foodchem.2025.145836.

[7] S. Abraham, J. Bhagavathsingh, E. Shaji, Z. Thaliyakuzhy, H.S. Abd‐Rabboh, C.Y. Kuo, M. Govindasamy, Electrochemical Detection of Food Antioxidant Propyl Gallate Using a Mo2C‐Modified Benzimidazole–Graphene Oxide Nanostructure, Advanced Materials Technologies. 10 (2025) e00878, https://doi.org/10.1002/admt.202500878Digital

[8] I.J.D. Priscillal, S.-F. Wang, Synchronously activated strontium aluminate nanoflakes anchored functionalized carbon nanofiber nanocomposite for sensitive amperometric detection of food additive: Propyl gallate, Food chemistry. 389 (2022) 133119, https://doi.org/10.1016/j.foodchem.2022.133119.