Flame Retardancy and Mechanical Properties of Chitosan and DOPO with Different Mass Ratios in Epoxy Resin

Junjie Wang a, Xinyu Wang a, Chenyu Zhou a, Zhiquan Pan a, Hong Zhou a,*

Supporting information

Fig. S1. Element Composition of the surface of the char residues

| EP | EP/10% CS |
| --- | --- |
| EP/10% CS1/DOPO2 | EP/10% CS2/DOPO1 |

Fig.S2. The 3D TG-FTIR images of EP, EP/10% CS1/DOPO2 and EP/10% CS2/DOPO1 at various temperatures

Fig. S3. Time curves of EP, EP/10% CS1/DOPO2 and EP/10% CS2/DOPO1 starting to decompose into gases

Table S1 The flame retardancy effects of flame inhibition, charring, and formation of a protective barrier layer for EP/10% CS1/DOPO2 and EP/10% CS2/DOPO1samples

| sample | Flame-inhibition effect | Charring effect | Barrier and protective effect |
| --- | --- | --- | --- |
| EP/10% CS1/DOPO2 | 27.60% | 8.23% | 20.36% |
| EP/10%CS2/DOPO1 | 0.68% | 4.06% | 36.52% |

Table S2 XPS data of different chemical bonds for EP, EP/10% CS1/DOPO2 and EP/10% CS2/DOPO1

| Samples | C1s (area (%)) |  |  | N1s (Area (%)) |  | O1s (Area (%)) |  | P2s (Area (%)) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | - H C-C | C-OHC-N C-O-P | C=CC=O | C-N | C=N | C-O-CC-OH C-O-P | C=OP=O | C-O-P | P=O |
| EP | 54 | 25 | 21 | 22 | 78 | 69 | 31 | 0 | 0 |
| EP/10% CS1/DOPO2 | 59 | 28 | 13 | 24 | 76 | 73 | 27 | 68 | 32 |
| EP/10% CS2/DOPO1 | 62 | 14 | 24 | 19 | 81 | 66 | 34 | 56 | 44 |