Flame Retardancy and Mechanical Properties of Chitosan and DOPO with Different Mass Ratios in Epoxy Resin

Junjie Wang a, Xinyu Wang a, Chenyu Zhou a, Zhiquan Pan a, Qingrong Cheng a, Hong Zhou a,*

a College of Chemistry and Environmental Technology, Wuhan Institute of Technology, Wuhan, China.

* Corresponding author, E-mail: hzhouh@126.com

Contents:

Fig. S1

Fig. S2

Fig. S3

Table S1

Table S2

Table S3

Fig. S1. Element Composition of the surface of the char residues

| EP | EP/10% CS |
| --- | --- |
| EP/10% CS1/DOPO2 | EP/10% CS2/DOPO1 |

Fig.S2. The 3D TG-FTIR images of EP, EP/10% CS1/DOPO2 and EP/10% CS2/DOPO1 at various temperatures

Fig. S3. Time curves of EP, EP/10% CS1/DOPO2 and EP/10% CS2/DOPO1 starting to decompose into gases

Table S1 Thermal decomposition parameters of EP and EP/CS/DOPO samples under air atmosphere

|  | Air |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Sample | Tmax1% (°C) | αmax1 (%/℃) | Tmax2% (°C) | αmax2 (%/℃) | Residue at 750 °C (%) |
| EP | 380.4 | 9.7 | 576.5 | 2.9 | 0.8 |
| EP/10% CS | 311.1 | 8.5 | 532.3 | 11.5 | 0.2 |
| EP/10% DOPO | 309.0 | 7.6 | 537.4 | 11.5 | 1.3 |
| EP/10% CS1/DOPO2 | 309.9 | 7.7 | 536.6 | 11.6 | 1.1 |
| EP/10% CS2/DOPO1 | 309.7 | 7.7 | 532.6 | 11.7 | 0.6 |

Table S2 The flame retardancy effects of flame inhibition, charring, and formation of a protective barrier layer for EP/10% CS1/DOPO2 and EP/10% CS2/DOPO1samples

| sample | Flame-inhibition effect | Charring effect | Barrier and protective effect |
| --- | --- | --- | --- |
| EP/10% CS1/DOPO2 | 27.60% | 8.23% | 20.36% |
| EP/10%CS2/DOPO1 | 0.68% | 4.06% | 36.52% |

Table S3 XPS data of different chemical bonds for EP, EP/10% CS1/DOPO2 and EP/10% CS2/DOPO1

| Samples | C1s (area (%)) |  |  | N1s (Area (%)) |  | O1s (Area (%)) |  | P2s (Area (%)) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | - H C-C | C-OHC-N C-O-P | C=CC=O | C-N | C=N | C-O-CC-OH C-O-P | C=OP=O | C-O-P | P=O |
| EP | 54 | 25 | 21 | 22 | 78 | 69 | 31 | 0 | 0 |
| EP/10% CS1/DOPO2 | 59 | 28 | 13 | 24 | 76 | 73 | 27 | 68 | 32 |
| EP/10% CS2/DOPO1 | 62 | 14 | 24 | 19 | 81 | 66 | 34 | 56 | 44 |