Table 4. Comparison of imidazolium-based ionic liquids as catalysts for butyl acetate synthesis*.

| Imidazolium-based catalyst |  | Ester yield, % |  | Hammett acidity (H₀) |  | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| [C1Im]+[HSO4]– |  | 20 |  | 1.94 |  | [36] |
| [C1Im]+[BF4]– |  | 15 |  | n.d. |  | [36] |
| [C3SO3(CH2=CH2)Im]+[HSO4]– |  | 66 |  | n.d. |  | [37] |
| [POM-Iml]2+[HPW12O40]2– |  | 73 |  | n.d. |  | [38] |
| [C1Im]+[HSO4]– |  | 18 |  | 1.92 |  | [39] |
| [C3SO3Hlm]+[HSO4]– |  | 36 |  | 1.57 |  | [39] |
| [C3SO3Hlm]+[CH3SO4]– |  | 37 |  | 1.54 |  | [39] |
| [C3SO3HBnzlm]2+[HSO4]2– |  | 68 |  | 0.98 |  | [39] |
| [Im]+[C4O4H]– |  | 16 |  | 1.90 |  | this work |
| Non-catalyzed reaction |  | 6 |  | 2.82** |  | this work |

*Reaction conditions: reaction temperature of 80°C; 2 h of reaction.

**Hammett acidity value for bare acetic acid [40] in a non-catalyzed reaction.