Supplementary Information for

Layer Number Dependent Ferroelasticity in 2D Ruddlesden-Popper Organic-inorganic Hybrid Perovskites

Xun Xiao1, Jian Zhou2, Kepeng Song3, Jingjing Zhao1, Yu Zhou1, Peter Neil Rudd1, Yu Han3, Ju Li2,* and Jinsong Huang1,*

1 Department of Applied Physical Sciences, University of North Carolina, Chapel Hill, NC 27599, USA.

2 Department of Nuclear Science and Engineering and Department of Materials Science and Engineering, Massachusetts Institute of Technology, Cambridge, MA 02139, USA.

3 Advanced Membranes and Porous Materials (AMPM) Center, Physical Sciences and Engineering Division, King Abdullah University of Science and Technology (KAUST), Thuwal, Saudi Arabia

Supplementary Figure 1: XRD patterns for BAI-N1, BAI-N2 and BAI-N3 single crystals, respectively.

Supplementary Figure 2: (a) Cross section TEM for BAI-N2, (b) is the zoom-in image corresponding to golden rectangular mark in (a).

Supplementary Figure 3: scheme of applying external stress on layered perovskite crystals

Supplementary Figure 4: (a), (b) and (c) are non-polarized optical microscope images for BAI-N1, BAI-N2 and BAI-N3 single crystals, respectively.

Supplementary Note 1: DFT calculation models for BAI-N1 and BAI-N2.

BAI-N1 (VASP form)

BAI-N1

1.0000000000

8.55045    0.00000    0.000-0

0.00000    8.55045    0.00000

0.00000    0.00000   27.53405

H    C    N    Pb   I

96    32     8     4    16

Direct

0.264512	0.434668	0.722538

0.448592	0.219584	0.732024

0.324343	0.318234	0.808609

0.340386	0.959671	0.806062

0.206742	0.058346	0.881770

0.127183	0.291085	0.504313

0.337771	0.088998	0.511514

0.341462	0.293102	0.419305

0.571102	0.118750	0.418764

0.409909	0.119418	0.340055

0.419348	0.785804	0.234368

0.228105	0.569407	0.230342

0.331166	0.650854	0.311553

0.976041	0.598218	0.316671

0.111149	0.652115	0.398157

0.048159	0.767957	0.025720

0.243944	0.559132	0.002678

0.160509	0.814605	0.928055

0.360865	0.630670	0.895265

0.140022	0.714567	0.839713

0.609833	0.695036	0.719338

0.786989	0.919224	0.724617

0.659479	0.808683	0.800467

0.997433	0.920135	0.816562

0.866364	0.812146	0.892932

0.761190	0.572377	0.506677

0.952090	0.780775	0.505935

0.700299	0.829664	0.427189

0.912974	0.039499	0.433045

0.787302	0.979469	0.352820

0.769325	0.053132	0.237126

0.566141	0.246391	0.238012

0.691376	0.185798	0.320194

0.580734	0.520869	0.301025

0.734967	0.517728	0.378039

0.692234	0.081292	0.019149

0.870840	0.264780	0.986111

0.541370	0.339139	0.946510

0.752064	0.523875	0.917452

0.532423	0.450864	0.860344

0.762813	0.569270	0.723503

0.945431	0.786467	0.732416

0.823515	0.685290	0.809048

0.836008	0.044082	0.807266

0.707277	0.940451	0.883264

0.610521	0.701575	0.505419

0.798131	0.920666	0.508319

0.849973	0.687211	0.424635

0.053816	0.892338	0.423570

0.924781	0.830351	0.341787

0.912681	0.190051	0.236724

0.707522	0.396775	0.229671

0.822490	0.342957	0.310869

0.465221	0.362941	0.321003

0.623280	0.359512	0.400348

0.549459	0.214127	0.025669

0.749394	0.422825	0.004542

0.656385	0.178792	0.927400

0.862369	0.362126	0.896686

0.642470	0.287148	0.839823

0.112177	0.308058	0.718915

0.292039	0.084904	0.723852

0.161505	0.193733	0.799464

0.499857	0.085197	0.816528

0.363233	0.189010	0.892620

0.267538	0.430494	0.502144

0.474526	0.242022	0.500846

0.214193	0.134403	0.430924

0.457477	0.960448	0.439571

0.300242	0.960844	0.363145

0.270406	0.917011	0.234129

0.076512	0.711558	0.234524

0.186074	0.797631	0.315859

0.112326	0.447982	0.305744

0.244021	0.499944	0.385478

0.191871	0.900202	0.020173

0.369817	0.716307	0.986520

0.040077	0.655745	0.944990

0.248481	0.468673	0.914666

0.029530	0.549085	0.858577

0.251155	0.309781	0.675787

0.395661	0.984524	0.895879

0.251564	0.314222	0.550735

0.501798	0.935460	0.349846

0.297626	0.796854	0.186889

0.042839	0.456095	0.394353

0.209424	0.752901	0.060562

0.205596	0.524893	0.825273

0.750020	0.692875	0.676546

0.895676	0.017008	0.896717

0.731159	0.695941	0.553240

0.987761	0.028303	0.344854

0.791335	0.171447	0.189405

0.532966	0.544150	0.390512

0.711008	0.225480	0.060526

0.709320	0.478124	0.827698

0.324028	0.198550	0.739693

0.289042	0.203687	0.793805

0.372390	0.073727	0.821801

0.332849	0.076387	0.875783

0.356264	0.199937	0.492130

0.333240	0.179125	0.437811

0.453709	0.065812	0.416598

0.415331	0.018142	0.364624

0.196060	0.682835	0.246305

0.209830	0.679925	0.301283

0.097512	0.561544	0.324018

0.124360	0.541357	0.378341

0.246567	0.679631	0.988659

0.163140	0.691674	0.940190

0.239834	0.590128	0.901295

0.148921	0.594513	0.853716

0.820736	0.805908	0.740338

0.786935	0.799789	0.794509

0.870105	0.929900	0.822488

0.833354	0.924813	0.876625

0.832735	0.806600	0.493347

0.821816	0.805032	0.438298

0.931826	0.925373	0.415446

0.907565	0.941817	0.360875

0.684595	0.284834	0.248002

0.703294	0.301025	0.302661

0.582922	0.414897	0.323740

0.619576	0.461218	0.375943

0.748576	0.303990	0.989194

0.663118	0.300030	0.940919

0.741831	0.403878	0.902958

0.651690	0.405414	0.855206

0.232763	0.320164	0.712924

0.243822	0.315376	0.513121

0.302030	0.802608	0.224500

0.169601	0.780869	0.025884

0.730615	0.683335	0.713644

0.727652	0.686882	0.515659

0.796039	0.168311	0.227043

0.670836	0.200330	0.025663

0.208855	0.238425	0.125609

0.709777	0.737072	0.124658

0.312015	0.751780	0.612859

0.815755	0.253838	0.612876

0.524211	0.053345	0.134787

0.023966	0.921793	0.134976

0.878726	0.406471	0.119273

0.379588	0.567637	0.117064

0.237507	0.192740	0.009316

0.736560	0.786833	0.008461

0.713027	0.761924	0.243246

0.206622	0.204089	0.244574

0.987130	0.580952	0.615417

0.135188	0.074088	0.613030

0.631025	0.935218	0.615055

0.490350	0.428195	0.613812

0.829992	0.291412	0.495869

0.314673	0.717190	0.495699

0.318421	0.720981	0.730304

0.819519	0.281865	0.730435

BAI-N2 (VASP form)

BAI-N2

1.00000000000000

8.51265    0.00000    0.00000

0.00000    8.68462    0.00000

0.00000    0.00000   40.90000

H    C    N    Pb   I

120    36    12     8    28

Direct

0.25061	0.43368	0.48401

0.43541	0.22094	0.49147

0.29916	0.32052	0.54169

0.31859	0.96732	0.54068

0.17774	0.06523	0.59089

0.10986	0.28835	0.18262

0.31148	0.08332	0.18376

0.32191	0.29575	0.12333

0.54033	0.10618	0.12198

0.38802	0.14190	0.06850

0.40375	0.78299	0.98786

0.21453	0.56789	0.98748

0.32640	0.65669	0.04107

0.97221	0.59298	0.04668

0.10784	0.66079	0.10071

0.03217	0.77076	0.69521

0.21450	0.55813	0.67907

0.15920	0.81925	0.62924

0.35121	0.62507	0.60830

0.14571	0.72675	0.56886

0.59460	0.69617	0.47962

0.76768	0.91817	0.48510

0.63660	0.80459	0.53531

0.97480	0.91389	0.54790

0.83914	0.80488	0.59854

0.74721	0.57046	0.18127

0.93732	0.77881	0.17941

0.67519	0.81817	0.12801

0.87981	0.03202	0.12949

0.75667	0.95835	0.07570

0.76259	0.05352	0.99215

0.56191	0.24894	0.99369

0.68458	0.17772	0.04817

0.60210	0.51895	0.03870

0.74462	0.48284	0.09187

0.68648	0.08967	0.68872

0.86077	0.27648	0.66614

0.52798	0.32690	0.63810

0.72910	0.52204	0.61910

0.51593	0.43673	0.58006

0.74806	0.57342	0.48348

0.92857	0.78983	0.49067

0.80137	0.68314	0.54122

0.81333	0.03667	0.54134

0.68010	0.93252	0.59191

0.59573	0.69696	0.18219

0.78047	0.91388	0.18184

0.82961	0.68214	0.12559

0.02769	0.89237	0.12402

0.90257	0.81703	0.06950

0.90795	0.18680	0.99035

0.70812	0.39353	0.98848

0.82660	0.32436	0.04262

0.46971	0.37026	0.04868

0.61531	0.33240	0.10292

0.54010	0.21663	0.69296

0.73024	0.42699	0.67731

0.65559	0.17678	0.62607

0.85065	0.37002	0.60551

0.63745	0.28282	0.56653

0.10068	0.30820	0.47901

0.27840	0.08936	0.48458

0.13825	0.19600	0.53438

0.47696	0.09235	0.54845

0.33354	0.19521	0.59874

0.25249	0.42270	0.17916

0.45560	0.22838	0.17704

0.18376	0.14694	0.13027

0.41097	0.95601	0.13272

0.26187	0.98991	0.08026

0.25406	0.91076	0.98844

0.06086	0.70584	0.99077

0.17675	0.79718	0.04452

0.11483	0.44938	0.03995

0.24737	0.51457	0.09313

0.18029	0.89624	0.69104

0.35394	0.70420	0.66970

0.02461	0.67112	0.63892

0.22341	0.47370	0.61949

0.01979	0.57164	0.57973

0.24922	0.31444	0.45184

0.36694	0.99423	0.60133

0.24447	0.30987	0.21228

0.46315	0.95189	0.07232

0.27542	0.78996	0.95670

0.04738	0.46500	0.09970

0.19449	0.75202	0.71852

0.19993	0.53586	0.55923

0.73993	0.69547	0.45174

0.86918	0.00624	0.60163

0.72490	0.69088	0.21310

0.95554	0.01492	0.07026

0.77873	0.16991	0.95969

0.54293	0.52334	0.09878

0.70353	0.23463	0.71604

0.69311	0.47501	0.55865

0.70655	0.37135	0.81672

0.74596	0.09481	0.82126

0.28151	0.88094	0.86468

0.20934	0.61551	0.85510

0.26719	0.91521	0.82147

0.20271	0.64363	0.81469

0.70414	0.38102	0.86059

0.74346	0.10527	0.86209

0.55086	0.28014	0.83923

0.41651	0.78919	0.83721

0.06888	0.72864	0.83898

0.89093	0.18992	0.84087

0.62254	0.70344	0.31064

0.89866	0.77194	0.31145

0.12209	0.30594	0.35335

0.39761	0.23555	0.35313

0.12744	0.30757	0.30943

0.40227	0.23638	0.31227

0.62570	0.70257	0.35456

0.90093	0.77229	0.35230

0.73942	0.56405	0.33210

0.24090	0.44489	0.33223

0.29466	0.10266	0.33205

0.79519	0.90602	0.33209

0.30920	0.20105	0.49551

0.26684	0.20695	0.53162

0.34862	0.08028	0.55126

0.30465	0.08385	0.58741

0.33421	0.19374	0.17148

0.30652	0.18186	0.13484

0.41839	0.06529	0.11911

0.38155	0.03594	0.08316

0.18256	0.68016	0.99799

0.20259	0.68118	0.03493

0.09598	0.56258	0.05148

0.12556	0.55012	0.08817

0.22765	0.67696	0.67014

0.15106	0.69764	0.63689

0.22601	0.59431	0.61095

0.14353	0.60759	0.57796

0.80250	0.80641	0.49547

0.76500	0.79670	0.53177

0.84663	0.92348	0.55140

0.80690	0.91652	0.58774

0.81567	0.80170	0.17175

0.79903	0.79776	0.13476

0.90371	0.91870	0.11843

0.87893	0.92775	0.08156

0.68248	0.28244	0.00023

0.70407	0.29184	0.03706

0.59175	0.40964	0.05221

0.62473	0.43837	0.08834

0.73596	0.30890	0.66765

0.65301	0.29680	0.63488

0.72688	0.40339	0.60940

0.63866	0.39952	0.57696

0.67586	0.31024	0.83924

0.29586	0.83052	0.84035

0.69436	0.68222	0.33236

0.19512	0.32699	0.33180

0.22239	0.32138	0.47661

0.22881	0.31017	0.18707

0.28490	0.79793	0.98196

0.15435	0.77993	0.69515

0.71630	0.68555	0.47659

0.71482	0.68287	0.18784

0.78958	0.16646	0.98497

0.66234	0.20652	0.69277

0.18709	0.69732	0.83717

0.77026	0.16626	0.84095

0.32982	0.21800	0.33234

0.82975	0.79046	0.33204

0.20285	0.24814	0.75810

0.21718	0.24416	0.91849

0.70103	0.75173	0.75911

0.71608	0.74082	0.91857

0.27585	0.75037	0.25231

0.77942	0.24863	0.25210

0.28086	0.75716	0.41099

0.78139	0.25338	0.41089

0.52539	0.06995	0.77015

0.01530	0.94163	0.76785

0.88104	0.43062	0.75023

0.36797	0.58244	0.75832

0.23172	0.18849	0.68102

0.71993	0.79791	0.68156

0.90051	0.42811	0.92319

0.39010	0.56764	0.91265

0.54618	0.06755	0.91338

0.03457	0.92810	0.91619

0.75987	0.73720	0.83952

0.21028	0.19574	0.99673

0.69875	0.77383	0.99735

0.17682	0.27712	0.83844

0.95149	0.57377	0.25985

0.09992	0.06965	0.25140

0.59660	0.93289	0.25129

0.45310	0.42768	0.25945

0.80892	0.29110	0.17413

0.29530	0.70603	0.17412

0.60277	0.93610	0.41261

0.45325	0.42915	0.40512

0.95465	0.57923	0.40527

0.10276	0.07381	0.41233

0.26129	0.80401	0.33175

0.80192	0.29002	0.48928

0.29640	0.71826	0.48940

0.76135	0.20382	0.33164

* Correspondence to J.H. (email: jhuang@unc.edu) or to J.L. (email: liju@mit.edu)