Supplementary Material

of

Predictive parametric inference of lithium-ion battery degradation trajectory through high-throughput physics-based simulation

Peiheng Lai1, Chenhang Zheng1, Hao Wu1, Hao Cheng1, Bing Li2, Viktor Korzhikov-Vlakh3, Xiaohe Song4, Minggang Zeng5,*, Ming Yang1,6,7,*

1 Department of Physics and Material, The Hong Kong Polytechnic University, Hong Kong SAR, China

2 Harbin Institute of Technology, School of Chemistry and Chemical Engineering, Harbin, 150001 China

3 Institute of Chemistry, Saint-Petersburg State University, 198504 St. Petersburg, Russia

4 Shenzhen Eacomp Technology Co., Ltd., Shenzhen 518000, China

5 Institute of Advanced Intelligence and Computing (IAIC), Agency for Science, Technology and Research (A*STAR), 1 Fusionopolis Way, #16–16 Connexis, Singapore 138632, Republic of Singapore

6 Research Centre on Data Sciences & Artificial Intelligence, The Hong Kong Polytechnic University, Kowloon, Hong Kong SAR, China

7 Research Centre for Nanoscience and Nanotechnology, The Hong Kong Polytechnic University, Kowloon, Hong Kong SAR, China

Corresponding Author Email: kevin.m.yang@polyu.edu.hk (Ming Yang), Zeng_Minggang@a-star.edu.sg (Minggang Zeng)

Table of Content

Supplementary Note 1: P2D modeling	3

Supplementary Note 2: Bayesian scoring for parametric inference	6

Supplementary Note 3: Anchor-neighborhood inference for prediction	8

Supplementary Note 1: P2D modeling

The physics-based simulation (PBS) data were generated using a pseudo-two-dimensional (P2D) lithium-ion battery model coupled with degradation sub-models. The P2D model describes lithium transport in electrolyte and solid particles, charge conservation in both phases, and interfacial electrochemical reactions. In the electrolyte phase, lithium-ion transport was governed by

∂(εece)∂t=∇⋅Deeff∇ce+1-t+0Fasj#1

where where ce is electrolyte concentration, εe is electrolyte volume fraction, Deeff is the effective electrolyte diffusivity, t+0 is the transference number, F is the Faraday constant, as is the specific interfacial surface area, and j is the total interfacial current density.

Lithium diffusion inside the active-material particles was described by spherical diffusion,

∂cs∂t=1r2∂∂rDsr2∂cs∂r#2

with boundary condition

-Ds∂cs∂rr=Rs=jintF#3

where cs is the solid-phase lithium concentration, Ds is the solid diffusivity, Rs is the particle radius, and jint is the intercalation current density.

Charge conservation in the solid and electrolyte phases followed

∇⋅σeff∇ϕs=asj#4

and

∇⋅κeff∇ϕe+∇⋅κDeff∇lnce=-asj#5

where ϕs and ϕe are solid- and electrolyte-phase potentials, and σeff, κeff, and κDeff are effective transport coefficients.

The intercalation reaction was represented by Butler-Volmer kinetics,

jint=2i0sinhFη2RT#6

where i0 is the exchange current density, R is the ideal gas constant, T is temperature, and η is the interfacial overpotential.

Degradation was introduced through sub-models for solid electrolyte interphase (SEI) growth, lithium plating and dead lithium decay, and loss of active material (LAM). SEI growth was initialized from the sampled initial SEI thickness,

LSEIt=0=LSEI0#7

The solvent-diffusion-limited SEI side reaction was controlled by the sampled SEI solvent diffusivity Dsol,

jSEI=FDsolcsolLSEIexp-αSEIFηSEIRT#8

where jSEI is the SEI side-reaction current density, csol is the solvent concentration at the SEI/electrolyte interface, αSEI is the SEI charge-transfer coefficient, ηSEI is the SEI side-reaction overpotential. The SEI thickness evolved as

dLSEIdt=VSEIFjSEI#9

where VSEI is the SEI molar volume. Thus, LSEI0 determined the initial SEI resistance, while Dsol controlled the rate of solvent transport through the SEI layer and hence the SEI-growth rate.

Lithium plating was controlled by the sampled plating kinetic rate constant kpl. The plating current density was written as

jpl=FkplcLiexp-αplFηplRT#10

where jpl is the lithium-plating current density, cLi is the lithium concentration associated with the plating reaction, αpl is the plating charge-transfer coefficient, and ηpl is the plating overpotential. The plated lithium inventory evolved according to

dcplateddt=-asjplF-γdeadcplated#11

where cplated is the concentration or inventory of plated lithium and as is the specific interfacial surface area. The second term describes conversion of plated lithium into electrochemically inactive dead lithium. The sampled dead lithium decay constant γdead therefore controlled the irreversible loss from the plated lithium reservoir,

dcdeaddt=γdeadcplated#12

where cdead is the concentration or inventory of electrochemically inactive dead lithium.

Loss of active material in the negative electrode was represented by reaction-driven and stress-driven contributions. The negative-electrode active-material volume fraction evolved as

dεs,ndt=-ΓLAM,n#13

where εs,n is the negative-electrode active-material volume fraction and ΓLAM,n is the negative-electrode LAM rate. The LAM rate was written as

ΓLAM,n=βLAMkstressσn-σcrσcr+#14

where βLAM is the sampled NE LAM proportional term, kstress is the stress-driven LAM rate constant, σn is the mechanical stress in negative-electrode particles, σcr is the sampling defined critical stress.

Supplementary Note 2: Bayesian scoring for parametric inference

Bayesian full-trajectory inference was used to map each experimental degradation curve into the PBS-emulated latent physical space. For an experimental cell i, the observed degradation trajectory was represented by SOH-cycle positions yi=ciss=10080 where cis denotes the cycle number at given data reached SOH level s. For each sampled parameter vector θk, the PBS emulator generated a corresponding trajectory yk=cs;θks=10080.

Experimental and PBS-emulated trajectories were normalized within their own cycle ranges before shape comparison. This normalization allowed the scoring function to focus on relative degradation shape and pacing rather than absolute lifetime scale.

For each experimental cell, a high-throughput emulator search first identified a candidate pool of PBS-emulated trajectories with low trajectory mismatch. Candidate k for cell i was then assigned a posterior-like probability,

wik=exp-Eikk'∈Kiexp-Eik'#15

where Ki is the candidate pool for given cell i, and Eik is the total scoring energy. The candidate with the highest wik was selected as the inferred effective parameter set.

The total energy combined trajectory fitting and prior/constraint terms,

Eik=λtrajDtrajyi,yk+λgroupDgroupθk+λdensDdensθk+λTDTθk,Ti#16

Here, Dtrajyi,yk measured full-trajectory mismatch, Dgroupθk imposed hierarchical group consistency, Ddensθk penalized poorly supported candidates, DTθk,Ti imposed temperature-informed constraints. The coefficients λ controlled the relative weight of each term.

The trajectory-mismatch term contained two components. The first compared normalized SOH-crossing positions,

Dpos=1Ss∈Scis-cks2#17

where cis and cks are respective normalized cycle positions. The second compared coarse degradation slopes over predefined SOH segments,

Dslope=1Bb∈Bmib-mkb2#18

The segment set B included 100-95%, 95-90%, 90-85%, and 85-80% SOH. The final trajectory mismatch was

Dtraj=Dpos+λslopeDslope#19

The group prior encouraged cells with similar operating conditions to occupy nearby regions in latent parameter space. If μg denotes the current group center for operating group g, the group penalty was written as

Dgroupθk=θk-μgiΣg-12#20

where Σg-1 controls the allowed spread within the group.

The density prior discouraged isolated edge candidates. For each candidate θk, its local support was estimated from the distance to neighboring PBS-emulated samples,

Ddensθk=1Knnl∈NKkθk-θl2#21

Candidates with large nearest-neighbor distances were penalized because they were located in sparse regions of the sampled PBS manifold.

The temperature-informed term constrained selected effective parameters using expected temperature trends. For example, SEI solvent diffusivity was encouraged to increase with temperature, while lithium plating tendency was encouraged to decrease under warmer conditions. This term was implemented as a monotonic or Arrhenius-informed consistency penalty across temperature groups,

DTθk,Ti=m∈MTρmzmθk-fmTi2#22

where MT denotes temperature-sensitive effective parameters, zmθk is the normalized parameter value, and fmTi encodes the expected temperature trend, following Arrhenius relations.

The inferred parameters were interpreted as effective degradation descriptors in the PBS-emulated latent physical space. They were used for relative comparison across cells, temperatures, and protocols. They were not treated as uniquely identifiable physical constants, because multiple parameter combinations can generate similar degradation trajectories and many aging-related parameters cannot be directly observed in experiments.

Supplementary Note 3: Anchor-neighborhood inference for prediction

Anchor-neighborhood inference was developed for early-to-late degradation prediction under limited experimental data. The goal was to predict the later SOH trajectory of a test cell using only its early-life degradation segment. The method used the PBS emulator as a physically constrained trajectory generator and used Bayesian posterior information from one complete anchor cell to define a condition-specific local search space.

For each operating-condition group g, one complete experimental cell was selected as the anchor cell. This anchor provided a reference degradation trajectory for the group and constrained the candidate PBS-emulated parameter space used during prediction. From Bayesian full-trajectory inference, the anchor cell had a posterior-like candidate distribution θak,wakk∈Ka, where θak is candidate k for anchor cell a, and wak is its posterior-like probability. The anchor neighborhood was defined from the high-probability region of this distribution,

Ng=θak:wak≥τg#23

or equivalently from the top-K posterior candidates,

Ng=TopKθak,wak#24

This local neighborhood formed the condition-specific PBS-emulated manifold searched during early-life inference.

For a test cell i in group g, only the early SOH segment was provided. If the observed early window ended at SOH level s0, the available trajectory was yiearly=ciss=100s0. The three prediction tasks used s0=95, 90, 85, corresponding to prediction windows of 94-80%, 89-80%, and 84-80% SOH. Each candidate θk∈Ng generated a complete emulator trajectory yk=cs;θks=10080. Only the early segment of this trajectory was used for candidate scoring ykearly=cs;θks=100s0. The early-life inference score was the same to Supplementary Note 2.

This anchor-neighborhood design reduced the experimental data requirement by using only one complete cell per operating-condition group to define the local candidate space. It also restricted predictions to PBS-derived degradation trajectories, which helped prevent physically implausible extrapolation when only sparse early-life information was available.