- Table. S1 Appearance characteristics of Kangxi period underglaze copper-red specimens

| Sample ID | Appearance characteristics |
| --- | --- |
| QYLH-1 | The body is relatively thin with a fine, lustrous fracture surface. The glaze exhibits a slight bluish tint. The pattern is rendered using outline tracing with distinct lines. The pigment displays a bright-red hue, with a few green spots scattered within the red pigment area. |
| QYLH-2 | The body is relatively thin, with a fine and lustrous fracture surface; the glaze has a faint bluish tint. The pattern is rendered using the line-drawing technique, with clear lines; the red pigment is slightly dull. |
| QYLH-3 | The body is relatively thin, with a fine and lustrous fracture surface; the glaze has a faint bluish tint. The pattern is rendered using the line-drawing technique, with clear lines; the red pigment is slightly dull. |
| QYLH-4 | The body is relatively thin, with a fine and lustrous fracture surface; the glaze has a faint bluish tint. The pattern is rendered using the line-drawing technique, with clear lines; the red pigment is a deep red colour |
| QYLH-5 | The cross-section of the bowl’s base is fine-grained and lustrous; the base bears the blue-and-white mark ‘Made during the Kangxi period of the Great Qing’ (大清康熙年制); the glaze has a faint bluish tinge, and the interior of the bowl features patterns rendered in line-drawing technique with relatively clear lines; the red pigment varies in depth, with some instances of colour loss. |
| QYLH-6 | The body is relatively thin, with a fine-grained and lustrous cross-section; the glaze has a faint bluish tinge, and the exterior features a design of dragon claws rendered in line-drawing technique, with clear lines and a relatively even red colour. |
| QYLH-7 | The body is rather thin, with a fine-grained and lustrous cross-section; the glaze has a faint bluish tinge, and the exterior is decorated with a design executed in line drawing, with clear lines and a vivid red colour, interspersed with a few green spots within the red pigment areas. |
| QYLH-8 | The body is relatively thin, with a fine-grained and lustrous cross-section; the glaze has a slight bluish tinge, The pattern is rendered using the line-drawing technique, with clear lines and a red colour that tends towards black. |
| QYLH-9 | The body is relatively thin, with a fine-grained and lustrous cross-section; the glaze has a slight bluish tinge, The pattern is rendered using the line-drawing technique, featuring clear lines and a deep red colour, with a few green spots interspersed amongst the red pigment areas. |
| QYLH-10 | The body is relatively thin, with a fine-grained and lustrous cross-section; the glaze has a faint bluish tinge, The pattern is rendered using the line-drawing technique, with clear lines and a relatively pale red colour, some of which exhibits colour loss. |
| QYLH-11 | The body is relatively thin, with a fine and lustrous fracture surface; the glaze has a faint bluish tint. The pattern is rendered using the line-drawing technique, with clear lines; the red pigment is slightly dull. |
| QYLH-12 | The base of the bowl is damaged; the cross-section is fine-grained and lustrous. The base bears the blue-and-white mark ‘Made during the Kangxi period of the Qing Dynasty’; the glaze has a faint bluish tinge, and the interior of the bowl features patterns executed in line-drawing technique, with clear lines and a slightly subdued red colour. |
| QYLH-13 | The base of the bowl is broken; the cross-section reveals a fine-grained and lustrous texture; the glaze has a faint bluish tinge; the patterns are rendered using line-drawing techniques, with clear lines and a slightly subdued red colour. A few green spots interspersed amongst the red pigment areas. |
| QYLH-14 | The base of the bowl is broken; the cross-section is fine-grained and lustrous; the base bears the blue-and-white mark ‘Da Qing Kang Nian’; the glaze has a slight bluish tinge; the interior features a design executed in line drawing, with clear lines and a slightly subdued red colour. |
| QYLH-15 | The base of the bowl is broken; the cross-section reveals a fine, lustrous texture, and the base bears the blue-and-white mark ‘Xi Nian Zhi’; the glaze has a faint bluish tinge, and the interior features designs executed in line-drawing technique, with clear lines and a slightly subdued red colour. |
| QYLH-16 | The base of the bowl is broken; the cross-section reveals a fine, lustrous texture, and the base bears the blue-and-white mark ‘Da Qing Xi Nian’; the glaze has a faint bluish tinge, and the interior features patterns rendered in line drawing, with clear lines and a slightly subdued red colour. |
| QYLH-17 | The base of the bowl is broken; the cross-section reveals a fine, lustrous texture, and the base bears the mark ‘Xi Nian’ in blue-and-white; the glaze has a faint bluish tinge, and the interior features patterns rendered in line drawing, with clear lines; the red pigment is somewhat dull. A few green spots interspersed amongst the red pigment areas. |
| QYLH-18 | The base of the bowl is broken; the cross-section is fine-grained and lustrous, with the mark ‘大’ written in blue-and-white on the base; the glaze has a faint bluish tinge; the interior features a design executed in line-drawing technique, with relatively clear lines; the red pigment is pure. A few green spots interspersed amongst the red pigment areas. |
| QYLH-19 | The base of the bowl is broken; the cross-section reveals a fine, lustrous texture, and the base bears the blue-and-white mark ‘Kang Zhi’; the glaze has a faint bluish tinge; the interior features a design executed in line-drawing technique, with relatively clear lines; the red pigment is on the deeper side. A few green spots interspersed amongst the red pigment areas. |
| QYLH-20 | The body is relatively thin; the cross-section is fine-grained and lustrous; the glaze has a slight bluish tinge; the design on the exterior is executed in line drawing, with clear lines; the red pigment is on the darker side. A few green spots interspersed amongst the red pigment areas. |

Table .S2 Chemical composition of the pigments in specimens (wt%)

| Sample ID | Na2O | MgO | Al2O3 | SiO2 | K2O | CaO | TiO2 | Fe2O3 | CuO | n(SiO2/Al2O3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| QYLH-1-RP | 2.90 | 0.50 | 15.03 | 70.76 | 3.44 | 5.94 | 0.08 | 0.36 | 0.32 | 8.00 |
| QYLH-1-GS | 1.93 | 0.06 | 13.99 | 74.25 | 2.33 | 6.03 | 0.02 | 0.39 | 0.37 | 9.02 |
| QYLH-2-RP | 2.81 | 0.16 | 13.94 | 73.40 | 3.42 | 4.83 | 0.04 | 0.40 | 0.10 | 8.95 |
| QYLH-3-RP | 3.48 | 0.32 | 13.55 | 72.46 | 3.42 | 5.13 | 0.06 | 0.57 | 0.08 | 9.09 |
| QYLH-4-RP | 3.23 | 0.33 | 14.18 | 72.67 | 3.50 | 4.57 | 0.06 | 0.46 | 0.06 | 8.71 |
| QYLH-5-RP | 2.58 | 0 | 14.05 | 73.85 | 3.1 | 5.16 | 0.06 | 0.53 | 0.09 | 8.94 |
| QYLH-6-RP | 3.36 | 0.19 | 13.50 | 72.32 | 3.01 | 5.88 | 0.08 | 0.67 | 0.07 | 9.11 |
| QYLH-7-RP | 4.40 | 0.39 | 14.40 | 71.63 | 3.68 | 3.88 | 0.05 | 0.58 | 0.06 | 8.46 |
| QYLH-7-GS | 3.84 | 0.03 | 14.21 | 72.21 | 3.85 | 4.21 | 0.07 | 0.58 | 0.09 | 8.64 |
| QYLH-8-RP | 3.08 | 0.26 | 13.93 | 72.73 | 3.43 | 4.90 | 0.06 | 0.62 | 0.08 | 8.88 |
| QYLH-9-RP | 3.62 | 0.00 | 13.29 | 73.90 | 3.53 | 4.22 | 0.11 | 0.46 | 0.12 | 9.45 |
| QYLH-9-GS | 3.03 | 0.00 | 13.72 | 73.82 | 3.74 | 4.22 | 0.02 | 0.57 | 0.16 | 9.15 |
| QYLH-10-RP | 2.38 | 0.00 | 14.35 | 73.55 | 3.30 | 5.06 | 0.06 | 0.63 | 0.08 | 8.71 |
| QYLH-11-RP | 3.84 | 0.16 | 14.29 | 73.57 | 3.77 | 3.07 | 0.08 | 0.45 | 0.06 | 8.75 |
| QYLH-12-RP | 4.34 | 0.04 | 13.74 | 72.24 | 3.59 | 4.46 | 0.09 | 0.50 | 0.17 | 8.94 |
| QYLH-13-RP | 3.56 | 0.00 | 13.06 | 72.99 | 3.12 | 5.63 | 0.07 | 0.65 | 0.22 | 9.50 |
| QYLH-13-GS | 4.77 | 1.11 | 14.19 | 67.24 | 2.49 | 8.85 | 0.03 | 0.71 | 0.32 | 8.06 |
| QYLH-14-RP | 2.88 | 0.00 | 14.05 | 74.02 | 3.55 | 4.03 | 0.08 | 0.54 | 0.04 | 8.96 |
| QYLH-15-RP | 3.02 | 0.19 | 14.28 | 71.95 | 3.53 | 5.42 | 0.06 | 0.55 | 0.19 | 8.57 |
| QYLH-16-RP | 3.26 | 0.07 | 14.16 | 72.90 | 3.66 | 4.44 | 0.04 | 0.48 | 0.11 | 8.75 |
| QYLH-17-RP | 2.60 | 0.04 | 14.52 | 71.50 | 3.54 | 6.30 | 0.10 | 0.54 | 0.20 | 8.37 |
| QYLH-17-GS | 3.27 | 0.11 | 14.29 | 69.26 | 3.21 | 7.98 | 0.02 | 0.88 | 0.27 | 8.24 |
| QYLH-18-RP | 1.39 | 0.09 | 14.20 | 72.71 | 3.36 | 6.79 | 0.11 | 0.71 | 0.17 | 8.70 |
| QYLH-18-GS | 3.04 | 0.00 | 14.21 | 70.14 | 3.17 | 7.66 | 0.04 | 0.77 | 0.46 | 8.39 |
| QYLH-19-RP | 3.42 | 0.00 | 13.95 | 75.14 | 3.23 | 3.29 | 0.05 | 0.24 | 0.02 | 9.16 |
| QYLH-19-GS | 3.20 | 0.00 | 13.19 | 76.12 | 3.25 | 3.52 | 0.09 | 0.31 | 0.02 | 9.81 |
| QYLH-20-RP | 5.50 | 0.03 | 13.17 | 73.02 | 3.89 | 2.98 | 0.04 | 0.36 | 0.04 | 9.43 |
| QYLH-20-GS | 2.58 | 0.00 | 13.67 | 75.16 | 4.00 | 3.53 | 0.05 | 0.40 | 0.10 | 9.35 |

- Note: RP stands for red pigment, GS stands for green spot

Table .S3 Chromaticity test result of underglaze copper-red for some specimens

| 编号 | X | Y | Z | x | y | z | L* | a* | b* |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| QYLH-1 | 22.79 | 20.04 | 18.17 | 0.37 | 0.33 | 0.3 | 51.88 | 18.05 | 6.94 |
| QYLH-4 | 18.01 | 15.43 | 13.98 | 0.38 | 0.32 | 0.29 | 45.68 | 19.36 | 6.48 |
| QYLH-8 | 18.13 | 18.57 | 19.04 | 0.33 | 0.33 | 0.34 | 50.1 | 2.65 | 2.29 |
| QYLH-9 | 12.26 | 10.93 | 9.81 | 0.37 | 0.33 | 0.3 | 39.38 | 13.63 | 6.05 |
| QYLH-10 | 38.69 | 40.64 | 42.23 | 0.32 | 0.33 | 0.35 | 69.92 | 0.21 | 2.28 |
| QYLH-20 | 15.66 | 14.36 | 13.11 | 0.36 | 0.33 | 0.3 | 44.62 | 12.34 | 5.99 |