Supporting Information

Mass Production of Calendering-Compatible Sulfur-Rich Secondary Particles via Hail-Inspired Nanostorm Technology for Advanced Metal-Sulfur Batteries

Lanxiang Fenga, Peng Yua, Xuewei Fub, Mingbo Yanga, Wei Yanga,* and Yu Wanga,*

a College of Polymer Science and Engineering, State Key Laboratory of Polymer Materials Engineering, Sichuan University, Chengdu, 610065, Sichuan, China

b School of Mechanical and Materials Engineering, Washington State University, Pullman, WA, 99164, USA

Email: weiyang@scu.edu.cn and yu.wang3@scu.edu.cn

Figure S1. SEM image of pristine a) sulfur, b) KB and c) Co2O3,scale bar is 5 um.

Figure S2. TEM image of KB with a half-open hollow structure.

Figure S3. a) N2 adsorption-desorption isotherms and b) the pore size distribution of sulfur AP@HTM-12h, sulfur SP@HSN-2min, sulfur SP@HSN-3min and sulfur SP@HSN-5min.

Figure S4. SEM image of the resulted a) sulfur SP-HSN-2min, b) sulfur SP-HSN-3min and c) sulfur SP-HSN-5min, scale bar is 5 um.

Table S1. Summarize of the pore property of all samples.

| Sample | KB | sulfur AP@HTM | sulfur SP@HSN-2min | sulfur SP@HSN-3min | sulfur SP@HSN-5min |
| --- | --- | --- | --- | --- | --- |
| S(BET) (m2/g) | 1423 | 28.5 | 12.9 | 8.1 | 3.2 |

Figure S5. SEM image of the a) sulfur AP@HTM cathode and b) sulfur SP@HSN with same sulfur loading of ~ 5 mg cm-2, scale bar is 500 um.

Figure S6. The photo of a) sulfur AP@HTM cathodes with a sulfur loading of 5 mg cm-2 and 10 mg cm-2, b) sulfur SP@HSN cathodes with a sulfur loading of 5 mg cm-2 and 15 mg cm-2.

Figure S7. SEM image of the AP@HTM cathodes after calendering at 4 Mpa in various temperature, a) 40℃, b) 60℃, c) 80℃, and the SP@HSM cathodes e) before and after calendering at 4 Mpa in various temperature, d) 40℃, e) 60℃, f) 80℃, the sacle bar is 20 um.

Figure S8. Comparsion of the thickness of sulfur AP@HTM and sulfur SP@HSN electrodes under various compression perssures.

Figure S9. SEM image of the sulfur AP@HTM cathodes a) before and b) after calnedering at 4 Mpa, sulfur SP@HSN cathodes c) before and d) after calendering at 4 Mpa.

Figure S10. The discharge/charge curves of sulfur SP@HSN cathdoes at various current desnities from 0.1C to 2C.

Figure S11. Nyquist plots of the sulfur AP@HTM and sulfur SP@HSN cathodes at open potential.

Figure S12. a) Cycle performance of pouch-cells assembled by various sulfur loading of sulfur SP@HSN cathodes. The discharge/charge curves of pouch-cells based on different cathodes with sulfur loading of b) 6 mg cm-2 c) 9 mg cm-2 and d) 12 mg cm-2.