Supplementary Material

Generative Inverse Design of Solid-State Fluoride-Ion Electrolyte Candidates in Data-Sparse Chemical Space

Joohyeon Park1,†, Seonwoo Choi1,†, Myeongjae Heo2, and Heonjae Jeong2,3,*

1 Department of Electronic Engineering, Gachon University, Seongnam, Gyeonggi 13120, South Korea

2 Department of Mechanical Engineering, Sogang University, Seoul 04107, South Korea

3 Research Institute for Smart Design & Manufacturing Technology, Sogang University, Seoul 04107, South Korea

† These authors contributed equally to this work

*Corresponding: hjeong@sogang.ac.kr

Supplementary Figures

Fig. S1. Interfacial reaction energies (eV atom-1) of the five retained FIB electrolyte candidates against six representative electrode materials (BiF3, FeF3, CuF2, Sn, Pb, and Ce). The same values are shown as a heatmap in Fig. 7 of the main text.

Supplementary Tables

Table S1. Crystal-structure information of the five retained FIB electrolyte candidates from non-spin-polarized PBE relaxations. Space groups are those assigned at the per-candidate symmetry tolerance given in the main text.

| Datasets | Chemical composition | Space group | Number of atoms | Lattice distance (Å) |  |  | Lattice angles (°) |  |  | Volume (Å3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | a | b | c | α | β | γ |  |
| Alex-MP-20 | LiNi2F5 | P1 | 8 | 4.0 | 5.4 | 5.2 | 74.3 | 67.3 | 68.2 | 94.5 |
| MP-F | CsNaNi2F6 | P4/mmm | 10 | 5.8 | 4.0 | 5.8 | 90.0 | 89.9 | 90.0 | 135.1 |
|  | NiF2 | P-1 | 9 | 3.1 | 4.7 | 7.5 | 94.7 | 102.1 | 89.9 | 106.0 |
|  | KNi2F5 | C2 | 8 | 4.1 | 3.9 | 6.6 | 90.1 | 71.7 | 90.0 | 99.9 |
|  | NaNi2F5 | Pm | 8 | 3.9 | 4.0 | 6.5 | 72.1 | 89.9 | 89.9 | 95.6 |

Table S2. Average absolute magnetic moment per Ni of the five retained FIB electrolyte candidates in the ferromagnetic (FM) and antiferromagnetic (AFM) configurations, from spin-polarized PBE+U calculations.

| Chemical composition | Ferromagnetic | Antiferromagnetic |
| --- | --- | --- |
|  | Magnetic moment (μB per Ni) | Magnetic moment (μB per Ni) |
| LiNi2F5 | 1.87 | 1.87 |
| CsNaNi2F6 | 1.89 | 1.85 |
| NiF2 | 1.82 | 1.82 |
| KNi2F5 | 1.92 | 1.91 |
| NaNi2F5 | 1.92 | 1.92 |

Table S3. Total energies per formula unit (f.u.) of the five retained FIB electrolyte candidates in the non-spin-polarized (nonmagnetic, NM), ferromagnetic (FM), and antiferromagnetic (AFM) configurations, from PBE+U calculations (spin-polarized for FM and AFM). For NiF2, whose cell contains three Ni atoms, supercells were used to ensure an even number of Ni atoms.

| Chemical composition | Non-Magnetic | Ferromagnetic | Antiferromagnetic |
| --- | --- | --- | --- |
|  | Total energy (eV f.u.-1) | Total energy (eV f.u.-1) | Total energy (eV f.u.-1) |
| LiNi2F5 | -28.28 | -34.11 | -34.10 |
| CsNaNi2F6 | -35.79 | -39.63 | -39.82 |
| NiF2 | -10.74 | -11.38 | -11.57 |
| KNi2F5 | -29.97 | -32.31 | -32.35 |
| NaNi2F5 | -29.79 | -32.01 | -32.06 |

Table S4. Space-group and crystal-system assignments of NiF2 as a function of the symmetry tolerance (symprec) from 0.10 to 0.001 Å, evaluated on the non-spin-polarized PBE-relaxed structure.

| Symprec (Å) | Space group | Crystal system |
| --- | --- | --- |
| 0.100 | C2/m | monoclinic |
| 0.090 | C2/m | monoclinic |
| 0.080 | C2/m | monoclinic |
| 0.070 | C2/m | monoclinic |
| 0.060 | C2/m | monoclinic |
| 0.050 | C2/m | monoclinic |
| 0.040 | C2/m | monoclinic |
| 0.030 | C2/m | monoclinic |
| 0.020 | C2/m | monoclinic |
| 0.010 | P-1 | triclinic |
| 0.001 | P1 | triclinic |

Table S5. Polycrystalline elastic moduli (Voigt, Reuss, and Hill averages) of the five retained FIB electrolyte candidates from non-spin-polarized PBE calculations.

| Chemical composition | Bulk modulus (GPa) |  |  | Young’s modulus (GPa) |  |  | Shear modulus (GPa) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Voigt | Reuss | Hill | Voigt | Reuss | Hill | Voigt | Reuss | Hill |
| LiNi2F5 | 65.74 | 53.35 | 59.54 | 74.62 | 61.19 | 67.90 | 28.46 | 23.37 | 25.92 |
| CsNaNi2F6 | 72.02 | 71.87 | 71.94 | 81.54 | 76.94 | 79.25 | 31.10 | 29.11 | 30.10 |
| NiF2 | 83.65 | 66.84 | 75.24 | 71.38 | 62.46 | 66.94 | 26.29 | 23.23 | 24.76 |
| KNi2F5 | 86.12 | 84.22 | 85.17 | 99.63 | 87.87 | 93.78 | 38.11 | 33.13 | 35.62 |
| NaNi2F5 | 84.27 | 66.50 | 75.38 | 81.80 | 52.61 | 67.28 | 30.56 | 19.23 | 24.90 |

Table S6. Space-group and crystal-system assignments of LiNi2F5 as a function of the symmetry tolerance (symprec) from 0.10 to 0.001 Å, evaluated on the non-spin-polarized PBE-relaxed structure.

| Symprec (Å) | Space group | Crystal system |
| --- | --- | --- |
| 0.100 | Cm | monoclinic |
| 0.090 | Cm | monoclinic |
| 0.080 | Cm | monoclinic |
| 0.070 | Cm | monoclinic |
| 0.060 | Cm | monoclinic |
| 0.050 | Cm | monoclinic |
| 0.040 | Cm | monoclinic |
| 0.030 | Cm | monoclinic |
| 0.020 | Cm | monoclinic |
| 0.010 | Cm | monoclinic |
| 0.001 | P1 | triclinic |

Table S7. Space-group and crystal-system assignments of CsNaNi2F6 as a function of the symmetry tolerance (symprec) from 0.10 to 0.001 Å, evaluated on the non-spin-polarized PBE-relaxed structure.

| Symprec (Å) | Space group | Crystal system |
| --- | --- | --- |
| 0.100 | P4/mmm | tetragonal |
| 0.090 | P4/mmm | tetragonal |
| 0.080 | P4/mmm | tetragonal |
| 0.070 | P4/mmm | tetragonal |
| 0.060 | P4/mmm | tetragonal |
| 0.050 | P4/mmm | tetragonal |
| 0.040 | P4/mmm | tetragonal |
| 0.030 | P4/mmm | tetragonal |
| 0.020 | P4/mmm | tetragonal |
| 0.010 | Pm | monoclinic |
| 0.001 | P1 | triclinic |

Table S8. Space-group and crystal-system assignments of KNi2F5 as a function of the symmetry tolerance (symprec) from 0.10 to 0.001 Å, evaluated on the non-spin-polarized PBE-relaxed structure.

| Symprec (Å) | Space group | Crystal system |
| --- | --- | --- |
| 0.100 | Cmmm | orthorhombic |
| 0.090 | Cmmm | orthorhombic |
| 0.080 | Cmmm | orthorhombic |
| 0.070 | Cmmm | orthorhombic |
| 0.060 | Cmmm | orthorhombic |
| 0.050 | Cmmm | orthorhombic |
| 0.040 | Cmmm | orthorhombic |
| 0.030 | Cmmm | orthorhombic |
| 0.020 | Cmmm | orthorhombic |
| 0.010 | C2 | monoclinic |
| 0.001 | P1 | triclinic |

Table S9. Space-group and crystal-system assignments of NaNi2F5 as a function of the symmetry tolerance (symprec) from 0.10 to 0.001 Å, evaluated on the non-spin-polarized PBE-relaxed structure.

| Symprec (Å) | Space group | Crystal system |
| --- | --- | --- |
| 0.100 | Cmmm | orthorhombic |
| 0.090 | Cmmm | orthorhombic |
| 0.080 | Cmmm | orthorhombic |
| 0.070 | Cmmm | orthorhombic |
| 0.060 | Cmmm | orthorhombic |
| 0.050 | Cmmm | orthorhombic |
| 0.040 | Cmmm | orthorhombic |
| 0.030 | Cmmm | orthorhombic |
| 0.020 | Pm | monoclinic |
| 0.010 | P1 | triclinic |
| 0.001 | P1 | triclinic |